ANALYTICAL AND EXPERIMENTAL ASSESSMENT OF REINFORCED CONCRETE BLOCK STRUCTURAL WALLS RESPONSE TO BLAST LOADS

ANALYTICAL AND EXPERIMENTAL ASSESSMENT OF RESINFORCED CONCRETE BLOCK STRUCTURAL WALLS RESPONSE TO BLAST LOADS

By

MOSTAFA MOHAMMED ABD-EL-WAHAB ELSAYED

B.Sc., M.A.Sc.

A Thesis Submitted to the School of Graduate Studies in Partial Fulfillment of the Requirements for the Degree Doctor of Philosophy

McMaster University

© Copyright by Mostafa Mohammed Abd-El-Wahab ElSayed

August 2014

Doctor of Philosophy (2014)                                                   	McMaster University

(Civil Engineering)                                                                       Hamilton, Ontario

TITLE:          	Analytical and Experimental Assessment of Reinforced Concrete Block Structural Walls Response to Blast Loads

AUTHOR:        			Mostafa M. AW. ElSayed

B.Sc., M.A.Sc. (Cairo University)

SUPERVISORS:       		Dr. Wael W. El-Dakhakhni

Dr. Michael Tait (Co-Supervisor)

NUMBER OF PAGES:	xviii, 172

Abstract

The current thesis focuses on estimating the damage levels and evaluating the out-of-plane behavior of fully-grouted reinforced masonry (RM) structural walls under blast loading, a load that they are typically not designed to resist. Twelve third-scale RM walls were constructed and tested under free-field blast tests. Three different reinforcement ratios and three different charge weights have been used on the walls, with scaled distances down to 1.7 m/kg1/3 and two different boundary conditions, to evaluate the walls’ performances. In general, the results show that the walls are capable of withstanding substantial blast load levels with different extents of damage depending on their vertical reinforcement ratio and scaled distance.

It worth mention that the current definitions of damage states, specified in ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012) standards, involve global response limits such as the component support rotations that are relatively simple to calculate. However, these quantitative damage state descriptors can be less relevant for cost–benefit analysis. Moreover, the reported experimental results showed that the use of quantitative versus qualitative damage descriptors specified by North American blast standards [ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012)] can result in inconstancies in terms of damage state categorization. Therefore, revised damage states that are more suitable for a cost–benefit analysis, including repair technique and building downtime, were presented. These damage states are currently considered more meaningful and have been used to quantify the post-earthquake performance of buildings.

In addition, a nonlinear single-degree-of-freedom (SDOF) model is developed to predict the out-of-plane behavior of RM structural walls under blast loading. The proposed SDOF model is first verified using quasi-static and free-field blast tests and then subsequently used to extend the results of the reported experimental test results with different design parameters such as threat level, reinforcement ratio, available block width, wall height, and material characteristics. In general, brittle behavior was observed in the walls with a reinforcement ratio higher than 0.6%. This is attributed to the fact that seismically detailed structural masonry walls designed to respond in a ductile manner under in-plane loads might develop brittle failure under out-of-plane loads because of their reduced reinforcement moment arm. In addition, increased ductility can be achieved by using two reinforcement layers instead of a single layer, even if the reinforcement ratio is reduced. Also, it is recommended to consider the use of larger concrete masonry blocks for the construction of RM structural walls that are expected to experience blast loads in order to reduce the slenderness ratio and for the placement of two reinforcement layers.

Finally, a probabilistic risk assessment (PRA) framework is proposed in order to develop design basis threat (DBT) fragility curves for reinforced concrete block shear wall buildings, which can be utilized to meet different probabilities of failure targets. To illustrate the proposed methodology, an application is presented involving a medium–rise reinforced masonry building, under different DBT levels. The DBT fragility curves are obtained via Monte Carlo sampling of the random variables and are used to infer the locations, within the building premises, that are most suitable for the erection of barriers for blast hardening.

Keywords: Blast loads, Blast scaling, Experimental tests, Out-of-plane resistance, Probabilistic risk assessment, Reinforced concrete masonry, Risk, Site planning, Structural walls, Uncertainty.

Acknowledgements

First of all, praise and thanks to Allah for his grace and mercy and giving me the effort to complete this work. Also I would like to especially thank my parents who supported me throughout this work.

It was an honor to me to work under the supervision of eminent professor, who I appreciate his wholehearted support and immense facilities. To him, I owe more than I can record. I was fortunate enough to carry out this work under the supervision of Dr. Wael W. El-Dakhakhni. He gave me the opportunity to grow as a researcher and treated me like a research partner rather than his student. Thanks for his generous help and advice. It was a great honor to work with great professor like him. Words will never be able to express my deepest gratitude and appreciation to Dr. El-Dakhakhni for his kindness, great patience, continuous support and unlimited help throughout the work. This research would not have been successfully completed without his advice and support.

Furthermore I would also like to acknowledge with much appreciation the crucial role of my committee members, Dr. Michael J. Tait and Dr. Philip Koshy who offered guidance and support during the develop of this work.

Thanks are due to technical support of Kent Wheeler and Paul Heerema of McMaster University, Rick Guilbeault and Don Wilson of Canadian Explosives Research Laboratory (CERL) during the experimental phase of this study. In addition, I would like to acknowledge both the Canadian Concrete Masonry Producers Association (CCMPA) and the Natural Sciences and Engineering Research Council of Canada (NSERC) Collaborative Research and Development (CRD) Program, for co-funding the experimental work presented in this thesis, the Canada Masonry Design Centre (CMDC) and Mr. David Stubbs of CMDC for the industrial mentorship and wall constructing, and the CERL staff for conducting the blast tests, and the Canadian Armed Forces for the use of their test range.

Finally, I would like to express my best thanks to all persons who helped me in throughout my Ph.D., Amr Nassr, Anna-Krystyna Rzezniczak, Badr AbouZaid, Brent Wybenga, Kevin Simonds, Mark Hayman, Miqdad Khalfan, Mustafa Syiam, Nick Smith, Omar El-Azizy, Saeid Mojiri and Tashnuva Masud.

Co-Authorship

This thesis has been prepared and written in accordance to the rules for a sandwich thesis format required by the faculty of graduate studies at McMaster University. This thesis consists of the following papers:

Chapter 2

ElSayed, M., El-Dakhakhni, W., and Tait, M. (2014), “Performance Assessment of Reinforced Concrete Block Structural Walls Under Blast Loading”. ASCE Journal of Structural Engineering, submitted for publication in March 2014.

Design of Experimental program and analysis of experimental data were performed by Mostafa ElSayed. Chapter 2 was written by Mostafa Elsayed under the supervision of Dr. Wael El-Dakhakhni. Dr. Michael Tait reviewed the journal paper.

Chapter 3

# ElSayed, M., Tait, M., and El-Dakhakhni, W. (2014), “Out-of-Plane Performance Quantification of Reinforced Concrete Block Shear Walls under Blast”. ASCE Journal of Performance of Constructed Facilities, submitted for publication in June 2014.

SDOF modeling, nonlinear time history analysis and parametric study were designed and conducted by Mostafa ElSayed. Chapter 3 was written by Mostafa Elsayed under the supervision of Dr. Michael Tait. Dr. Wael El-Dakhakhni reviewed the journal paper.

Chapter 4

ElSayed, M., Campidelli, M., El-Dakhakhni, W., and Tait, M. (2014), “A Simplified Framework for Blast Risk-based Cost-Benefit Analysis for Reinforced Concrete Block Buildings”. ASCE Journal of Performance of Constructed Facilities, submitted for publication in June 2014.

Chapter 4 was written by Mostafa ElSayed under the supervision of Dr. Manuel Campidelli.  Dr. Wael El-Dakhakhni and Dr. Michael Tait reviewed the journal paper.

Table of Content

Abstract	iv

Acknowledgements	vi

Co-Authorship	viii

List of Tables	xxi

List of Figures	xxii

Chapter 1: Introduction	1

1.1 Statement of the Problem	1

1.2 Motivation	2

1.3 Objectives	3

1.4 Scope	4

1.5 Summary and Main Conclusions	5

1.6 Recommendations for Future Research	10

Chapter 2: Performance Assessment of Reinforced Concrete Block Structural Walls Under Blast Loading	12

2.1 Introduction	13

2.2 Experimental Program and Test Observations	15

2.2.1 Scaling	15

2.2.2 Construction	16

2.2.3 Material	18

2.2.4 Test Matrix	19

2.2.5 Test Set-up and Instrumentation	21

2.2.6 Wall Failure Modes	22

2.3 Analysis of Experimental Results	24

2.3.1 Qualitative Wall Damage Classification according to ASCE 59-11 and CSA S850-12	24

2.3.2 Pressure Response History Curve Fitting	26

2.3.3 Simplified SDOF Model	27

2.3.4 Comparison Between the Walls’ Analytical and Experimental Support Rotations	30

2.3.5 Quantitative Wall Damage Classification according to ASCE 59-11 and CSA S850-12	30

2.3.6 Component Damage Classification Consequence on Building of LOP	32

2.4 Conclusions	34

Appendix 2.1 Notations	36

Appendix 2.2 References	37

Chapter 3: Out-of-Plane Performance Quantification of Reinforced Concrete Block Shear Walls under Blast	59

3.1 Introduction	60

3.2 Analytical Model	63

3.2.1 Quasi-Static Test Set-up and Instrumentation	64

3.2.2 Comparison Between Experimental and Analytical Wall Responses	66

3.2.3 Validation of the Analytical Model Using Free-Field Blast Test Results	67

3.3 Wall Damage Classification According to ASCE/SEI 59-11 And CAN/CSA S850-12	69

3.4 Effects of Different Parameters on Wall Performance	69

3.4.1 Influence of Charge Weight and Standoff Distance	70

3.4.2 Influence of Reinforcement Ratio and Block Size	72

3.4.3 Influence of Different Reinforcement Layer Configurations	74

3.4.4 Influence of Compressive Strength and Wall Height	75

3.4.5 Influence of Yield Strength of Reinforcement Bars	76

3.5 Performance Charts	77

3.5 Conclusions	78

Appendix 3.1 Notation	82

Appendix 3.2 References	84

Chapter 4: A Simplified Framework for Blast Risk-based Cost-Benefit Analysis for Reinforced Concrete Block Buildings	110

4.1 Introduction	111

4.2 Summary of Previous Research	114

4.3 Methodologies for Probabilistic Risk Assessment of Blast Damage	115

4.3.1 Generalized PRA Framework	115

4.3.2 Simplified PRA Framework	117

4.3.3 Threat Scenario	118

4.3.4 Uncertainty in the Structural Component and System Response	118

4.3.5 Structural Response Model	119

4.4 Damage States Identification	119

4.4.1 Damage State I (DS-I): Superficial Damage	121

4.4.2 Damage State II (DS-II): Moderate Damage	121

4.4.3 Damage State III (DS-III): Heavy Damage	122

4.4.4 Damage State IV (DS-IV): Hazardous Failure	123

4.5 Fragility Curves	124

4.6 Application of the PRA Framework to a RMSW Building Archetype	126

4.6.1 DBT Scenarios	128

4.6.2 Material Uncertainty	128

4.6.3 Archetype Building Configuration	129

4.6.4 Structural Response Model of RMSW Components	130

4.6.5 RMSW Fragility Curves	132

4.6.6 Option for Premises Zoning	133

4.7 Conclusions	135

Appendix 4.1 Notation	137

Appendix 4.2 References	139

Chapter 5: Additional Information	157

5.1 Material Characteristics	157

5.1.1 Concrete Masonry Units (CMU)	157

5.1.2 Mortar Cubes	158

5.1.3 Grout Cylinders	159

5.1.4 Fully-Grouted Masonry Prisms	160

5.1.5 Steel Reinforcement Stress-Strain Relationships	161

5.2 Test Setup and Boundary Conditions	162

5.3 Post-Blast Wall Damage	163

5.4 Measuring Peak Support Rotation	167

5.5 Analytical Model	168

5.5.1 Moment-Curvature Relationship	168

5.5.2 Validation of the Analytical Resistance Function of Masonry Specimens	171

5.5.3 Validation of the Equivalent SDOF Model Predictions	172

List of Tables

Table 2. 1: Scale factors for blast loading	42

Table 2. 2: Experimental test matrix of free field blast tests	43

Table 2. 3: ASCE/SEI 59-11 and CSA S850-12 Response Limits	44

Table 2. 4: Theoretical and measured reflected pressure and impulse of hemispherical air blast	45

Table 2. 5: Characteristics of SDOF system for different wall types	46

Table 2. 6: Wall support rotations and corresponding damage states and LOP	47

Table 3. 1: Experimental and theoretical RM wall peak resistances	89

Table 3. 2: Experimental and analytical wall support rotations	90

Table 3. 3: ASCE/SEI 59-11 and CSA S850-12 Response Limits	91

Table 3. 4: Default values used in the parametric study	92

Table 3. 5: Scaled distances (m/kg1/3) for different threat scenarios	92

Table 3. 6: Reinforcement ratios (%)	92

Table 3. 7: Wall configurations	93

Table 3. 8: (a) Walls’ support rotation, and (b) corresponding reduction (%) in response	94

Table 4. 1: Description of damage states and recommended repair techniques (adapted from FEMA (1998) and FEMA (2012a–e))	146

Table 4. 2: Comparison between different estimates of the probability of exceeding the lower bound of moderate damage state (DS-II) as a sample	147

Table 4. 3: Threat scenarios and corresponding probabilities of exceeding damage limit states	148

List of Figures

Fig. 2. 1(a): Third-scale concrete block dimensions, and (b): typical wall dimensions in meters	48

Fig. 2. 2 Specimens characteristics: (a) hinged-hinged, (b) fixed-fixed boundary conditions, and (c) cross section of typical masonry specimens	49

Fig. 2. 3 Testing frame: (a) main skeleton, (b) reaction structure, (c) final shape after installing wing walls and specimens, and (d) concrete blocks	50

Fig. 2. 4: Displacement transducers layout for wall specimens	50

Fig. 2. 5: Pressure transducer location (a) inside the frame, and (b) on the front side of the frame	51

Fig. 2. 6: Crack Pattern for Walls (a) SL11, (b) FL11, (c) FM11 and (d) FH11. Rear face (tension cracks), Front Face (mortar or block spalling/scabbing)	52

Fig. 2. 7: Crack Pattern for Walls (a) SL22, (b) FL22, (c) FM22 and (d) FH22. Rear face (tension cracks), Front Face (mortar or block spalling/scabbing)	53

Fig. 2. 8: Crack Pattern for Walls (a) SL55, (b) FL55, (c) FM55 and (d) FH55. Rear face (tension cracks), Front Face (mortar or block spalling/scabbing)	54

Fig. 2. 9: Sample of qualitative damage states experienced by RM shear walls subjected to blast loading: (a) Superficial damage of specimen SL11; (b) Hazardous failure of specimen FH55, extensive scabbing; (c) Hazardous failure of specimen FL55, fracture of the steel reinforcement	55

Fig. 2. 10: Reflected pressure-time history developed from: (a) 11 lb explosive charge, (b) 22 lb explosive charge, and (c) 55 lb explosive charge	56

Fig. 2. 11: (a) Moment-Curvature curves for different wall sections, and the definition of support rotation in according to ASCE/SEI59-11 for (b) simply supported boundary conditions, and (c) fixed-fixed boundary conditions, and finally (d) the influence of changing on the maximum support rotation	57

Fig. 2. 12: Rotation-time profiles from (a) Wall FL11, and (b) Wall FM22	58

Fig. 2. 13: Effect of Test Matrix Parameters on Support Rotation: (a) scaled distance, and (b) reinforcement ratio	58

Fig. 3. 1: Effect of strain rate on material characteristics: (a) concrete, (b) reinforcement bars	95

Fig. 3. 2: Algorithm used to develop the peak RM wall response under out-of-plane blast loading	96

Fig. 3. 3 (a): The behavior of one-way RM wall with fixed-fixed boundary conditions and the definition of support rotation in according to ASCE/SEI 59-11, and (b): fiber model	97

Fig. 3. 4: (a) Typical wall dimensions (mm), (b) the construction of fixed-fixed boundary conditions, and (c) cross section of typical masonry specimens	98

Fig. 3. 5: Quasi-static test setup	99

Fig. 3. 6: Crack Pattern for Walls (a) FLS, (b) FMS and (c) FHS	100

Fig. 3. 7: Nonlinear Single Degree of Freedom System	101

Fig. 3. 8: Impact of scaled distance on (a) the peak reflected pressure, and (b) the peak reflected impulse	102

Fig. 3. 9: Effect of changing standoff distance and charge weight on support rotation of one-way RM walls	103

Fig. 3. 10: Impact of reinforcement ratio and block size on RM wall support rotation considering two threats: (a) 300 kg of TNT at standoff distance 20 m (Z=3.0 m/kg1/3), and (b) 1,000 kg of TNT at standoff distance 30 m (Z=3.0 m/kg1/3)	104

Fig. 3. 11: (a) Different Distributions for reinforcement bars, and (b) the corresponding moment-curvature relationships having a block strength of 30 MPa	105

Fig. 3. 12: (a) Effect of using different prism compressive strength on the plastic moment of typical RM wall having Rft-I configuration, and (b) Effect of wall height on the resistance function of RM wall having a block strength of 30 MPa	106

Fig. 3. 13: Effect of wall height and masonry compressive strength on the peak support rotation using three different reinforcement layouts	107

Fig. 3. 14: Effect of yield strength of reinforcement on the peak support rotation of 3.0 m height RM shear wall under different blast threats	107

Fig. 3. 15: Predicted support rotation of 3.0 m height RM shear wall considering two block thicknesses: 190 mm (the upper surface), and 240 mm (the lower surface) under blast loads from typical standoff distance 20.0 m	108

Fig. 3. 16: Sample of design aids for reinforced masonry walls under different blast scenarios and wall width	109

Fig. 4. 1: Framework for decision making in land acquisition and perimeter protection of buildings subjected to blast threats (based on Stewart and Netherton (2008)): blue = fragility analysis; red = analysis of load uncertainty; green = threat assessment; grey = risk evaluation; orange = cost–benefit analysis; black = executive decisions	149

Fig. 4. 2: Simplified framework for decision making in land acquisition and perimeter protection of buildings subjected to blast threats	150

Fig. 4. 3: Damage states experienced by RMSWs subjected to blast loading: (a) Moderate damage of specimen FL11, maximum crack width ≤ 1.0 mm; (b) Heavy damage of specimen FH55, extensive spalling (ElSayed et al. 2014a); (c) Hazardous failure of specimen FL55, fracture of the steel reinforcement (ElSayed et al. 2014a)	151

Fig. 4. 4: Effect of standoff distance: (a) Normally reflected peak pressure; (b) Normally reflected specific impulse; (c) Costs of protection.	152

Fig. 4. 5: Normal distributions associated with masonry assemblage compressive strength and position of steel reinforcement (depth)	152

Fig. 4. 6: Prototypical four–storey RMSW building	153

Fig. 4. 7: Crack widths along the mortar bed joints of RMSWs subjected to out–of–plane uniform static pressure	154

Fig. 4. 8: Effect of the number of randomly sampled variates on the estimator N’/N of the probability of exceeding the lower bound of DS-III	154

Fig. 4. 9: Fragility curves of fictitious RMSW subjected to three threat scenarios: (a) Personal attack – 50 kg TNT; (b) Car bomb – 300 kg TNT; (c) Truck bomb – 2,000 kg TNT	155

Fig. 4. 10: Blast protection of four storey RMSW building by “zoning” of the premises: Zone–A, access restricted to authorized pedestrians; Zone–B, access granted to all pedestrians (no vehicles); Zone–C, access granted to small vehicles (cars); Zone D, unrestricted access	156

Chapter 1: Introduction

1.1 Statement of the Problem

In recent years, significant damage to structures due to accidental or deliberate explosions has created a requirement where several types of civilian structures must be designed to withstand this type of extreme dynamic loading. Moreover, the introduction of the new American (ASCE/SEI 59-11) and Canadian (CAN/CSA S850-12) Standards for blast resistance design has led to a situation where the procedures used for detailing structural components to resist in-plane seismic loads, need to be revised to withstand out-of-plane blast loads. Since existing structures are not typically designed to resist such blast loads, recently reported research studies have mainly focused on evaluating and improving the performance of existing reinforced concrete (RC) and steel components under blast loading. The problem is magnified for a structural wall subjected to a blast load. This is attributed to the fact that, compared to RC columns, structural walls are more vulnerable under blast as they attract more load, under the same design basis threat (DBT) level, due to their increased surface area. In addition, it should not be assumed that a reinforced structural wall, designed and detailed to behave in a ductile manner under in-plane loads, would remain ductile under out-of-plane loads. This is due to the reduced moment arm of the steel reinforcement in the out-of-plane direction, compared to the in-plane direction. The reduction in ductility problem is magnified for reinforced masonry (RM) walls as a result of the typical mid-cell placement of steel reinforcement within concrete masonry units (CMU) compared to the typical two reinforcement layers within RC walls.

Furthermore, the recently introduced North American standards for the design and analysis of structures subjected to blast loading [ASCE/SEI 59-11 (ASCE 2011) and the CAN/CSA S850-12 (CSA 2012)] use quantitative damage indicators (i.e. support rotations) to classify the performance of structural components and the expected level of damage. Such indicators do not lend themselves to qualitative damage assessment and thus, repair cost and subsequently cost–benefit analysis. The current thesis focuses on evaluating (experimentally and analytically) the influence of the DBT level and the design parameters on the behavior of fully-grouted seismically-detailed RM structural walls and the subsequent damage classification specified by ASCE 59-11 (ASCE 2011), CSA S850-12 (CSA 2012). In addition, the four damage states designated by ASCE/SEI 59-11 (ASCE 2011) for reinforced concrete block wall buildings are linked to qualitative local damage descriptors/criteria such as the maximum crack width and amount of spalling experienced by the masonry wall.

1.2 Motivation

Review of available literature indicates that few experimental research programs have been carried out to estimate the blast response of structural components. This is attributed to the cost and complex nature of this type of testing. On the other hand, the majority of experimental and analytical research studies have mainly dealt with RC, steel, and unreinforced masonry components under blast loading with only a limited number of studies focused RM walls. In this regard, further development of analytical models is needed in order to extend limited experimental based findings and advance the current level of understanding on the behavior of RM structural walls under blast loads. To evaluate the accuracy of the developed (as well as the current) analytical models, experimental data obtained from free-field blast tests are required. In addition, the use of quantitative versus qualitative damage descriptors stated by ASCE 59-11 (ASCE 2011), CSA S850-12 (CSA 2012) can result in discrepancies in terms of damage state categorization. The work presented in this thesis is expected to significantly affect the development of masonry design approaches under blast loading, while maintaining the advantage of simplicity and cost effectiveness of such a construction system.

1.3 Objectives

The objectives of this research are as follows:

- Introduce the basic definitions and the main characteristics of the blast loading. Also, review the experimental blast methodologies and measurement techniques used in field and laboratory testing. In addition, propose and utilize a new field set-up and compare it with real blast testing.

- To experimentally evaluate the influence of different blast load levels and different design parameters on the behavior of fully-grouted seismically-detailed RM structural walls and the subsequent damage classification specified by ASCE/SEI 59-11 (ASCE 2011), CAN/CSA S850-12 (CSA 2012).

- To develop a simplified analytical model that capable to estimate the dynamic response of masonry walls due to blast loading, which will be vital for decision makers.

- To extend, through a parametric study, the results of current experimental test results with different design parameters, such as material characteristics and reinforcement ratio. Therefore, an appropriate conclusion can be drawn and recommendation for future work can be taken.

- Utilize the analytical model to develop Performance Design Aids for different RM walls that will contribute to the future development of RM design provisions under blast loading in North America.

- Revise the current description of damage states presented in the modern blast standards to be more suitable for a cost–benefit analysis, including repair technique and building downtime.

- Propose probabilistic risk assessment (PRA) framework that can be utilized to identify target performance requirements formulated in terms of the facility stakeholders’ specified tolerable probability of failure and consequent risk management manners.

1.4 Scope

The experimental program focuses on evaluating the damage levels and the out-of-plane behavior of fully-grouted RM shear walls under different levels of scaled-distances representing a wide range of threat levels. Fifteen third-scale walls, with typical dimensions of 1,000 mm length x 1,000 mm width x 63.3 mm thickness, were constructed using third-scale replica of the standard 190 mm concrete blocks and then tested under out-of-plane quasi-static and free-field blast tests. In addition, a nonlinear analytical model, based on a SDOF model, was utilized in the current study to evaluate the out-of-plane response of RM shear walls under blast loads. This model has the capability of predicting the damage states that could occur to RM shear walls in terms of maximum crack width and amount of spalling. The proposed analytical model was validated using the experimental data obtained from quasi-static and free-field blast tests. In order to achieve the research goals, the research program included the following phases:

- Design and construction of wall test matrix (fifteen third scale masonry walls that divided into four categories based on reinforcement ratio and boundary conditions).

- Test twelve specimens under free field blast test (to simulate different damage levels) and develop experimentally the resistance function by applying quasi-static load on the remaining three masonry walls.

- Analyze both out-of-plane free-field explosions and quasi-static tests.

- Develop a nonlinear analytical model that has the capability of predicting both quantitative and qualitative damage states (i.e. predicting maximum support rotation and maximum crack width) that could occur to RM shear walls.

- Perform an analytical parametric study with different design parameters, in order to develop recommendation for enhance the blast performance of masonry shear walls.

- Develop DBT fragility curves using the proposed analytical model. These DBT fragility curves give the probability of failure and thus, they are essential to evaluate different options for blast risk management.

1.5 Summary and Main Conclusions

1.5.1 Chapter 2: Performance Assessment of Reinforced Concrete Block Structural Walls Under Blast Loading

Compared to columns, structural walls are more vulnerable to blast loading because of their increased surface areas. In addition, it should not be assumed that a RM wall, designed and detailed to behave in a ductile manner under in-plane loads, would remain ductile under out-of-plane loads. This is mainly attributed to the reduced moment arm of the reinforcement in the out-of-plane direction, because of the typical mid-cell reinforcement placement within CMU.

To address the above, twelve third-scale one-way fully-grouted masonry walls were tested under free field explosion to determine their out-of-plane behavior. The influences of explosion level, boundary conditions and reinforcement ratio on the performance of the RM masonry walls were evaluated. None of the tested masonry walls experienced shear failure; instead, they all were dominated by flexural response as is evident by the observed horizontal cracks along the interface between mortar beds and concrete blocks within the mid-span vicinity of the wall.

The captured out-of-plane displacements were used to calculate support rotations, which are used to describe the damage levels occurred in accordance to the ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012). Finally, the experimental responses were compared to the predictions of a nonlinear SDOF model presented in the UFC 3-340-02 (2008). The model predictions were in good agreement, with errors generally less than 25%. Increased reinforcement ratio and using fixed-fixed boundary conditions instead of simply supported boundaries enhanced the behavior of tested masonry walls by reducing support rotation and induced damage. Support rotations and the corresponding damage are mainly related to the explosion level and scaled distance, while wall stiffness of structural elements did not significantly affect the post-blast behavior. Based on the experimental study presented previously, the use of quantitative versus qualitative damage descriptors can result in inconstancies in terms of damage state categorization. On the other hand, fully-grouted RM walls can withstand low and medium explosion levels before experiencing excessive damage.  Moreover, increasing the out-of-plane ductility of RM walls, without increasing its capacity does not enhance their response nor reduce the level of damage and thus, both design parameters (ductility and resistance) need to be considered for components designed to resist blast loads.

1.5.2 Chapter 3: Out-of-Plane Performance Quantification of Reinforced Concrete Block Shear Walls under Blast

With the introduction of the new American (ASCE/SEI 59-11) and Canadian (CAN/CSA S850-12) standards for blast resistant design a method to quantify the performance of different structural components under such extreme loads is needed. As such, there is an urgent need to develop analytical models that have the capability of predicting the response of structural components under blast loads. In this regard, a nonlinear analytical model, based on a SDOF model, was used in the current study to evaluate the out-of-plane response of RM shear walls under blast loads. The proposed analytical model was validated using experimental data obtained from quasi-static and free-field blast tests. First, the analytical model determines the blast load parameters in accordance to CAN/CSA S850-12. Next, the nonlinear resistance of the structural wall using fiber model and load-deflection analysis by double integration of the curvature distribution is carried out. Finally, the peak mid-span deflection and the corresponding support rotation are determined. This model was subsequently used via a parametric study to evaluate various design parameters, such as threat level and reinforcement ratio, on the blast induced damage in RM structural walls. In addition, Performance Design Aids, which can be used in the preliminary design of new structures or the prediction of damage that may occur to an existing masonry component subjected to a certain blast level, were developed and presented in the current study. Based on the findings from the analyses, the following conclusions can be stated:

- RM structural walls are capable of withstanding blast load from substantial blast loads with different extend of damage depending on the threat level and walls characteristics.

- A block thickness of less than 190 mm are not recommended in the construction of masonry walls which are expected to experience blast loading. On the other hand, concrete masonry blocks with a thickness of 240 mm (or higher) perform better under blast loading.

- Although TMS 402-13/ACI 530-13/ASCE 5-13 specifies a maximum reinforcement ratio of 1.4% for special RM shear walls, using reinforcement ratios higher than 0.7% is not suggested for RM walls that are expected to experience out-of-plane blast loading in order to ensure that the walls remain ductile. This is due to the reduced reinforcement moment arm. As such, two reinforcement layers, instead of the typical single layer of bars placed at the mid-cell of CMUs can be used to enhance performance. A significant increase in the ductility (up to 2.3) was observed at using two reinforcement layers, compared to the predicted less ductile behavior when a single layer is used.

- Increased masonry compressive strength enhanced the plastic moment, and thus the resistance of the masonry wall. However, an increase in the masonry compressive strength did not result in increased ductility. As such, the enhancement in the compressive strength of the masonry may be suitable as long as the resulting blast strength demand does not exceed the wall capacity, which would typically lead to a brittle failure.

- The impact of reinforcement yield strength on the RM walls damage is inversely proportional to the support rotation. This relationship is only valid to a certain limit; for yield strengths higher than the certain limit, the support rotation will be slightly affected. This limit is directly related to the blast load level.

- For a given blast threat, increasing the reinforcement ratio was found to improve the behavior of RM shear walls under out-of-plane blast loads. However, this enhancement is valid only for reinforcement ratios less than 0.7 %, which indicate a brittle response is expected for RM walls with higher reinforcement ratios. This is attributed to the fact that seismically RM walls that are designed to act in a ductile way under in-plane loads are not guaranteed to behave in the same manner under out-of-plane loads.

1.5.3 Chapter 4: A Simplified Framework for Blast Risk-based Cost-Benefit Analysis for Reinforced Concrete Block Buildings

This study presents a general framework for PRA for RM shear wall buildings considered under blast threats. A simplified PRA methodology is also proposed, which overcomes the need for probabilistic assessment of threat and load parameters and leads to the expedient calculation of DBT fragility curves. The developed DBT fragility curves give the probability of failure as it varies with the selected DBT parameters (charge mass and standoff distance). The use of the DBT fragility curves would expedite the final stage of the PRA framework (decision making), by replacing a rigorous cost–benefit analysis with a simpler process based on the stakeholders’ judgment. The latter formulated in terms of tolerable probability of different damage states. For illustrative purposes, the simplified PRA framework is applied for the preliminary site planning of the premises surrounding a four–storey RM shear wall building archetype, whose vulnerability is analyzed by assuming three DBT blast scenarios, namely, personal attack, car bomb, and truck bomb. The uncertainty in the RM shear wall system characteristics is partly accounted for by modeling both the masonry assemblage compressive strength and the position of the longitudinal reinforcement as normally distributed random variables. The RM shear wall response to out–of–plane blast pressure, including maximum crack width and spalling ratio, is evaluated by stochastic SDOF modeling. The results suggest the erection of fences, anti–ram car barriers, and truck barricades at specific minimum standoff distances from the RM shear wall building, in order to meet the target design requirements in terms of specified probabilities of incurring moderate, heavy, and hazardous damage. Finally, based on the fragility curves results, consideration of a range of potential interventions (e.g. strengthening) as well as the use of more sophisticated means, including a generalized PRA, and a more detailed analytical model for the prediction of the RM shear wall building blast response might be required.

1.5.4 Chapter 5: Additional Information

As the name indicates, this chapter presents a collection of data that covers material characterization, analytical model development, wall damage pattern, and SDOF validation.

1.6 Recommendations for Future Research

In the glance of the experimental test data; numerical model results and research results, several research topics are suggested for future studies such as follows:

- In the present experimental study, only one-way masonry walls were examined. Future tests can include the effect of boundary conditions on the out-of-plane performance of masonry walls under blast loading. It is expected that two-way masonry walls and masonry wall systems with boundary elements under out-of-plane loading will possess beneficial characteristics compared with one-way walls, but the relation among the different systems need to be studied.

- Axial load is neglected in this study, and such load will produce extra deflection due to P-δ effect. The residual axial resistance of damaged masonry walls can be determined experimentally and compared to corresponding axial resistance of undamaged walls. There is a correlation between the drop of axial resistance and damage occurred, but the relation between them is not defined yet for masonry wall. Such relation can be obtained using many methods such as Monte Carlo simulation, while Copula method is more suitable for this case.

- The SDOF model used in this study is based on the fundamental deformed shape and hence, higher mode effect is neglected. For future research, MDOF and FE models need to be developed. By comparing the analytical results of the three models (SDOF, MDOF, and FE models) to the corresponding experimental results, the accuracy of using the different models can be compared to examine which is the most suitable for such analysis.

Chapter 2: Performance Assessment of Reinforced Concrete Block Structural Walls Under Blast Loading

Abstract: With the introduction of the new American (ASCE 59-11) and Canadian (CSA S850-12) standards for blast resistant design, there is a need to quantify the performance of different structural components under such extreme loads. This paper focuses on experimentally evaluating the damage levels and the out-of-plane response of fully-grouted reinforced masonry structural walls under blast loading (in their impulsive regime); a load that they are typically not designed to resist. The scaled walls reported in this paper cover a range of design parameters and charge weights that reflect different design basis threat levels. Three different reinforcement ratios and three different charge weights have been used on the walls, with scaled distances down to 1.7 m/kg1/3 and two different boundary conditions, to evaluate the walls’ performances. In general, the results show that the walls are capable of withstanding substantial blast load levels with different extents of damage depending on their vertical reinforcement ratio and scaled distance. However, brittle behavior was observed in the walls with a reinforcement ratio higher than 0.6%. This is attributed to the fact that seismically detailed structural masonry walls designed to respond in a ductile manner under in-plane loads might develop brittle failure under out-of-plane loads because of their reduced reinforcement moment arm. The peak experimental support rotation values were compared to the corresponding values obtained using an available nonlinear single-degree-of-freedom (SDOF) model presented in the Unified Facilities Criteria UFC 3-340-02 (2008) document. In general, the comparison between the experimentally obtained and the analytically predicted support rotation values indicated reasonable agreement. The test results are expected to contribute to the growing masonry blast performance database of experimental results and to the future development of reinforced masonry design provisions under blast loading in North America, where a balance between the wall strength and ductility might be needed to remain below the damage thresholds provided by the performance-based-oriented ASCE 59-11 and CSA S850-12 standards.

Keywords: Blast Loads, Blast Scaling, Experimental Tests, Flexural Out-of-plane Resistance, Reinforced Concrete Masonry, Structural Walls.

2.1 Introduction

With the increased demand for higher safety levels and enhanced structural performance under extreme dynamic loading, quantifying the behavior of different structural components under such loading conditions is becoming necessary. Due to the complex nature of and the resulting damage from blast loads, the recent North American blast resistant design standards [ASCE 59-11 (ASCE/SEI 2011), CSA S850-12 (CSA 2012)] have been focused on developing detailing techniques for civilian structures designed to withstand different combinations of blast load levels generated by a range of explosive charges and standoff distances. When a combination of a specific charge weight and a standoff distance is selected for design purposes, it is referred to as the design basis threat (DBT) [ASCE 59-11 (ASCE/SEI 2011)]. Since existing structures are not typically designed to resist such DBT, recently reported research studies have mainly focused on evaluating and improving the performance of existing reinforced concrete (RC) and steel components under blast loading [Wang et al. (2012), Li et al. (2012), Nassr et al. (2012), Stoddart et al. (2014)]. Other recent studies have focused on hardening (retrofit for blast) concrete components using fiber-reinforced polymer (FRP) [Rodriguez-Nikl et al. (2012), Coughlin et al. (2010)]. As far as masonry construction is concerned, the majority of masonry blast research reported in literature has focused either on unreinforced masonry (URM) wall behavior [Dennis et al. (2004), Abou-Zeid et al. (2011-a) Baylot et al. (2004)], or relevant hardening applications attempting to enhance the response of URM walls strengthened with FRP sheets or other external reinforcement systems [Abou-Zeid et al. (2011-b), Al-Salloum and Almusallam (2005), Irshidat et al. (2011)] with only a limited number of studies focused on reinforced masonry (RM) walls [Mayrhofer (2002), Wu et al. (2005)].

Within a typical RM building, the resistance to lateral forces, such as those generated from seismic events, and corresponding deformations are typically provided by the in-plane strength and stiffness of the RM structural walls. On the other hand, it should not be assumed that a RM structural wall, designed and detailed to behave in a ductile manner under in-plane loads, would remain ductile under out-of-plane loads. This is mainly attributed to the reduced moment arm of the steel reinforcement in the out-of-plane direction, as a result of the typical mid-cell placement of steel reinforcement within concrete masonry units (CMU) compared to the typical double reinforcement layers within RC walls. The tendency to develop a brittle response is also attributed to the reduced strength of RM construction compared to their RC counterparts, which further increases the depth of the wall cross section’s compression zone under out-of-plane flexure. Moreover, the typical lack of confinement (e.g. using stirrups) in RM walls compared to their RC counterparts may result in significant damage and further reduction of the wall cross-section’s ductility under out-of-plane deformation demands.

Although blast design is essentially component-based, performance-based standards take a more holistic approach by considering the overall building state following DBT. As such, it is also important to recognize that the failure of a gravity load-resisting component (e.g. structural wall) may seriously impact the overall structural integrity of the building and lead to progressive collapse [ASCE 59-11 (ASCE/SEI 2011), CSA S850-12 (CSA 2012)]. Within this context, although recent research studies have focused mainly on the failure (removal) of columns under extreme loads [Williams and Williamson (2011), Krishnappa et al. (2013), Lew et al. (2013), Sadek et al. (2013), Yu and Tan (2013), Bao et al. (2014)], the problem is magnified for a structural wall subjected to a blast load. This is attributed to the fact that, compared to RC columns, RM walls are more vulnerable under blast as they attract more load, under the same DBT level, due to their increased surface area. As such, the scenario of a structural RM wall with a large surface area attracting more load, combined with the walls’ reduced weak axis moment of inertia and the possibility of brittle failure, might prove to be significantly more critical than a RC column under the same DBT.

The current study focuses on experimentally evaluating the influence of the DBT level and the design parameters on the behavior of fully-grouted seismically-detailed third-scale RM structural walls and the subsequent damage classification specified by ASCE 59-11 (ASCE 2011), CSA S850-12 (CSA 2012). The test results include details of the test protocol, measured support rotations, and the observed wall damage levels and corresponding failure modes. In addition, the experimental results were compared to the predictions of a single degree of freedom (SDOF) model, described in UFC 3-340-02 (2008) and then correlated to code specified damage threshold levels, and corresponding system level of performance.

2.2 Experimental Program and Test Observations

2.2.1 Scaling

Hopkinson-Cranz or cube root scaling is commonly used for explosive scaling where self-similar blast waves are produced at identical scaled distances, Z=R3W, where R is the standoff distance from the detonation source, and W is the charge mass. The scaled distance approach can be used to correlate two explosive charges of similar geometry and of the same type of explosive, but with different charge sizes, detonated under the same atmospheric conditions (Baker et al. 1983) but at different standoff distances. The DBT levels adopted in the current study considered charge weights between 100 and 1,000 kg at a standoff distance of 15.0 m (at full-scale) in order to produce a range of damage based on the preliminary results of a nonlinear SDOF model that is discussed later in the paper.

With third-scale walls being used, keeping the same Z value as that of the full-scale to meet the similitude requirements would result in the same blast peak pressure, while the load duration must be reduced to one-third (Harris and Sabnis 1999). As such, the standoff distance, and subsequently the impulse, should also be scaled accordingly in order to scale down the load duration, while keeping the blast pressures the same as that at full-scale (Harris and Sabnis 1999). The charge weights used in the current test program were scaled to maintain the same scaled distance and thus, to produce the same incident (and reflected pressure). Using a geometrical scale factor of SL=1/3 results in the standoff distance of 5.0 m (compared to 15.0 m at full-scale). The walls were constructed using third-scale replicas of the standard 190 mm CMU available in North America with specified dimensions (63.3 mm thick x 63.3 mm high x 126.6 mm long), as shown in Fig. 2.1-a, and tested under free field explosions. Subsequently, the twelve third-scale walls, had typical dimensions of 1,000 mm length x 1,000 mm width x 63.3 mm thickness. The scaling factors are listed in Table 2.1.

2.2.2 Construction

Each wall consisted of 15 courses high with seven and half blocks in each, as illustrated in Fig. 2.1-b. All walls were constructed in a half-block running bond using third-scale face-shell mortar bedding to simulate common construction practice in North America. In order to simulate the actual construction process, the masonry walls were built in two stages (i.e. to allow for low lift grouting). In addition, in order to reduce the possibility of creating a cold joint, a shear key was introduced by limiting the grout within the first grouting stage to the mid height of the 8th course.

With typical RM construction utilizing precast RC hollow slab systems, the out-of-plane partially fixed boundary conditions of the walls fall between fixed and simply-supported. In order to simulate the simply supported boundary condition, as shown in Fig. 2.2-a, the walls were built on and capped with steel C-channel sections 101.6 mm (4 in) height by 40.2 mm (1.6 in) width in order to facilitate placing the walls within their setup during the blast tests. Each of the two upper and lower C-channels had mortar beddings at their interface with their corresponding walls for leveling. In addition to the above, the fixed-fixed walls had their vertical reinforcement bars welded to both the upper and lower C-channels, as illustrated in Fig. 2.2-b, to simulate reinforcement going through the RC slabs/foundation.  In addition, two welded steel members were used to connect the top and bottom C-channels, as can be seen in Fig. 2.2-b to provide fixation against their rotation. In addition to the blast-loaded walls reported in the current paper, three identical masonry walls, with identical fixation boundary conditions (i.e. side plates connected to top and bottom steel channels), were tested under quasi-static loading (ElSayed et al., 2014). The experimental wall peak resistances were in good agreements with mechanics-based models considering fixed-fixed boundary conditions.

Unlike RC walls when a two layers of reinforcement exist, the size of concrete block construction that practically limits the reinforcement at mid-wall thickness result in a significantly reduced stiffness, and moment capacity, at RM wall ends compared to their RC counterparts. This is also more relevant to RM walls compared to RC walls because of the weak interface between the RM walls and slab system, unlike RC walls and slabs, where the construction is monolithic. In addition, in RM construction, the floor system is typically constructed of pre-cast hollow-core concrete panels that offer less wall-end restrains than cast-in-place RC slab systems. As such, the current study did not account for possible membrane forces that might have developed by the side plate clamping effect can be conservatively ignored.

It should also be noted that it is almost impossible to apply a constant axial load on a RM wall (or any structural component to that matter) under blast, expect by testing the component as a part of a complete system (building or a part of a building). This became apparent as the use of prestressing was omitted, as the prestressed wires would both change the resistance function of the walls as they deflect, and would not maintain the same level of initial axial forces, which will complicate the wall behavior analysis even further. In addition, the use of hydraulic actuators would not have worked as well as hydraulic actuators would not be capable of maintaining (adjusting) their force level under blast loading within milliseconds increments, while the wall is deflecting

2.2.3 Material

Eighteen scaled blocks were randomly selected and tested in accordance to the CSA A165.1 (CSA 2004-a) to obtain an average compressive strength. The average compressive strength and corresponding coefficient of variation (COV) were 20.3 MPa, and 15.2%, respectively. These values were calculated based on an average net area of 4,789 mm2. Type-S mortar with an average flow of approximately 125% was used in all the batches and proportioned by weight for better quality control. The proportion of portland cement: lime: sand: water was 1.0: 0.2: 3.5: 0.9. Water was added gradually to achieve the workability requirements as determined by the mason. In accordance to the CSA A179-04 (CSA 2004-c), three 51 mm cubes were cast from each mortar batch and tested after 28 days resulting in an average compressive strength of 17.3 MPa and a COV of 17.1 %. The average grout compressive strength was 16.8 MPa with a corresponding COV of 18.5%. Seventeen four-block high by one-block long (270 mm high x 126 mm long x 63 mm thick) fully-grouted masonry prisms were constructed and tested according to the CSA S304.1-04 (CSA 2004-b) with an average compressive strength (fm') of 18.4 MPa (COV= 17.0%). This is equivalent to 21.2 MPa for the standard two-blocks high prisms in accordance to the C1314-11 ASTM Standards (ASTM 2011-a). Finally, two different types of scaled bars were used as vertical reinforcement, D4 and D7 bars (with areas of 26 and 45 mm2, respectively) corresponding approximately to M15 and M25 bars, respectively at full-scale. For the horizontal reinforcement, W1.7 wires (with area of 11 mm2) were used to simulate M10 bars in full-scale. By performing tensile tests on D4 and D7 reinforcement samples, the average yield strengths were found to be 515 and 481 MPa (COV= 3.5 and 2.8%), respectively.  Further details and summaries of research studies pertaining to the use of scaled steel and scaled CMU can be found elsewhere (Harris and Sabnis 1999).

2.2.4 Test Matrix

The main objective of the current study is to quantify the performance of seismically detailed RM walls that are not designed for out-of-plane loads and to link the wall support rotations to expected damage level specified by the ASCE 59-11 (ASCE 2011), CSA S850-12 (CSA 2012). The minimum vertical reinforcement ratio for RM structural walls, in accordance to both North American blast resistant standards, is 0.25%. The Canadian standard for structural masonry design [CSA S304.1-04 (CSA 2004-b)] specified a maximum reinforcement ratio of 2.0% for moderately ductile RM shear walls. On the other hand, the maximum reinforcement ratio for Special RM shear walls is evaluated as 1.4% per the requirements of the MSJC (2013) [TMS 402-13/ACI 530-13/ASCE 5-13]. As such, three different reinforcement ratios, as shown in Fig 2.2-c, representing low (0.33%), moderate (0.62%), and high reinforcement ratios (1.07%), were used in this study.

The damage expected from a DBT is typically a function of the severity of the blast impulse, which increases as a function of the size (mass) of explosive charge and/or the proximity of the charge (i.e. the standoff distance). Therefore, far-field explosions (i.e. scaled distances higher than 1.2 m/kg1/3) (Dusenberry 2010) were adopted in this study to ensure uniform pressure distributions on the RM wall surface and to avoid localized failure mechanisms (e.g. breaching) that might develop under close-in explosions (Dusenberry 2010).

The three charge weights selected aimed at producing three damage levels: Moderate, Heavy, and Hazardous failure (in accordance to both ASCE/SEI 59-11 and CSA S850-12). As such, three wall groups: Group I (subjected to 5 kg), Group II (subjected to 10 kg) and Group III (subjected to 25 kg) of Pentex-D explosive charge (with a TNT pressure equivalency factor of 1.2) were tested under the same standoff distance of 5.0 m, which all fell within the 1.2 m/kg1/3 scaled distance threshold of far-field explosions as presented in Table 2.2. The designation of the masonry walls given in Table 2.2 consisted of two letters followed by two numbers representing the charge weight in lbs. The first letter represents the support conditions (S: Simply supported or F: Fixed-fixed), while the second letter represents the vertical reinforcement ratio (L: Low, M: Moderate or H: High). For example, Wall SL11 represents a Simply supported wall with Low vertical reinforcement ratios (0.33%) that is subjected to 5 kg (11 lb) of Pentex-D explosive charge at the same standoff distance of 5.0 m as the rest of the walls.

2.2.5 Test Set-up and Instrumentation

As shown in Fig. 2.3-a, the main components of the steel bunker used in testing the RM walls consisted of the reaction frame, the displacement transducers mounting system, and the bunker walls. The reaction frame as illustrated in Fig. 2.3-b consisted of six welded rectangular hollow steel sections (HSS) with the dimensions of 101.6 mm (4 in) x152.4 mm (6 in) x 11.1 mm (3.5/8 in). The flange side of the C-section members on the top and the bottom of the walls were in direct contact with two 50.8 mm (2 in) diameter solid steel rods that were welded to the two upper and lower HSS forming the bunker frame. Another six HSS members were welded to form the mounting system used to fix the displacement transducers and string potentiometers needed to measure wall displacements. The reaction frame and the displacement transducer mounting system were welded to a 6.4 mm (0.25 in) base steel plate. The two sides, bottom and rear face of the bunker had plates that were welded to the built-up steel frame of the bunker. Additionally, the upper side of the bunker had a steel hatch, which provided access to the displacement transducers between the blast shots. To reduce the clearing effects, three steel plates (two-side and an upper parapet wing walls) were installed on the test bunker, as shown in Fig. 2.3-c thus ensuring uniform pressure on the wall surface. The dimensions of the wing walls were selected based on ConWep (Hyde 1990) analysis to minimize variation in the pressure and the impulse for the specific range of scaled distance utilized.

Three displacement transducers were used to monitor the out-of-plane displacement behavior with two 300 mm stroke connected at the quarter points of each wall specimen, as shown in Fig. 2.4, and one, with a 360 mm stroke connected to each wall’s central point to record the wall mid-span deflection response history. In addition, two strain gauges were installed on the middle vertical steel reinforcement bar at its half and three-quarter height. To measure the reflected pressure, three piezoelectric pressure transducers were used around the tested wall. An additional pressure transducer was placed inside the steel bunker to measure any pressure variation that might result from possible over pressure leakage, as shown in Fig. 2.5.

2.2.6 Wall Failure Modes

Group I walls (see Table 2.2), tested under 5 kg (11 lb) of Pentex-D, generally developed tension cracks within the bed joints of the mid-height zone of the walls on the rear face. Wall SL11 cracked between the 6th and 10th courses, as shown in Fig. 2.6-a, while Wall FL11 cracked above the 7th course, as illustrated in Fig. 2.6-b. For Wall FM11, two horizontal cracks formed in Fig. 2.6-c, occurring above the 7th and 8th courses. On the other hand, there were no compression or tension cracks observed in Wall FH11. Spalling/scabbing was not observed in the front face of Group I walls, except for Wall SL11 where spalling occurred above the 8th course. In addition, the practical limitation of concrete block construction, which limits the reinforcement at mid-wall thickness, results in tension cracks propagating well into the grout cells for more than half the wall thickness.

Group II walls, tested under 10 kg (22 lb) of Pentex-D, was subjected to double the charge weight at the same standoff distance. As shown in Fig. 2.7, the majority of the cracks occurred horizontally in mortar joints with some minor cracks propagating through the concrete blocks in Wall SL22. The full length horizontal bed joint cracks on the top or the bottom of the mortar joints indicated loss of bond between the mortar and the block. The cracks were visible and more extensive compared to the corresponding cracks in Group I walls. Moreover, the extent of cracking and deflection reduced significantly from Wall SL22 to Wall FH22 due to the changes in the boundary conditions and reinforcement ratio. Wall SL22 cracked between the 5th and 12th courses, compared with Wall SL11 where it experienced horizontal tension cracks extended between the 6th and 10th courses. Similar behavior was observed in Wall FL22 where three full length horizontal bed joint cracks on the top and the bottom of the mortar joint above the 6th, 7th, and 8th course occurred compared to a single crack above the 7th course in Wall FL11. On the other hand, two cracks were observed in Wall FM22 above the 7th and 8th courses compared to two hair cracks above the 6th and 7th courses in Wall FM11. Finally, Wall FH11 did not suffer any visible tension cracks, while Wall FH22 had two horizontal cracks above the 7th and 8th courses.

Group III walls were tested under a relatively high blast load in order to quantify the wall damage under high strength and ductility demands. Walls SL55, FL55, FM55, and FH55 were all subjected to 25 kg (55 lb) of Pentex-D (five times the charge weight used in the Group I) while maintaining the same standoff distance as in Groups I and II. As illustrated in Fig. 2.8, generally more damage developed in Group III compared to Groups I and II with the extent of damage depending on the tested specimen. Walls SL55 and FL55 were split into two halves and both tensile cracks and compressive spalling were observed in both parts. In Wall SL55, only one failure surface occurred above the 7th course (almost at wall mid-height), while on Wall FL55 there were two cut surfaces above the 8th course (almost the wall mid-height), and between the wall top and the upper steel C-channel. Wall splitting occurred due to excessive plastic strains in the vertical reinforcement bars, as the necking of steel bars was observed at the failure edge, as shown in Fig. 2.8-b. In spite of the fact that Wall FH11 did not suffer cracking or visible deformation in Group I and only two horizontal cracks were observed in Wall FH22, a significant amount of tension cracks occurred in mortar joints and propagated through the concrete blocks in Wall FH55, as shown in Fig. 2.8-d. The face shell and parts of the grout on the compression side of the walls also spalled off leaving the vertical and horizontal reinforcement at the corresponding areas exposed. In addition, full length tension cracks propagated along the wall width in both mortar joints and concrete blocks. The same behavior was observed in Wall FM55, in which several tension cracks propagated along the wall width in both mortar joints and concrete blocks from the 6th to the 10th. In addition, vertical reinforcement was exposed due to splitting of the compression face shell. The deformed shape of both Walls FM55 and FH55 were characterized by large permanent deformations.

2.3 Analysis of Experimental Results

Based on visual observations following the blast shots, it was noted that the walls with reinforcement ratio higher than 0.6% responded in a brittle manner under the highest DBT evaluated. This is attributed to the fact that seismically detailed walls, which are designed to be ductile under in-plane loading, might not necessary behave in the same way under out-of-plane loads. Subsequently, further analysis is necessary to study the response of the walls under different levels of DBT.

2.3.1 Qualitative Wall Damage Classification according to ASCE 59-11 and CSA S850-12

As can be seen in Table 2.3, the ASCE 59-11 (ASCE/SEI 2011) and CSA S850-12 (CSA 2012) classify four damage levels ranging between Superficial (where visible permanent damage is unlikely), Moderate (where permanent damage might be visible, but reparable and component failure is unlikely), Heavy (where significant, mostly non-repairable, damage develops yet component failure remains unlikely), and Hazardous (where component fails).

According to the qualitative damage descriptions in Table 2.3, the damage of Group I walls could be classified as Superficial as none of the walls exhibited permanent damage. For Group II walls, the extent of cracking and the significant permanent deflections in Wall SL22 would classify it under the Heavy damage category. On the other hand, the permanent deflection and cracks propagated only within mortar joints in Walls FL22, FM22 and FH22 and thus, these walls could be classified under the Moderate damage category in accordance to ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012). Finally, Group III wall damage would be classified as Hazardous failure or higher in according to ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012). Because of the complete collapse of Walls SL55 and FL55 they were designated under the blowout category according to the CSA S850-12 (CSA 2012), which is also a damage category not permitted in the ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012).

Within the low range of DBT, there was no significant influence of the wall boundary conditions or the flexural reinforcement ratio on the wall performance as all walls fell within the superficial damage state. On the other hand, at the highest DBT considered, the reinforcement ratio played a major role on the wall performance and its post-blast structural integrity. The hazardous failure mode of Group III walls indicate that a balance between ductility and strength should be carefully considered in blast resistant RM walls as increased ductility with reduced strength might result in a wall displacement demand, under a specific range of DBT levels, that might exceed the displacement capacity of the wall or result in permanent deformations that might be detrimental to the wall. On the other hand, having a less-ductile, stronger wall is expected to result in less permanent deformation and increased capacity. However, this is only valid as long as the resulting blast strength demand does not exceed the wall capacity, which would typically lead to brittle failure. To explore this behavior, the following sections, will attempt to quantitatively categorize wall damage levels in accordance to the ASCE 59-11 (ASCE/SEI 2011) and the CSA S850-12 (CSA 2012). Prior to the wall quantitative categorization, and in order to validate the experimental wall support rotation results through comparisons to analytical predictions, a simplified SDOF will be utilized to analytically predict the response of the tested RM walls using a blast pressure history curve fitting technique based on the modified Friedlander equation (Baker et. al 1983), as will be explained next.

2.3.2 Pressure Response History Curve Fitting

A typical reflected blast pressure wave signature resulting from high explosive charge consists of two main phases: a positive and a negative pressure phases, and the peak incident pressure, Pso, and the positive phase duration depend on the characteristics of the DBT level (Baker et al. 1983). The reflected pressure wave is a function of several blast environment parameters such as the characteristics of the ground surface and the surrounding atmospheric condition. In order to predict the air blast parameters, sets of empirical equations or charts are available [UFC 3-340-02 (2008)]. In addition, software such as ConWep (Hyde, 1990) can be also utilized to determine blast parameters, based on experimental data collected from TNT blast test database.

In addition to the typical variability in blast profile measurements, the aim of the paper is to introduce a simplified SDOF model to predict the experimental data. This model includes an idealized load profile that can be re-developed by design engineers. Based on the above, the simplified analytical model presented in the study neglected the effect of negative impulse, not only because it is considered even more uncertain in terms of blast load profile (Baker et al. 1973) but because ignoring the negative phase effects would also result in a more conservative estimate of the wall displacements.

For the current study, the peak reflected overpressures and the corresponding impulses are predicted using the simplified formulation of the CSA S850-12 and listed in the 5th and 8th columns in Table 2.4, respectively. The peak overpressures and the corresponding impulses are predicted also using ConWep software and are presented in the 6th and 10th columns in Table 2.4. The experimental pressure values were recorded using a high-speed data acquisition system with a sampling rate of 1 MHz. Figures 2.10-a, 2.10-b and 2.10-c illustrate the recorded pressure histories for Groups I, II and III walls, respectively. To evaluate the positive phase duration required for the Friedlander equation (Baker et. al 1983), the blast pressure histories were numerically integrated, to yield the corresponding impulse values. The point of maximum impulse would then represent the end of the positive phase duration. Consequently, least square regression using the Modified Friedlander Equation (Baker et. al 1983) were performed to determine the peak reflected pressure and the corresponding impulse values (the 4th and 8th columns in Table 2.4, respectively) in order to facilitate their inclusion in the SDOF.

In general, the recorded blast parameters were close to the corresponding values determined using ConWep (Hyde, 1990) and the CSA S850-12 (CSA 2012) equations. The difference between the measured and predicted reflected pressure is about 10%, except at the 9th shot in which the difference was around 15%. The same difference was observed from comparing the recorded impulses to the corresponding values determined using Conwep software and the CSA S850-12 (CSA 2012), except the 11th shot in which the difference was around 17%.  Based on the recorded pressure response histories and according to ConWep and CSA S850-12 (CSA 2012) predictions, the reflected blast pressure and impulse analytical predictions are considered in a reasonable agreement with the obtained experimental data, considering the typically high level of uncertainty in blast load parameter predictions.

2.3.3 Simplified SDOF Model

As stated previously, a simplified equivalent SDOF model would facilitate analytical prediction of the RM wall response reported in the current study. Such SDOF model would serve two purposes. The first purpose was to preliminary predict the response of the walls within the test matrix and ensure that different damage levels can be achieved under the selected scale distances. The second purpose was to verify the application of this SDOF model by comparing the experimental test results to their corresponding analytical predictions. The UFC 3-340-02 (2008) provides guidelines to develop a simplified SDOF to predict the response of reinforced concrete-type components, under blast, responding mainly in flexure. The material properties used within the SDOF model, such as the compressive strength of the grouted masonry prisms and the yield strength of the reinforcement accounted for the dynamic increase factors specified by the ASCE 59-11 (ASCE 2011). Because of the very weak bond strength at the interface between the concrete block and mortar, such tensile bond strength was not included in the analysis, which conforms to the CAN/CSA S304.1-04. In this study, the plastic moment (Mp) of a RM wall was determined using the fiber model, in which the typical cross-section of the RM wall was divided into 125 layers. For each extreme upper fiber’s strain value (), the stress distribution along the wall cross-section is determined considering Euler-Bernoulli bending theory; in which a linear strain profile is assumed; and the position of the natural axis is allocated to satisfy the equilibrium condition (which was satisfied by equating the difference between tension and compression forces to the external applied axial load). As illustrated in Fig. 2.11-a, walls within the FH group are expected to behave in a brittle manner under out-of-plane loads, although designed to respond in a ductile manner under in-plane loads. The slopes of the moment-curvature curves in their elastic zones (Em I) and the plastic moment (Mp) of wall category SL and FL; FM; and FH wall are presented in Table 2.5. This elastic slope is defined as the average slope developed until the yield of reinforcement point on the moment-curvature diagram. Due to the uncertainty associated with quantifying the membrane action induced through the use of the side plates, the SDOF model utilized in this study did not account for such effects which would have resulted in a flat-arch mechanism in addition to the RM wall flexure.  This is consistent with the MSJC 2013 approach, which consider either the arching or the flexure independently even though they might develop simultaneously.

The deformed shape of one-way RM walls can be expressed as shown in Fig. 2.11-b for the simply-supported walls and Fig. 2.11-c for the fixed-fixed walls. For the fixed-fixed walls, the typical resistance functions can be expressed as piecewise linear two-step elasto-plastic functions, while elastic-perfectly-plastic resistance functions can be used to represent the simply-supported walls according to UFC 3-340-02 (2008). The resistances and stiffness of the equivalent SDOF systems representing four wall categories are presented in Table 2.5. A load-mass factor (KLM), for the SDOF system used in this study, is used to transform the walls into equivalent SDOF systems as described in Biggs (1964) and the corresponding values utilized within the SDOF model are listed in Table 2.5. The values in Table 2.5 account for the different material strength- and dynamic-increase-factors as given in the ASCE/SEI 59-11 and CSA S850-12 standards. In addition, the average measured weight of the RM structural walls, which is accounted for in the SDOF model, was 1.45 kN (148 kg mass). As it can be observed from Table 2.6 and Fig. 2.11-d, the SDOF model results indicate that, at low DBT, changing the boundary conditions is more effective than increasing the flexural reinforcement ratio in terms of reducing the maximum support rotations. Support rotation is defined as the angle through which a flexural element subjected to blast loading has rotated at its supports when it achieves its maximum dynamic deflection. Support rotation is calculated assuming straight segment between hinge or yield line locations and the point of maximum deflection. (ASCE 2011).

2.3.4 Comparison Between the Walls’ Analytical and Experimental Support Rotations

The experimental deflection response histories of the walls under different scaled distances were captured using the displacement transducers measurements (see Fig. 2.4). Using these measurements, each wall’s maximum support rotation, defined as the chord angle, as can be seen in figures 2.11-b and c, is used to classify the performance of structural components under blast loads, in accordance to the ASCE/SEI 59-11 (ASCE 2011) and the CSA S850-12 (CSA 2012). Figures 2.12-a and b show sample wall chord rotations based on displacement transducer measurements of Walls FL11 and FM22, respectively. Figure 2.12-b shows permanent shifts in the support rotation responses, following the first cycle, corresponding to wall damage. The peak experimental support rotations for the twelve walls are presented in Table 2.6. The displacement under out-of-plane profiles of Walls SL11 and SL22 could not be captured due to a data acquisition and triggering mechanism malfunction. In general, the SDOF predicted peak support rotations for the different walls are in agreement with the corresponding measured support rotations (see Table 2.6), with a maximum difference of approximately 20%.

2.3.5 Quantitative Wall Damage Classification according to ASCE 59-11 and CSA S850-12

Figure 2.13 shows the effect of test matrix parameters on the observed support rotations along with the standards damage thresholds. As mentioned earlier, Wall FL55 split into two halves and thus, its support rotation was outside the maximum support rotation limit specified by the standards for Hazardous failure, as shown in Figs. 2.13-a and 1.13-b. As can be observed from Table 2.6 and Figs. 2.13-a and b, the experimental support rotations vary with the charge weight (under the same standoff distance), and vary with the inverse of the vertical reinforcement ratio. Based on the quantitative (numerical) damage threshold specified by ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012), and listed in Table 2.3, the damage experienced by Group I walls (with Z = 2.75 m/kg1/3) is classified as a Moderate damage. As illustrated in Table 2.3, the Moderate damage region is identified by an upper response limit of support rotations equal to 2° in accordance to ASCE/SEI 59-11 and CSA S850-12. However, the minor cracks that propagated only within the mortar joint-CMU interfaces would classify Group I damage as Superficial, in accordance to the ASCE/SEI 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012) qualitative description, even though the average support rotations developed in Group I walls is close to the upper limit of the Moderate damage specified by the ASCE/SEI 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012). Regardless of the damage classification, the maximum support rotation for Group I walls decreased negligibly as the wall reinforcement ratio increased.

According to post blast observations, there was a clear difference in terms of both the deformed shapes and the extent of cracks between Group I and Group II walls. As mentioned earlier, the qualitative damage state of Group II of walls (except Wall SL22) were considered as Moderate. In addition to blast, there are other attempts to define and correlate qualitative damage states to universally-applicable numbers (and thus quantitative damage states), such as inter-story drift ratios, in the area of seismic performance [FEMA P58, 2012]. Such numbers are usually based on experimental observations or post-event damage surveys. However, because of the complex response and the spectrum of design variables of any type of structural components, the codified correlations between qualitative and quantitative damage states might not be applicable in all cases, similar to the cases reported in the current paper. However, as the code quantitative damage thresholds are based on the maximum, rather than the permanent support rotations, the damage of all Group II walls is considered Heavy according the standards’ numerical damage thresholds.

Walls FM55 and FH55 had support rotation values between approximately 11° and 12°, which is within the Hazardous failure threshold of 15° (see Table 2.3) specified by the ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012), within which the walls should fail but the probability of debris is minimal. This is also consistent with the qualitative damage threshold of the standards where both walls experienced extensive spalling/scabbing and permanent deflections, in addition to a significant amount of tension cracks. Walls SL55 and FL55 (Group III) split into two halves and thus, they are designated under the blowout category according to the CSA S850-12 (CSA 2012), as their damage presented a case where the support rotation would exceed the 15° threshold for Hazardous failure in the ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012).

2.3.6 Component Damage Classification Consequence on Building of LOP

The above discussion shows that the use of quantitative versus qualitative damage descriptors listed in Table 2.3 can result in inconstancies in terms of damage state categorization, especially at damage levels that are below complete specimen failure. In addition, although seismically detailed RM structural walls possess reinforcement ratios that fall within the limits specified to ensure a ductile performance under in-plane loads, such ratios might result in an under-reinforced, a balanced or an over-reinforced wall section in the out-of-plane direction. Such change of behavior would need to be considered when a RM wall could be subjected to blast loading. It might then be argued that an under-reinforced section behavior would be desirable to safeguard against hazardous failure that would develop in the case of an over-reinforced section. However, the typically reduced strength associated with an under-reinforced section (compare to an over-reinforced one) and the expected subsequent large support rotations would be indicative of damage and proportional to the DBT levels. As such, a thorough DBT-specific analyses would be required to balance between the RM wall capacity and ductility for blast-resistant design.

Both the CSA and ASCE standards utilize the maximum support rotations as the quantitative measure of specimen damage state. In addition, both standards identify other qualitative damage state indicators that are implicitly related to permanent deformations, although no limits are explicitly stated. As such, the use of “ductility” was intended to reflect the fact that some (less stronger) walls might experience excessive deformation demands (that will be satisfied by their ductility capacity) that would designate these walls as heavily damaged. On the other hand, some other (stronger) walls might experience only very little deformation demands (and thus their limited ductility might not be even mobilized) under blast loading, which would designate their damage as superficial.

Unlike seismic performance assessment when the overall system-level behavior determines the response, blast analysis is essentially component-based. However, it is well understood that the overall building structural integrity remains influenced by the individual response of its key component. Subsequently, the ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012) standards correlate the component-level response to different system (i.e. building) target performance levels as can be seen in Table 2.3. Within this context, the qualitatively assessed superficial damage established in Group I walls is associated with High to Medium Level of Protection (LOP) corresponding to the Operational-Immediate Occupancy performance targets, in which temporary evacuation of occupants might be necessary but re-entry and return to operation is likely since building contents are likely to remain at least partly operational. The Moderate damage state established for Group II walls is associated with Low LOP, which corresponds to the Life Safety performance targets. With this performance target, progressive collapse is unlikely although repairs might be costly. In addition, building occupants could be evacuated and their temporarily return is likely. Finally, as both the ASCE 59-11 (ASCE 2011) and the CSA S850-12 (CSA 2012) do not allow damage higher than heavy damage for primary structural components, Group III walls essentially experienced a range of hazardous failure to complete blowout and indicating a LOP that falls below the Very Low LOP which is associated with the Collapse Prevention performance level. As such, progressive collapse might develop in this case for buildings with main RM structural walls experience such severe blast load combinations.

2.4 Conclusions

In this paper, twelve third-scale one-way fully-grouted masonry walls were tested under free field explosion to determine their out-of-plane behavior. The influences of explosion level, boundary conditions and reinforcement ratio on the performance of the RM masonry walls were evaluated. None of the tested masonry walls experienced shear failure; instead, they all were dominated by flexural response as is evident by the observed horizontal cracks along the interface between mortar beds and concrete blocks within the mid-span vicinity of the wall.

The captured out-of-plane displacements were used to calculate support rotations, which are used to describe the damage levels occurred in accordance to the ASCE 59-11 (ASCE 2011) and CSA S850-12 (CSA 2012). Finally, the experimental responses were compared to the predictions of a nonlinear SDOF model presented in the UFC 3-340-02 (2008). The model predictions were in good agreement, with errors generally less than 25%, for walls experiencing superficial and moderate damage states. However the SDOF model support rotation predictions did not correspond well with those of the corresponding experimental results for RM walls that experienced hazardous failure and complete blowout.

Based on the experimental results, the use of quantitative versus qualitative damage descriptors can result in inconstancies in terms of damage state categorization, especially at damage levels that are below complete specimen failure. On the other hand, fully-grouted RM walls can withstand low and medium explosion levels before experiencing excessive damage.

Compared to columns, structural walls are more vulnerable to blast loading because of their increased surface areas. In addition, it should not be assumed that a RM wall, designed and detailed to behave in a ductile manner under in-plane loads, would remain ductile under out-of-plane loads. This is mainly attributed to the reduced moment arm of the reinforcement in the out-of-plane direction, because of the typical mid-cell reinforcement placement within CMU. Finally, increasing the out-of-plane ductility of RM walls, without increasing its capacity does not enhance their response nor reduce the level of damage and thus, both design parameters (ductility and resistance) need to be considered for components designed to resist blast loads.

Appendix 2.1 Notations

The following symbols are used in this paper:

| E | Explosion energy (J) |
| --- | --- |
| Em | Masonry’s Young's modulus (MPa) |
| I | Second moment of inertia (m4) |
| IR | Reflected impulse (kPa.msec) |
| Mp | Plastic Moment (MPa) |
| L | Length (m) |
| M | Mass (kg) |
| P | Blast pressure (kPa) |
| PR0 | Peak reflected pressure (kPa) |
| PS0 | Peak incident pressure (kPa) |
| R | Standoff distance from the detonation source (m) |
| SL | Geometric scale factor |
| W | Charge mass (kg) |
| Z | Scale distance (m/kg1/3) |
|  | Support rotation (degree) |

Appendix 2.2 References

Abou Zeid, B.M., El-Dakhakhni, W.W., Razaqpour, A.G., and Foo, S. (2011-a). “Response of Arching Unreinforced Masonry Walls to Blast Loading.” Journal of Structural Engineering, ASCE, Vol. 137(10), pp.1205-1214.

Abou Zeid, B.M., El-Dakhakhni, W.W., Razaqpour, A.G., and Foo, S. (2011-b). “Performance of Unreinforced Masonry Walls Rertofitted with Externally Anchored Steel Studs under Blast Loading.” Journal of Performance of constructed facilities, ASCE, Vol. 25(5), pp.441-453.

Al-Salloum, Y.A., and Almusallam, T. (2005). “Load Capacity of Concrete Masonry Block Walls Strengthened with Epoxy-bonded GFRP Sheets.” International Journal of Composite Materials, Vol. 39 (19), pp. 1719-1745.

American Society for Testing and Materials (ASTM) (2011-a). “Standard Test Methods for Compressive Strength of Masonry Prisms.”, C1314-11a, West Conshohocken, Pa.

American Society for Testing and Materials (ASTM) (2011-b). “Standard Test Methods for Sampling and Testing Concrete Masonry Units and Related Units.”, C140-11, West Conshohocken, Pa.

American Society of Civil Engineers (ASCE) (2011). “Blast Protection of Buildings.” ASCE/SEI 59-11, Reston, Virginia.

Bao, Y., Lew, H.S., and Kunnath, S.K. (2014). “Modeling of Reinforced Concrete Assemblies Under Column Removal Scenario.” Journal of Structural Engineering, Vol. 140(1), ISSN 0733-9445/04013026 (13).

Baker, W.E., Westine, P.S., and Dodge, F.T. (1973). “Similarity Methods in Engineering Dynamics.” New Jersey, USA: Hyden Book Company Inc.

Baker, W.E., Cox, P.A., Westine, P.S., Kulesz, J.J., and Strehlow, R.A. (1983). “Explosion Hazard and Evaluation.” Oxford, New York, USA: Elservier Scientific Publishing Company.

Baylot, J.T., Bullock, B., Siawson, T.R., and Woodson, S.C. (2004). “Blast Response of Lightly Attached Concrete Masonry Unit Walls.” Journal of Structural Engineering, ASCE, 131(8), August 2005, pp. 1186-1193.

Biggs, J.M. (1964). “Introduction to Structural Dynamics.” New York, USA: McGraw-Hill Inc.

Canadian Standards Association (CSA). (2004-a). “CSA Standards on Concrete Masonry Units.”, CSA A165, Mississauga, Ontario, Canada.

Canadian Standards Association (CSA). (2004-b). “Design of Masonry Structures.”, CSA S304.1-04, Mississauga, Ontario, Canada.

Canadian Standards Association (CSA). (2004-c). “Mortar and Grout for Unit Masonry.”, CSA A179-04, Mississauga, Ontario, Canada.

Canadian Standards Association (CSA). (2012). “Design and Assessment of Buildings Subjected to Blast Loads.”, CSA S850-12, Mississauga, Ontario, Canada.

Coughlin, A.M., Musselman, E.S., Schokker, A.J., and Linzell, D.G. (2010). “Behavior of Portable Fiber Reinforced Concrete Vehicle Barriers Subject to Blasts from Contact Charges.” International Journal of Impact Engineering, Vol. 37 (5), pp. 521-529.

Dennis, S.T., Baylot, J.T., and Woodson, S.C. (2002). “Response of ¼-Scale Concrete Masonry Unit (CMU) walls to blast.” Journal of Engineering Mechanics, Vol. 128(2), pp.134-142.

Dusenberry, D.O. (2010). “Handbook for Blast Resistant Design of Buildings.” New-Jersey, USA: Wiley & Sons Inc., First Edition.

ElSayed, M., Tait, M., and El-Dakhakhni, W. (2014). “Out-of-Plane Performance Quantification of Reinforced Concrete Block Shear Walls under Blast”. ASCE Journal of Performance of Constructed Facilities, submitted for publication in June 2014.

Harris, H.G., and Sabnis, G.M. (1999). “Structural Modeling and Experimental Techniques: Second Edition.” New York, USA: CRC Press.

Hyde, D.W., (1990). “Conventional weapons effect (ConWep).” Application of TM5-855-1. US Army Engineer Waterways Experiment Station, Vicksburg, USA.

Irshidat, M., Al-Ostaz, A., Cheng, A.H.D., and Mullen, C. (2011). “Nanoparticle Reinforced Polymer for Blast Protection of Unreinforced Masonry Walls: Laboratory Blast Load Simulation and Design Model.” Journal of Structural Engineering, ASCE, Vol. 137(10), pp.1193-1204.

Krauthammer, T. (2008). “Modern Protective Structures.” New-York, USA: CRC Press, Taylor & Francis Group.

Krishnappa, N., Bruneau, M., and Warn, G.P. (2013). “Weak-Axis Behavior of Wide Flange Columns Subjected to Blast.” Journal of Structural Engineering, ASCE. ST.1943-541X.0000917.

Lew, H.S., Main, J.A., Robert, S.D., Sadek, F., and Chiarito, V.P. (2013). “Performance of Steel Moment Connections Under a Column Removal Scenario. I: Experiments.” Journal of Structural Engineering, Vol. 139(1), pp.98-107.

Li, B., Nair, A., and Kai, Q. (2012). “Residual Axial Capacity of Reinforced Concrete Columns with Simulated Blast Damage.”  Journal of Performance of Constructed Facilities, ASCE, Vol. 26(3), pp. 287-299.

Masonry Standards Committee Joints (MSJC). (2013). “Building Code Requirements for Masonry Structures.”, TMS 402-13/ACI 530-13/ASCE 5-13. USA.

Mayrhofer, C. (2002). “Reinforced Masonry Walls Under Blast Loading.” International Journal of Mechanical Sciences, Vol. 44, pp. 1067-1080.

Nassr, A.A., Razaqpur, A.G., Tait, M.J., Campidelli, M., and Foo, S. (2012). “Experimental Performance of Steel Beams under Blast Loading.” Journal of Performance of Constructed Facilities, ASCE, Vol. 26(5), pp. 600-619.

Natio, C.J., and Wheaton, K.P. (2006). “Blast Assessment of Load-Bearing Reinforced Concrete Shear Walls.” Journal of Structural Engineering, ASCE, Vol. 11(2), pp. 112-121.

Priestley, M.J.N., Calvi, G.M., and Kowalsky, M.J. (2007). “Displacement Based Seismic Design of Structures.” IUSS Press, Pavia ,Italy, First Edition.

Rodriguez-Nikl, T., Lee, C., Hegemier, G.A., and Seible, F. (2012). “Experimental Performance of Concrete Columns with Composite Jackets under Blast Loading.” Journal of Structural Engineering, ASCE, Vol. 138(1), pp. 81-89

Sadek, F., Main, J.A., Lew, H.S. and El-Tawil, S. (2013). “Performance of Steel Moment Connections Under a Column Removal Scenario. II: Analysis.” Journal of Structural Engineering, ASCE, Vol. 139(1), pp.108-119.

Stoddart, E.P., Byfield, M.P., and Tyas, A. (2014). “Blast Modeling of Steel Frames with Simple Connections.” Journal of Structural Engineering, ASCE, Vol. 140(1), CID: 04013027.

US Army Corps of Engineers, Naval Facilities Engineering Command, and Air Forces Civil Engineer Support Agency (2008), “Structures to Resist the Effect of Accidental Explosions.” Unified Facilities Criteria, UFC 3-340-02.

Wang, W., Zhang, D., Lu, F., Wang, S.C., and Tang, F. (2012). “Experimental Study on Scaling the Explosion Resistance of a One-Way Square Reinforced Concrete Slab Under a Close-in Blast Loading.” International Journal of Impact Engineering, Vol. 49, pp. 158-164.

Williams, G.D., and Williamson E.B. (2011). “Response of Reinforced Concrete Bridge Columns Subjected to Blast Loads.” Journal of Structural Engineering, ASCE, Vol. 137(9), pp. 903-913.

Wu, C., Hao, H., and Lu, Y. (2005). “Dynamic Response and Dynamic Analysis of Masonry Structures and Masonry Infilled RC Frames to Blast Ground Motion.” Engineering Structures, Vol. 27, pp. 323-333.

Yu, J., and Tan, K., (2013). “Structural Behavior of RC Beam-Column Subassemblages Under a Middle Column Removal Scenario” Journal of Structural Engineering, ASCE, Vol. 139(2), pp. 233-250.

Table 2.1: Scale factors for blast loading

| Characteristics | Quantity | Dimension | Model |
| --- | --- | --- | --- |
| Geometry | Linear dimension, l | L | 1/3 |
|  | Area, A | L2 | 1/9 |
|  | Displacement,  | L | 1/3 |
|  | ## Support rotation, θ | Degree | 1 |
| Loading | Pressure, P | M L-1 S-2 | 1 |
|  | Force, F | M L S-2 | 1/9 |
|  | Time, t | T | 1/3 |
|  | Impulse, I | M L S-1 | 1/3 |
|  | Velocity, v | LT-1 | 1 |

Table 2.2: Experimental test matrix of free field blast tests

| Shot No. | Group | Specimen | Pentex-D charge weight in kg (lb) | Equivalent TNT (kg) | Scaled Distance Z (m/kg1/3) |
| --- | --- | --- | --- | --- | --- |
| 1 | I | SL11 | 5.0 (11) | 6.0 | 2.75 |
| 2 |  | FL11 |  |  |  |
| 3 |  | FM11 |  |  |  |
| 4 |  | FH11 |  |  |  |
| 5 | II | SL22 | 10.0 (22) | 12.0 | 2.18 |
| 6 |  | FL22 |  |  |  |
| 7 |  | FM22 |  |  |  |
| 8 |  | FH22 |  |  |  |
| 9 | III | SL55 | 25.0 (55) | 30.0 | 1.61 |
| 10 |  | FL55 |  |  |  |
| 11 |  | FM55 |  |  |  |
| 12 |  | FH55 |  |  |  |

Table 2.3: ASCE/SEI 59-11 and CSA S850-12 Response Limits

| RM Wall Damage State | Qualitative Damage Description In Accordance to |  | Quantitative Damage Description in the ASCE/SEI 59-11 and CSA S850-12 Standards | Expected Building LOP | Building Performance |
| --- | --- | --- | --- | --- | --- |
|  | ASCE/SEI 59-11 | CSA S850-12 |  |  |  |
| Superficial Damage | The wall is unlikely to exhibit any permanent deflection or visible damage. |  | Ductility level less than 1 (elastic response) | Medium/High | Immediate Occupancy/ Operational |
| Moderate Damage | The wall likely will have permanent deflections and visible cracks. Damaged wall is generally repairable, although replacement may be more economical and aesthetic. |  | Support rotation less than 2° | Low | Life Safety |
| Heavy Damage | The cover over the reinforcement has scabbed. The wall has not failed but likely will have significant permanent deflections. |  | Support rotation between 2° and 8° | Very Low | Collapse Prevention |
| Hazardous Failure | The wall is likely to fail and produce significant spalling and scabbing. | The wall has failed with no significant velocities. | Support rotation between 8° and 15° | N.A. | N.A. |
| Blowout | N.A. | The wall has overwhelmed causing debris with significant velocities. | Support rotation greater than 15° a | N.A. | N.A. |

a Not applicable in the ASCE/SEI 59-11

Table 2.4: Theoretical and measured reflected pressure and impulse of hemispherical air blast

| Shot No. | Specimen | Scaled Distance (m/kg1/3) | Fitted reflected pressure (kPa)a | Predicted Reflected pressure (kPa)b | Predicted Reflected pressure (kPa) c | Average pressure prediction error (%) | Fitted reflected impulse (kPa.msec)a | Predicted Reflected impulse (kPa.msec)b | Predicted Reflected impulse (kPa.msec)c | Average impulse prediction error (%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | SL11 | 2.75 | 417.0 | 412.4 | 416.2 | 0.7 | 483.6 | 450.3 | 449.3 | 7.5 |
| 2 | FL11 |  | 372.5 |  |  | -10.1 | 431.2 |  |  | -4.1 |
| 3 | FM11 |  | 380.8 |  |  | -8.1 | 494.7 |  |  | 10.0 |
| 4 | FH11 |  | 421.5 |  |  | 1.7 | 462.1 |  |  | 2.7 |
| 5 | SL22 | 2.18 | N.A. | 814.7 | 807.3 | N.A. | N.A. | 747.3 | 745.3 | N.A. |
| 6 | FL22 |  | 872.8 |  |  | 7.6 | 685.2 |  |  | -8.2 |
| 7 | FM22 |  | 785.0 |  |  | -3.2 | 726.3 |  |  | -2.7 |
| 8 | FH22 |  | 775.7 |  |  | -4.4 | 784.0 |  |  | 5.1 |
| 9 | SL55 | 1.61 | 1747.8 | 2067.6 | 2032.4 | -14.7 | 1365.6 | 1478.1 | 1474.2 | -7.5 |
| 10 | FL55 |  | N.A. |  |  | N.A. | N.A. |  |  | N.A. |
| 11 | FM55 |  | 1941.8 |  |  | -5.3 | 1225.4 |  |  | -17.0 |
| 12 | FH55 |  | 2077.0 |  |  | 1.3 | 1529.6 |  |  | 3.6 |

Table 2.5: Characteristics of SDOF system for different wall types

| Wall category | EmI (kN.m2) | Mp (kN.m) | Elastic Resistance (kN) | Elasto-Plastic Resistance (kN) | Elastic Stiffness (kN/m) | Elasto-plastic Stiffness (kN/m) | Fundamental Period (msec)a |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SL | 18.8 ×103 | 4.0 | 032.2×103 | N.A. | 01.4×103 | N.A. | 64.6 |
| FL | 18.8×103 | 4.0 | 048.3×103 | 064.4×103 | 07.2×103 | 1.4×103 | 28.5 |
| FM | 31.6×103 | 6.8 | 082.0×103 | 109.3×103 | 12.1×103 | 2.4×103 | 22.0 |
| FH | 41.1×103 | 8.5 | 102.1×103 | 136.2×103 | 15.8×103 | 3.2×103 | 19.2 |

a Fundamental period is calculated based on the elastic stiffness of the RM structural wall

Table 2.6: Wall support rotations and corresponding damage states and LOP

| Shot No. | Wall ID | Scaled distance (m/kg1/3) | Measured support rotation (degree) |  | Code-Qualitative Damage State | Code-Quantitative Damage State | SDOF Predicted support rotation (degree) | Predicted support rotationMeasured support rotation |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Maximum | Permanent |  |  |  |  |
| 1 a | SL11 | 2.75 | N.A. | N.A. | Superficial Damage | N.A. | 4.5 | N.A. |
| 2 | FL11 |  | 1.8 (8 msec.)b | 0.2 | Superficial Damage | Moderate Damage | 2.0 (9 msec.)b | 1.09 |
| 3 | FM11 |  | 1.7 (7 msec.)b | 0.1 | Superficial Damage | Moderate Damage | 1.7 (7 msec.)b | 1.00 |
| 4 | FH11 |  | 1.6 (6 msec.)b | 0.1 | Superficial Damage | Moderate Damage | 1.3 (5.5 msec.)b | 0.79 |
| 5 a | SL22 | 2.18 | N.A. | N.A. | Heavy Damage | N.A. | 8.6 | N.A. |
| 6 | FL22 |  | 4.3 (9 msec.)b | 0.2 | Moderate Damage | Heavy Damage | 4.1 (8.5 msec.)b | 0.95 |
| 7 | FM22 |  | 3.7 (8 msec.)b | 0.7 | Moderate Damage | Heavy Damage | 3.0 (7 msec.)b | 0.80 |
| 8 | FH22 |  | 2.7 (6 msec.)b | 0.2 | Moderate Damage | Heavy Damage | 2.7 (6 msec.)b | 1.00 |
| 9 | SL55 | 1.61 | Failure | Failure | Blowout | Blowout | 23.8 | N.A. |
| 10 | FL55 |  | Failure | Failure | Blowout | Blowout | 14.7 | N.A. |
| 11 | FM55 |  | 8.7 (12 msec.)b | 7.4 | Hazardous Failure | Hazardous Failure | 7.2 (10 msec.)b | 0.83 |
| 12 | FH55 |  | 7.9 (11 msec.)b | 4.8 | Hazardous Failure | Hazardous Failure | 7.0 (9 msec.)b | 0.88 |

a  Displacement data acquisition module malfunctioned

b Timing of peak response

| (a) | (b) |
| --- | --- |
| Fig. 2. 1(a): Third-scale concrete block dimensions, and (b): typical wall dimensions in meters |  |

| Vertical Direction |  |
| --- | --- |
| (a) |  |
| Vertical Direction |  |
| (b) |  |
| (c) |  |
| Fig. 2. 2 Specimens characteristics: (a) hinged-hinged, (b) fixed-fixed boundary conditions, and (c) cross section of typical masonry specimens |  |

| (a) | (b) |
| --- | --- |
| Steel wing walls | Concrete blocks |
| (c) | (d) |
| Fig. 2. 3 Testing frame: (a) main skeleton, (b) reaction structure, (c) final shape after installing wing walls and specimens, and (d) concrete blocks |  |

| Fig. 2. 4: Displacement transducers layout for wall specimens |  |  |
| --- | --- | --- |
| Inner Pressure Transducer |  | PE4 PE5 PE3 Outer Pressure Transducer |  |
| (a) |  | (b) |  |
| Fig. 2. 5: Pressure transducer location (a) inside the frame, and (b) on the front side of the frame |  |  |  |

PE4

| Rear Face Front Face | Rear Face Front Face |
| --- | --- |
| (a) | (b) |
| Rear Face Front Face | Rear Face Front Face |
| (c) | (d) |
| Fig. 2. 6: Crack Pattern for Walls (a) SL11, (b) FL11, (c) FM11 and (d) FH11. Rear face (tension cracks), Front Face (mortar or block spalling/scabbing) |  |

| Rear Face Front Face | Rear Face Front Face |
| --- | --- |
| (a) | (b) |
| Rear Face Front Face | Rear Face Front Face |
| (c) | (d) |
| Fig. 2. 7: Crack Pattern for Walls (a) SL22, (b) FL22, (c) FM22 and (d) FH22. Rear face (tension cracks), Front Face (mortar or block spalling/scabbing) |  |

| Rear Face Front Face | Rear Face Front Face |
| --- | --- |
| (a) | (b) |
| Rear Face Front Face | Rear Face Front Face |
| (c) | (d) |
| Fig. 2. 8: Crack Pattern for Walls (a) SL55, (b) FL55, (c) FM55 and (d) FH55. Rear face (tension cracks), Front Face (mortar or block spalling/scabbing) |  |

| (a) | (b) | (c) |
| --- | --- | --- |
| Fig. 2. 9: Sample of qualitative damage states experienced by RM shear walls subjected to blast loading: (a) Superficial damage of specimen SL11; (b) Hazardous failure of specimen FH55, extensive scabbing; (c) Hazardous failure of specimen FL55, fracture of the steel reinforcement |  |  |

(a)

(b)

(c)

Fig. 2. 10: Reflected pressure-time history developed from: (a) 11 lb explosive charge, (b) 22 lb explosive charge, and (c) 55 lb explosive charge

| (a) |  |
| --- | --- |
| Simply Supported Elastic Plastic | Fixed-Fixed Elastic Elasto-Plastic Plastic |
| (b) | (c) |
| (d) |  |
| Fig. 2. 11: (a) Moment-Curvature curves for different wall sections, and the definition of support rotation in according to ASCE/SEI59-11 for (b) simply supported boundary conditions, and (c) fixed-fixed boundary conditions, and finally (d) the influence of changing on the maximum support rotation |  |

(a)

(b)

Fig. 2. 12: Rotation-time profiles from (a) Wall FL11, and (b) Wall FM22

| Moderate Damage Heavy Damage Hazardous Failure | Heavy Damage Hazardous Failure |
| --- | --- |
| (a) | (b) |
| Fig. 2. 13: Effect of Test Matrix Parameters on Support Rotation: (a) scaled distance, and (b) reinforcement ratio |  |

Chapter 3: Out-of-Plane Performance Quantification of Reinforced Concrete Block Shear Walls under Blast

Abstract: An increasing demand for structures with high levels of performance under the action of blast loads has resulted in an urgent need to quantify the performance of both existing and new buildings under this type of extreme loading. It is often necessary to employ computational analysis to investigate the blast behavior of structural elements through parametric studies because experimental studies utilizing live explosives are both challenging and costly. This study focuses on analytically estimating the damage levels and the out-of-plane response of fully-grouted reinforced masonry (RM) walls subjected to blast load. This type of a wall is not typically designed to resist such loads. In this paper, an advanced nonlinear single-degree-of-freedom (SDOF) model is developed to predict the out-of-plane response of RM walls subjected to blast loading. This proposed SDOF model is first verified using quasi-static and free-field blast tests and then subsequently used to extend the results of currently experimental test results with different design parameters such as threat level, reinforcement ratio, available block width, wall height, and material characteristics. In general, the parametric study shows that RM walls are capable of withstanding substantial blast load levels with different levels of induced damage depending on wall width and reinforcement ratio. In addition, increased ductility can be achieved by using two reinforcement layers instead of a single layer, even if the reinforcement ratio is reduced. This is a consequence of the reduced reinforcement moment arm for the single reinforcement layer case compared to the two reinforcement layer arrangement. Also, it is recommended to consider the use of larger concrete masonry blocks for the construction of RM structural walls that are expected to experience blast loads in order to reduce the slenderness ratio and for the placement of two reinforcement layers. Finally, the proposed SDOF model was utilized to develop performance aids for different RM walls that will contribute to the future development of RM design provisions under blast loading in North America. In general, findings from this study indicate that seismically detailed RM walls, designed to behave in a ductile way under in-plane loads, might not respond in a ductile manner under out-of-plane loads. Therefore, the procedures used for the design and the construction of RM walls, which are expected to experience out-of-plane blast loads, need to be revised and implemented in the future versions of current blast standards.

Keywords: Blast Loads, Single Degree of Freedom, Nonlinear Analysis, Pushover Analysis, Out-of-plane Resistance, Reinforced Concrete Masonry, Strain Rate Effect, Shear Walls.

3.1 Introduction

The introduction of the new American (ASCE/SEI 59-11) and Canadian (CAN/CSA S850-12) Standards for blast resistance design has led to the situation where the procedures used for detailing structural components to resist in-plane seismic loads, need to be revised to withstand out-of-plane blast loads. Furthermore, few experimental research programs have been carried out to estimate the blast response of structural components due to the cost and complex nature of this type of testing. In this regard, analytical models capable of simulating the structural behavior under blast loading are required. Recently reported studies have primarily focused on analytically predicting the performance of reinforced concrete (RC) [Krauthammer et al. (1986), Krauthammer et al. (1990), Silva and Lu (2009), Li and Hao (2014), and Stolz et al. (2014)] and steel components [Warn and Bruneau (2009), Nassr et al. (2012), and Nassr et al. (2013)] under the action of blast loads. With regards to masonry construction, the majority of studies reported in the literature have mainly focused on either typical un-reinforced masonry (URM) walls [Hamed and Rabinovitch (2008), Hrynyk and Mayers (2008), and Abou Zeid et al. (2014)], or hardening URM components using fiber-reinforced polymers (FRP) [Davidson et al. (2005), Coughlin et al. (2010, and Urgessa and Maji (2010)], with only a limited amount of research work focusing on reinforced masonry (RM) walls [ElSayed et al. (2014)].

For typical RM buildings, the resistance to lateral loads, such as seismic and wind, is provided by the RM shear walls. Although the RM components are designed to behave in a ductile manner under in-plane loads, they may not exhibit sufficient ductility when subjected to out-of-plane loads. This is primarily due to the reduced moment arm associated with the wall width under out-of-plane loads compared to that associated with the wall length for the case of in-plane loading. Furthermore, the typical mid-cell placement of vertical reinforcement within concrete masonry units (CMU), in comparison to the two reinforcement layers in RC walls, also leads to reduced ductility in the out-of-plane direction.

Under the action of blast loads, the dynamic properties of materials used in typical masonry construction (e.g. reinforcement and concrete) differ from the corresponding static properties due to strain rate effects. As a result, strain rate effects should be considered in the analytical model. For the case of pure axial deformation, stresses (and subsequently strain) are uniformly distributed over the entire specimen allowing the strain rate to be considered constant at every point within the specimen. Under such circumstances, experimental studies have focused on evaluating the effect of higher strain rates on both concrete [Bischoff and Perry 1991] and steel [Malvar (1998)]. Figures 3.1-a and 3.1-b illustrate the effect of strain rate on the dynamic compressive strength of concrete and the dynamic yield and ultimate strengths of steel reinforcement, respectively [CEB 1988, ASCE 2011, and Malvar 1998]. For flexural one-way RM walls subjected to out-of-plane loads, which is the focus of this study, the strain rate varies over the entire specimen as a result of the variation of both moment along the wall height and strain within the wall depth. In this regard, both ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012) suggested constant dynamic increase factors (DIFs) and strength increase factors (SIFs); based on the material and the predicted failure mode; to simulate the influence of higher strain rates.

The current study focuses on analytically evaluating the response of fully-grouted RM shear walls under blast loading, which is a load that this type of shear wall is typically not designed to resist. A nonlinear single-degree-of-freedom (SDOF) model is developed and subsequently verified using experimental results obtained from quasi-static and free-field tests. Next, this model is used to extend the results of experimental work with different design parameters such as threat level, reinforcement ratio, block width, wall height, and material characteristics. Finally, sample Performance Design Aids for different RM walls that are expected to contribute to the future development of RM design provisions under blast loading are presented.

3.2 Analytical Model

Further development of analytical models is needed in order to extend limited experimental based findings and advance the current level of understanding on the behavior of RM structural walls under blast loads. In this study, a SDOF model is employed to predict the out-of-plane behavior of RM shear walls corresponding to a pre-defined design basis threat (DBT). A DBT refers to a combination of specified charge mass (W) and standoff distance (SD) in accordance to ASCE/SEI 59-11(ASCE 2011). As illustrated in Fig. 3.2, the blast load parameters [e.g. peak reflected pressure (Pr) and impulse (Ir)] are evaluated using the CAN/CSA S850-12 (CSA 2012).

For a typical one-way fixed-fixed wall, such as the RM shear walls considered in this study, the resistance function due to an external uniform load can be expressed as a piecewise linear two-step elasto-plastic function (UFC 3-340-02 2008), as shown in Fig. 3.3-a. The stiffness and resistance corresponding to each loading stage can be defined as a function of wall height (H), plastic moment (Mp), and stiffness (E I), as follows (Biggs 1964):

|  | (Elastic Stiffness) | (3.1-a) |
| --- | --- | --- |
|  | (Elasto-Plastic Stiffness) | (3.1-b) |
|  | (Plastic Stiffness) | (3.1-c) |
|  | (Elastic Resistance) | (3.2-a) |
|  | (Elasto-Plastic Resistance) | (3.2-b) |

In this study, the nonlinear resistance function is determined by load-deflection analysis, which involves the computation of the moment-curvature relationship of the typical wall cross-section, the bending moment distribution resulting from the applied blast pressure, the curvature distribution along the wall span, and the deflection curve by double integration of the curvature distribution. As such, the moment-curvature relationship is developed using a fiber model (Prisetly et al. 2007), in which a linear strain profile is assumed, as shown in Fig. 3.3-b. The rate dependent material properties are accounted for by adopting both SIF and DIF values recommended by CAN/CSA S850-12 (CSA 2012) for masonry and steel reinforcement assuming a flexural type failure mode. The load-mass factor (KLM), which is used to transform the real structure into an equivalent SDOF system (Biggs 1964, Baker et al. 1983, and UFC 3-340-02 2008), is determined for each value of mid-span deflection by numerical integrating of the shape function () using Eq 3.3.

|  | (3.3) |
| --- | --- |

The proposed equivalent SDOF model, which simulates the RM shear wall, is then analyzed under the action of the DBT, where	 the peak mid-span deflection and corresponding support rotation (chord rotation in accordance to ASCE/SEI 59-11) are determined. The maximum support rotation experienced by each wall (see Fig. 3.3-a) is used to classify the performance of structural components and the expected level of damage, in accordance with both ASCE/SAI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012). To evaluate the accuracy of the model, the predicted resistance functions are compared to results obtained from quasi-static tests. In addition, the predicted analytical support rotations are compared with experimental results obtained from free-field blast tests.

3.2.1 Quasi-Static Test Set-up and Instrumentation

In this study quasi-static tests were performed on three third-scale one-way fully-grouted RM shear walls. All walls had typical dimensions of 1,000 mm height x 1,000 mm length x 63.3 mm thickness (see Fig. 3.4-a) and were built using a third scale replica of the standard 190 mm CMU available in North America. Each wall was 15 courses high and constructed in a half block running bond using 3.5 mm face-shell mortar bedding to simulate common construction practice in North America. The experimental work presented herein is considered an extension of a previous experimental research study (ElSayed et al. 2014) that aimed to experimentally evaluate the damage levels and the out-of-plane behavior of fully-grouted RM shear walls when subjected to blast loading. In order to facilitate the placement of the RM walls within their setup during the quasi-static tests, the masonry walls were built on and capped with two steel C-channel sections 101.6 mm (4 in) height by 40.2 (1.6 in) width. The vertical reinforcement was welded to both the upper and lower C-channels in order to simulate reinforcement going through the RC slabs/foundation. Moreover, two steel plates were welded to the ends of the two C-channels to prevent rotations simulating fixed-fixed boundary conditions (see Fig. 3.4-b).

The average compressive strength (), obtained from masonry prism tests in accordance with C1314-11 ASTM Standards (ASTM 2011), was 21.2 MPa, while the average yield strengths of the D4 and D7 reinforcement bars (with areas of 26 and 45 mm2, respectively) were 515 and 481 MPa, respectively. Additional details on construction of the specimens and their material properties are presented in ElSayed et al. (2014).

Three vertical reinforcement ratios were selected for this study (shown in Fig. 3.4-c), which represent low (0.33%), moderate (0.62%), and high reinforcement ratios (1.07%), according to both North American blast standards and the MSJC (2013) [TMS 402-13/ACI 530-13/ASCE 5-13]. The masonry wall specimens are identified using a three letter designation system. The first letter represents the support condition (F: Fixed-fixed), the second letter represents the vertical reinforcement ratio (L: Low, M: Moderate, or H: High), and the third letter refers to the loading type (S: Quasi-Static). As shown in Fig. 3.5-a, the load was transferred from the actuator to the masonry wall specimen through sixteen contact points in order to represent a uniform-like load. In this regard, sixteen rubber pads (50.8 mm depth x 150 mm width x 150 mm length) were arranged in a regular pattern above the tested masonry wall, as illustrated in Fig. 3.5-b. Each row of rubber pads (four pads in the perpendicular direction to wall span) was loaded by a 50.8 mm (2 in) diameter steel rod, which was attached to two rectangular hollow steel sections [HSS 152.4 x 101.6 x 11.1 (mm)]. A second 600 mm HSS section was used to transfer the load from the actuator to the two HSS members through three 50.8 mm (2 in) steel balls at contact points between actuator and HSS members. The setup consisted of multiple statically determinate sub-systems, thus the applied load was expected to be divided equally to the sixteen rubber pads.

Four displacement transducers (LVDTs) were used to monitor the out-of-plane displacement behavior, as shown in Fig. 3.5-c. In addition, a load cell was attached to the actuator in order to measure the applied load. As illustrated in Fig. 3.5-a, masonry specimens were placed horizontally during the quasi-static test, and therefore their self-weight resulted in an additional uniformly distributed load of 1.45 kN (148 kg), which was accounted for.

3.2.2 Comparison Between Experimental and Analytical Wall Responses

As shown in Fig. 3.6-a, Wall FLS experienced horizontal cracks in the mortar joints on both rear and front faces, but no spalling was observed. On the other hand, spalling was observed on the front face of Wall FMS, as illustrated in Fig. 3.6-b, and the level of spalling increased significantly in Wall FHS (see Fig. 3.6-c). This is similar to what was observed in the free field blast tests (ElSayed et al. 2014), in which the level of spalling is directly proportional to the vertical reinforcement ratio. This is attributed to the fact that seismically detailed walls, which are designed to be ductile under in-plane loading, might not exhibit the same ductile behavior under out-of-plane loads. The peak experimental resistances for the three RM walls are presented in Table 3.1 along with predicted values obtained from load-deflection analysis, which was described earlier in the analytical model section, and the UFC 3-340-02 (2008). In general the predicted peak resistances, determined using the load–deflection analysis for the three walls, are in good agreement with the corresponding measured values with a maximum difference of approximately 9%. As shown in Table 3.1, a larger maximum difference of 20% exists between the peak resistance values obtained using the UFC 3-340-02 (2008) (Eq 2-a and 2-b) and the corresponding measured values.

3.2.3 Validation of the Analytical Model Using Free-Field Blast Test Results

The equation of motion for the equivalent nonlinear SDOF system shown in Fig. 3.7 can be written as follows (Biggs 1964):

|  | (3.4) |
| --- | --- |

where M, C and R(X) are the total mass of the real structure, the damping and the nonlinear resistance function of the system at a particular displacement, and ,, and are the displacement, velocity and acceleration of the equivalent SDOF system, respectively. The load-mass factor (KLM) is defined using Eq 3.3. In accordance with ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012), the damping ratio of reinforced concrete, and subsequently reinforced masonry, components is assumed to be 0.05. In order to verify the accuracy of SDOF model, the recorded peak reflected pressures and the corresponding impulses (the 6th and the 7th columns in Table 3.2) were used. Eq 4 is solved using Newmark’s method (Linear Acceleration) to evaluate the nonlinear peak dynamic reposes; such as support rotation.

For typical RM construction utilizing a RC slab, the out-of-plane partially fixed boundary conditions of the wall fall between fixed and simply-supported. Based on the comparison between the experimental and the analytical resistances of the scaled RM walls under quasi-static loading (Table 3.1), it was considered acceptable to assume fixed-fixed boundary conditions to simulate the actual out-of-plane behavior. In addition, mid-cell placement of the vertical reinforcement was assumed. In an effort to provide relevant experimental data, ElSayed et al. (2014) studied the out-of-plane behavior of RM shear walls under free-field explosions. Nine third-scale RM one-story shear walls, matching the wall specimens tested under quasi-static loading, were constructed and tested using three blast scenarios: 6, 12 and 30 kg of explosives at a typical standoff distance of 5.0 m (with scaled distances 2.75, 2.18, and 1.61 m/kg1/3, respectively). The test matrix and test results are listed in Table 3.2. The support rotation, which is defined as the chord angle [ASCE/SEI 59-11 (ASCE 2011) and the CAN/CSA S850-12 (CSA 2012)] (see Fig. 3.3-a), is used to classify the performance of structural components under blast loading. Additional details of the experimental program and the damage that occurred to the RM components following the free-field explosion tests can be found elsewhere (ElSayed et al. 2014).

It can be observed from Table 3.2 that the SDOF predicted peak support rotations for the different walls are in agreement with the corresponding measured support rotations, with a maximum difference of approximately 20%. Discrepancies between the experimental and analytical results can be partially attributed to the assumed boundary conditions and actual rebar allocation, combined with the influence of utilizing constant SIF and DIF values to account for strain rate effects.

3.3 Wall Damage Classification According to ASCE/SEI 59-11 And CAN/CSA S850-12

The maximum deflections at the mid-height of the RM walls under different scaled distances were determined using the validated SDOF model. Using the mid-height deflection value, the maximum support rotation, defined as the chord angle (see Fig. 3.3), is defined and subsequently used to identify the damage that could occur under blast loading, according to ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012). As can be seen in Table 3.3, both North American Standards for blast resistance design consist of four damage levels: Superficial (where the RM wall is unlikely to exhibit any permanent deflection or visible damage), Moderate (where the RM wall will likely have permanent deflections, but this damage is generally repairable; although replacement may be more economical), Heavy (where RM wall has not failed but will likely have significant permanent deflections), and Hazardous (where the RM is more susceptible to failure).

3.4 Effects of Different Parameters on Wall Performance

An objective of this study is to use the validated analytical model to predict the out-of-plane response of RM shear walls under blast load and to develop Performance Design Aids. Design aids such as these are expected to be implemented in future masonry design provisions and guidelines covering such extreme loads. Simulations were performed using the SDOF model to evaluate the maximum support rotations, which were then used to classify the performance of the RM shear walls under blast loads, according to ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012) performance definitions. This parametric study was designed to explore the influence of different design parameters such as threat level, reinforcement ratio, and the different concrete masonry block sizes used in North America. By considering a set of default design parameters, which are specified in Table 3.4, and monitoring the change in peak support rotation with respect to the variation of each design parameter, the impact of such parameters were evaluated. Using this information, a design optimization procedure could be performed to reduce the damage expected to occur in a RM wall under blast loading.

The default masonry wall was a 3.0 m fully-grouted RM shear wall, constructed from standard 190 mm CMU with an average grouted masonry prism compressive strength of = 13.5 MPa and a mass density of 2,300 kg/m3. In addition, 15M reinforcement bars (area = 200 mm2 and yield strength = 400 MPa) were assumed to be located at the center of each cell, providing a longitudinal (vertical) reinforcement ratio of = 0.53%. The default masonry wall was analyzed under the detonation of 300 kg of TNT at a standoff distance 20.0 m resulting in a scaled distance of 3.0 m/kg1/3.

3.4.1 Influence of Charge Weight and Standoff Distance

The selected blast scenarios employed in this study cover a range of charge weights and standoff distances that reflect different DBT levels. The threat scenarios were modeled as hemispherical surface bursts of different magnitude, while charge weights were selected in accordance to FEMA 428 (2003) to account for different types of attacks. As such, four charge weights, as illustrated in Table 3.5, representing personal attack (50 kg of TNT), car bomb (300 kg of TNT), and truck bombs (1,000 and 2,000 kg of TNT) were selected. For each charge weight, four different standoff distances were chosen in order to perform a parametric study with scaled distances ranging from 1.4 to 5.4 m/kg1/3. Smaller scaled distances were used to ensure a far-field type explosion (i.e. scaled distances higher than 1.2 m/kg1/3) (Dusenberry 2010) that results in an uniform pressure distribution on the RM wall surfaces and avoids local modes of failure (e.g. breaching).

As can be observed from Fig. 3.8-a, the peak reflected pressures are inversely proportional to the scaled distance (under different charge weights). For example, the peak reflected pressure that results from the detonation of 1,000 kg of TNT at a standoff distance 30.0 m (Z=3.0 m/kg1/3) is 331 kPa, which is the same as the peak reflected pressure due to the detonation of 300 kg of TNT at a standoff distance 20.0 m (Z=3.0 m/kg1/3). Conversely, the reflected impulses are directly proportional to the charge weight, and inversely proportional to the scaled distance, as illustrated in Fig. 3.8-b. It can also be observed that increasing the value of the scaled distance when the original value is small (1-2) can lead to a significant reduction in both the reflected pressure and reflected impulse.

As shown in Fig. 3.9, the support rotation obtained from different threats is dependent on the charge weight and as such is typically a function of the severity of the reflected impulse. The default RM shear wall investigated in this study is expected to experience Moderate damage when subjected to a blast load resulting from the detonation of 50 kg of TNT at standoff distances of less than 8.0 m. For the detonation of 300 kg of TNT, the RM wall is expected to experience Hazardous failure at standoff distances less than 11.0 m, while Heavy damage is expected to occur at standoff distances ranging from 11.0 to 20.0 m. Moreover, the detonation of 1,000 kg of TNT is expected to cause Hazardous failure at standoff distances less than 22.0 m, while Heavy damage is expected to occur at standoff distances less than 38.0 m. Finally, the damage state of the RM wall is considered Hazardous failure when subjected to blast loads from 2,000 kg of TNT at standoff distances less than 30.0 m, while it is considered Heavy damage under the same charge weight at standoff distances ranging between 30.0 m to 50.0 m. Based on these results, fully-grouted RM shear walls are expected to be capable of withstanding blast loads, albeit with different levels of induced damage that will be dependent on the charge weight and the standoff distance.

3.4.2 Influence of Reinforcement Ratio and Block Size

The effect of different concrete masonry blocks sizes and reinforcement ratios on the response of typical fully-grouted RM shear walls was investigated for two threat scenarios (with the same scaled distance): 300 kg of TNT at standoff distance 20.0 m and 1,000 kg of TNT at a standoff distance of 30.0 m. Four concrete blocks, with thicknesses (bw) of 140, 190, 240, and 290 mm, representing the standard hollow concrete blocks used in North America (Drysdale and Hamid 2005) were considered. To facilitate a comparison, the height of all the walls was held constant at 3.0 m and thus, the slenderness ratio (), which is the ratio of wall height (H) to the concrete block thickness, varied from 10 to 21. The North American blast resistant standards specify a minimum vertical reinforcement for RM structural walls of 0.25%, while the MSJC (2013) [TMS 402-13/ACI 530-13/ASCE 5-13] specifies a maximum reinforcement ratio of 1.4% for special RM shear walls and the maximum reinforcement ratio for moderately ductile RM shear walls is evaluated to be 2.0% by the Canadian standard for masonry design [CAN/CSA S304.1-04 (CSA 2004)]. As such, 27 different reinforcement ratios, as shown in Table 3.6, representing low, moderate, and high reinforcement ratios, were considered in this study.

Figures 3.10-a and 3.10-b illustrate the relationship between reinforcement ratio and peak support rotation for different block sizes for the two blast threats considered. As mentioned earlier, blast induced support rotations are directly proportional to the charge weight (for a given scaled distance). The use of larger concrete block was found to enhance the wall behavior by reducing the support rotation and related damage. Fig. 3.10-a indicates that walls with 290 mm () or 240 mm () thickness are expected to experience Moderate damage, and the impact of increasing the reinforcement ratio on reducing support rotation was found to be insignificant. Increasing the reinforcement ratio was found to lead to a reduction in support rotation for walls with 190 mm () or 140 mm () thickness and reinforcement ratios less than 0.7 %. In general, increasing the reinforcement ratio enhanced the out-of-plane behavior of RM walls, particularly for lower block width values, by reducing the support rotation and subsequently the expected damage. Similar trends were found for the higher threat level, as shown in Fig. 3.10-b. As such, RM shear walls that are designed to withstand blast loads constructed using concrete masonry blocks with thicknesses of 240 or 290 mm are expected to exhibit enhanced performance. In addition, using reinforcement ratios less than 0.7% should ensure that the wall cross-section remains under-reinforced and values above this ratio are not expected to lead to substantial improvement in wall performance.

3.4.3 Influence of Different Reinforcement Layer Configurations

This section focuses on the effect of using two reinforcement layers (as in reinforced concrete walls), compared to the typical mid-cell placement of steel reinforcement within CMU, on the support rotation and corresponding blast induced damage. CMUs with a thickness of 240 mm were used as this block size provides sufficient width for the placement of two reinforcement layers. As can be seen from Fig. 3.11-a and Table 3.7, three reinforcement layouts (Rft-I, Rft-II, and Rft-III) were considered. The first distribution of the reinforcement (Rft-I), which represents the typical construction of RM structural walls in North America, a single layer of 25M bars (= 1.0%) was placed at each mid-cell within the CMUs. In the second layout (Rft-II), the reinforcement area was held constant at but two reinforcement layers of 15M and 20M bars, as shown in Fig. 3.11-a, and therefore the value of  is 0.5%, as only the tensile reinforcement is considered in calculating the reinforcement ratio according to the Canadian standard for masonry design [CAN/CSA S304.1-04 (CSA 2004)]. Finally, Rft-III represents double the reinforcement area of Rft-I, in which two layers of 25M bars were used. As such, the vertical reinforcement ratio in this case is 1.0 %. Fig. 3.11-b illustrates the calculated moment-curvature relationship for the three RM walls, having a block strength of 30 MPa and height of 3.0 m, considering the three reinforcement layouts. Using Rft-II instead of Rft-I increased the maximum plastic moment capacity of the wall cross-section by approximately 30%, while using Rft-III instead of Rft-I increased the plastic moment by approximately 240%. In addition, there is a notable increase in the ductility for two reinforcement configurations compared to a single layer configuration. For example, using Rft-II instead of Rft-I resulted in an increase in the curvature ductility from 1.0 to 2.8 (see Fig. 3.11-b).  In this study, the curvature ductility is calculated from bi-linear idealization technique of moment-curvature relationships using equal energy principal (Tomaževič 1999).

3.4.4 Influence of Compressive Strength and Wall Height

A total of 27 RM shear walls (see Table 3.7), with three different heights and three masonry compressive strengths were investigated. The three wall heights were selected to represent a RM wall in: a typical residential building with floor height of 3.0 m (), a mezzanine story in a commercial building with a typical height of 4.6 m (), and finally a loft building with height 6.0 m (). It should be noted that CAN/CSA S304.1-04 (CSA 2004) specifies an upper limit of 30.0 for the slenderness ratio of RM walls. In addition, the three values of  used in this study (see Table 3.7) represent minimum (= 10.0 MPa), moderate (= 13.5 MPa), and high (= 17.0 MPa) strengths of concrete masonry blocks. As expected, an increase in the masonry compressive strength results in an increase in the cross sectional plastic moment capacity (see Fig. 3.12-a) and subsequently the overall resistance of the wall. However, the ductility of the wall is not affected by the variation of the masonry compressive strength, as illustrated in Fig. 3.12-a where using three different masonry compressive strength resulted in the same brittle type response. As shown in Fig. 3.12-b, the maximum uniform distributed load (and blast pressure) that can be applied on a RM shear wall is inversely proportional to the wall height. In addition, the expected ductility is proportional to wall height. For example, an increase in the wall height from 3.0 m to 6.0 m results in an increase in the wall ductility from 1.7 to 2.3. (see Fig. 3.12-b). The ductility is calculated from bi-linear idealization technique of resistance function using equal energy principal (Tomaževič 1999).

The shear walls presented in Table 3.7 were tested under 2,000 kg of TNT at standoff distance 30.0 m and the calculated peak support rotations for all 27 walls are listed in Table 3.8-a. Fig. 3.13 illustrates the variation of support rotation with respect to the wall height and the masonry prism compressive strength considering the three previously mentioned reinforcement layouts. The three surfaces shown in Fig. 3.13 from top to bottom refer to reinforcement layouts Rft-I, Rft-II, and Rft-III, respectively. Table 3.8-b list the related reduction in the predicted peak support rotations when Rft-II or Rft-III layouts relative to Rft-I. As expected, either increasing the reinforcement ratio or the masonry compressive strength results in a reduction in support rotation and corresponding blast induced damage. On the other hand, increasing the wall height results in an increase in the support rotation obtained under the same DBT.

These results show that the use of two reinforcement layers instead of a single layer (even at lower reinforcement ratios) can result in a significant reduction in support rotation, which is a damage indicator in both North American blast resistant standards. In addition, although seismically detailed RM structural walls possess reinforcement ratios that fall within the limits specified to ensure a ductile response under in-plane loads, such ratios might result in a brittle type response under out-of-plane loads.

3.4.5 Influence of Yield Strength of Reinforcement Bars

As the yield strength of the steel reinforcement () directly influences wall strength, this component of the parametric study considered three values of = 400, 500 and 600 MPa in order to investigate the effect of  on the peak support rotation under blast loads. Four blast loads were selected in order to produce different impulse values and subsequently different damage levels. As such, four blast scenarios: 50 kg of TNT, 300 kg of TNT, 1,000 kg of TNT, and 2,000 kg of TNT were simulated at standoff distances of 8.0 m, 15.0 m, 22.5 m, and 28.0 m, respectively. All RM walls in this part of the parametric study were 3.0 m height with a 190 mm wall thickness. The compressive strength of the grouted masonry prisms was 13.5 MPa not considering reinforcement, while 15M bars were placed at the center of every cell.

Fig. 3.14 illustrates the effect of changing the reinforcement yield strength on the out-of-plane peak support rotation of one-way fully-grouted RM shear walls under different threat levels. As can be observed from the results, peak support rotation is inversely proportional to the yield strength of the reinforcement up to a certain limit. This limit is related to the blast load level. For example, a 35 % reduction in the support rotation for charge size of 2,000 kg of TNT at a standoff distance of 28.0 m is expected when fy is increased to 500 MPa from 400MPa, however the reduction in support rotation is expected to be only 8% when fy is increased to 600 MPa from 500MPa.

3.5 Performance Charts

Fig. 3.15 illustrates the effect of charge weight and reinforcement ratio on peak support rotation considering two concrete block widths: 190 mm (the upper surface) and 240 mm (the lower surface). It can be observed from Fig. 3.15 that the support rotation of a RM shear wall is proportional to the charge weight (under the same standoff distance), and inversely proportional to the vertical reinforcement ratio. Wall height is also an important parameter which influences wall resistance and subsequently the peak support rotation and blast induced damage, as shown in the compressive strength and wall height component of the parametric study. (As such, the current study proposes Performance Design Aids that can serve two purposes. First, the design aid scan be used for preliminary design of RM walls to ensure that the expected damage after an explosion would not exceed the wall damage demand. Secondly, the design aids can be used to predict the damage that could occur in an existing wall when subjected to a blast load. Fig. 3.16 presents a sample of the proposed Performance Design Aids, which illustrate the effect of wall height and reinforcement ratio on the predicted peak support rotation. These samples of Performance Design Aids were developed for different threat scenarios and wall width values. It can be observed from these charts that using reinforcement ratio higher than 0.7 % does not result in any appreciable reduction in either support rotation or damage. This indicates that the increased strength (with reduced ductility) might not enhance the blast response of RM walls and thus, a balance between the ductility and strength should be carefully considered in blast resistant design.

3.5 Conclusions

With the introduction of the new American (ASCE/SEI 59-11) and Canadian (CAN/CSA S850-12) standards for blast resistant design a method to quantify the performance of different structural components under such extreme loads is needed. As such, there is an urgent need to develop analytical models that have the capability of predicting the response of structural components under blast loads.

In this regard, a nonlinear analytical model, based on a SDOF model, was used in the current study to evaluate the out-of-plane response of RM shear walls under blast loads. The proposed analytical model was validated using experimental data obtained from quasi-static and free-field blast tests. First, the analytical model determines the blast load parameters in accordance to CAN/CSA S850-12. Next, the nonlinear resistance of the structural wall using fiber model and load-deflection analysis by double integration of the curvature distribution is carried out. Finally, the peak mid-span deflection and the corresponding support rotation are determined. This model was subsequently used via a parametric study to evaluate various design parameters, such as threat level and reinforcement ratio, on the blast induced damage in RM structural walls. In addition, Performance Design Aids, which can be used in the preliminary design of new structures or the prediction of damage that may occur to an existing masonry component subjected to a certain blast level, were developed and presented in the current study. Based on the findings from the analyses, the following conclusions can be stated:

- The model predictions were in good agreement with both the quasi-static test results (with a maximum difference of about 9%) and the free-field blast support rotation (with a maximum difference up to 20%).

- RM structural walls are capable of withstanding blast load from substantial blast loads with different extend of damage depending on the threat level and walls characteristics.

- A block thickness of less than 190 mm are not recommended in the construction of masonry walls which are expected to experience blast loading. On the other hand, concrete masonry blocks with a thickness of 240 mm (or higher) perform better under blast loading.

- Although TMS 402-13/ACI 530-13/ASCE 5-13 specifies a maximum reinforcement ratio of 1.4% for special RM shear walls, using reinforcement ratios higher than 0.7% is not suggested for RM walls that are expected to experience out-of-plane blast loading in order to ensure that the walls remain ductile. This is due to the reduced reinforcement moment arm. As such, two reinforcement layers, instead of the typical single layer of bars placed at the mid-cell of CMUs can be used to enhance performance. A significant increase in the ductility (up to 2.3) was observed at using two reinforcement layers, compared to the predicted less ductile behavior when a single layer is used.

- Increased masonry compressive strength enhanced the plastic moment, and thus the resistance of the masonry wall. However, an increase in the masonry compressive strength did not result in increased ductility. As such, the enhancement in the compressive strength of the masonry may be suitable as long as the resulting blast strength demand does not exceed the wall capacity, which would typically lead to a brittle failure.

- The impact of reinforcement yield strength on the RM walls damage is inversely proportional to the support rotation. This relationship is only valid to a certain limit; for yield strengths higher than the certain limit, the support rotation will be slightly affected. This limit is directly related to the blast load level.

- For a given blast threat, increasing the reinforcement ratio was found to improve the behavior of RM shear walls under out-of-plane blast loads. However, this enhancement is valid only for reinforcement ratios less than 0.7 %, which indicate a brittle response is expected for RM walls with higher reinforcement ratios. This is attributed to the fact that seismically RM walls that are designed to act in a ductile way under in-plane loads are not guaranteed to behave in the same manner under out-of-plane loads.

The above findings are limited to the range of walls considered in this study. It is recommended that further studies be carried out in order to expand the applicability of the above conclusions.

Appendix 3.1 Notation

The following symbols are used in this paper:

| SDOF | = | Single degree of freedom |
| --- | --- | --- |
| MDOF | = | Multi degree of freedom |
| FE | = | Finite element |
| DBT | = | Design basis threat |
| W | = | TNT charge mass in kg |
| SD | = | Standoff distance from the detonation source to target (meters) |
| Pr | = | Peak reflected pressure (kPa) |
| Ir | = | Reflected impulse (kPa.msec) |
| Z | = | Scale distance (m/kg1/3) |
| t0 | = | Positive phase duration (msec) |
| Em | = | Masonry’s Young's modulus |
| Ieff | = | Effective second moment of inertia |
| Mp | = | Plastic Moment |
| SIF | = | Strength increase factor |
| DIF | = | Dynamic increase factor |
|  | = | Extreme upper fiber’s strain value |
| Ke | = | Elastic stiffness |
| Kep | = | Elasto-plastic stiffness |
| Kp | = | Plastic stiffness |
| Re | = | Elastic resistance |
| Rep | = | Elasto-plastic resistance |
| H | = | Wall height (m) |
|  | = | Out-of-plane deformed shape |
|  | = | Average compressive strength of the grouted masonry prisms (MPa) |
| X | = | Displacement of SDOF system (m) |
| X | = | Velocity of SDOF system (m/sec) |
| X | = | Acceleration of SDOF system (m/sec2) |
| KLM | = | Transformation load-mass factor |
| M | = | Total mass of the RM wall (kg) |
| R(X) | = | Resistance function as a function in the mid-height deflection |
| P(t) | = | Pressure response history |
|  | = | Vertical reinforcement ratio |
| TNT | = | Trinitrotoluene |
|  | = | Yield strength of reinforcement |

Appendix 3.2 References

Abou Zeid, B.M., El-Dakhakhni, W.W., Razaqpour; A.G., and Foo, S. (2014). “Time-Response Analysis of Arching Unreinforced Concrete Block Walls Subjected to Blast Loads.” Journal of Structural Engineering, ASCE, Vol. 140(4) Permalink: http://dx.doi.org/10.1061/(ASCE)ST.1943-541X.0000893

American Society for Testing and Materials (ASTM) (2011). “Standard Test Methods for Compressive Strength of Masonry Prisms.”, C1314-11, West Conshohocken, Pa.

American Society of Civil Engineers (ASCE) (2011). “Blast Protection of Building.” ASCE/SEI 59-11, Reston, Virginia.

Baker, W.E., Cox, P.A., Westine, P.S., Kulesz, J.J., and Strehlow, R.A. (1983). “Explosion Hazard and Evaluation.” Oxford, New York, USA: Elservier Scientific Publishing Company.

Bao, Y., Lew, H.S., and Kunnath, S.K. (2014). “Modeling of Reinforced Concrete Assemblies Under Column Removal Scenario.” Journal of Structural Engineering, Vol. 140(1), Permalink: http://dx.doi.org/10.1061/(ASCE)ST.1943-541X.0000773

Biggs, J.M. (1964). “Introduction to Structural Dynamics.” New York, USA: McGraw-Hill Inc.

Bischoff, P.H., and Perry, S.H. (1991). “Compressive Behaviour of Concrete at High Strain Rates.” Journal of Materials and Structures, Vol. 24, pp. 425-450.

Canadian Standards Association (CSA). (2004). “Design of Masonry Structures.”, CAN/CSA S304.1-04, Mississauga, Ontario, Canada.

Canadian Standards Association (CSA). (2012). “Design and Assessment of Buildings Subjected to Blast Loads.”, CAN/CSA S850-12, Mississauga, Ontario, Canada.

CEB, Comité Euro-International du Béton, (1988). “Concrete structures under impact and impulsive loading.” CEB Bulletin 187, Lausanne, Switzerland.

Chopra, A.K. (2007). “Dynamics of Structures.” Pearson Edition Inc., New-Jersey, USA, Third Edition.

Coughlin, A.M., Musselman, E.S., Schokker, A.J., and Linzell, D.G. (2010). “Behavior of Portable Fiber Reinforced Concrete Vehicle Barriers Subject to Blasts from Contact Charges.” International Journal of Impact Engineering, Vol. 37 (5), pp. 521-529.

Davidson, J., Fisher, J., Hammons, M., Porter, J., and Dinan, R. (2005). ”Failure Mechanisms of Polymer-Reinforced Concrete Masonry Walls Subjected to Blast.” Journal of Structural Engineering, ASCE, Vol. 131(8), pp. 1194-1205.

Drysdale, R.G., and Hamid, A.A. (2005). “Masonry Structures: Behavior and Design, Canadian Edition.” Mississauga, Ontario, Canada.

Dusenberry, D.O. (2010). “Handbook for Blast Resistant Design of Buildings.” New-Jersey, USA: Wiley & Sons Inc., First Edition.

ElSayed, M., El-Dakhakhni, W., and Tait, M. (2014). “Performance Assessment of Reinforced Concrete Block Structural Walls Under Blast Loading.” Submitted to Journal of Structural Engineering, ASCE, in April 2014.

FEMA (2003). Premier to Design Safe School Projects in Case of Terrorist attacks – FEMA 428. Federal Emergency Management Agency (FEMA), Washington, DC. Available at http://www.fema.gov/pdf/plan/prevent/rms/428/fema428.pdf [accessed 27 March 2014].

Hamed, E. and Rabinovitch, O. (2008). “Nonlinear Dynamic Behavior of Unreinforced Masonry Walls Subjected to Out-of-Plane Loads.” Journal of Structural Engineering, ASCE, Vol. 134(11), pp. 1734-1753.

Harris, H.G., and Sabnis, G.M. (1999). “Structural Modeling and Experimental Techniques: Second Edition.” New York, USA: CRC Press.

Hrynyk, T.D., and Myers, J.J. (2008). “Out-of-Plane Behavior of URM Arching Walls with Modern Blast Retrofits: Experimental Results and Analytical Model.” Journal of Structural Engineering, ASCE, Vol. 134(10), pp. 1589-1597.

Krauthammer, T., Bazeos, N., Holmquist, T.J. (1986). “Modified SDOF Analysis of RC Box-Type structures.” Journal of Structural Engineering, ASCE, Vol. 112(4), pp. 726-744.

Krauthammer, T., Shahriar, S., and Shanaa, H.M. (1990). “Response of Reinforced Concrete Elements to Severe Impulsive Loads.” Journal of Structural Engineering, ASCE, Vol. 116(4), pp. 1061-1079.

Krishnappa, N., Bruneau, M., and Warn, G.P. (2013). “Weak-Axis Behavior of Wide Flange Columns Subjected to Blast.” Journal of Structural Engineering, ASCE, Permalink: http://dx.doi.org/10.1061/(ASCE)ST.1943-541X.0000917

Lew, H.S., Main, J.A., Robert, S.D., Sadek, F., and Chiarito, V.P. (2013). “Performance of Steel Moment Connections Under a Column Removal Scenario. I: Experiments.” Journal of Structural Engineering, Vol. 139(1), pp.98-107.

Li, J., and Hao, H. (2014). “Numerical Study of Concrete Spall Damage to Blast Loads.” International Journal of Impact Engineering. Vol. 68, pp. 41-55.

Malvar, L.J. (1998), “Review of Static and Dynamic Properties of Steel Reinforcing Bars.” ACI Material Journal, Vol. 95(5), pp. 609-616.

Masonry Standards Committee Joints (MSJC). (2013). “Building Code Requirements for Masonry Structures.”, TMS 402-13/ACI 530-13/ASCE 5-13. USA.

Morison, C.M. (2006). “Dynamic Responses of Walls and Slabs by Single-Degree-of-Freedom Analysis – A Critical Review and Revision” International Journal of Impact Engineering, Vol. 32, pp. 1214-1247.

Nassr, A.A., Razaqpur, A.G., Tait, M.J., Campidelli, M., and Foo, S. (2012). “Single and Multi Degree of Freedom Analysis of Steel Beams under blast loading.” Nuclear engineering and design, 242(1), pp. 63-77.

Nassr, A.A., Razaqpur, A.G., Tait, M., Campidelli, M., and Foo, S. (2013). “Dynamic Response of Steel Columns Subjected to Blast Loading.” Journal of Structural Engineering, ASCE, Permalink: http://dx.doi.org/10.1061/(ASCE)ST.1943-541X.0000920.

Priestley, M.J.N., Calvi, G.M., and Kowalsky, M.J. (2007). “Displacement Based Seismic Design of Structures.” IUSS Press, Pavia ,Italy, First Edition.

Sadek, F., Main, J.A., Lew, H.S. and El-Tawil, S. (2013). “Performance of Steel Moment Connections Under a Column Removal Scenario. II: Analysis.” Journal of Structural Engineering, ASCE, Vol. 139(1), pp.108-119.

Silva, P.F., and Lu, B. (2009). “Blast Resistance Capacity of Reinforced Concrete Slabs.” Journal of Structural Engineering, ASCE, Vol. 135(6), pp. 708-716.

Stolz, A., Fischer, K., and Lu, B. (2014). “Dynamic Bearing Capacity of Ductile Concrete Plates Under Blast Loading.” International Journal of Impact Engineering, Vol. 69, pp. 25-38.

The MathWorks (2013). MATLAB – Statistics ToolboxTM User’s Guide. Version 8.1.0.604 – Release 2013 [online]. The MathWorks Inc., Natick, MA. Available from http://www.mathworks.com/help/stats/ [accessed 15 February 2013].

Tomaževič, M. (1999). “Earthquake resistant design of masonry buildings.”  Imperial College Press, London.

Urgessa, G. and Maji, A. (2010). “Dynamic Response of Retrofitted Masonry Walls for Blast Loading.” Journal of Engineering Mechanics, ASCE, Vol. 136(7), 858–864.

US Army Corps of Engineers, Naval Facilities Engineering Command, and Air Forces Civil Engineer Support Agency (2008), “Structures to Resist the Effect of Accidental Explosions.” Unified Facilities Criteria, UFC 3-340-02.

Williams, G.D., and Williamson E.B. (2011). “Response of Reinforced Concrete Bridge Columns Subjected to Blast Loads.” Journal of Structural Engineering, ASCE, Vol. 137(9), pp. 903-913.

Warn, G.P., and Bruneau, M. (2009). “Blast Resistance of Steel Plate Shear Walls Designed for Seismic Loading.” Journal of Structural Engineering, ASCE, Vol. 135(10), pp. 1222-1230.

Yu, J., and Tan, K., (2013). “Structural Behavior of RC Beam-Column Subassemblages Under a Middle Column Removal Scenario” Journal of Structural Engineering, ASCE, Vol. 139(2), pp. 233-250.

Table 3. 1: Experimental and theoretical RM wall peak resistances

| Wall ID | Vertical Reinforcement Ratio (%) | Experimental Peak Resistance (kN) | UFC 3-340-02 (2008) Model |  | Load-deflection Analysis |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Rep (kN) | Error (%) | Rep (kN) | Error (%) |
| FLS | 0.33 | 063.1 | 050.9 | -19.3 | 060.5 | - 4.1 |
| FMS | 0.62 | 087.4 | 079.9 | -08.6 | 095.1 | + 8.8 |
| FHS | 1.07 | 139.1 | 123.2 | -11.4 | 145.5 | + 4.6 |

Table 3. 2: Experimental and analytical wall support rotations

| Shot No. | Group | Wall ID | Equivalent TNT charge mass in (kg) | Scaled distance (m/kg1/3) | Reflected pressure (kPa) | Reflected impulse (kPa.msec) | Measured support rotation (degree) | Analytical support rotation (degree) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | I | FL11 | 6.0 | 2.75 | 372.5 | 431.2 | 1.8 | 2.0 | 1.09 |
| 2 |  | FM11 |  |  | 380.8 | 494.7 | 1.7 | 1.7 | 1.00 |
| 3 |  | FH11 |  |  | 421.5 | 462.1 | 1.6 | 1.3 | 0.79 |
| 4 | II | FL22 | 12.0 | 2.18 | 872.8 | 685.2 | 4.3 | 4.1 | 0.95 |
| 5 |  | FM22 |  |  | 785.0 | 726.3 | 3.7 | 3.0 | 0.80 |
| 6 |  | FH22 |  |  | 775.7 | 784.0 | 2.7 | 2.7 | 1.00 |
| 7 | III | FL55 | 30.0 | 1.61 | N.A. | N.A. | Failure | --- | N.A. |
| 8 |  | FM55 |  |  | 1941.8 | 1225.4 | 8.7 | 7.2 | 0.83 |
| 9 |  | FH55 |  |  | 2077.0 | 1529.6 | 7.9 | 7.0 | 0.88 |

Table 3. 3: ASCE/SEI 59-11 and CSA S850-12 Response Limits

| RM Wall Damage State | Quantitative Damage Description in the ASCE/SEI 59-11 and CSA S850-12 Standards | Expected Building LOP | Building Performance |
| --- | --- | --- | --- |
| Superficial Damage | Ductility level less than 1 (elastic response) | Medium/High | Immediate Occupancy/ Operational |
| Moderate Damage | Support rotation less than 2° | Low | Life Safety |
| Heavy Damage | Support rotation between 2° and 8° | Very Low | Collapse Prevention |
| Hazardous Failure | Support rotation higher than 8° | N.A. | N.A. |

# Table 3. 4: Default values used in the parametric study

| Parameter | Symbol | Units | Default Value |
| --- | --- | --- | --- |
| Charge Mass | W | kg | 300 |
| Standoff Distance | SD | m | 20.0 |
| No. of Reinforcement Layers |  |  | 1.0 |
| Wall Height | H | m | 3.0 |
| Block Width | bw | mm | 190 |
| Reinforcement | Rft |  | 15M each cell (0.53%) |
| Yield Strength of reinforcement | Fy | MPa | 400 |
| Compressive Strength of masonry Prism |  | MPa | 13.5a |

a Assumed block strength of 30 MPa

# Table 3. 5: Scaled distances (m/kg1/3) for different threat scenarios

| Charge Weight (kg TNT) | Standoff Distance (m) |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | 5 | 10 | 15 | 20 | 30 | 40 | 50 |
| 0,050 | 1.4 | 2.7 | 4.1 | 5.4 |  |  |  |
| 0,300 |  | 1.5 | 2.2 | 3.0 | 4.5 |  |  |
| 1,000 |  |  | 1.5 | 2.0 | 3.0 | 4.0 | 5.0 |
| 2,000 |  |  |  | 1.6 | 2.4 | 3.2 | 4.0 |

# Table 3. 6: Reinforcement ratios (%)

| Reinforcement | Block Width (mm) |  |  |  |
| --- | --- | --- | --- | --- |
|  | 140 | 190 | 240 | 290 |
| 10M each cell | 0.4 | 0.3 |  |  |
| 10M each other cell + 15M each other cell | 0.5 | 0.4 | 0.3 |  |
| 15M each cell | 0.7 | 0.5 | 0.4 | 0.3 |
| 15M each other cell + 20M each other cell | 0.9 | 0.7 | 0.5 | 0.4 |
| 20M each cell | 1.1 | 0.8 | 0.6 | 0.5 |
| 20M each other cell + 25M each other cell | 1.4 | 1.1 | 0.8 | 0.7 |
| 25M each cell |  | 1.3 | 1.0 | 0.9 |
| 25M each other cell + 30M each other cell |  |  | 1.3 | 1.0 |
| 30M each cell |  |  |  | 1.2 |

# Table 3. 7: Wall configurations

| Masonry Compressive Strength (MPa) | Rft-I |  |  | Rft-II |  |  | Rft-III |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | H=3.0m | H=4.6m | H=6.0m | H=3.0m | H=4.6m | H=6.0m | H=3.0m | H=4.6m | H=6.0m |
| 10.0 (Block 20 MPa) | Wall #1 | Wall #2 | Wall #3 | Wall #4 | Wall #5 | Wall #6 | Wall #7 | Wall #8 | Wall #9 |
| 13.5 (Block 30 MPa) | Wall #10 | Wall #11 | Wall #12 | Wall #13 | Wall #14 | Wall #15 | Wall #16 | Wall #17 | Wall #18 |
| 17.0 (Block 40 MPa) | Wall #19 | Wall #20 | Wall #21 | Wall #22 | Wall #23 | Wall #24 | Wall #25 | Wall #26 | Wall #27 |

# Table 3. 8: (a) Walls’ support rotation, and (b) corresponding reduction (%) in response

# (a)

| Masonry Compressive Strength (MPa) | Rft-I |  |  | Rft-II |  |  | Rft-III |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | H=3.0m | H=4.6m | H=6.0m | H=3.0m | H=4.6m | H=6.0m | H=3.0m | H=4.6m | H=6.0m |
| 10.0 (Block 20 MPa) | 3.3 | 5.8 | 8.1 | 2.1 | 4.5 | 6.3 | 1.1 | 2.3 | 3.1 |
| 13.5 (Block 30 MPa) | 2.7 | 4.9 | 6.6 | 2.1 | 4.6 | 6.2 | 0.9 | 2.1 | 2.9 |
| 17.0 (Block 40 MPa) | 2.3 | 4.2 | 5.9 | 2.0 | 4.4 | 6.1 | 0.9 | 2.1 | 3.0 |

# (b)

| Masonry Compressive Strength (MPa) | Rft-I |  |  | Rft-II |  |  | Rft-III |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | H=3.0m | H=4.6m | H=6.0m | H=3.0m | H=4.6m | H=6.0m | H=3.0m | H=4.6m | H=6.0m |
| 10.0 (Block 20 MPa) |  |  |  | 34.1 | 22.0 | 22.6 | 66.3 | 59.9 | 62.2 |
| 13.5 (Block 30 MPa) |  |  |  | 23.0 | 7.7 | 6.8 | 65.3 | 57.4 | 56.3 |
| 17.0 (Block 40 MPa) |  |  |  | 12.7 | -5.9 | -3.6 | 62.7 | 48.8 | 49.1 |

Quasi-static Earthquake Blast Impact Creep

(a)

Earthquake Quasi-static Creep Impact Blast

(b)

Fig. 3. 1: Effect of strain rate on material characteristics: (a) concrete, (b) reinforcement bars

Design Basis Threat (DBT)

- Charge mass (W)

- Standoff distance (SD)

- Load-mass factor KLM(x) and total mass M

- Damping C

- Resistance function R(x)

- Stiffness (K)

Blast Load Parameters

- Reflected pressure (Pr)

- Reflected impulse (Ir)

- Load duration (td)

- Dynamic compressive strength of masonry prisms (fmd’)

- Dynamic yield strength of reinforcement bars (fyd)

- Dynamic ultimate strength of reinforcement bars (fud)

- Typical cross-section dimensions

Blast Load Model

(CSA 2012)

Moment-Curvature Model (Using fiber model)

- Moment-Curvature relationship considering strain rate effect

Resistance Function Model (Using load-deflection analysis)

- Wall length (L)

- Boundary conditions

SDOF Model

- SDOF response parameters:

- Maximum mid-span deflection

- Peak support rotation (in accordance to ASCE/SEI 59-11 and CSA S850-12)

- Quantitative Damage (in accordance to ASCE/SEI 59-11 and CSA S850-12)

Fig. 3. 2: Algorithm used to develop the peak RM wall response under out-of-plane blast loading

|  |  | Plastic Hinges |  |
| --- | --- | --- | --- |
|  | Elastic behavior | Elasto-Plastic behavior | Plastic behavior |
| (a) |  |  |  |
| Neutral Axis |  |  |  |
| Divide sections into layers Strain profile and idealization force distribution |  |  |  |
| (b) |  |  |  |

Fig. 3. 3 (a): The behavior of one-way RM wall with fixed-fixed boundary conditions and the definition of support rotation in according to ASCE/SEI 59-11, and (b): fiber model

| (a) | (b) |
| --- | --- |
| 15 W1.7 (0.26 %) Horizontal Reinforcement 15 D7 (1.07 %) Vertical Reinforcement 7 W1.7 (0.12 %) Horizontal Reinforcement 8 D4 (0.33 %) Vertical Reinforcement 15 W1.7 (0.26 %) Horizontal Reinforcement 15 D4 (0.62 %) Vertical Reinforcement |  |
| (c) |  |

Fig. 3. 4: (a) Typical wall dimensions (mm), (b) the construction of fixed-fixed boundary conditions, and (c) cross section of typical masonry specimens

|  | Actuator Load Cell |
| --- | --- |
| (a) |  |
| (b) | (c) |

Fig. 3. 5: Quasi-static test setup

| Rear Face Front Face | Rear Face Front Face |
| --- | --- |
| (a) | (b) |
| Rear Face Front Face |  |
| (c) |  |

Fig. 3. 6: Crack Pattern for Walls (a) FLS, (b) FMS and (c) FHS

Fig. 3. 7: Nonlinear Single Degree of Freedom System

(a)

(b)

Fig. 3. 8: Impact of scaled distance on (a) the peak reflected pressure, and (b) the peak reflected impulse

Heavy Damage Hazardous Failure Moderate Damage

Fig. 3. 9: Effect of changing standoff distance and charge weight on support rotation of one-way RM walls

Moderate Damage Heavy Damage

(a)

Heavy Damage Hazardous Failure Moderate Damage

(b)

Fig. 3. 10: Impact of reinforcement ratio and block size on RM wall support rotation considering two threats: (a) 300 kg of TNT at standoff distance 20 m (Z=3.0 m/kg1/3), and (b) 1,000 kg of TNT at standoff distance 30 m (Z=3.0 m/kg1/3)

Rft-I Rft-II Rft-III

(a)

(b)

Fig. 3. 11: (a) Different Distributions for reinforcement bars, and (b) the corresponding moment-curvature relationships having a block strength of 30 MPa

(a)

(b)

Fig. 3. 12: (a) Effect of using different prism compressive strength on the plastic moment of typical RM wall having Rft-I configuration, and (b) Effect of wall height on the resistance function of RM wall having a block strength of 30 MPa

Fig. 3. 13: Effect of wall height and masonry compressive strength on the peak support rotation using three different reinforcement layouts

Heavy Damage Hazardous Failure Moderate Damage

Fig. 3. 14: Effect of yield strength of reinforcement on the peak support rotation of 3.0 m height RM shear wall under different blast threats

Fig. 3. 15: Predicted support rotation of 3.0 m height RM shear wall considering two block thicknesses: 190 mm (the upper surface), and 240 mm (the lower surface) under blast loads from typical standoff distance 20.0 m

W = 50 kg (Equivalent TNT)

SD = 5.0 m

bw = 190 mm

f'm = 13.5 MPa

f y = 400 MPa

f u = 600 MPa

W = 300 kg (Equivalent TNT)

SD = 15.0 m

bw = 190 mm

f'm = 13.5 MPa

f y = 400 MPa

f u = 600 MPa

W = 1,000 kg (Equivalent TNT)

SD = 30.0 m

bw = 240 mm

f'm = 13.5 MPa

f y = 400 MPa

f u = 600 MPa

W = 2,000 kg (Equivalent TNT)

SD = 50.0 m

bw = 290 mm

f'm = 13.5 MPa

f y = 400 MPa

f u = 600 MPa

Fig. 3. 16: Sample of design aids for reinforced masonry walls under different blast scenarios and wall width

Chapter 4: A Simplified Framework for Blast Risk-based Cost-Benefit Analysis for Reinforced Concrete Block Buildings

Abstract: Probabilistic risk assessment (PRA) is essential to evaluate different options for blast risk management. However, a rigorous blast PRA study can be quite demanding depending on the risk management approach being considered. To expedite this process, a simplified PRA framework is proposed in order to determine design basis threat (DBT) fragility curves for reinforced concrete block shear wall buildings. The current definitions of damage states by North American standards (ASCE/SEI 59-11 and CAN/CSA S850-12) for blast resistant design involve global response limits such as the component support rotations that are relatively simple to calculate. However, these quantitative damage state descriptors can be less relevant for cost–benefit analysis. Therefore, revised damage states are presented that result in metrics that are more suitable for a cost–benefit analysis, including repair technique and building downtime. These metrics are currently considered more meaningful and have been used to quantify the post-earthquake performance of buildings. To illustrate the proposed methodology, an application is presented involving a medium–rise reinforced masonry building, under different DBT levels. The DBT fragility curves are obtained via Monte Carlo sampling of the random variables and are used to infer the locations, within the building premises, that are most suitable for the erection of barriers for blast hardening. As such, the proposed PRA framework can be utilized to identify target performance requirements formulated in terms of the facility stakeholders’ specified tolerable probability of failure and consequent risk management manners.

Keywords: Blast performance, Concrete block, Qualitative damage state descriptors, Probabilistic risk assessment, Reinforced masonry, Shear wall, Site planning, Risk, Uncertainty.

4.1 Introduction

The recently introduced North American standards for the design and analysis of structures subjected to blast loading [ASCE/SEI 59-11 (ASCE 2011) and the CAN/CSA S850-12 (CSA 2012)] adopt damage criteria based on metrics that are related to the overall structural component response (e.g. ductility ratios and support rotations). However, developed methodologies for the assessment of the seismic performance of buildings, as laid out in the Federal Emergency Management Agency document FEMA P-58 (FEMA 2012a) and its background reports (FEMA 2012b–2012e), make use of local damage descriptors (e.g. maximum crack width, deformation of the steel reinforcement, etc.) that can be easily linked to various repair techniques – as described in FEMA 308 (FEMA 1998) – and consequent costs. Subsequently, linkage between seismic– and blast–induced damage and associated repair costs would be of significant benefit to stakeholders and analysts tasked with the cost–benefit analysis for potential blast hardening and short- and long-term risk management.

In order to evaluate different risk mitigation options, probabilistic risk assessment (PRA) methodologies, such as those used by Stewart et al. (2006) and Stewart and Netherton (2008) for the assessment of window glazing under explosive loading, are currently considered as the most comprehensive procedures. A rigorous PRA study is needed when the consequences of failure are exceedingly severe (Ellingwood 2006; and Pekau and Cui 2006), however, carrying out every step in a PRA can be very demanding, as it requires the assessment of threat (likelihood of an explosion), load uncertainty (caused by systematic and random errors in the blast load descriptor characteristics), response uncertainty (caused by variability in the material properties, geometry, etc.), probability of damage limit state violation, consequences (e.g. economic losses), and finally risk evaluation and subsequent risk management (Stewart et al. 2006). If the latter is considered intolerable, the cost of several interventions of risk mitigation can be weighed against the benefit of the corresponding increased safety, in order to find a financially viable solution that entails an acceptable level of risk. Such an acceptable risk level would in turn be correlated to a target facility level of protection (LOP) described in ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012).

A key element in this laborious PRA process is meaningful definitions of the pertinent component damage states, which are based on the modes of failure that the component being considered is expected to experience under a specific design basis threat (DBT). The response and failure mechanism of masonry walls subjected to out–of–plane blast pressure have been the subject of several recent studies. However, most of these studies have been focused on unreinforced masonry walls (URM) (e.g. Myers et al. 2004; Carney and Myers 2005; Milani and Lourenço 2009; Seyedrezai 2011; Abou-Zeid et al. 2014), while fewer research programs have addressed the dynamic behavior of reinforced concrete block walls (Mayrhofer 2002; Browning et al. 2014) or walls with near–surface–mounted reinforcement (e.g. Mierzejewski 2010).

The scope of the current study is to propose a simplified PRA framework for blast risk management by adapting the methodologies currently adopted for quantifying buildings damage following seismic events (FEMA 2012a–e) to the expected damage under blast loads. In accordance to previous experimental research conducted by the authors (ElSayed et al. 2014a), quantitative damage indicators traditionally used by modern blast standards such as ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012) (i.e. support rotation) do not lend themselves to qualitative damage assessment and thus, repair cost and subsequently cost–benefit analysis. As such, the four damage states designated by ASCE/SEI 59-11 (ASCE 2011) for reinforced concrete block wall buildings as superficial, moderate, heavy, and hazardous will be linked to qualitative local damage descriptors/criteria such as the maximum crack width and amount of spalling experienced by the masonry wall. In addition, each damage state can be associated with a recommended repair technique and an estimate of building downtime, which would have a direct impact on cost–benefit analyses. Subsequently, the lower bounds of each damage state are adopted as a limit state within a simplified framework proposed for blast performance assessment, which is largely based on a more general PRA methodology.

Finally, an application is presented to illustrate how such simplified framework can be utilized to establish the likelihood of experiencing a certain damage state given a DBT scenario, namely, the surface detonation of explosive charges over a range of standoff distances from the target. The example presented considers the case of a four–story structure featuring fully–grouted, reinforced masonry shear walls (RMSW) that may represent an archetypical low and medium–rise building (NIST 2010). The probability density functions (PDFs), used to assess the probability of a specific (qualitative) level of damage, are obtained by Monte Carlo sampling of the random variables that describe the wall resistance. DBT fragility curves showing the probability of experiencing moderate, heavy, and hazardous damage versus the standoff distance for several DBT scenarios, are generated and used to evaluate the different risk mitigation options. For the current application, the developed DBT fragility curves are employed to determine the best allocation of blast protection barriers, in order to meet the tolerable probabilities of failure targets. As a result, the building’s premises can be classified into four zones characterized by increasing level of security and access restrictions as their distance from the building diminishes.

4.2 Summary of Previous Research

In an effort to provide relevant data to meet the scope of the current paper, ElSayed et al. (2014a) conducted arena testing of RMSW under out-of-plane loading resulting from surface explosions. In their study, ElSayed et al. (2014a) tested nine third-scale RMSW; considering three different reinforcement ratios and three different explosion weights. The test results consistently showed a flexural mode of failure, with both ductile and brittle responses observed. This experimental study showed that use of qualitative versus quantitative damage descriptors could result in inconsistent, and in fact ambiguous, damage state classification that might lead to inaccurate cost–benefit analysis in terms of estimating post–blast repair and replacement costs. ElSayed et al. (2014b) also developed a Single-degree-of-freedom (SDOF) model to predict the out-of-plane response of RMSWs subjected to blast loadings. This SDOF model was subsequently used to extend the results of the experimental work with different design parameters in order to further study the influence of these design parameters on the out-of-plane response of RMSW under blast loads. In general, findings from both studies (ElSayed et al. 2014a and 2014b) indicate that seismically–detailed RMSW designed to behave in a ductile manner under in-plane loads might be exhibit a brittle-type response (fracture critical) under out–of–plane loads. The proposed SDOF model developed by ElSayed et al. (2014b) is revised in the current study to facilitate quantification and prediction of different level of damage states that could occur to RMSW in terms of maximum crack width and amount of spalling.

4.3 Methodologies for Probabilistic Risk Assessment of Blast Damage

4.3.1 Generalized PRA Framework

Even with the assumption of deterministic knowledge of the parameters defining a range of DBT Θij, given a combination of charge mass (mi) and standoff distance (Rj), there is still a considerable degree of uncertainty affecting the prediction of the subsequent component structural response. This is attributed to the numerous sources of variability pertaining to both the blast load and the structural system, which can be designated under parameter uncertainty, model error, and inherent variability (Stewart et al. 2006). Therefore, a rational approach for building safety assessment under blast loads requires probabilistic evaluation of limit state violation (Melchers 1987), in which the pertinent limit states are represented by the lower bounds of different damage states of the RMSW system components. A generalized PRA framework is illustrated in Fig. 4.1, for building with ordinary RMSW, adapted from the methodology introduced by Stewart et al. (2006) and Stewart and Netherton (2008) for PRA of window glazing under explosive loading. As Fig. 4.1 shows, the generalized PRA framework can be utilized as a risk–based decision support system (DSS) tool developed to facilitate optimal allocation of the available resources for blast risk mitigation. This DSS tool can be used, for example, to select the best strategy for protecting a building’s perimeter by erecting a number of barriers (or barricades). The generalized PRA framework is structured in three levels:

Level I considers the variability associated with the structural component/system, including material properties, geometry, systematic and random errors in the model, etc., and has the objective of determining the fragility of the structural system, i.e. its probability of exceeding a predefine damage state (probability of failure) given the probability distributions associated with the component properties and a range of assumed load parameters (e.g. the peak pressure, specific impulse, peak ground acceleration, etc.) (Twisdale et al. 1994; Low and Hao 2001, 2002; FEMA 2009; Netherton and Stewart 2009; Kelliher and Sutton–Swaby 2012). The fragility curves developed in this level can represent the different LOP, described in ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012) by considering the influence of component damage on the overall building structural integrity, designated as “system–level” in Fig. 4.1 (Bishop and McInerney 2014, and Mohamed et al. 2014).

Level II is concerned with the analysis of load uncertainty and the first step of risk evaluation. The load uncertainty is quantified by estimating the probability distributions associated with the blast wavefront parameters (Campidelli et al. 2013, and 2014; Netherton and Stewart 2010; Bogosian et al 2002; Low and Hao 2001). Subsequently, the load PDFs and fragility curves are used to determine blast reliability curves, which show the probability of failure (the probability of exceeding a predefined damage state) Pf|Θij conditional on the occurrence of the specified DBT scenario Θij.

Level III involves threat assessment, the conclusion of risk evaluation, cost–benefit analysis of possible measures for risk mitigation, and the subsequent selection of the most appropriate risk mitigation option, which might involve hardening and/or zoning of the premises, as will be illustrated later in the current study. Finally, this can be followed by a long–term risk management plan that involves different insurance options and risk mitigation. Threat assessment is based on statistical analysis of intelligence and/or historical data by blast analysts, other expert as well as the stakeholders’ judgments. Threat assessment provides the probability of occurrence of a number of possible DBT P(Θij). The risk is then quantified on the basis of the aggregate probability of failure  and the consequences of an attack. The latter includes the cost of repair and reconstruction, building downtime, the expected number of casualties, etc. If the resulting risk is deemed intolerable by the stakeholders several options of risk mitigation can be considered and their cost can be weighed against the benefit of enhancing safety through detailed cost-benefit analysis. Finally, a risk management plan has to be implemented in order to select the best available option with tolerable risk level.

4.3.2 Simplified PRA Framework

The process outlined above is expected to be quite laborious as well as resource demanding. Alternatively, a simplified PRA framework (Fig. 4.2) can be used, which is organized in two levels:

Level A merges both Levels I and II of the generalized PRA and is focused on the probability of failure Pf |Θij, for which the blast load is calculated from assumed DBT scenarios Θij (i.e. in a deterministic manner). As such, the subsequent structural response and probability of damage state violation are evaluated using the same approach utilized for fragility analysis. The result of this process consists of DBT fragility curves, which is defined herein as blast reliability curves obtained from the deterministic model adopted for blast loading prediction. In practice, the curves would show how the probability of exceeding a predefined damage state increases as a result of increasing the charge mass or reducing the standoff distance.

Level B presents a simplified version of Level III of the generalized PRA and its objective is the decision making process through a risk–based cost–benefit analysis where risk management is guided by cost–benefit analysis for different risk mitigation options. However, in this case, the executive decision can be realized in a more basic manner, on the basis of the viable risk mitigation options and the stakeholders’ best judgment, the latter being linked to the information provided through the DBT fragility curves.

4.3.3 Threat Scenario

In the simplified PRA framework, different levels of DBT (ASCE 2011 and CSA 2012) are considered to represent different threat scenarios using charges of different weights. In accordance with FEMA 428 (FEMA 2003), the different levels of DBT scenarios vary from charge masses that can be delivered by a single person (e.g. using an explosive belt i.e. a personal attack) to larger charge masses delivered by a passenger vehicle or a truck.

4.3.4 Uncertainty in the Structural Component and System Response

There is considerable level of uncertainty, as shown in Level I in the generalized PRA framework (Fig. 4.1) and in Level A in the simplified PRA framework (Fig. 4.2). This is particularly relevant in terms of prediction of damage level and risk following a blast event attributed to the RMSW component response. This is attributed to the fact that the response of different RMSW components are subjected to various sources of uncertainties including:

- Input parameter (materials): uncertainty in the characteristics of used materials, such as the compressive strength of masonry prisms and the yield and ultimate strengths of reinforcement, combined with uncertainty in other input parameters like the position of the longitudinal reinforcement within the concrete masonry units comprising the RMSW,

- Model error: uncertainty in the accuracy of the used model, such as assuming the consistency of workmanship and construction technique, and

- Inherent variability: influence of weather condition and blast environment on blast loading parameters from specified DBT scenarios.

4.3.5 Structural Response Model

Nonlinear dynamic analysis approaches are necessary for determining the structural response of RMSW under blast loads due to the nature of such extreme loading, where the load duration is significantly less than the fundamental period of the RMSW target (Biggs 1964). Dynamic analysis methods may be categorized under two major types, which are: Finite Element (FE) models and analytical (macro) models such as simple Single-Degree-of-Freedom (SDOF) and more elaborate Multi-Degree-of-Freedom (MDOF) models (El-Dakhakhni et al. 2009). As mentioned earlier, qualitative; rather than quantitative; damage descriptors are more meaningful in terms of cost–benefit analysis for PRA analysis. Therefore, the structural response model utilized in the PRA framework should be capable of qualitatively describing damage as will be discussed next.

4.4 Damage States Identification

For the design and assessment of buildings subjected to blast loads, the ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012) adopt performance criteria based on the target facility LOP, which is defined in terms of the potential level of damage that can be tolerated for the structure considered, be it superficial, moderate, heavy, or hazardous. In turn, these damage categories are identified by a range of allowable values for response parameters such as the displacement ductility level and support rotation (ASCE 2011) where, for example, the heavy damage level for a RMSW is associated with support rotations between 2˚ and 8˚.

Quantitative descriptors of the overall structural response/damage such as those traditionally used for blast resistant design (ASCE 2011, CSA 2012), although relatively simple to calculate, do not readily lend themselves to available damage identification, method of repair (MOR) and thus cost–benefit analysis. This is critical as the latter aspects are key for selecting the appropriate risk mitigation and hardening strategies, including strengthening, fencing, enhanced security, etc. As stated previously, ElSayed et al. (2014a) illustrated experimentally that quantitative damage descriptors proposed by the current North American blast resistant design standards may need to be revised for better definition of damage states and thus, facilitate linkage to the overall possible losses. On the other hand, well established guidelines for the damage identification and repair of reinforced concrete components, such as FEMA P-58/BD-3.8.6 (FEMA 2012b) and FEMA P-58/BD-3.8.8 (FEMA 2012d), provide more detailed metrics, e.g. the maximum crack width, amount of crushed and spalled concrete, and deformation of the steel reinforcement, including yielding, fracture, and buckling. The damage thresholds that identify each damage state (e.g. a maximum crack width between 0.5 and 3.0 mm) are then associated with the appropriate MOR, which are extensively discussed in FEMA 308 (FEMA 1998). This latter approach constitutes the backbone of performance-based damage evaluation (PBDE) as described in FEMA 1998, and its outcomes can be more easily translated into practical metrics, such as building downtime and repair cost. Such metrics are more meaningful to the stakeholders (owners, insurance companies, authorities having jurisdiction, etc.) and individuals tasked with performing cost–benefit analysis of potential interventions of risk mitigation and subsequently risk management.

Therefore, in the present study, the four damage states designated by ASCE 59-11 as superficial, moderate, heavy, and hazardous are redefined in terms of qualitative damage descriptors such as the maximum crack width and amount of spalling experienced. A summary description of each of the following damage state (DS), as well as the recommended MOR and a preliminary estimate of the associated downtime is included in Table 4.1.

4.4.1 Damage State I (DS-I): Superficial Damage

Superficial damage is unlikely to produce any permanent deformation (ASCE 2011), loss of stiffness, or load–bearing capacity. As indicated in Table 4.1, post blast visual inspection may reveal hairline cracks in the mortar beds or concrete masonry units with a maximum width (Wm) not greater than 0.5 mm. Therefore, buildings experiencing superficial damage (DS-I) are expected to remain safe and fully operational, and their downtime is expected to be in the order of days. In accordance with FEMA P-58/BD-3.8.8 (FEMA 2012d), cosmetic repair, consisting in simple surface coating, is the proper MOR when Wm ≤ 0.5 mm. Such MOR would be adequate in order to ensure fire resistance, restore the aesthetic appearance by concealing the cracks, and prevent water infiltration (FEMA 1998; FEMA 2012e).

4.4.2 Damage State II (DS-II): Moderate Damage

In accordance to ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012), moderate damage of one-way flexural components is associated with a maximum support rotation not greater than 2˚. In Table 4.1, moderate damage (DS-II) is redefined in terms of initiation of yielding in the steel reinforcement and a maximum crack width in the range 0.5–3.0 mm; accompanied by negligible concrete masonry unit crushing and spalling. One way of distinguishing between DS-I and DS-II is to evaluate Wm with sufficient accuracy. A visual example of RMSW that had sustained moderate damage is shown in Figure 4.3-a, which shows the crack pattern resulting from a field test conducted by ElSayed et al. (2014a). The cracks are generally expected to (mainly) propagate in the mortar joints as well as the masonry blocks, thereby causing significant reduction in wall stiffness and strength. To restore both, FEMA 308 (FEMA 1998) and FEMA P-58 (FEMA 2012b–e) recommend either grout or epoxy injection as the appropriate MOR whereas epoxy is best suited for small cracks (0.5 ≤ Wm ≤ 1.0 mm), whereas grout is more appropriate for larger ones (1.0 ≤ Wm ≤ 3.0 mm). This type of intervention is classified in FEMA 308 as structural repair (SR), and includes in removal of loose material, sealing of the cracks as appropriate, and subsequent application structural binding agent (cementitious grout or resin epoxy) into the crack by pressure injection through the entry ports, thereby filling the voids and adhering to the substrate material. The time required for repair completion is estimated in the order of weeks (generally less than a month), because this type of intervention is intended to address minor damage, as the lateral displacement of the structure did not exceed its displacement at peak resistance.

4.4.3 Damage State III (DS-III): Heavy Damage

As per ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012), heavy damage in RMSW is characterized by significant permanent deflection and maximum support rotation between 2˚ and 8˚. Conversely, by following the description given for severe flexural damage in FEMA P-58/BD-3.8.10 (FEMA 2012e), Table 4.1 associates heavy damage (DS-III) with initiation of concrete masonry unit spalling at the compression side of the member accompanied by buckling of the steel reinforcement, as illustrated in Figure 4.3-b. To better identify DS-III, the associated level of spalling is assumed in accordance with the definition of heavy damage given by FEMA P-58/BD-3.8.6 (FEMA 2012b). In the current study, DS-III is defined for RMSW when spalling starts to occur up to spalling ratio (S/h) not greater than 10%, where S represents the spalling height per RMSW unit width while h is the wall height. In addition, a widespread array of flexural cracks, having maximum width Wm greater than 3.0 mm, is expected to form at the tension side of the wall and the lateral displacement is likely to have exceeded the displacement corresponding to peak resistance.

Unlike DS-I and DS-II, DS-III should be considered a major damage state as spalling may expose the longitudinal reinforcement leading to buckling and possible long-term damage. Adequate MOR side can be undertaken following the procedure laid out in FEMA 308 (FEMA 1998), which consists of the removal of loose material; the treatment of the exposed reinforcement; and subsequent the application of mortar mix, the latter comprised of pea gravel in case of deep spall (deeper than the thickness of the face shell of the concrete masonry unit). On the RMSW tension side, where wide cracks have opened, epoxy and/or grout injections is deemed insufficient to restore pre–blast stiffness and strength. In this case, the most appropriate repair method is best left to the engineering judgment. However, as a general rule, partial wall replacement and structural enhancement (SE) procedures (FEMA 1998), which would involve the application of concrete overlay and fabric sheets of composite fibers, may be necessary. The building downtime for this type of intervention may extend to several months.

4.4.4 Damage State IV (DS-IV): Hazardous Failure

Both ASCE/SEI 59-11 (ASCE 2011) and CAN/CSA S850-12 (CSA 2012) define hazardous failure in reinforced masonry components as a state characterized by large deformations, quantified by a maximum support rotation greater than 8˚, which may possibly cause structural collapse. On the other hand, the description given by FEMA P-58/BD-3.8.8 (FEMA 2012d) of the most sever damage state pertaining to reinforced concrete components involves Wm > 3.0 mm of maximum width, initiation of sliding, widespread crushing of concrete, and fracture of the steel reinforcement. There is no similar definition of such damage state pertaining to RMSW under out-of-plane loads, and thus the former description is utilized to define DS-IV. However, as this study is only focused on the out–of–plane behavior of flexurally dominated RMSW, Table 4.1 includes only damage descriptors associated with the flexural mode of failure, i.e. rupture of steel reinforcement (as in Figure 4.3-c) and extensive concrete masonry spalling on the compression side. The formation of fragments (USDOD 2008), although quite common as a result of extensive blast induced damage, is not included among the damage criteria as the limited tests reported by ElSayed et al. (2014a) suggest that negligible flying debris are produced under blast when typical seismic reinforcement is provided in RMSW. Nevertheless, a more comprehensive list of damage criteria should probably include secondary fragmentation, owing to the facility occupant life threatening possibility under such failure mode.

The extreme nature of the hazardous failure (DS-IV) level renders intervention and structural enhancement, including partial replacement, unlikely to be financially sound. Restoration of the full capacity of the damaged RMSW is probably best achieved, in a cost–effective manner, by its complete replacement.

4.5 Fragility Curves

The fragility curves are calculated on the basis of several assumed blast threats. Given the scaled distances , where R is the standoff distance and m is the charge mass in kg, associated with each threat Θij, the normally reflected peak pressure and specific impulse are obtained from the polynomial expression provided by the CAN/CSA S850-12 and are used to draw the pressure history experienced by the target structure. Also, for simplicity, a number of assumptions are made, including planarity of the produced shock waves, which entail uniform overpressure distribution over the reflecting target surface, normal reflection (angle of incidence equal to zero), and linear pressure profile.

Such input is implemented with the SDOF model of an archetypical RMSW to determine its response and the resulting damage descriptors. These include the maximum crack width and spalling that are statistically analyzed to determine the probabilities Pm|Θij, Ph|Θij, PH|Θij, of exceeding the damage states DS-II, DS-III, and DS-IV, respectively, conditional on the occurrence of the given threat Θij. The probability of incurring superficial damage (DS-I) is not evaluated in this study as it is assumed to have less importance. For any of the three remaining damage states, the computation of the probability of failure is defined as follows,

(4.1)

where Pf = Pm, Ph, and PH for the damage states DS-II, -III, and -IV, respectively, and Wlim = 0.5, 3.0, and 3.0 mm, for damage states DS-II, -III, and -IV respectively; also, (S/h)lim = 0% and 10% for the damage states DS-III and –IV, respectively, while it is not applicable for DS-II. Equation (4.1) is numerically evaluated by using the following (Melchers 1987)

(4.2)

where I denotes the indicator function, which has value one when its argument is “true” and zero otherwise; N is the number of variates randomly sampled from the normal distributions associated with different design parameters (e.g. compressive strength of masonry prisms); Wm,k and Sk are the k-th values of Wm and S obtained from the k-th variate; N’ is the result of the summation, i.e. the number of variates that cause limit state violation and thus trigger the indicator function (I = 1); N’/N can be termed as frequency of exceedence, which provides better approximations of Pf as N becomes larger. By noting that, the limit state for spalling while the moderate damage state is not defined, Eq. (4.2) can be reduced to the following:

(4.3)

which may be evaluated by direct sampling as:

(4.4)

On the other hand, when the computed Wm is normally distributed, its probability of exceeding the limit state Wlim can be more easily estimated by using the standard normal distribution Φ,

(4.5)

where μ and σ are the maximum likelihood estimators (MLEs) of the mean and standard deviation associated with the normal distribution representing Wm.

4.6 Application of the PRA Framework to a RMSW Building Archetype

The objective of this section is to illustrate one application of the simplified PRA framework shown in Fig. 4.2 to blast risk mitigation of low– to medium–rise RMSW buildings. In this respect, it should be noted that options that may be considered by the analyst for reducing blast risk can be classified in two categories, namely, interventions (capacity enhancement) and DBT reduction (Stewart et al. 2006). Capacity enhancement may involve the retrofit of existing RMSW or their replacement with new ones in order to withstand large out-of-plane pressure. On the other hand, DBT reduction (i.e. through increasing the standoff distance) may require the acquisition of considerable area of land surround the facility in order to setup protected perimeters and prevent explosions at close distance from the building.

A demand reduction (DBT reduction) strategy is greatly beneficial, as shown in Figures 4.4-a and 4.4-b, which show the variation of the normally reflected peak pressure and specific impulse generated by a surface detonation of several TNT charges of different weight. The rapid variation in both wavefront parameters is particularly evident at close distances, where for example, the peak pressure generated by a 50.0 kg TNT charge detonated at 5.0 m (Z=1.4 m/kg1/3) is approximately 75% higher than the corresponding values when the standoff distance is increased to merely 6.0 m (Z=1.6 m/kg1/3), while the impulse developed from the detonation of the 50.0 kg TNT charge at 5.0 m is approximately 25% higher than the corresponding value when the standoff distance is increased to 6.0 m.

The difficulty faced by the analyst as well as the stakeholders while considering the cost–benefit of strengthening versus perimeter protection is represented in Figure 4.4-c, which gives a conceptual appraisal of the costs of intervention versus increasing standoff distance: as the distance increases, the cost of strengthening is expected to diminish while the cost of perimeter protection (cost of land, barriers, security, etc.) is significantly increased. Therefore, it seems reasonable to seek an optimum standoff distance that for the selected LOP should entail the minimum overall cost of protection. For demonstration, the example presented in the next section considers only one strategy of risk mitigation, namely, DBT reduction by land acquisition and construction of protective barriers and barricades (i.e. for zoning purposes).

4.6.1 DBT Scenarios

In the current example, three DBT scenarios are considered, namely, a personal attack, a car bomb, and a truck bomb. As a first approximation, the three scenarios are modeled as hemispherical surface bursts of different magnitude, the latter selected in accordance with FEMA 428 (FEMA 2003): the maximum charge mass that can be delivered by a single person on foot, who is using an explosive belt and/or a bomb briefcase, is assumed to be equivalent to 50 kg of trinitrotoluene (TNT). In the case of a car bomb, the amount of explosive can be as large as 300 kg of TNT equivalent and for a truck it can reach up to 2000 kg of TNT equivalent.

4.6.2 Material Uncertainty

This study takes into consideration the uncertainty affecting some of the most relevant input parameters of the RMSW structural system, namely, the compressive strength of fully-grouted prisms (), as inferred from standard prism tests (ASTM 2011), and the position of the longitudinal reinforcement, as indicated by the distance (d) of the steel bars from the wall side directly exposed to the blast. Both  and d are modeled as random variables whose probability distributions, represented in Figure 4.5, are estimated on the basis of the experimental results reported by ElSayed et al. (2014a, 2014b), which include seventeen masonry prisms built under the same conditions as the specimens subjected to blast loading and tested in accordance with ASTM standard C1314-11a (ASTM 2011). The results revealed a compressive strength ranging from 12 to 23 MPa, with sample mean value 18.4 MPa, sample standard deviation 3.1 MPa, and coefficient of variation COV = 17.0%. A normal distribution is found to fit the data adequately: the MLEs for and  are found to be virtually identical to the sample mean and standard deviation, and the Chi–square (Chi2) goodness–of–fit–test shows a p–value = 62% (Ang and Tang 1975, The MathWorks 2011). It should be noted that number of data points used herein may be considered insufficient for a normal distribution fit and more data would be required to utilize such distribution. Nevertheless, the normal distribution is utilized for illustrative purposes.

To determine the position of the longitudinal steel reinforcement, six walls were cut after being tested: the depth d of 46 bars was measured and found ranging between 23 and 40 mm, with sample mean value and standard deviation equal to 32.1 mm and 4.4 mm, respectively, and COV = 13.6%. The dataset is well represented by a normal distribution and no significant discrepancies are found between the foregoing estimates of and  and their MLEs. In addition, the depth–to–wall–thickness ratio (d/t) features = 0.51 and  = 0.07.

4.6.3 Archetype Building Configuration

The archetypical building selected to illustrate the simplified PRA methodology is adapted from one of the archetypes used in NIST (2010) to evaluate the seismic performance of a typical hotel, condominium, or college residence constructed with RMSW system. Several schematic views of the RMSW building’s structural system, including building layout, lateral view, and typical cross–section of one of the RMSW are shown in Figure 4.6. The building is constructed as four storey high, with 3.0 m storey height, and features eight identical, 9.0 m long, RMSWs in both the longitudinal and transverse directions.

Each RMSW is constructed of standard 190×190×390 mm concrete blocks and the average compressive strength of the masonry prisms is assumed to be 20.0 MPa. In addition, longitudinal reinforcement is provided in the form of 15M bars (area = 200 mm2) placed approximately in the centre of each block cell (one bar per cell); the steel average yield stress and tensile strength are equal to 420 and 620 MPa, respectively. The resulting reinforcement ratio (0.53%) can be qualified as intermediate, based on the minimum (0.13%) and maximum (2.00%) ratios given by CAN/CSA S304.1-04 (CSA 2004c) for in–plane seismic loading.

4.6.4 Structural Response Model of RMSW Components

To predict the structural response of RMSW, the single–degree–of–freedom (SDOF) model described in ElSayed et al. (2014b), which was calibrated on the basis of the test results presented in ElSayed et al. (2014a), was adopted. This SDOF model was further improved in the current study to determine the maximum crack width and spalling ratio in RMSW when subjected to out–of–plane blast loading.

A simplistic approach is adopted to calculate the width of the flexural cracks. The typical tensile failure mechanism is assumed to be debonding of the mortar from the masonry unit along the bed joint (Drysdale and Hamid 2005, ElSayed et al. 2014a). Furthermore, a crack is assumed to open as soon as the tensile normal strain (ε) at the extreme fiber of a mortar joint cross–section exceeds the strain associated with the flexural tensile strength normal to the bed joint. The strain profile is calculated by strain compatibility, given the curvature and the position of the neutral axis. The crack width is then calculated as W = ε∙ΔL, where ΔL denotes the distance between adjacent mortar joints; at the wall ends, for both the first and last mortar joint, ΔL is replaced with ΔL/2.

To illustrate the results of this simple model, Figure 4.7 shows the crack width calculated at the mortar joints of a RMSW, utilized in the previous building, subjected to four out-of-plane, static, uniformly distributed loads of magnitude equal to 25%, 50%, 75% and 100% of the wall resistance. The spalling ratio is also calculated in a straightforward manner as the ratio of the number of failed mortar joints to the total number of joints. While evaluating this ratio, a mortar joint is considered to have failed when the compressive strain at the extreme fibre exceeds the critical value of 0.0035 mm/mm (ElSayed et al. 2014b). Also, the joints at both ends of the wall are counted as 1/2, so that if n is the actual number of mortar joints, the number assumed for calculating the amount of spalling is (n-1). The foregoing definition of spalling, although not consistent with the spalling ratio defined in FEMA P-58/BD-3.8.6 (FEMA 2012b), appears to empirically match the S/h ratio observed in the specimens tested by ElSayed et al. (2014a). Therefore, the definitions of different damage states (see Table 4.1) are adopted for illustrative purposes, in order to predict the level of damage in the archetype building wall as follows.

The number N of randomly sampled variates cannot be established beforehand as it depends on the number of variables and associated degree of uncertainty which characterize the problem at hand (Melchers 1987). For the building archetype considered herein, N = 250 is found to yield sufficiently accurate estimates of Pf. As Fig. 4.8 shows, the estimator N’/N resulting in a reasonable rate of convergence for several blast scenarios as N increases, and for most scenarios the frequency of exceedence does not change significantly when N > 250. Also, a comparison between Pf estimates from Eqs. (4.4) and (4.5) is reported in Table 4.2 for nine DBT scenarios, which shows reasonable agreement when the probability of failure is greater than 50%; for smaller values of Pf, a greater random sample is needed.

Finally, the probability of exceeding each damage limit state is estimated by direct sampling of the random variables, using Monte Carlo simulation (Melchers 1987). Given the PDFs in Figure 4.5 obtained for  and d, a number N of values are randomly sampled from each distribution and the resulting maximum crack width and level of spalling are computed by SDOF analysis. Subsequently, the probability of failure, i.e. the probability of exceeding the limit states established in terms of crack width or amount of spalling, is estimated by calculating the of DBT fragility curves.

4.6.5 RMSW Fragility Curves

A total of 27 threat scenarios Θij are considered in order to draw the building’s DBT fragility curves, on the basis of the three DBT categories described earlier. For each category, nine standoff distances are selected, in order to perform a parametric study in the far range (ASCE 2011), i.e. with scaled distances Z ranging from 1.2 to 20 m/kg1/3. Smaller scaled distances are intentionally avoided as the resulting uneven pressure distributions and the possible subsequent modes of failure (e.g. breaching) that may be engaged are beyond the scope of the current investigation. The resulting charge mass and standoff distance combinations Θij = (mi, Rj) are reported in Table 4.3, and for each combination, the probability of exceeding the lower bounds of damage states DS-II, -III, and -IV is calculated by using Eq. (4.2).

The same results are plotted in Figures 4.9-a, 4.9-b, and 4.9-c in the form of DBT fragility curves associated with personal attack, car bomb, and truck bomb scenarios, respectively.  In general, a decrease in the probability of limit state violation as the standoff distance becomes greater is observed. Although the same information can be represented in a more compact form by selecting the scaled distance as the independent variable, the use of charge mass and standoff distance may be preferable as it facilitates a clearer picture of the archetype building response, which can be more easily utilized by decision makers.

For example, under the threat Θ50,5 the probability of exceeding the lower bounds of DS-II, -III, and -IV is approximately equal to 100%, 55%, and 55%, respectively. Therefore, the probability of experiencing moderate damage (DS-II) is given by the difference 100%-55% = 45%. In addition, heavy damage (DS-III) is unlikely to occur, as its probability is about 55%-55% = 0%, although the latter result may be a consequence of the adopted model. Finally, hazardous failure (DS-IV) has a probability of occurrence of 55%. Similarly, the Θ2000,50 blast scenario leads to a probability of moderate, heavy, and hazardous damage equal to 100%-8%=92%, 8%-6%=2%, and 6%, respectively. Hence, if the objective pursued by the stakeholders is a probability of incurring DS-III to be limited to 2%, a truck barrier at 50 m and a car barrier at 5 m from the building may suffice.

It should be pointed out that the estimates in Table 4.3 and Figure 4.9 are considered accurate – in terms of random sampling – only for N’/N > 0.5; as anticipated earlier with reference to Table 4.2, accurate estimates of smaller probabilities of failure would require a greater sample size N, which would impose an unnecessary computational burden, particularly considering that the calculations presented herein are solely for illustrative purposes. Furthermore, even in the case of relatively large probabilities of failure, owing to the oversimplified nature of the SDOF model adopted for predicting the crack width and amount of spalling, the number of significant figures that can be reasonably assumed for the estimate of Pf is usually limited to two.

4.6.6 Option for Premises Zoning

In the current application, the final stage of risk mitigation and decision making pertains to the locations where protective barriers shall be utilized, i.e. the selection of their distances from the building. This decision can be based on the DBT fragility curves as well as the design requirements or the target LOP criteria established by the stakeholders in terms of tolerable probability of damage. For instance, the building owner may decide to accept a probability of incurring moderate, heavy, and hazardous damage not greater 10%, 1%, and 0.1%, respectively. Given these thresholds, from the curves in Fig. 4.9 it is clear that when hazardous damage is considered, pedestrian fences, car barriers, and truck barricades should be erected at a minimum standoff distance of 7.5, 20, and 75 m, respectively. In addition, for preventing heavy damage (or greater) with a 99% confidence, the results in Table 4.3 demand that the same barriers be placed at a minimum distance of 15, 40, and 100 m, respectively. Finally, to avoid moderate damage (or grater) with a 90% confidence, the barriers should be erected at a minimum distance of 35, 100, and 250 m, respectively. Hence, if all three criteria are applied, the last set of prescribed minimum distances would determine the position of the blast barriers.

The result of this process can be presented as the partition of the building’s premises in four zones, A, B, C, and D, as depicted in Figure 4.10. Zone–A, the innermost area, is delimited by a security fence located at a minimum distance of 35 m from the building and is provided with check points in order to grant access to authorized pedestrians only. Zone–B extends to an outer perimeter located at a minimum distance of 100 m and provided with anti–ram barriers in order to prohibit access to cars but grant entrance to all pedestrians. Zone–C has an outer perimeter at a minimum distance of 250 m from the building that features anti–ram barricades for trucks and gates of entry for small vehicles (cars) and pedestrians. Finally, Zone–D includes all the areas within the premises on the outside of the truck barricades and access to it is unrestricted.

It can be noticed that the adopted framework constitutes a very expedient DSS tool, owing to its heavy reliance the stakeholders’ judgment in order to establish acceptable levels of protection. Such a DSS tool may be very useful for the purpose of preliminary site planning; however, to finalize the decision, a more comprehensive approach may be advisable, especially for urban areas where the cost of land is particularly high. In such a case, site planning should be based on cost–benefit analysis, which considers, at the very least, the costs of land acquisition and potential repairs; if the result if found to be unsatisfactory in terms of the safety–to–cost (benefits) ratio, alternative strategies should be considered, including measures for strengthening the building, so as to reduce to overall cost to a minimum, given the target facility LOP.

4.7 Conclusions

This study presents a general framework for probabilistic risk assessment (PRA) for RMSW buildings considered under blast threats. A simplified PRA methodology is also proposed, which overcomes the need for probabilistic assessment of threat and load parameters and leads to the expedient calculation of design basis threat (DBT) fragility curves. The developed DBT fragility curves give the probability of failure as it varies with the selected DBT parameters (charge mass and standoff distance). The use of the DBT fragility curves would expedite the final stage of the PRA framework (decision making), by replacing a rigorous cost–benefit analysis with a simpler process based on the stakeholders’ judgment, the latter formulated in terms of tolerable probability of different damage states. For illustrative purposes, the simplified PRA framework is applied for the preliminary site planning of the premises surrounding a four–storey RMSW building archetype, whose vulnerability is analyzed by assuming three DBT blast scenarios, namely, personal attack, car bomb, and truck bomb. The uncertainty in the RMSW system characteristics is partly accounted for by modeling both the masonry assemblage compressive strength and the position of the longitudinal reinforcement as normally distributed random variables. The RMSW response to out–of–plane blast pressure, including maximum crack width and spalling ratio, is evaluated by stochastic SDOF modeling. The results suggest the erection of fences, anti–ram car barriers, and truck barricades at specific minimum standoff distances from the RMSW building, in order to meet the target design requirements in terms of specified probabilities of incurring moderate, heavy, and hazardous damage. Finally, based on the fragility curves results, consideration of a range of potential interventions (e.g. strengthening) as well as the use of more sophisticated means, including a generalized PRA, and a more detailed analytical model for the prediction of the RMSW building blast response might be required.

Appendix 4.1 Notation

COV	=	Coefficient of variation

d	=	Position of vertical reinforcement (mm)

DIF	=	Dynamic increase factor

=	Prism average compressive strength (MPa)

LOP	=	Level of protection

mi	=	i-th explosive charge mass (kg of TNT)

MLE	=	Maximum likelihood estimator

n	=	Number of mortar joints

Pf	=	Probability of failure

Pm	=	Probability of experiencing moderate damage or greater

PH	=	Probability of experiencing hazardous damage or greater

Ph	=	Probability of experiencing heavy damage or greater

PBDE	= 	Performance–based damage evaluation

PDF	= 	Probability density function

PRA	=	Probabilistic risk assessment

Rj	=	i-th standoff distance (m)

RMSW	= 	Reinforced masonry shear wall

S	=	Amount of spalling, i.e. length along the wall span of the region experiencing

spalling (mm)

Sk	=	k-th amount of spalling (mm)

SDOF	=	Single–degree–of–freedom

SIF	=	Strength increase factor

t	=	Concrete block wall thickness, i.e. cross-section depth (mm)

W	=	Crack width (mm)

Wlim	=	Crack width limit state (mm)

Wm	=	Maximum crack width (mm)

Wm,k	=	k-th maximum crack width (mm)

Z	=	Scaled distance

ε	=	Strain normal to the cross–section

εcr	=	Normal strain corresponding to the flexural tensile strength

Θ	=	Threat scenario

Θij	=	Threat scenario resulting from the combination (mi, Rj)

μ	=	Mean value

ρv	=	Vertical reinforcement ratio

σ	=	Standard deviation

Φ	=	Standard normal cumulative distribution function

Appendix 4.2 References

Abou-Zeid BM, El-Dakhakhni WW, Razaqpur AG, and Foo S (2014). Time-Response Analysis of Arching Unreinforced Concrete Block Walls Subjected to Blast Loads. ASCE Journal of Structural Engineering, 140(4): 04013099-1–14. Permalink: http://dx.doi.org/10.1061/(ASCE)ST.1943-541X.0000893.

Ang AH-S and Tang WH (1975). Probability Concepts in Engineering Planning and Design – Volume I-Basic Principles. John Wiley & Sons Inc., New York, NY.

ASCE (2011). Blast protection of buildings. ASCE/SEI standard 59-11. American Society of Civil Engineers (ASCE), Reston, VA.

ASTM (2011). Standard Test Methods for Compressive Strength of Masonry Prisms. ASTM C1314-11a. American Society for Testing and Materials (ASTM), West Conshohocken, PA.

Biggs, J.M. (1964). “Introduction to Structural Dynamics.” New York, USA: McGraw-Hill Inc.

Bishop, C.D., and McInerney, E.H. (2014). Disproportionate Collapse Design Considerations - A Comprehensive Approach. ASCE Structures Congress: 2221-2232.

Bogosian D, Ferritto J and Shi Y (2002). Measuring uncertainty and conservatism in simplified blast models. In 30th Explosive Safety Seminar, Atlanta, Georgia, 13-15 August 2002. Fort Belvoir Defense Technical Information Center, Fort Belvoir, VA. Available from http://www.dtic.mil/cgi-bin/GetTRDoc?AD=ADA526954 [accessed 23 April 2014].

Browning R, Dinan R and Davidson J (2014). Blast Resistance of Fully Grouted Reinforced Concrete Masonry Veneer Walls. ASCE Journal of Performance of Constructed Facilities, 28(2): 228–241. Permalink: http://dx.doi.org/10.1061/(ASCE)CF.1943-5509.0000434.

Campidelli M, Razaqpur AG and Foo S (2013). Reliability–Based Load Factors for Blast Design. Canadian Journal of Civil Engineering, 40(5): 461–474. Permalink: http://dx.doi.org/10.1139/cjce-2011-0411.

Campidelli M, Tait MJ, El-Dakhakhni WW and Mekky W (2014). Inference of blast wavefront parameter uncertainty for probabilistic risk assessment. ASCE Journal of Structural Engineering (ASCE), submitted for publication.

Carney P and Myers JJ (2005). Out-of-Plane Static and Blast Resistance of Unreinforced Masonry Wall Connections Strengthened with FRP. International Concrete Abstracts Portal, 230: 229–248. DOI: 10.14359/14835.

CSA (2012). Design and assessment of buildings subjected to blast loads. CSA standard S850-12. Canadian Standards Association (CSA), ON.

Drysdale RG and Hamid AA (2005). Masonry Structures Behaviour and Design – Canadian Edition. Canada Masonry Design Centre, Mississauga, ON.

El-Dakhakhni WW, Changiz Rezaei SH, Mekky WF, and Razaqpur AG (2009). Response Sensitivity to Blast-Loaded Reinforced Concrete Structures to the Number of Degrees of Freedom. Canadian Journal of Civil Engineering, 36(8): 1305-1320.

Ellingwood BR (2006). Mitigating Risk from Abnormal Loads and Progressive Collapse. ASCE Journal of Performance of Constructed Facilities, 20(4): 315–323. Permalink: http://dx.doi.org/10.1061/(ASCE)0887-3828(2006)20:4(315).

ElSayed M, El-Dakhakhni WW and Tait MJ (2014a). Performance Assessment Of Reinforced Concrete Block Structural Walls Under Blast Loading. ASCE Journal of Structural Engineering, submitted for publication.

ElSayed M., Tait MJ and El-Dakhakhni WW (2014b). Out-of-Plane Performance Quantification of Reinforced Concrete Block Shear Walls under Blast. ASCE Journal of Performance of Constructed Facilities, submitted for publication.

FEMA (1998). Repair of Earthquake Damaged Concrete and Masonry Wall Buildings – FEMA 308. Federal Emergency Management Agency (FEMA), Washington, DC. Available at http://www.fema.gov/media-library-data/20130726-1453-20490-4004/fema-308.pdf [accessed 27 March 2014].

FEMA (2003). Premier to Design Safe School Projects in Case of Terrorist attacks – FEMA 428. Federal Emergency Management Agency (FEMA), Washington, DC. Available at http://www.fema.gov/pdf/plan/prevent/rms/428/fema428.pdf [accessed 27 March 2014].

FEMA (2009). Quantification of Building Seismic Performance Factors – FEMA P695. Federal Emergency Management Agency (FEMA), Washington, DC. Available at http://www.fema.gov/media-library-data/20130726-1716-25045-9655/fema_p695.pdf [accessed 27 March 2014].

FEMA (2012a). Seismic Performance Assessment of Buildings – FEMA P-58. Federal Emergency Management Agency (FEMA), Washington, DC. Available at http://www.fema.gov/media-library/assets/documents/90380 [accessed 27 March 2014].

FEMA (2012b). Fragility Functions for Reinforced Concrete Moment Frames – FEMA P-58/BD-3.8.6. Federal Emergency Management Agency (FEMA), Washington, DC. Available at http://www.fema.gov/media-library/assets/documents/90380 [accessed 27 March 2014].

FEMA (2012c). Fragility Curves for Slab-Column Connections – FEMA P-58/BD-3.8.7. Federal Emergency Management Agency (FEMA), Washington, DC. Available at http://www.fema.gov/media-library/assets/documents/90380 [accessed 27 March 2014].

FEMA (2012d). Damage States and Fragility Curves for Low Aspect Ratio Reinforced Concrete Walls – FEMA P-58/BD-3.8.8. Federal Emergency Management Agency (FEMA), Washington, DC. Available at http://www.fema.gov/media-library/assets/documents/90380 [accessed 27 March 2014].

FEMA (2012e). Damage States and Fragility Curves for Reinforced Masonry Shear Walls – FEMA P-58/BD-3.8.10. Federal Emergency Management Agency (FEMA), Washington, DC. Available at http://www.fema.gov/media-library/assets/documents/90380 [accessed 27 March 2014].

GSA (2013). Alternative Path Analysis & Design Guidelines For Progressive Collapse Resistance. General Service Administration (GSA). Available at http://www.gsa.gov/portal/content/103205  [accessed 5 May 2014].

Kelliher D and Sutton-Swaby K (2012). Stochastic representation of blast load damage in a reinforced concrete building. Structural Safety, 34(1):407–417. Permalink: http://dx.doi.org/10.1016/j.strusafe.2011.08.001.

Low HY and Hao H (2001). Reliability analysis of reinforced concrete slabs under explosive loading. Structural safety, 23(2):157–178. Permalink: http://dx.doi.org/10.1016/S0167-4730(01)00011-X.

Low HY and Hao H (2002). Reliability analysis of direct shear and flexural failure modes of RC slabs under explosive loading. Engineering Structures, 24(2):189–198. Permalink: http://dx.doi.org/10.1016/S0141-0296(01)00087-6.

Mayrhofer Chr (2002). Reinforced masonry walls under blast loading. International Journal of Mechanical Sciences, 44(6): 1067–1080. Permalink: http://dx.doi.org/10.1016/S0020-7403(02)00014-0.

Melchers RE (1987). Structural Reliability: Analysis and Prediction. John Wiley & Sons Inc., New York, NY.

Mierzejewski W (2010). Out-of-plane bending of masonry walls with near-surface-mounted and externally-bonded corrosion-resistant reinforcement. Master thesis, Department of Civil Engineering, Queen’s University, Kingston, ON, Canada. Available at https://qspace.library.queensu.ca/bitstream/1974/5695/1/Mierzejewski_Wojciech_201005_MASc.pdf [accessed 22 April 2014].

Milani G and Lourenço PB (2009). Blast Analysis of Enclosure Masonry Walls Using Homogenization Approaches. International Journal for Multiscale Computational Engineering, 7(2): 91–113. Permalink: http://dx.doi.org/10.1615/IntJMultCompEng.v7.i2.30.

Mohamed, I., Rahman, N.A., and Seracino, R. (2014). Numerical Analysis of Strengthened Steel Stud Bearing Walls to Resist Disproportionate Collapse. ASCE structures Congress: 2174-2185.

Myers JJ, Belarbi A and El-Domiaty KA (2004). Blast Resistance of FRP Retrofitted Un-Reinforced Masonry (URM) Walls with and without Arching Action. The Masonry Society Journal, September 2004: 9–26. Available at http://www.masonrysociety.org/html/resources/journal/ [accessed 22 April 2014].

Netherton MD and Stewart MG (2009). The Effects of Explosive Blast Load Variability on Safety Hazard and Damage Risks for Monolithic Window Glazing. International Journal of Impact Engineering, 36(12): 1346 –1354. Permalink: http://dx.doi.org/10.1016/j.ijimpeng.2009.02.009.

Netherton MD and Stewart MG (2010). Blast Load Variability and Accuracy of Blast Load Prediction Models. International Journal of Protective Structure, 1(4): 543–570. Permalink: http://dx.doi.org/10.1260/2041-4196.1.4.543.

NIST 2010. Evaluation of the FEMA P-695 Methodology for Quantification of Building Seismic Performance Factors – NIST GCR 10-917-8. US Department of Commerce Engineering Laboratory – National Institute of Standards and Technology (NIST), Gaithersburg, MD. Available at http://www.nehrp.gov/pdf/nistgcr10-917-8.pdf [accessed 27 March 2014].

Pekau OA and Cui Y (2006). Progressive Collapse Simulation of Precast Panel Shear Walls During Earthquake. Journal of Computer and Structures, 84(5-6): 400–412. Permalink: http://dx.doi.org/10.1016/j.compstruc.2005.09.027.

Seyedrezai S (2011). Modeling of arching unreinforced masonry walls subjected t o blast loadings. Master thesis, Dep. of Civil Engineering, McMaster University, Hamilton, ON, Canada. Available at http://digitalcommons.mcmaster.ca/opendissertations/6287/ [accessed 22 April 2014].

Stewart MG, Netherton MD and Rosowsky DV (2006). Terrorism Risks and Blast Damage to Built Infrastructure. ASCE Natural Hazards Review, 7(3): 114–122. Permalink: http://dx.doi.org/10.1061/(ASCE)1527-6988(2006)7:3(114).

Stewart MG and Netherton MD (2008). Security Risks and Probabilistic Risk Assessment of Glazing Subject to Explosive Blast Loading. Reliability Engineering and System Safety, 93(2): 627–638. Permalink: http://dx.doi.org/10.1016/j.ress.2007.03.007.

The MathWorks (2011). MATLAB – Statistics ToolboxTM User’s Guide. Version 8.1 – Release 2012b [online]. The MathWorks Inc., Natick, MA. Available from http://www.mathworks.com/help/stats/ [accessed 22 January 2013].

Twisdale LA, Sues RH and Lavelle FM (1994). Reliability-based design methods for protective structures. Structural Safety, 15(1-2): 17–33. Permalink: http://dx.doi.org/10.1016/0167-4730(94)90050-7.

USDOD (2008). Unified Facilities Criteria. Structures to Resist the Effects of Accidental Explosions. Document No. UFC 3-340-02. US Department of Defense (USDOD), Washington, DC. Available from http://www.wbdg.org/ccb/DOD/UFC/ufc_3_340_02.pdf [accessed 22 January 2013].

Wei X and Stewart MG (2010). Model validation and parametric study on the blast response of unreinforced brick masonry walls. International Journal of Impact Engineering, 37(11): 1150–1159. Permalink: http://dx.doi.org/10.1016/j.ijimpeng.2010.04.003.

Table 4. 1: Description of damage states and recommended repair techniques (adapted from FEMA (1998) and FEMA (2012a–e))

Damage State; Damage State Description; Approximate Building Downtime; Method of Repair (MOR). DS-I: Superficial Damage; - Initiation of cracking in mortar joints; Days; Cosmetic repair. - Initiation of flexural cracking in masonry units. - Maximum crack widths less than 0.5 mm. DS-II: Moderate Damage; - Initiation of yielding in the steel reinforcement; Weeks; Epoxy or grout injections. - Maximum flexural crack width larger than 0.5 mm but less than 3.0 mm.. DS-III: Heavy Damage; - Initiation of masonry spalling at the compression side (0 < S/h ≤ 10%).; Months; Partial wall replacement. - Buckling of longitudinal reinforcement. - Maximum flexural crack width larger 3.0 mm. DS-IV: Hazardous Damage; N/A1; Wall replacement. - Extensive masonry spalling (S/h > 10%). - Fracture of longitudinal reinforcement. - Maximum flexural crack width larger 3.0 mm. 1Not Applicable

Table 4. 2: Comparison between different estimates of the probability of exceeding the lower bound of moderate damage state (DS-II) as a sample

Threat Scenario (kg of TNT); Threat Scenario Θij; Standoff Distance R (m); Scaled Distance Z (m/kg1/3); Probability of Exceeding the Lower Bound of DS-II. ; Frequency N’/N. Personal Attack (50); Θ50,20; 020; 05.43; 0.84; 0.90. Θ50,25; 025; 06.79; 0.50; 0.42. Θ50,30; 030; 08.14; 0.17; 0.13. Car Bomb (300); Θ300,50; 050; 07.47; 0.92; 0.96. Θ300,80; 080; 11.95; 0.36; 0.27. Θ300,100; 0100; 14.94; 0.04; 0.06. Truck Bomb (2000); Θ2000,125; 125; 09.92; 0.86; 0.91. Θ2000,150; 150; 11.91; 0.71; 0.67. Θ2000,200; 200; 15.87; 0.24; 0.18.

Table 4. 3: Threat scenarios and corresponding probabilities of exceeding damage limit states

Threat Type (kg of TNT); Threat Scenario Designation; Standoff Distance R (m); Scaled Distance Z (m/kg1/3); Probability of Limit State Violation (Lower Bounds of Damage States). DS-II; DS-III; DS-IV. Personal Attack (50); Θ50,5; 5; 1.36; 1.00; 0.55; 0.55. Θ50,7.5; 7.5; 2.04; 1.00; 0.06; 0.00. Θ50,10; 10; 2.71; 1.00; 0.05; 0.00. Θ50,15; 15; 4.07; 1.00; 0.00; 0.00. Θ50,20; 20; 5.43; 0.90; 0.00; 0.00. Θ50,25; 25; 6.79; 0.42; 0.00; 0.00. Θ50,30; 30; 8.14; 0.13; 0.00; 0.00. Θ50,35; 35; 9.50; 0.07; 0.00; 0.00. Θ50,40; 40; 10.86; 0.02; 0.00; 0.00. Car Bomb (300); Θ300,10; 10; 1.49; 1.00; 0.60; 0.60. Θ300,15; 15; 2.24; 1.00; 0.58; 0.58. Θ300,20; 20; 2.99; 1.00; 0.05; 0.00. Θ300,30; 30; 4.48; 1.00; 0.03; 0.00. Θ300,40; 40; 5.98; 1.00; 0.00; 0.00. Θ300,50; 50; 7.47; 0.96; 0.00; 0.00. Θ300,60; 60; 8.96; 0.66; 0.00; 0.00. Θ300,80; 80; 11.95; 0.27; 0.00; 0.00. Θ300,100; 100; 14.94; 0.06; 0.00; 0.00. Truck Bomb (2000); Θ2000,25; 25; 1.98; 1.00; 0.55; 0.55. Θ2000,50; 50; 3.97; 1.00; 0.08; 0.06. Θ2000,75; 75; 5.95; 1.00; 0.07; 0.00. Θ2000,100; 100; 7.94; 1.00; 0.00; 0.00. Θ2000,125; 125; 9.92; 0.91; 0.00; 0.00. Θ2000,150; 150; 11.91; 0.67; 0.00; 0.00. Θ2000,175; 175; 13.89; 0.42; 0.00; 0.00. Θ2000,200; 200; 15.87; 0.18; 0.00; 0.00. Θ2000,250; 250; 19.84; 0.06; 0.00; 0.00.

Uncertainty in structural response

- Input parameters (materials)

- Model error

- Inherent variability

Structural response model

- Crack width

- Spalling

Fragility curves

(probability of exceeding a damage limit state)

Assumed DBT scenario Θij

Sources of uncertainty

- Input parameters

- Model error

- Inherent variability

Blast load model

- Peak pressure

- Specific impulse

- Load duration

Probability distributions of the blast load parameters

Blast reliability curves

Pf |Θij

Judgment call by stakeholders

Risk Management

Threat assessment

P(Θij)

Aggregate probability of failure Pf

Risk Analysis

Cost–benefit analysis

(e.g. cost of repairing and building downtime)

Consequences

(e.g. cost of reconstruction)

Damage states

(DS-I, -II, -III, -IV)

- Method of repair

- Building downtime

Assumed range of load parameters

(peak pressure, specific impulse, duration)

Intelligence

Expert opinion

Risk mitigation options

(e.g. fencing)

PRA Level I

PRA Level II

PRA Level III

System–Level response evaluation

- ASCE 2011

- CSA 2012

- GSA 2013

Fig. 4. 1: Framework for decision making in land acquisition and perimeter protection of buildings subjected to blast threats (based on Stewart and Netherton (2008)): blue = fragility analysis; red = analysis of load uncertainty; green = threat assessment; grey = risk evaluation; orange = cost–benefit analysis; black = executive decisions

Uncertainty in structural response

- Input parameters (materials)

- Model error

- Inherent variability

Structural response model

- Crack width

- Spalling

Assumed DBT scenario Θij

Blast load model

- Peak pressure

- Specific impulse

- Load duration

DBT Fragility curves Pf |Θij

Cost–benefit analysis (e.g. cost of repairing and building downtime)

Risk

Damage states

(DS-I, -II, -III, -IV)

- Method of Repair

- Building downtime

Risk mitigation options

Level A: performance assessment

Level B: decision making

Fig. 4. 2: Simplified framework for decision making in land acquisition and perimeter protection of buildings subjected to blast threats

(a)                                            (b)                                            (c)

Fig. 4. 3: Damage states experienced by RMSWs subjected to blast loading: (a) Moderate damage of specimen FL11, maximum crack width ≤ 1.0 mm; (b) Heavy damage of specimen FH55, extensive spalling (ElSayed et al. 2014a); (c) Hazardous failure of specimen FL55, fracture of the steel reinforcement (ElSayed et al. 2014a)

- (b)

(c)

Fig. 4. 4: Effect of standoff distance: (a) Normally reflected peak pressure; (b) Normally reflected specific impulse; (c) Costs of protection.

Fig. 4. 5: Normal distributions associated with masonry assemblage compressive strength and position of steel reinforcement (depth)

Building layout                                                      3D view

Typical wall cross–section                                   Lateral view

Fig. 4. 6: Prototypical four–storey RMSW building

Fig. 4. 7: Crack widths along the mortar bed joints of RMSWs subjected to out–of–plane uniform static pressure

Fig. 4. 8: Effect of the number of randomly sampled variates on the estimator N’/N of the probability of exceeding the lower bound of DS-III

(a)

(b)

(c)

Fig. 4. 9: Fragility curves of fictitious RMSW subjected to three threat scenarios: (a) Personal attack – 50 kg TNT; (b) Car bomb – 300 kg TNT; (c) Truck bomb – 2,000 kg TNT

Zone–A

Zone–D

Zone–B

Zone–C

Fig. 4. 10: Blast protection of four storey RMSW building by “zoning” of the premises: Zone–A, access restricted to authorized pedestrians; Zone–B, access granted to all pedestrians (no vehicles); Zone–C, access granted to small vehicles (cars); Zone D, unrestricted access

Chapter 5: Additional Information

5.1 Material Characteristics

5.1.1 Concrete Masonry Units (CMU)

| CMU No.; Load (kN); Stress (MPa). 1; 93.50; 19.52. 2; 87.00; 18.17. 3; 95.50; 19.94. 4; 101.50; 21.19. 5; 103.75; 21.66. 6; 107.50; 22.45. 7; 72.50; 15.14. 8; 80.00; 16.70. 9; 102.00; 21.30. 10; 106.00; 22.13. 11; 103.75; 21.66. 12; 111.00; 23.18. 13; 80.00; 16.70. 14; 92.00; 19.21. 15; 86.75; 18.11. 16; 129.50; 27.04. 17; 117.50; 24.54. 18; 79.50; 16.60. | Mean= 20.3 MPa COV = 15.2 % |  |
| --- | --- | --- |
|  | Fig. 5.1: Testing of Concrete Masonry Units |  |

5.1.2 Mortar Cubes

| Sample No.; Load (kN); Stress (MPa). 1; 39.2; 15.1. 2; 41.1; 15.8. 3; 57.8; 22.2. 4; 48.7; 18.7. 5; 51.9; 20.0. 6; 54.3; 20.9. 7; 48.3; 18.6. 8; 45.8; 17.6. 9; 47.2; 18.1. 10; 59.0; 22.7. 11; 50.9; 19.6. 12; 32.2; 12.4. 13; 28.4; 10.9. 14; 43.3; 16.6. 15; 34.3; 13.2. 16; 42.3; 16.3. 17; 43.6; 16.8. 18; 45.1; 17.3. 19; 41.9; 16.1. 20; 43.0; 16.5. 21; 47.6; 18.3. | Mean = 17.3 MPa COV = 17.1 % |
| --- | --- |
|  | Fig. 5.2: Testing of Mortar Cubes |

5.1.3 Grout Cylinders

| Cylinder No.; Load (kN); Stress (MPa). 1; 200.2; 11.2. 2; 280.2; 15.4. 3; 282.5; 15.4. 4; 333.6; 18.1. 5; 355.9; 19.4. 6; 367.0; 20.2. 7; 322.5; 17.8. 8; 313.6; 17.3. 9; 200.2; 10.9. 10; 320.3; 17.4. 11; 375.9; 20.4. 12; 333.6; 17.5. | Mean = 16.8 MPa COV = 18.5 % |  |
| --- | --- | --- |
|  | Fig. 5.3: Testing of Grout Cylinders |  |

5.1.4 Fully-Grouted Masonry Prisms

| Prism No.; Stress (MPa). 1; 14.7. 2; 23.0. 3; 19.9. 4; 20.3. 5; 15.8. 6; 19.6. 7; 19.0. 8; 20.8. 9; 16.0. 10; 19.8. 11; 11.9. 12; 20.7. 13; 13.8. 14; 18.4. 15; 22.6. 16; 16.4. 17; 20.4. Fig 5.4: Testing of fully-grouted masonry prisms | Mean = 18.4 MPa COV = 17.0 % |
| --- | --- |

5.1.5 Steel Reinforcement Stress-Strain Relationships

5.2 Test Setup and Boundary Conditions

Fig. 5.5: Two 50.8 mm (2 in) diameter solid steel rods were used to prevent the movement of the masonry structural walls way from the blast source

Top Parapet

Wing Wall

Wing Wall

Fig. 5.6: Steel framing elements within the wing walls and top parapet were used to prevent the movement of the masonry structural walls toward the blast source

5.3 Post-Blast Wall Damage

| (a) | (b) |
| --- | --- |
| (c) | (d) |
| Fig. 5.7: (a) Sample of compression cracks on the first sample, and tension side crack pattern (b) SL11, (c) FL11, and (d) FM11 |  |

| Fig. 8: Compression cracks in the front face of SL11 after the first shot |  |
| --- | --- |

| (a) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (b) |  |  |  |  |  |  |  |  |
| (c) |  |  |  |  |  |  |  |  |
| (d) |  |  |  |  |  |  |  |  |
| Fig. 5.9: Sample of compression cracks on the first wall, (a) Shot No. 5 (b) Shot No. 6, (c) Shot No. 7, and (d) Shot No. 8 |  |  |  |  |  |  |  |  |

| (a) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| (b) |  |  |  |  |  |
| (c) |  |  |  |  |  |
| (d) |  |  |  |  |  |
| Fig. 5.10: Sample of compression cracks on the first wall, (a) Shot No. 9 (b) Shot No. 10, (c) Shot No. 11, and (d) Shot No. 12 |  |  |  |  |  |

5.4 Measuring Peak Support Rotation

The experimental deflection response histories of the RM structural walls under different scaled distances were captured using the displacement transducers measurements at their three-quarter height when the mid-height experimental deflection histories were not available. Subsequently, the mid-height deflection histories were generated assuming an elasto-plastic deformed shape (Eq. 5.1), for Group I and Group II walls, and a plastic deformed shape (Eq. 5.2), for Group III walls. Using these measurements, each wall’s maximum support rotation was obtained as the cord angle (see Fig. 5.11), as specified by the ASCE/SEI 59-11 (ASCE 2011) and the CAN/CSA S850-12 (CSA 2012).

| ψx=165 L4 x4-2 x3 L+x L3 | (5.1) |
| --- | --- |

| ψx=2 xL | at 0 ≤x≤L2 | (5.2) |
| --- | --- | --- |
| ψx=2 (L-x)L | at L2 ≤x≤L |  |

Elasto-Plastic                    Plastic

Fig. 5.11: Elasto-plastic and plastic deformed shape

5.5 Analytical Model

5.5.1 Moment-Curvature Relationship

Moment-curvature analysis of the masonry wall section was used to define the wall section strength, curvature and stiffness (Em Ieff) at all stages of loading. The tested masonry walls were subjected to pure bending resulted from out-of-plane blast loading while the axial load due to self-weight was neglected, and therefore fiber model is used in order to develop moment-curvature relationships for different masonry cross-sections. The following assumptions were considered in the analytical model:

- An average strain rate was considered for the concrete blocks, the grout and the reinforcing bars.

- The concrete block and grout layers were incapable of providing tensile strength.

- The non-linear stress-strain relationship of grouted masonry specimens was based on the test results from 17 fully-grouted masonry prisms, and hence the relationships used were:

| fm' ε=fm' ×C0+C1ε+C2ε2+C3ε3 | at ε≤0.006 | (5.3-a) |
| --- | --- | --- |
| fm' ε=0.0 | at ε>0.006 | (5.3-b) |

where fm'  is the average compressive strength of masonry, which equals 21.18 MPa, and ε is the strain at the center of each fiber. Coefficients C0 to C3 are listed in Table 5.1, and they were determined by averaging experimental results of prism tests, as illustrated earlier.

Table 5.1: Coefficients of the fitting polynomials obtained for stress-strain relationship of grouted masonry

| Strain range | C0 | C1 | C2 | C3 |
| --- | --- | --- | --- | --- |
|  | 0.0 | 144 | 193,700 | -44,000,000 |
|  | 4.8 | -2,975 | 783,700 | -69,500,000 |

As mentioned earlier, axial force due to the masonry wall self-weight was neglected, and then equating compression to tension forces (resulting from stress resultants) satisfies the equilibrium at any level of response. Analytically, adjusting the position of neutral axis by trial and error until equilibrium is satisfied satisfies equilibrium. Hence, the moment and the corresponding curvature were given by (Priestley et al. 2007):

| M=i=1Nfm'εi bi hi yi +fsεs As ys | (5.4) |
| --- | --- |

| ϕ=εsys | (5.5) |
| --- | --- |

where εi and εs were the strain at the centroid of layer i and the level of the reinforcing bars, respectively. bi and hi are the width and height of layer i, respectively, while As is the total area of all reinforcing bars. Finally, yi and ys are the distances from neutral axis to layer i and reinforcing bars, respectively.

The algorism used for developing the moment-curvature relationship using the fiber model technique is shown in Fig. 5.12. This algorism consisted of three main parts: the input section, creating the fiber model part, and finally developing the moment-curvature curve. Creating the fiber model was carried out on masonry specimens, in which typical wall cross-section was divided into N1 (for face-shell) and N2 (for grout) layers. The stress-strain relationship for each layer was used to determine the stress distribution along wall cross-section considering an initially assumed natural axis location. The location of neutral axis was then adjusted, using a trial and error approach, to satisfy the equilibrium condition (which was governed by equating the difference between tension and compression forces to the external applied axial load), and thus the moment-curvature relationship associated to this cross-section could be developed. Starting with a low value of extreme fiber compression strain and adjusting the position of neutral axis that satisfy the axial equilibrium, moment and curvature corresponding to this strain were determined. After this, the compression strain of extreme fiber was incrementally increased and hence the moment and the curvature corresponding to this strain were calculated. Moreover, the maximum value of the moment, which represents the plastic moment, was updated automatically after each moment and curvature determination loop.

Fig. 5.12: Algorism used to develop Moment-Curvature relationship using the fiber model

5.5.2 Validation of the Analytical Resistance Function of Masonry Specimens

| (a) | (b) |
| --- | --- |
| Fig. 5.13: Experimental versus analytical resistance functions for walls (a) FMS and (b) FHS |  |

5.5.3 Validation of the Equivalent SDOF Model Predictions

| Shot # 2 | Shot # 3 |
| --- | --- |
| Shot # 4 | Shot # 7 |
| Shot # 8 |  |
| Fig. 5.14: Sample of the experimental versus analytical wall response histories |  |