# Appendix:  X-ray Crystallographic Data

Table A1:  Crystal data and structure refinement for 33.

Empirical formula 	C24 H11 Co3 O9

Formula weight 	620.12

Temperature 	197(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 16.793(4) Å	(= 90°.

b = 7.874(2) Å	(= 96.923(4)°.

c = 36.834(8) Å	(= 90°.

Volume	4834.6(19) Å3

Z	8

Density (calculated)	1.704 Mg/m3

Absorption coefficient	2.086 mm-1

F(000)	2464

Crystal size	.08 x .28 x .34 mm3

( range for data collection	1.11 to 24.99°.

Index ranges	-20≤h≤21, -10≤k≤10, -46≤l≤47

Reflections collected	16663

Independent reflections	4236 [R(int) = 0.1102]

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4195 / 0 / 326

Goodness-of-fit on F2	1.008

Final R indices [I>2((I)]	R1 = 0.0612, wR2 = 0.1294

R indices (all data)	R1 = 0.1109, wR2 = 0.1546

Extinction coefficient	0.00078(12)

Largest diff. peak and hole	0.715 and -0.581 e.Å-3

Ratio of min/max apparent transmission  		0.503387

Table A2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 33.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	800(1)	192(1)	804(1)	28(1)

Co(2)	2257(1)	714(1)	870(1)	26(1)

Co(3)	1318(1)	2853(1)	571(1)	27(1)

C(1)	1406(3)	1954(8)	1060(2)	28(2)

C(2)	1502(4)	2917(7)	1397(2)	26(2)

C(3)	1192(3)	2727(7)	1716(2)	22(2)

C(4)	597(4)	1364(7)	1776(2)	23(1)

C(5)	851(4)	-137(8)	1948(2)	36(2)

C(6)	293(5)	-1332(9)	2028(2)	53(2)

C(7)	-499(6)	-1037(11)	1941(3)	63(3)

C(8)	-767(5)	424(13)	1773(3)	66(3)

C(9)	-216(4)	1640(9)	1685(2)	39(2)

C(10)	1412(3)	3867(7)	2033(2)	20(1)

C(11)	1031(4)	3752(8)	2345(2)	29(2)

C(12)	1257(4)	4755(8)	2650(2)	34(2)

C(13)	1881(4)	5888(8)	2653(2)	35(2)

C(14)	2253(4)	6035(9)	2348(2)	45(2)

C(15)	2030(4)	5069(8)	2039(2)	38(2)

C(16)	-209(5)	940(9)	815(2)	41(2)

O(16)	-850(3)	1456(7)	810(2)	58(2)

O(17)	761(4)	-2831(7)	1267(2)	61(2)

C(17)	775(4)	-1624(9)	1098(2)	37(2)

O(18)	693(3)	-1707(7)	107(2)	53(2)

C(18)	722(4)	-994(8)	372(2)	34(2)

O(19)	2669(4)	-1752(8)	1458(2)	72(2)

C(19)	2502(4)	-815(10)	1220(2)	43(2)

O(20)	2781(3)	-930(6)	212(2)	55(2)

C(20)	2565(4)	-325(8)	466(2)	32(2)

C(21)	3117(4)	2031(8)	992(2)	36(2)

O(21)	3675(3)	2836(7)	1072(2)	63(2)

C(22)	410(5)	4092(9)	538(2)	43(2)

O(22)	-143(3)	4908(7)	520(2)	66(2)

C(23)	1990(4)	4608(8)	646(2)	35(2)

O(24)	2389(3)	5776(6)	703(2)	53(2)

O(24)	1400(4)	1890(7)	-204(2)	57(2)

C(24)	1367(4)	2275(8)	93(2)	37(2)

________________________________________________________________________________

Table A3:  Bond lengths [Å] and angles [°] for 33.

_______________________________________________________________________________________

Co(1)-C(17) 	1.797(8)

Co(1)-C(16) 	1.798(9)

Co(1)-C(18) 	1.834(8)

Co(1)-C(1) 	1.903(6)

Co(1)-Co(3) 	2.4626(12)

Co(1)-Co(2) 	2.4640(13)

Co(2)-C(19) 	1.776(8)

Co(2)-C(21) 	1.791(7)

Co(2)-C(20) 	1.826(8)

Co(2)-C(1) 	1.929(6)

Co(2)-Co(3) 	2.4723(12)

Co(3)-C(23) 	1.785(7)

Co(3)-C(22) 	1.802(8)

Co(3)-C(24) 	1.829(9)

Co(3)-C(1) 	1.925(7)

C(1)-C(2) 	1.447(9)

C(2)-C(3) 	1.351(9)

C(3)-C(10) 	1.484(8)

C(3)-C(4) 	1.500(8)

C(4)-C(9) 	1.383(9)

C(4)-C(5) 	1.384(9)

C(5)-C(6) 	1.384(10)

C(6)-C(7) 	1.350(12)

C(7)-C(8) 	1.358(12)

C(8)-C(9) 	1.396(10)

C(10)-C(11) 	1.384(9)

C(10)-C(15) 	1.403(8)

C(11)-C(12) 	1.386(9)

C(12)-C(13) 	1.374(9)

C(13)-C(14) 	1.355(10)

C(14)-C(15) 	1.382(10)

C(16)-O(16) 	1.148(8)

O(17)-C(17) 	1.138(8)

O(18)-C(18) 	1.123(8)

O(19)-C(19) 	1.155(9)

O(20)-C(20) 	1.146(8)

C(21)-O(21) 	1.141(8)

C(22)-O(22) 	1.124(8)

C(23)-O(24) 	1.142(7)

O(24)-C(24) 	1.142(8)

C(17)-Co(1)-C(16)	99.0(3)

C(17)-Co(1)-C(18)	96.4(3)

C(16)-Co(1)-C(18)	102.6(3)

C(17)-Co(1)-C(1)	109.4(3)

C(16)-Co(1)-C(1)	101.5(3)

C(18)-Co(1)-C(1)	141.1(3)

C(17)-Co(1)-Co(3)	157.2(2)

C(16)-Co(1)-Co(3)	95.9(2)

C(18)-Co(1)-Co(3)	97.0(2)

C(1)-Co(1)-Co(3)	50.4(2)

C(17)-Co(1)-Co(2)	99.7(2)

C(16)-Co(1)-Co(2)	150.4(2)

C(18)-Co(1)-Co(2)	97.8(2)

C(1)-Co(1)-Co(2)	50.5(2)

Co(3)-Co(1)-Co(2)	60.24(3)

C(19)-Co(2)-C(21)	95.8(3)

C(19)-Co(2)-C(20)	102.9(3)

C(21)-Co(2)-C(20)	99.4(3)

C(19)-Co(2)-C(1)	101.3(3)

C(21)-Co(2)-C(1)	103.0(3)

C(20)-Co(2)-C(1)	144.8(3)

C(19)-Co(2)-Co(1)	95.7(2)

C(21)-Co(2)-Co(1)	152.0(2)

C(20)-Co(2)-Co(1)	102.8(2)

C(1)-Co(2)-Co(1)	49.5(2)

C(19)-Co(2)-Co(3)	149.8(3)

C(21)-Co(2)-Co(3)	99.7(2)

C(20)-Co(2)-Co(3)	99.8(2)

C(1)-Co(2)-Co(3)	50.0(2)

Co(1)-Co(2)-Co(3)	59.85(4)

C(23)-Co(3)-C(22)	96.1(3)

C(23)-Co(3)-C(24)	103.9(3)

C(22)-Co(3)-C(24)	101.9(4)

C(23)-Co(3)-C(1)	99.4(3)

C(22)-Co(3)-C(1)	103.3(3)

C(24)-Co(3)-C(1)	143.3(3)

C(23)-Co(3)-Co(1)	148.0(2)

C(22)-Co(3)-Co(1)	98.7(2)

C(24)-Co(3)-Co(1)	100.5(2)

C(1)-Co(3)-Co(1)	49.6(2)

C(23)-Co(3)-Co(2)	95.8(2)

C(22)-Co(3)-Co(2)	152.5(3)

C(24)-Co(3)-Co(2)	99.1(2)

C(1)-Co(3)-Co(2)	50.2(2)

Co(1)-Co(3)-Co(2)	59.91(4)

C(2)-C(1)-Co(1)	143.6(5)

C(2)-C(1)-Co(3)	126.7(4)

Co(1)-C(1)-Co(3)	80.1(3)

C(2)-C(1)-Co(2)	124.5(4)

Co(1)-C(1)-Co(2)	80.0(3)

Co(3)-C(1)-Co(2)	79.8(3)

C(3)-C(2)-C(1)	132.4(5)

C(2)-C(3)-C(10)	122.2(5)

C(2)-C(3)-C(4)	122.7(6)

C(10)-C(3)-C(4)	115.1(5)

C(9)-C(4)-C(5)	119.0(6)

C(9)-C(4)-C(3)	120.5(6)

C(5)-C(4)-C(3)	120.3(6)

C(4)-C(5)-C(6)	120.0(7)

C(7)-C(6)-C(5)	120.3(7)

C(6)-C(7)-C(8)	121.2(7)

C(7)-C(8)-C(9)	119.6(8)

C(4)-C(9)-C(8)	120.0(7)

C(11)-C(10)-C(15)	116.5(6)

C(11)-C(10)-C(3)	121.2(5)

C(15)-C(10)-C(3)	122.3(6)

C(10)-C(11)-C(12)	121.7(6)

C(13)-C(12)-C(11)	120.8(7)

C(14)-C(13)-C(12)	118.3(7)

C(13)-C(14)-C(15)	122.0(6)

C(14)-C(15)-C(10)	120.7(7)

O(16)-C(16)-Co(1)	177.1(7)

O(17)-C(17)-Co(1)	176.1(6)

O(18)-C(18)-Co(1)	178.2(6)

O(19)-C(19)-Co(2)	177.0(7)

O(20)-C(20)-Co(2)	177.4(6)

O(21)-C(21)-Co(2)	178.3(6)

O(22)-C(22)-Co(3)	177.9(7)

O(24)-C(23)-Co(3)	176.2(6)

O(24)-C(24)-Co(3)	179.0(6)

_______________________________________________________________________________________

Table A4:  Anisotropic displacement parameters (Å2 x 103) for 33.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	30(1) 	23(1)	30(1) 	-2(1)	7(1) 	-12(1)

Co(2)	26(1) 	25(1)	28(1) 	0(1)	5(1) 	-6(1)

Co(3)	30(1) 	22(1)	29(1) 	1(1)	7(1) 	-7(1)

C(1)	16(3) 	30(3)	40(5) 	7(3)	11(3) 	-10(2)

C(2)	26(4) 	23(3)	31(4) 	-1(3)	8(3) 	-14(2)

C(3)	15(3) 	20(3)	30(4) 	0(3)	0(3) 	-2(2)

C(4)	21(4) 	23(3)	27(4) 	-2(3)	9(3) 	-7(2)

C(5)	36(4) 	27(4)	45(5) 	3(3)	9(4) 	-9(3)

C(6)	79(7) 	27(4)	54(6) 	9(4)	9(5) 	-18(4)

C(7)	59(7) 	63(6)	68(7) 	8(5)	19(5) 	-45(5)

C(8)	23(5) 	93(7)	82(7) 	6(6)	11(4) 	-28(4)

C(9)	23(4) 	47(4)	48(5) 	4(4)	8(3) 	-4(3)

C(10)	19(3) 	16(3)	25(4) 	3(3)	5(3) 	1(2)

C(11)	27(4) 	29(3)	30(4) 	-10(3)	6(3) 	-7(3)

C(12)	42(4) 	33(4)	31(4) 	-3(3)	17(3) 	5(3)

C(13)	31(4) 	41(4)	34(5) 	-12(3)	6(3) 	2(3)

C(14)	36(5) 	48(4)	54(6) 	-19(4)	13(4) 	-26(3)

C(15)	36(4) 	41(4)	39(5) 	-8(4)	13(3) 	-22(3)

C(16)	36(5) 	45(4)	45(5) 	-5(4)	10(4) 	-21(3)

O(16)	35(4) 	64(4)	78(5) 	8(3)	13(3) 	-8(3)

O(17)	97(5) 	37(3)	49(4) 	12(3)	8(3) 	-22(3)

C(17)	38(5) 	38(4)	36(5) 	-10(4)	7(4) 	-14(3)

O(18)	67(4) 	55(3)	36(4) 	-17(3)	8(3) 	-18(3)

C(18)	33(4) 	29(4)	41(5) 	-2(4)	7(4) 	-11(3)

O(19)	68(4) 	71(4)	75(5) 	41(4)	4(3) 	0(3)

C(19)	40(5) 	45(4)	47(6) 	2(4)	12(4) 	-7(3)

O(20)	67(4) 	46(3)	54(4) 	-21(3)	23(3) 	-5(3)

C(20)	38(4) 	24(4)	33(5) 	0(3)	1(4) 	-9(3)

C(21)	41(5) 	33(4)	34(5) 	-1(3)	10(4) 	-1(3)

O(21)	47(4) 	62(4)	77(5) 	-7(3)	-2(3) 	-27(3)

C(22)	37(5) 	35(4)	54(6) 	13(4)	-3(4) 	-5(3)

O(22)	44(4) 	46(3)	106(6) 	7(3)	2(3) 	10(3)

C(23)	44(5) 	29(4)	35(5) 	3(3)	18(4) 	-3(3)

O(24)	43(3) 	36(3)	80(4) 	2(3)	11(3) 	-23(2)

O(24)	86(5) 	55(4)	33(4) 	-6(3)	16(3) 	-16(3)

C(24)	42(5) 	27(4)	43(5) 	6(4)	6(4) 	-16(3)

______________________________________________________________________________

Table A5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 33.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(2A)	1849(4)	3867(7)	1393(2)	32

H(5A)	1407(4)	-347(8)	2011(2)	43

H(6A)	468(5)	-2364(9)	2146(2)	64

H(7A)	-875(6)	-1868(11)	1998(3)	75

H(8A)	-1327(5)	618(13)	1715(3)	79

H(9A)	-400(4)	2656(9)	1564(2)	47

H(11A)	604(4)	2965(8)	2351(2)	34

H(12A)	978(4)	4659(8)	2858(2)	41

H(13A)	2047(4)	6551(8)	2864(2)	42

H(14A)	2680(4)	6825(9)	2347(2)	54

H(15A)	2298(4)	5220(8)	1829(2)	45

________________________________________________________________________________

Table B1:  Crystal data and structure refinement for 39.

Empirical formula 	C26 H19 Co2 F O6 Si

Formula weight 	592.36

Temperature 	173(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)/n

Unit cell dimensions	a = 8.624(2) Å	(= 90°.

b = 20.573(5) Å	(= 95.017(4)°.

c = 14.556(4) Å	(= 90°.

Volume	2572.6(11) Å3

Z	4

Density (calculated)	1.529 Mg/m3

Absorption coefficient	1.382 mm-1

F(000)	1200

Crystal size	0.10 x 0.16 x 0.28 mm3

( range for data collection	1.72 to 27.00°.

Index ranges	-11(h(11, -23(k(26, -18(l(17

Reflections collected	22551

Independent reflections	5615 [R(int) = 0.0608]

Completeness to ( = 27.00°	100.0 %

Absorption correction	Empirical (SADABS)

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	5615 / 0 / 402

Goodness-of-fit on F2	1.010

Final R indices [I>2((I)]	R1 = 0.0389, wR2 = 0.0658

R indices (all data)	R1 = 0.0718, wR2 = 0.0742

Extinction coefficient	0.00005(15)

Largest diff. peak and hole	0.368 and -0.278 e.Å-3

Ratio of min/max apparent transmission	0.878006

Table B2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 39.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	38(1)	2186(1)	1347(1)	26(1)

Co(2)	-295(1)	2574(1)	2923(1)	27(1)

Si(1)	-3520(1)	2999(1)	1485(1)	30(1)

F(1)	-4334(2)	2694(1)	547(1)	59(1)

C(1)	-2542(3)	878(1)	1473(2)	30(1)

C(2)	-1576(3)	348(1)	1328(2)	33(1)

C(3)	-488(3)	260(1)	2153(2)	31(1)

C(4)	673(3)	-202(1)	2364(2)	40(1)

C(5)	1488(4)	-185(2)	3220(3)	47(1)

C(6)	1159(4)	274(2)	3874(3)	43(1)

C(7)	17(3)	745(1)	3659(2)	34(1)

C(8)	-787(3)	738(1)	2799(2)	27(1)

C(9)	-2060(3)	1199(1)	2402(2)	25(1)

C(10)	-3709(3)	1057(2)	808(2)	37(1)

C(11)	-3905(4)	701(2)	-7(2)	47(1)

C(12)	-2944(4)	187(2)	-158(2)	51(1)

C(13)	-1782(4)	-1(2)	505(2)	44(1)

C(14)	-3428(3)	1256(1)	3023(2)	32(1)

C(15)	-4210(3)	619(2)	3182(2)	41(1)

C(16)	-4278(4)	341(2)	3964(3)	53(1)

C(17)	-1432(3)	1873(1)	2219(2)	23(1)

C(18)	-1922(3)	2449(1)	1877(2)	23(1)

C(19)	-5027(4)	3013(2)	2309(3)	49(1)

C(20)	-2858(5)	3812(2)	1200(3)	53(1)

C(21)	1669(3)	1636(1)	1583(2)	36(1)

O(21)	2691(2)	1289(1)	1731(2)	56(1)

C(22)	-667(3)	1844(1)	248(2)	33(1)

O(22)	-1038(2)	1636(1)	-463(2)	48(1)

C(23)	853(3)	2924(1)	899(2)	36(1)

O(23)	1382(3)	3385(1)	628(2)	56(1)

C(24)	1436(3)	2194(1)	3498(2)	36(1)

O(24)	2557(2)	1976(1)	3836(2)	52(1)

C(25)	-1455(3)	2707(1)	3871(2)	35(1)

O(25)	-2222(2)	2813(1)	4448(2)	56(1)

C(26)	345(3)	3411(2)	2790(2)	37(1)

O(26)	743(3)	3928(1)	2692(2)	60(1)

________________________________________________________________________________

Table B3:  Bond lengths [Å] and angles [°] for 39.

____________________________________________________________________________________

Co(1)-C(22) 	1.802(3)

Co(1)-C(21) 	1.814(3)

Co(1)-C(23) 	1.817(3)

Co(1)-C(17) 	1.979(2)

Co(1)-C(18) 	1.994(2)

Co(1)-Co(2) 	2.4703(7)

Co(2)-C(25) 	1.795(3)

Co(2)-C(26) 	1.822(3)

Co(2)-C(24) 	1.823(3)

Co(2)-C(17) 	1.979(2)

Co(2)-C(18) 	1.994(3)

Si(1)-F(1) 	1.6068(19)

Si(1)-C(20) 	1.826(4)

Si(1)-C(18) 	1.836(3)

Si(1)-C(19) 	1.844(3)

C(1)-C(10) 	1.384(4)

C(1)-C(2) 	1.398(3)

C(1)-C(9) 	1.530(4)

C(2)-C(13) 	1.395(4)

C(2)-C(3) 	1.469(4)

C(3)-C(4) 	1.395(4)

C(3)-C(8) 	1.400(4)

C(4)-C(5) 	1.377(4)

C(5)-C(6) 	1.388(4)

C(6)-C(7) 	1.397(4)

C(7)-C(8) 	1.377(4)

C(8)-C(9) 	1.526(3)

C(9)-C(17) 	1.519(3)

C(9)-C(14) 	1.552(3)

C(10)-C(11) 	1.391(4)

C(11)-C(12) 	1.373(5)

C(12)-C(13) 	1.385(5)

C(14)-C(15) 	1.501(4)

C(15)-C(16) 	1.280(5)

C(17)-C(18) 	1.339(3)

C(21)-O(21) 	1.140(3)

C(22)-O(22) 	1.140(3)

C(23)-O(23) 	1.138(3)

C(24)-O(24) 	1.139(3)

C(25)-O(25) 	1.135(3)

C(26)-O(26) 	1.131(3)

C(22)-Co(1)-C(21)	96.98(12)

C(22)-Co(1)-C(23)	96.82(12)

C(21)-Co(1)-C(23)	105.73(12)

C(22)-Co(1)-C(17)	104.91(11)

C(21)-Co(1)-C(17)	101.82(11)

C(23)-Co(1)-C(17)	142.29(11)

C(22)-Co(1)-C(18)	102.58(11)

C(21)-Co(1)-C(18)	139.91(11)

C(23)-Co(1)-C(18)	106.23(11)

C(17)-Co(1)-C(18)	39.39(10)

C(22)-Co(1)-Co(2)	153.17(8)

C(21)-Co(1)-Co(2)	100.18(9)

C(23)-Co(1)-Co(2)	98.18(9)

C(17)-Co(1)-Co(2)	51.40(7)

C(18)-Co(1)-Co(2)	51.73(7)

C(25)-Co(2)-C(26)	97.65(12)

C(25)-Co(2)-C(24)	101.57(12)

C(26)-Co(2)-C(24)	102.15(13)

C(25)-Co(2)-C(17)	102.96(11)

C(26)-Co(2)-C(17)	140.76(12)

C(24)-Co(2)-C(17)	105.86(12)

C(25)-Co(2)-C(18)	101.80(11)

C(26)-Co(2)-C(18)	103.95(12)

C(24)-Co(2)-C(18)	142.00(11)

C(17)-Co(2)-C(18)	39.38(10)

C(25)-Co(2)-Co(1)	151.80(9)

C(26)-Co(2)-Co(1)	98.40(9)

C(24)-Co(2)-Co(1)	97.51(9)

C(17)-Co(2)-Co(1)	51.38(7)

C(18)-Co(2)-Co(1)	51.72(7)

F(1)-Si(1)-C(20)	106.67(18)

F(1)-Si(1)-C(18)	106.52(11)

C(20)-Si(1)-C(18)	113.20(15)

F(1)-Si(1)-C(19)	106.16(17)

C(20)-Si(1)-C(19)	112.66(19)

C(18)-Si(1)-C(19)	111.09(15)

C(10)-C(1)-C(2)	120.6(3)

C(10)-C(1)-C(9)	128.9(3)

C(2)-C(1)-C(9)	110.6(2)

C(13)-C(2)-C(1)	119.9(3)

C(13)-C(2)-C(3)	131.5(3)

C(1)-C(2)-C(3)	108.6(2)

C(4)-C(3)-C(8)	120.1(3)

C(4)-C(3)-C(2)	131.2(3)

C(8)-C(3)-C(2)	108.7(2)

C(5)-C(4)-C(3)	118.8(3)

C(4)-C(5)-C(6)	121.2(3)

C(5)-C(6)-C(7)	120.0(3)

C(8)-C(7)-C(6)	119.1(3)

C(7)-C(8)-C(3)	120.6(2)

C(7)-C(8)-C(9)	128.8(2)

C(3)-C(8)-C(9)	110.6(2)

C(17)-C(9)-C(8)	112.2(2)

C(17)-C(9)-C(1)	108.3(2)

C(8)-C(9)-C(1)	101.3(2)

C(17)-C(9)-C(14)	109.5(2)

C(8)-C(9)-C(14)	112.6(2)

C(1)-C(9)-C(14)	112.7(2)

C(1)-C(10)-C(11)	118.9(3)

C(12)-C(11)-C(10)	120.8(4)

C(11)-C(12)-C(13)	120.9(3)

C(12)-C(13)-C(2)	119.0(3)

C(15)-C(14)-C(9)	113.5(2)

C(16)-C(15)-C(14)	125.7(4)

C(18)-C(17)-C(9)	140.0(2)

C(18)-C(17)-Co(1)	70.90(14)

C(9)-C(17)-Co(1)	131.85(17)

C(18)-C(17)-Co(2)	70.90(15)

C(9)-C(17)-Co(2)	137.94(19)

Co(1)-C(17)-Co(2)	77.23(8)

C(17)-C(18)-Si(1)	149.90(18)

C(17)-C(18)-Co(1)	69.71(14)

Si(1)-C(18)-Co(1)	133.28(13)

C(17)-C(18)-Co(2)	69.72(15)

Si(1)-C(18)-Co(2)	128.05(14)

Co(1)-C(18)-Co(2)	76.56(9)

O(21)-C(21)-Co(1)	179.8(3)

O(22)-C(22)-Co(1)	176.3(2)

O(23)-C(23)-Co(1)	179.0(3)

O(24)-C(24)-Co(2)	176.9(3)

O(25)-C(25)-Co(2)	176.8(3)

O(26)-C(26)-Co(2)	178.8(3)

______________________________________________________________________________________

Table B4:  Anisotropic displacement parameters (Å2 x 103) for 39.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	28(1) 	27(1)	23(1) 	0(1)	9(1) 	-2(1)

Co(2)	30(1) 	29(1)	22(1) 	0(1)	6(1) 	-3(1)

Si(1)	32(1) 	30(1)	28(1) 	2(1)	2(1) 	4(1)

F(1)	68(1) 	63(1)	43(1) 	-12(1)	-21(1) 	16(1)

C(1)	31(1) 	30(2)	30(2) 	0(1)	11(1) 	-11(1)

C(2)	35(2) 	30(2)	35(2) 	-4(1)	13(1) 	-10(1)

C(3)	33(1) 	24(2)	40(2) 	0(1)	13(1) 	-3(1)

C(4)	45(2) 	25(2)	52(2) 	-3(2)	19(2) 	1(1)

C(5)	41(2) 	29(2)	70(3) 	9(2)	9(2) 	10(1)

C(6)	45(2) 	38(2)	47(2) 	4(2)	-3(2) 	4(1)

C(7)	38(2) 	26(2)	37(2) 	4(1)	6(1) 	4(1)

C(8)	30(1) 	23(2)	30(2) 	5(1)	8(1) 	-1(1)

C(9)	28(1) 	23(2)	27(2) 	1(1)	9(1) 	-1(1)

C(10)	33(2) 	42(2)	38(2) 	4(2)	4(1) 	-14(1)

C(11)	49(2) 	57(2)	35(2) 	0(2)	2(2) 	-26(2)

C(12)	58(2) 	61(3)	36(2) 	-15(2)	11(2) 	-33(2)

C(13)	49(2) 	37(2)	49(2) 	-14(2)	21(2) 	-16(2)

C(14)	32(2) 	31(2)	35(2) 	8(2)	13(1) 	4(1)

C(15)	42(2) 	36(2)	46(2) 	4(2)	20(2) 	-3(1)

C(16)	68(2) 	38(2)	56(3) 	8(2)	22(2) 	-11(2)

C(17)	23(1) 	30(2)	18(1) 	-2(1)	6(1) 	-4(1)

C(18)	26(1) 	28(2)	17(1) 	-1(1)	6(1) 	-4(1)

C(19)	43(2) 	43(2)	62(3) 	10(2)	20(2) 	13(2)

C(20)	49(2) 	45(2)	66(3) 	22(2)	13(2) 	7(2)

C(21)	33(2) 	44(2)	34(2) 	-4(1)	11(1) 	-4(1)

O(21)	38(1) 	60(2)	70(2) 	5(1)	11(1) 	15(1)

C(22)	35(2) 	32(2)	33(2) 	3(1)	14(1) 	-5(1)

O(22)	61(1) 	55(2)	29(1) 	-8(1)	10(1) 	-19(1)

C(23)	43(2) 	39(2)	27(2) 	-6(1)	12(1) 	-7(1)

O(23)	81(2) 	43(1)	47(2) 	4(1)	24(1) 	-23(1)

C(24)	41(2) 	39(2)	28(2) 	-5(1)	7(1) 	-9(1)

O(24)	40(1) 	61(2)	54(2) 	3(1)	-10(1) 	5(1)

C(25)	40(2) 	39(2)	27(2) 	3(1)	3(1) 	-4(1)

O(25)	55(1) 	81(2)	36(1) 	-2(1)	20(1) 	6(1)

C(26)	49(2) 	37(2)	24(2) 	-3(1)	7(1) 	-11(1)

O(26)	92(2) 	40(1)	48(2) 	-6(1)	14(1) 	-29(1)

______________________________________________________________________________

Table B5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 10 3)

for 39.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(4)	920(30)	-535(13)	1889(19)	37(8)

H(5)	2290(30)	-510(15)	3370(20)	56(9)

H(6)	1740(30)	306(12)	4430(20)	37(8)

H(7)	-190(30)	1071(12)	4101(18)	33(7)

H(10)	-4370(30)	1421(13)	935(18)	35(8)

H(11)	-4680(30)	848(14)	-460(20)	51(10)

H(12)	-3090(30)	-36(15)	-720(20)	62(10)

H(13)	-1140(30)	-361(14)	440(20)	43(9)

H(14A)	-4180(30)	1556(11)	2759(16)	21(6)

H(14B)	-3030(30)	1432(12)	3623(18)	27(7)

H(15)	-4730(40)	402(17)	2640(30)	77(12)

H(16A)	-3730(40)	524(17)	4500(30)	80(13)

H(16B)	-4830(30)	-81(15)	4000(20)	52(9)

H(19A)	-5850(40)	3279(16)	2070(20)	66(11)

H(19B)	-4610(40)	3160(17)	2850(20)	67(13)

H(19C)	-5410(40)	2558(19)	2450(30)	89(13)

H(20A)	-2110(40)	3802(14)	800(20)	60(10)

H(20B)	-2350(40)	4015(16)	1740(20)	63(12)

H(20C)	-3700(40)	4061(16)	960(20)	68(11)

________________________________________________________________________________

Table C1:  Crystal data and structure refinement for 42.

Empirical formula 	C26 H22 Co2 O8 Si

Formula weight 	608.39

Temperature 	173(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)/c

Unit cell dimensions	a = 20.445(7) Å	(= 90°.

b = 10.233(3) Å	(= 105.938(5)°.

c = 27.202(9) Å	(= 90°.

Volume	5472(3) Å3

Z	8

Density (calculated)	1.477 Mg/m3

Absorption coefficient	1.302 mm-1

F(000)	2480

Crystal size	.03 x .17 x .20 mm3

( range for data collection	1.04 to 23.75°.

Index ranges	-23(h(21, -11(k(11, -30(l(30

Reflections collected	35492

Independent reflections	8346 [R(int) = 0.1443]

Completeness to ( = 23.75°	100.0 %

Absorption correction	Empirical (SADABS)

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8346 / 243 / 834

Goodness-of-fit on F2	0.975

Final R indices [I>2((I)]	R1 = 0.0607, wR2 = 0.0762

R indices (all data)	R1 = 0.1486, wR2 = 0.0945

Extinction coefficient	0.00020(4)

Largest diff. peak and hole	0.425 and -0.377 e.Å-3

Ratio of min/max apparent transmission  	0.797769

Table C2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 42.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	4520(1)	6575(1)	6838(1)	31(1)

Co(2)	4766(1)	5251(1)	6152(1)	30(1)

Si(1)	4677(1)	8556(2)	5830(1)	32(1)

C(1)	2994(3)	4627(5)	6207(2)	25(2)

C(2)	2572(3)	4964(5)	6514(2)	27(2)

C(3)	2412(3)	6354(5)	6449(2)	29(2)

C(4)	1986(3)	7152(7)	6637(3)	39(2)

C(5)	1907(3)	8443(6)	6487(3)	47(2)

C(6)	2225(3)	8948(7)	6142(3)	43(2)

C(7)	2648(3)	8164(6)	5943(3)	35(2)

C(8)	2741(3)	6873(5)	6103(2)	26(2)

C(9)	3187(3)	5835(5)	5955(2)	24(2)

O(9)	3031(2)	5624(4)	5413(2)	29(1)

C(10)	3188(3)	3344(6)	6167(3)	31(2)

C(11)	2971(3)	2391(6)	6453(3)	40(2)

C(12)	2573(3)	2736(7)	6774(3)	41(2)

C(13)	2369(3)	4010(7)	6808(3)	40(2)

C(14)	3931(3)	6198(5)	6161(2)	25(2)

C(15)	4383(3)	7075(5)	6108(2)	24(2)

C(16)	4157(5)	10016(7)	5878(4)	53(2)

C(17)	5577(4)	8912(8)	6198(4)	50(2)

C(18)	4649(4)	8197(7)	5154(3)	38(2)

C(19)	3983(4)	8265(8)	4760(3)	53(2)

O(19)	3468(3)	7728(5)	4971(2)	45(2)

C(20)	3968(5)	7637(8)	4254(3)	49(2)

C(21)	4180(3)	8024(6)	7040(2)	43(2)

O(21)	3964(3)	8952(4)	7163(2)	72(2)

C(22)	4238(3)	5393(6)	7230(2)	34(2)

O(22)	4055(2)	4671(4)	7487(2)	57(1)

C(23)	5417(4)	6755(6)	7156(3)	43(2)

O(23)	5983(2)	6802(4)	7351(2)	63(2)

C(24)	4815(3)	3732(6)	6503(2)	32(2)

O(24)	4880(2)	2788(4)	6736(2)	53(1)

C(25)	5658(4)	5550(6)	6200(3)	48(2)

O(25)	6220(2)	5677(4)	6230(2)	79(2)

C(26)	4470(3)	4630(6)	5510(3)	38(2)

O(26)	4283(2)	4250(5)	5109(2)	63(2)

Co(1A)	312(1)	9136(1)	4105(1)	33(1)

Co(2A)	384(1)	8902(1)	3219(1)	34(1)

Si(1A)	376(1)	5838(2)	3799(1)	30(1)

C(1A)	2178(6)	8439(8)	3639(4)	31(2)

C(2A)	2465(5)	9587(10)	3495(4)	41(3)

C(3A)	2387(5)	10633(8)	3831(4)	45(3)

C(4A)	2636(5)	11938(9)	3870(5)	73(4)

C(5A)	2569(6)	12674(10)	4262(6)	99(5)

C(6A)	2315(5)	12193(9)	4652(5)	76(3)

C(7A)	2032(3)	10915(5)	4607(2)	56(3)

C(8A)	2078(3)	10178(5)	4191(2)	37(3)

C(9A)	1862(3)	8755(5)	4075(2)	26(2)

O(9A)	2109(3)	8104(5)	4515(2)	40(1)

C(10A)	2220(3)	7239(5)	3420(2)	43(3)

C(11A)	2564(6)	7170(12)	3025(4)	61(3)

C(12A)	2830(8)	8328(13)	2891(6)	65(4)

C(13A)	2785(5)	9508(12)	3113(4)	67(3)

C(1B)	2110(20)	7906(17)	3581(12)	31(2)

C(2B)	2374(12)	8813(19)	3295(9)	41(3)

C(3B)	2337(19)	10090(18)	3499(13)	45(3)

C(4B)	2547(12)	11321(18)	3346(10)	73(4)

C(5B)	2468(18)	12390(20)	3607(13)	99(5)

C(6B)	2143(13)	12330(20)	3994(11)	76(3)

C(7B)	1941(13)	11130(19)	4157(9)	56(3)

C(8B)	2054(15)	10016(16)	3909(9)	37(3)

C(9B)	1812(13)	8631(17)	3967(9)	26(2)

O(9B)	2117(11)	8098(18)	4483(7)	40(1)

C(10B)	2180(14)	6567(17)	3547(10)	43(3)

C(11B)	2504(13)	6100(20)	3179(9)	61(3)

C(12B)	2766(18)	7020(20)	2894(13)	65(4)

C(13B)	2660(30)	8330(30)	2924(17)	67(3)

C(14A)	1081(3)	8548(5)	3851(2)	27(2)

C(15A)	623(3)	7579(5)	3783(2)	26(2)

C(16A)	851(5)	4794(8)	3452(4)	54(2)

C(17A)	-548(4)	5676(8)	3474(3)	46(2)

C(18A)	523(3)	5299(7)	4477(3)	36(2)

C(19A)	1201(4)	4953(9)	4793(3)	80(3)

O(19A)	1723(3)	5685(6)	4704(3)	66(2)

C(20A)	1284(5)	4438(13)	5295(4)	82(4)

C(21A)	645(3)	10541(6)	3074(3)	47(2)

O(21A)	827(2)	11529(4)	2979(2)	72(2)

C(22A)	-527(4)	8862(6)	2952(3)	42(2)

O(22A)	-1106(2)	8850(4)	2798(2)	59(1)

C(23A)	628(3)	7998(6)	2735(3)	44(2)

O(23A)	776(2)	7437(5)	2421(2)	59(2)

C(24A)	305(3)	10900(7)	4092(3)	59(2)

O(24A)	280(3)	12009(4)	4074(2)	100(2)

C(25A)	-566(3)	8741(5)	4069(2)	37(2)

O(25A)	-1111(2)	8504(4)	4063(2)	56(1)

C(26A)	663(4)	8871(7)	4775(3)	58(2)

O(26A)	865(3)	8697(6)	5204(2)	101(2)

________________________________________________________________________________

Table C3:  Bond lengths [Å] and angles [°] for 42.

______________________________________________________________________________________

Co(1)-C(21) 	1.787(7)

Co(1)-C(22) 	1.808(7)

Co(1)-C(23) 	1.809(7)

Co(1)-C(14) 	1.941(6)

Co(1)-C(15) 	1.993(6)

Co(1)-Co(2) 	2.4653(13)

Co(2)-C(26) 	1.800(7)

Co(2)-C(24) 	1.813(7)

Co(2)-C(25) 	1.818(7)

Co(2)-C(14) 	1.969(5)

Co(2)-C(15) 	2.014(5)

Si(1)-C(16) 	1.859(8)

Si(1)-C(18) 	1.859(7)

Si(1)-C(15) 	1.866(6)

Si(1)-C(17) 	1.874(8)

C(1)-C(10) 	1.384(7)

C(1)-C(2) 	1.400(7)

C(1)-C(9) 	1.517(7)

C(2)-C(13) 	1.396(8)

C(2)-C(3) 	1.459(7)

C(3)-C(4) 	1.390(8)

C(3)-C(8) 	1.401(7)

C(4)-C(5) 	1.379(8)

C(4)-H(4) 	0.92(5)

C(5)-C(6) 	1.380(8)

C(5)-H(5C) 	0.9500

C(6)-C(7) 	1.393(8)

C(6)-H(6) 	0.97(5)

C(7)-C(8) 	1.388(7)

C(7)-H(7) 	0.93(5)

C(8)-C(9) 	1.526(7)

C(9)-O(9) 	1.435(6)

C(9)-C(14) 	1.515(7)

O(9)-H(9) 	0.87(4)

C(10)-C(11) 	1.393(8)

C(10)-H(10) 	1.06(5)

C(11)-C(12) 	1.392(9)

C(11)-H(11) 	0.99(6)

C(12)-C(13) 	1.380(8)

C(12)-H(12) 	0.99(4)

C(13)-H(13) 	0.87(4)

C(14)-C(15) 	1.325(7)

C(16)-H(14) 	1.07(6)

C(16)-H(16) 	0.91(6)

C(16)-H(15) 	0.87(6)

C(17)-H(18) 	0.90(6)

C(17)-H(17) 	0.86(9)

C(17)-H(19) 	1.00(7)

C(18)-C(19) 	1.486(9)

C(18)-H(21) 	0.90(4)

C(18)-H(20) 	1.01(6)

C(19)-O(19) 	1.442(8)

C(19)-C(20) 	1.510(10)

C(19)-H(22) 	1.12(8)

O(19)-H(23) 	0.72(5)

C(20)-H(24) 	1.04(6)

C(20)-H(26) 	1.00(6)

C(20)-H(25) 	0.93(6)

C(21)-O(21) 	1.135(6)

C(22)-O(22) 	1.149(6)

C(23)-O(23) 	1.134(7)

C(24)-O(24) 	1.142(6)

C(25)-O(25) 	1.138(7)

C(26)-O(26) 	1.124(7)

Co(1A)-C(26A) 	1.786(8)

Co(1A)-C(24A) 	1.805(7)

Co(1A)-C(25A) 	1.816(7)

Co(1A)-C(14A) 	1.977(5)

Co(1A)-C(15A) 	2.004(5)

Co(1A)-Co(2A) 	2.4671(15)

Co(2A)-C(23A) 	1.788(7)

Co(2A)-C(22A) 	1.804(7)

Co(2A)-C(21A) 	1.835(7)

Co(2A)-C(14A) 	1.942(6)

Co(2A)-C(15A) 	2.004(5)

Si(1A)-C(15A) 	1.856(6)

Si(1A)-C(17A) 	1.860(8)

Si(1A)-C(16A) 	1.866(8)

Si(1A)-C(18A) 	1.868(7)

C(1A)-C(10A) 	1.378(8)

C(1A)-C(2A) 	1.414(11)

C(1A)-C(9A) 	1.534(8)

C(2A)-C(13A) 	1.376(12)

C(2A)-C(3A) 	1.444(13)

C(3A)-C(8A) 	1.384(10)

C(3A)-C(4A) 	1.422(12)

C(4A)-C(5A) 	1.344(17)

C(4A)-H(4A) 	0.9500

C(5A)-C(6A) 	1.392(15)

C(5A)-H(5A) 	0.9500

C(6A)-C(7A) 	1.422(9)

C(6A)-H(6A) 	0.9500

C(7A)-C(8A) 	1.3829

C(7A)-H(7A) 	0.9500

C(8A)-C(9A) 	1.5298

C(9A)-O(9A) 	1.3409

C(9A)-C(14A) 	1.560(8)

O(9A)-H(9A) 	0.8400

C(10A)-C(11A) 	1.437(10)

C(10A)-H(10A) 	0.9503

C(11A)-C(12A) 	1.394(17)

C(11A)-H(11A) 	0.9500

C(12A)-C(13A) 	1.364(17)

C(12A)-H(12A) 	0.9500

C(13A)-H(13A) 	0.9500

C(1B)-C(10B) 	1.383(17)

C(1B)-C(2B) 	1.408(17)

C(1B)-C(9B) 	1.543(16)

C(1B)-H(10A) 	1.4703

C(2B)-C(13B) 	1.39(2)

C(2B)-C(3B) 	1.43(2)

C(3B)-C(8B) 	1.392(19)

C(3B)-C(4B) 	1.429(18)

C(4B)-C(5B) 	1.34(2)

C(4B)-H(4B) 	0.9500

C(5B)-C(6B) 	1.39(2)

C(5B)-H(5B) 	0.9500

C(6B)-C(7B) 	1.409(18)

C(6B)-H(6B) 	0.9500

C(7B)-C(8B) 	1.376(16)

C(7B)-H(7B) 	0.9500

C(8B)-C(9B) 	1.524(16)

C(9B)-C(14A) 	1.44(2)

C(9B)-O(9B) 	1.474(16)

C(10B)-C(11B) 	1.427(17)

C(10B)-H(10A) 	0.3159

C(10B)-H(10B) 	0.9500

C(11B)-C(12B) 	1.41(2)

C(11B)-H(10A) 	1.5834

C(11B)-H(11B) 	0.9500

C(12B)-C(13B) 	1.36(3)

C(12B)-H(12B) 	0.9500

C(13B)-H(13B) 	0.9500

C(14A)-C(15A) 	1.340(7)

C(16A)-H(16A) 	1.02(5)

C(16A)-H(14A) 	0.90(6)

C(16A)-H(15A) 	0.98(5)

C(17A)-H(19A) 	0.88(5)

C(17A)-H(18A) 	0.96(7)

C(17A)-H(17A) 	0.94(6)

C(18A)-C(19A) 	1.461(9)

C(18A)-H(21A) 	0.94(5)

C(18A)-H(20A) 	1.04(7)

C(19A)-O(19A) 	1.378(8)

C(19A)-C(20A) 	1.430(10)

C(19A)-H(22A) 	1.0000

O(19A)-H(23A) 	0.63(7)

C(20A)-H(26A) 	0.98(4)

C(20A)-H(24A) 	1.08(12)

C(20A)-H(25A) 	0.91(7)

C(21A)-O(21A) 	1.132(6)

C(22A)-O(22A) 	1.142(6)

C(23A)-O(23A) 	1.137(7)

C(24A)-O(24A) 	1.136(6)

C(25A)-O(25A) 	1.137(6)

C(26A)-O(26A) 	1.139(8)

C(21)-Co(1)-C(22)	99.2(3)

C(21)-Co(1)-C(23)	101.3(3)

C(22)-Co(1)-C(23)	103.4(3)

C(21)-Co(1)-C(14)	105.3(3)

C(22)-Co(1)-C(14)	102.1(3)

C(23)-Co(1)-C(14)	139.3(3)

C(21)-Co(1)-C(15)	97.7(3)

C(22)-Co(1)-C(15)	141.1(3)

C(23)-Co(1)-C(15)	107.3(3)

C(14)-Co(1)-C(15)	39.3(2)

C(21)-Co(1)-Co(2)	150.0(2)

C(22)-Co(1)-Co(2)	104.03(19)

C(23)-Co(1)-Co(2)	91.6(2)

C(14)-Co(1)-Co(2)	51.42(15)

C(15)-Co(1)-Co(2)	52.43(15)

C(26)-Co(2)-C(24)	99.4(3)

C(26)-Co(2)-C(25)	101.0(3)

C(24)-Co(2)-C(25)	101.4(3)

C(26)-Co(2)-C(14)	97.2(3)

C(24)-Co(2)-C(14)	109.8(2)

C(25)-Co(2)-C(14)	140.6(2)

C(26)-Co(2)-C(15)	104.4(2)

C(24)-Co(2)-C(15)	142.2(2)

C(25)-Co(2)-C(15)	102.4(2)

C(14)-Co(2)-C(15)	38.83(19)

C(26)-Co(2)-Co(1)	147.60(19)

C(24)-Co(2)-Co(1)	93.77(19)

C(25)-Co(2)-Co(1)	105.2(2)

C(14)-Co(2)-Co(1)	50.41(16)

C(15)-Co(2)-Co(1)	51.64(16)

C(16)-Si(1)-C(18)	111.5(4)

C(16)-Si(1)-C(15)	111.7(3)

C(18)-Si(1)-C(15)	108.4(3)

C(16)-Si(1)-C(17)	107.6(4)

C(18)-Si(1)-C(17)	109.0(4)

C(15)-Si(1)-C(17)	108.6(3)

C(10)-C(1)-C(2)	121.0(6)

C(10)-C(1)-C(9)	128.6(6)

C(2)-C(1)-C(9)	110.4(5)

C(13)-C(2)-C(1)	119.9(6)

C(13)-C(2)-C(3)	131.3(6)

C(1)-C(2)-C(3)	108.8(5)

C(4)-C(3)-C(8)	119.3(6)

C(4)-C(3)-C(2)	132.0(6)

C(8)-C(3)-C(2)	108.6(5)

C(5)-C(4)-C(3)	119.1(6)

C(5)-C(4)-H(4)	126(3)

C(3)-C(4)-H(4)	115(3)

C(4)-C(5)-C(6)	121.5(6)

C(4)-C(5)-H(5C)	119.3

C(6)-C(5)-H(5C)	119.3

C(5)-C(6)-C(7)	120.4(6)

C(5)-C(6)-H(6)	125(4)

C(7)-C(6)-H(6)	114(4)

C(8)-C(7)-C(6)	118.1(6)

C(8)-C(7)-H(7)	121(3)

C(6)-C(7)-H(7)	121(3)

C(7)-C(8)-C(3)	121.5(5)

C(7)-C(8)-C(9)	128.2(5)

C(3)-C(8)-C(9)	110.2(5)

O(9)-C(9)-C(14)	109.6(4)

O(9)-C(9)-C(1)	109.2(4)

C(14)-C(9)-C(1)	113.0(5)

O(9)-C(9)-C(8)	113.3(4)

C(14)-C(9)-C(8)	110.1(4)

C(1)-C(9)-C(8)	101.5(5)

C(9)-O(9)-H(9)	117(3)

C(1)-C(10)-C(11)	118.7(6)

C(1)-C(10)-H(10)	119(3)

C(11)-C(10)-H(10)	122(3)

C(12)-C(11)-C(10)	120.2(6)

C(12)-C(11)-H(11)	121(4)

C(10)-C(11)-H(11)	119(4)

C(13)-C(12)-C(11)	121.3(7)

C(13)-C(12)-H(12)	121(3)

C(11)-C(12)-H(12)	117(3)

C(12)-C(13)-C(2)	118.7(7)

C(12)-C(13)-H(13)	124(3)

C(2)-C(13)-H(13)	117(3)

C(15)-C(14)-C(9)	141.7(5)

C(15)-C(14)-Co(1)	72.5(4)

C(9)-C(14)-Co(1)	134.3(4)

C(15)-C(14)-Co(2)	72.4(3)

C(9)-C(14)-Co(2)	131.3(4)

Co(1)-C(14)-Co(2)	78.2(2)

C(14)-C(15)-Si(1)	155.0(5)

C(14)-C(15)-Co(1)	68.2(3)

Si(1)-C(15)-Co(1)	129.8(3)

C(14)-C(15)-Co(2)	68.7(3)

Si(1)-C(15)-Co(2)	127.8(3)

Co(1)-C(15)-Co(2)	75.93(19)

Si(1)-C(16)-H(14)	110(3)

Si(1)-C(16)-H(16)	110(4)

H(14)-C(16)-H(16)	107(5)

Si(1)-C(16)-H(15)	113(5)

H(14)-C(16)-H(15)	115(6)

H(16)-C(16)-H(15)	101(6)

Si(1)-C(17)-H(18)	101(4)

Si(1)-C(17)-H(17)	112(6)

H(18)-C(17)-H(17)	123(8)

Si(1)-C(17)-H(19)	109(4)

H(18)-C(17)-H(19)	99(5)

H(17)-C(17)-H(19)	112(7)

C(19)-C(18)-Si(1)	118.5(5)

C(19)-C(18)-H(21)	111(3)

Si(1)-C(18)-H(21)	110(3)

C(19)-C(18)-H(20)	105(4)

Si(1)-C(18)-H(20)	108(4)

H(21)-C(18)-H(20)	103(5)

O(19)-C(19)-C(18)	108.6(6)

O(19)-C(19)-C(20)	111.5(7)

C(18)-C(19)-C(20)	115.1(7)

O(19)-C(19)-H(22)	105(4)

C(18)-C(19)-H(22)	109(4)

C(20)-C(19)-H(22)	107(4)

C(19)-O(19)-H(23)	117(5)

C(19)-C(20)-H(24)	105(4)

C(19)-C(20)-H(26)	118(4)

H(24)-C(20)-H(26)	102(5)

C(19)-C(20)-H(25)	109(4)

H(24)-C(20)-H(25)	106(5)

H(26)-C(20)-H(25)	116(6)

O(21)-C(21)-Co(1)	179.2(6)

O(22)-C(22)-Co(1)	178.0(6)

O(23)-C(23)-Co(1)	176.5(6)

O(24)-C(24)-Co(2)	176.5(6)

O(25)-C(25)-Co(2)	176.9(6)

O(26)-C(26)-Co(2)	179.4(7)

C(26A)-Co(1A)-C(24A)	99.8(3)

C(26A)-Co(1A)-C(25A)	97.8(3)

C(24A)-Co(1A)-C(25A)	102.6(3)

C(26A)-Co(1A)-C(14A)	100.1(3)

C(24A)-Co(1A)-C(14A)	107.5(3)

C(25A)-Co(1A)-C(14A)	141.5(2)

C(26A)-Co(1A)-C(15A)	103.8(3)

C(24A)-Co(1A)-C(15A)	142.0(3)

C(25A)-Co(1A)-C(15A)	103.1(2)

C(14A)-Co(1A)-C(15A)	39.32(19)

C(26A)-Co(1A)-Co(2A)	150.1(2)

C(24A)-Co(1A)-Co(2A)	94.6(2)

C(25A)-Co(1A)-Co(2A)	104.4(2)

C(14A)-Co(1A)-Co(2A)	50.35(17)

C(15A)-Co(1A)-Co(2A)	51.99(16)

C(23A)-Co(2A)-C(22A)	99.1(3)

C(23A)-Co(2A)-C(21A)	99.1(3)

C(22A)-Co(2A)-C(21A)	105.3(3)

C(23A)-Co(2A)-C(14A)	105.6(3)

C(22A)-Co(2A)-C(14A)	141.0(3)

C(21A)-Co(2A)-C(14A)	100.1(3)

C(23A)-Co(2A)-C(15A)	98.9(3)

C(22A)-Co(2A)-C(15A)	107.5(3)

C(21A)-Co(2A)-C(15A)	139.3(3)

C(14A)-Co(2A)-C(15A)	39.7(2)

C(23A)-Co(2A)-Co(1A)	150.8(2)

C(22A)-Co(2A)-Co(1A)	93.6(2)

C(21A)-Co(2A)-Co(1A)	102.7(2)

C(14A)-Co(2A)-Co(1A)	51.63(16)

C(15A)-Co(2A)-Co(1A)	52.02(15)

C(15A)-Si(1A)-C(17A)	108.8(3)

C(15A)-Si(1A)-C(16A)	110.8(3)

C(17A)-Si(1A)-C(16A)	108.1(4)

C(15A)-Si(1A)-C(18A)	109.6(3)

C(17A)-Si(1A)-C(18A)	108.0(4)

C(16A)-Si(1A)-C(18A)	111.5(4)

C(10A)-C(1A)-C(2A)	122.8(7)

C(10A)-C(1A)-C(9A)	127.6(6)

C(2A)-C(1A)-C(9A)	109.5(7)

C(13A)-C(2A)-C(1A)	118.7(10)

C(13A)-C(2A)-C(3A)	132.8(10)

C(1A)-C(2A)-C(3A)	108.4(9)

C(8A)-C(3A)-C(4A)	119.1(10)

C(8A)-C(3A)-C(2A)	110.4(7)

C(4A)-C(3A)-C(2A)	130.1(10)

C(5A)-C(4A)-C(3A)	118.2(12)

C(5A)-C(4A)-H(4A)	120.9

C(3A)-C(4A)-H(4A)	120.9

C(4A)-C(5A)-C(6A)	123.2(11)

C(4A)-C(5A)-H(5A)	118.4

C(6A)-C(5A)-H(5A)	118.4

C(5A)-C(6A)-C(7A)	119.1(10)

C(5A)-C(6A)-H(6A)	120.4

C(7A)-C(6A)-H(6A)	120.4

C(8A)-C(7A)-C(6A)	117.1(5)

C(8A)-C(7A)-H(7A)	121.5

C(6A)-C(7A)-H(7A)	121.5

C(7A)-C(8A)-C(3A)	122.8(5)

C(7A)-C(8A)-C(9A)	127.4

C(3A)-C(8A)-C(9A)	109.7(5)

O(9A)-C(9A)-C(8A)	105.8

O(9A)-C(9A)-C(1A)	116.7(5)

C(8A)-C(9A)-C(1A)	101.6(3)

O(9A)-C(9A)-C(14A)	112.1(3)

C(8A)-C(9A)-C(14A)	114.6(3)

C(1A)-C(9A)-C(14A)	105.9(6)

C(1A)-C(10A)-C(11A)	117.8(7)

C(1A)-C(10A)-H(10A)	121.0

C(11A)-C(10A)-H(10A)	121.2

C(12A)-C(11A)-C(10A)	117.4(10)

C(12A)-C(11A)-H(11A)	121.3

C(10A)-C(11A)-H(11A)	121.3

C(13A)-C(12A)-C(11A)	124.0(11)

C(13A)-C(12A)-H(12A)	118.0

C(11A)-C(12A)-H(12A)	118.0

C(12A)-C(13A)-C(2A)	119.3(11)

C(12A)-C(13A)-H(13A)	120.3

C(2A)-C(13A)-H(13A)	120.3

C(10B)-C(1B)-C(2B)	123.7(16)

C(10B)-C(1B)-C(9B)	126.0(15)

C(2B)-C(1B)-C(9B)	110.0(14)

C(10B)-C(1B)-H(10A)	12.2

C(2B)-C(1B)-H(10A)	130.5

C(9B)-C(1B)-H(10A)	119.2

C(13B)-C(2B)-C(1B)	117.6(19)

C(13B)-C(2B)-C(3B)	133(2)

C(1B)-C(2B)-C(3B)	108.7(16)

C(8B)-C(3B)-C(2B)	109.8(15)

C(8B)-C(3B)-C(4B)	120.4(19)

C(2B)-C(3B)-C(4B)	130(2)

C(5B)-C(4B)-C(3B)	118(2)

C(5B)-C(4B)-H(4B)	120.8

C(3B)-C(4B)-H(4B)	120.8

C(4B)-C(5B)-C(6B)	121(2)

C(4B)-C(5B)-H(5B)	119.4

C(6B)-C(5B)-H(5B)	119.4

C(5B)-C(6B)-C(7B)	121(2)

C(5B)-C(6B)-H(6B)	119.4

C(7B)-C(6B)-H(6B)	119.4

C(8B)-C(7B)-C(6B)	117.9(18)

C(8B)-C(7B)-H(7B)	121.1

C(6B)-C(7B)-H(7B)	121.1

C(7B)-C(8B)-C(3B)	120.7(16)

C(7B)-C(8B)-C(9B)	128.0(17)

C(3B)-C(8B)-C(9B)	110.7(14)

C(14A)-C(9B)-O(9B)	109.2(13)

C(14A)-C(9B)-C(8B)	112.2(15)

O(9B)-C(9B)-C(8B)	112.3(17)

C(14A)-C(9B)-C(1B)	114(2)

O(9B)-C(9B)-C(1B)	109.1(17)

C(8B)-C(9B)-C(1B)	100.1(13)

C(1B)-C(10B)-C(11B)	117.0(17)

C(1B)-C(10B)-H(10A)	99.9

C(11B)-C(10B)-H(10A)	114.4

C(1B)-C(10B)-H(10B)	121.5

C(11B)-C(10B)-H(10B)	121.5

H(10A)-C(10B)-H(10B)	56.1

C(12B)-C(11B)-C(10B)	118.8(19)

C(12B)-C(11B)-H(10A)	123.6

C(10B)-C(11B)-H(10A)	10.5

C(12B)-C(11B)-H(11B)	120.6

C(10B)-C(11B)-H(11B)	120.6

H(10A)-C(11B)-H(11B)	115.0

C(13B)-C(12B)-C(11B)	122(2)

C(13B)-C(12B)-H(12B)	119.1

C(11B)-C(12B)-H(12B)	119.1

C(12B)-C(13B)-C(2B)	120(2)

C(12B)-C(13B)-H(13B)	119.9

C(2B)-C(13B)-H(13B)	119.9

C(15A)-C(14A)-C(9B)	135.7(8)

C(15A)-C(14A)-C(9A)	139.0(5)

C(9B)-C(14A)-C(9A)	10.9(9)

C(15A)-C(14A)-Co(2A)	72.6(4)

C(9B)-C(14A)-Co(2A)	130.4(9)

C(9A)-C(14A)-Co(2A)	138.1(4)

C(15A)-C(14A)-Co(1A)	71.4(3)

C(9B)-C(14A)-Co(1A)	141.3(9)

C(9A)-C(14A)-Co(1A)	130.5(4)

Co(2A)-C(14A)-Co(1A)	78.0(2)

C(14A)-C(15A)-Si(1A)	153.0(5)

C(14A)-C(15A)-Co(2A)	67.7(3)

Si(1A)-C(15A)-Co(2A)	131.0(3)

C(14A)-C(15A)-Co(1A)	69.2(3)

Si(1A)-C(15A)-Co(1A)	129.2(3)

Co(2A)-C(15A)-Co(1A)	75.98(18)

Si(1A)-C(16A)-H(16A)	101(3)

Si(1A)-C(16A)-H(14A)	120(4)

H(16A)-C(16A)-H(14A)	108(6)

Si(1A)-C(16A)-H(15A)	99(3)

H(16A)-C(16A)-H(15A)	117(5)

H(14A)-C(16A)-H(15A)	112(6)

Si(1A)-C(17A)-H(19A)	107(4)

Si(1A)-C(17A)-H(18A)	112(5)

H(19A)-C(17A)-H(18A)	96(5)

Si(1A)-C(17A)-H(17A)	110(4)

H(19A)-C(17A)-H(17A)	113(5)

H(18A)-C(17A)-H(17A)	118(6)

C(19A)-C(18A)-Si(1A)	121.5(5)

C(19A)-C(18A)-H(21A)	113(4)

Si(1A)-C(18A)-H(21A)	107(4)

C(19A)-C(18A)-H(20A)	112(4)

Si(1A)-C(18A)-H(20A)	107(4)

H(21A)-C(18A)-H(20A)	93(5)

O(19A)-C(19A)-C(20A)	118.3(7)

O(19A)-C(19A)-C(18A)	114.9(7)

C(20A)-C(19A)-C(18A)	119.7(7)

O(19A)-C(19A)-H(22A)	98.9

C(20A)-C(19A)-H(22A)	98.9

C(18A)-C(19A)-H(22A)	98.9

C(19A)-O(19A)-H(23A)	110(8)

C(19A)-C(20A)-H(26A)	117(3)

C(19A)-C(20A)-H(24A)	106(7)

H(26A)-C(20A)-H(24A)	98(7)

C(19A)-C(20A)-H(25A)	114(5)

H(26A)-C(20A)-H(25A)	113(5)

H(24A)-C(20A)-H(25A)	107(8)

O(21A)-C(21A)-Co(2A)	177.2(6)

O(22A)-C(22A)-Co(2A)	177.9(6)

O(23A)-C(23A)-Co(2A)	178.7(7)

O(24A)-C(24A)-Co(1A)	177.9(8)

O(25A)-C(25A)-Co(1A)	177.8(6)

O(26A)-C(26A)-Co(1A)	177.7(7)

______________________________________________________________________________________

Table C4:  Anisotropic displacement parameters (Å2 x 103) for 42.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	32(1) 	31(1)	27(1) 	-2(1)	4(1) 	0(1)

Co(2)	24(1) 	31(1)	35(1) 	-2(1)	9(1) 	1(1)

Si(1)	34(1) 	29(1)	36(1) 	-1(1)	13(1) 	-1(1)

C(1)	22(4) 	27(3)	19(4) 	0(3)	-2(3) 	-2(3)

C(2)	24(4) 	32(4)	23(4) 	3(3)	3(3) 	-6(3)

C(3)	26(4) 	38(4)	25(4) 	-4(3)	10(3) 	6(3)

C(4)	29(5) 	59(5)	32(5) 	2(4)	14(4) 	-4(4)

C(5)	38(5) 	50(5)	56(6) 	-18(4)	16(4) 	12(4)

C(6)	37(5) 	45(5)	45(5) 	-6(4)	9(4) 	5(4)

C(7)	26(4) 	42(4)	40(5) 	-2(4)	13(4) 	3(3)

C(8)	23(4) 	28(4)	28(4) 	-13(3)	7(3) 	0(3)

C(9)	25(4) 	35(4)	11(4) 	-5(3)	6(3) 	4(3)

O(9)	28(3) 	39(3)	23(3) 	4(2)	11(2) 	-1(2)

C(10)	21(4) 	31(4)	42(5) 	5(4)	8(4) 	-1(3)

C(11)	31(5) 	36(4)	47(6) 	-6(4)	1(4) 	-7(4)

C(12)	34(5) 	38(4)	47(6) 	21(4)	2(4) 	-14(4)

C(13)	14(4) 	62(5)	38(5) 	2(4)	1(4) 	-1(4)

C(14)	27(4) 	23(3)	25(4) 	3(3)	8(3) 	4(3)

C(15)	22(4) 	28(3)	21(4) 	-1(3)	4(3) 	7(3)

C(16)	72(7) 	27(4)	68(8) 	-7(5)	32(6) 	-1(4)

C(17)	54(6) 	43(5)	55(7) 	-6(5)	17(5) 	-21(4)

C(18)	30(5) 	43(5)	43(5) 	5(4)	14(4) 	-4(4)

C(19)	33(5) 	98(7)	32(5) 	-1(5)	17(4) 	-9(5)

O(19)	23(3) 	77(4)	32(4) 	16(3)	5(3) 	-3(3)

C(20)	51(6) 	67(6)	29(6) 	-5(5)	8(5) 	-1(5)

C(21)	48(5) 	47(4)	27(5) 	-5(4)	-1(4) 	3(4)

O(21)	97(4) 	52(3)	66(4) 	-15(3)	20(3) 	25(3)

C(22)	31(4) 	41(4)	24(4) 	0(3)	0(4) 	9(3)

O(22)	64(4) 	65(3)	43(4) 	20(3)	14(3) 	-1(3)

C(23)	50(5) 	31(4)	38(5) 	-6(3)	-4(4) 	1(4)

O(23)	45(3) 	55(3)	68(4) 	-2(3)	-19(3) 	-10(3)

C(24)	23(4) 	46(4)	25(4) 	-5(4)	1(3) 	6(3)

O(24)	57(3) 	45(3)	55(4) 	13(3)	12(3) 	11(3)

C(25)	47(5) 	37(4)	59(6) 	-12(4)	12(5) 	-6(4)

O(25)	26(3) 	67(3)	147(6) 	-20(3)	29(4) 	-13(3)

C(26)	27(4) 	42(4)	47(5) 	-5(4)	15(4) 	6(3)

O(26)	56(4) 	90(4)	39(4) 	-21(3)	8(3) 	19(3)

Co(1A)	27(1) 	30(1)	43(1) 	-6(1)	10(1) 	1(1)

Co(2A)	29(1) 	35(1)	38(1) 	10(1)	10(1) 	4(1)

Si(1A)	32(1) 	27(1)	31(1) 	0(1)	7(1) 	-3(1)

C(1A)	12(5) 	52(6)	22(5) 	-3(6)	-9(4) 	-9(6)

C(2A)	15(6) 	60(6)	40(7) 	7(5)	-5(5) 	-7(6)

C(3A)	22(6) 	45(5)	65(8) 	14(5)	7(6) 	-2(5)

C(4A)	36(7) 	48(6)	139(11) 	13(5)	30(8) 	-8(5)

C(5A)	65(8) 	34(5)	213(15) 	-1(6)	65(10) 	1(6)

C(6A)	35(7) 	56(5)	122(9) 	-39(6)	-3(7) 	-9(5)

C(7A)	28(5) 	52(5)	88(8) 	-30(6)	19(7) 	-1(4)

C(8A)	13(4) 	40(4)	56(9) 	-6(4)	6(6) 	7(4)

C(9A)	30(4) 	22(4)	28(6) 	-1(4)	11(4) 	-1(3)

O(9A)	28(3) 	58(3)	31(3) 	-2(2)	1(2) 	-12(2)

C(10A)	28(5) 	60(5)	40(7) 	-17(6)	7(4) 	-2(6)

C(11A)	39(8) 	101(7)	40(8) 	-20(7)	5(5) 	6(7)

C(12A)	26(10) 	135(7)	36(7) 	-3(7)	12(6) 	8(7)

C(13A)	39(7) 	116(6)	43(8) 	20(6)	8(5) 	-9(7)

C(1B)	12(5) 	52(6)	22(5) 	-3(6)	-9(4) 	-9(6)

C(2B)	15(6) 	60(6)	40(7) 	7(5)	-5(5) 	-7(6)

C(3B)	22(6) 	45(5)	65(8) 	14(5)	7(6) 	-2(5)

C(4B)	36(7) 	48(6)	139(11) 	13(5)	30(8) 	-8(5)

C(5B)	65(8) 	34(5)	213(15) 	-1(6)	65(10) 	1(6)

C(6B)	35(7) 	56(5)	122(9) 	-39(6)	-3(7) 	-9(5)

C(7B)	28(5) 	52(5)	88(8) 	-30(6)	19(7) 	-1(4)

C(8B)	13(4) 	40(4)	56(9) 	-6(4)	6(6) 	7(4)

C(9B)	30(4) 	22(4)	28(6) 	-1(4)	11(4) 	-1(3)

O(9B)	28(3) 	58(3)	31(3) 	-2(2)	1(2) 	-12(2)

C(10B)	28(5) 	60(5)	40(7) 	-17(6)	7(4) 	-2(6)

C(11B)	39(8) 	101(7)	40(8) 	-20(7)	5(5) 	6(7)

C(12B)	26(10) 	135(7)	36(7) 	-3(7)	12(6) 	8(7)

C(13B)	39(7) 	116(6)	43(8) 	20(6)	8(5) 	-9(7)

C(14A)	26(4) 	24(3)	32(4) 	-3(3)	9(3) 	4(3)

C(15A)	28(4) 	33(4)	19(4) 	-3(3)	11(3) 	3(3)

C(16A)	73(7) 	46(5)	47(7) 	-13(5)	20(6) 	-3(5)

C(17A)	53(6) 	34(5)	39(6) 	2(5)	-5(5) 	-16(4)

C(18A)	27(5) 	39(4)	35(5) 	10(4)	-2(4) 	-10(4)

C(19A)	29(5) 	149(8)	54(6) 	63(6)	-4(4) 	-19(5)

O(19A)	41(4) 	82(4)	61(5) 	36(3)	-10(4) 	-30(3)

C(20A)	33(6) 	139(10)	59(7) 	58(7)	-12(5) 	-12(6)

C(21A)	42(5) 	52(5)	51(5) 	9(4)	17(4) 	10(4)

O(21A)	76(4) 	41(3)	105(5) 	32(3)	35(4) 	0(3)

C(22A)	44(5) 	43(4)	39(5) 	13(4)	11(4) 	14(4)

O(22A)	34(3) 	88(4)	51(4) 	10(3)	7(3) 	9(3)

C(23A)	34(5) 	53(5)	45(6) 	8(4)	11(4) 	-3(4)

O(23A)	50(4) 	82(4)	48(4) 	-3(3)	19(3) 	-1(3)

C(24A)	41(5) 	45(5)	102(7) 	-14(5)	37(5) 	-5(4)

O(24A)	112(5) 	29(3)	187(7) 	-18(4)	87(5) 	-4(3)

C(25A)	47(5) 	28(4)	37(5) 	-4(3)	12(4) 	4(3)

O(25A)	38(3) 	54(3)	86(4) 	8(3)	33(3) 	0(3)

C(26A)	41(5) 	79(5)	51(6) 	-24(5)	7(5) 	13(4)

O(26A)	81(5) 	170(6)	40(4) 	-30(5)	-5(4) 	36(4)

______________________________________________________________________________

Table C5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 10 3)

for 42.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(4)	1770(20)	6740(40)	6846(19)	27(17)

H(5C)	1628	8996	6624	57

H(6)	2160(30)	9830(50)	6000(20)	80(20)

H(7)	2860	8488	5706	42

H(9)	3210(20)	6150(40)	5238(18)	14(16)

H(10)	3490(30)	3120(40)	5920(19)	36(17)

H(11)	3120(30)	1470(60)	6430(20)	90(30)

H(12)	2440(20)	2030(40)	6978(17)	19(14)

H(13)	2090(20)	4250(40)	6980(17)	8(15)

H(14)	3670(30)	9940(50)	5610(20)	60(20)

H(16)	4350(30)	10750(60)	5800(20)	70(20)

H(15)	4150(40)	10180(60)	6190(30)	80(30)

H(18)	5800(30)	8280(60)	6080(20)	60(30)

H(17)	5610(50)	9030(90)	6520(30)	160(50)

H(19)	5740(30)	9680(60)	6040(30)	90(30)

H(21)	4960(20)	8680(40)	5060(18)	25(17)

H(20)	4820(30)	7270(60)	5140(20)	90(30)

H(22)	3840(40)	9310(80)	4680(30)	160(40)

H(23)	3120(30)	7800(60)	4820(20)	40(20)

H(24)	4030(30)	6640(60)	4330(30)	100(30)

H(26)	3530(30)	7660(50)	3980(20)	60(20)

H(25)	4350(30)	7890(60)	4160(30)	80(30)

H(4A)	2843	12281	3624	88

H(5A)	2702	13566	4275	118

H(6A)	2331	12712	4945	91

H(7A)	1821	10581	4851	67

H(9A)	1871	7436	4517	60

H(10A)	2026	6482	3526	52

H(11A)	2607	6367	2862	73

H(12A)	3057	8293	2630	78

H(13A)	2974	10268	3004	80

H(4B)	2739	11378	3065	88

H(5B)	2637	13208	3527	118

H(6B)	2056	13120	4151	91

H(7B)	1733	11089	4429	67

H(10B)	2018	5984	3759	52

H(11B)	2542	5189	3126	73

H(12B)	3025	6713	2675	78

H(13B)	2776	8906	2690	80

H(16A)	1330(30)	4820(50)	3690(20)	40(20)

H(14A)	880(40)	5020(60)	3140(30)	80(30)

H(15A)	590(30)	3980(60)	3440(20)	60(20)

H(19A)	-650(30)	4850(50)	3510(20)	50(20)

H(18A)	-830(40)	6040(70)	3670(30)	100(30)

H(17A)	-640(30)	5940(50)	3130(20)	60(20)

H(21A)	190(30)	4670(50)	4480(20)	50(20)

H(20A)	290(40)	5990(70)	4650(30)	120(30)

H(22A)	1269	4130	4615	97

H(23A)	1980(40)	5660(80)	4890(30)	70(40)

H(26A)	1740(20)	4150(40)	5483(18)	13(14)

H(24A)	1250(60)	5260(110)	5530(50)	270(80)

H(25A)	950(40)	3850(60)	5310(30)	90(30)

________________________________________________________________________________

Table C6:  Hydrogen bonds for 42 [Å and °].

____________________________________________________________________________

D-H...A	d(D-H)	d(H...A)	d(D...A)	<(DHA)

____________________________________________________________________________

O(9)-H(9)...O(19)	0.87(4)	1.90(4)	2.732(6)	161(4)

O(9A)-H(9A)...O(19A)	0.84	1.91	2.691(7)	154.1

O(19)-H(23)...O(9A)	0.72(5)	2.03(5)	2.740(8)	170(7)

O(19A)-H(23A)...O(9)	0.63(7)	2.22(7)	2.835(8)	166(10)

____________________________________________________________________________

Table D1:  Crystal data and structure refinement for 43.

Empirical formula 	C24 H16 Co2 O8

Formula weight 	550.23

Temperature 	197(2) K

Wavelength 	0.71073 Å

Crystal system 	Tetragonal

Space group 	P-42(1)c

Unit cell dimensions	a = 22.489(5) Å	(= 90°.

b = 22.489(5) Å	(= 90°.

c = 9.846(3) Å	(= 90°.

Volume	4980(2) Å3

Z	8

Density (calculated)	1.468 Mg/m3

Absorption coefficient	1.376 mm-1

F(000)	2224

Crystal size	.02 x .04 x .25 mm3

( range for data collection	1.28 to 24.99°.

Index ranges	-26(h(26, -26(k(26, -11(l(11

Reflections collected	37626

Independent reflections	4385 [R(int) = 0.1088]

Completeness to ( = 24.99°	100.0 %

Absorption correction	Empirical (SADABS)

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4385 / 0 / 372

Goodness-of-fit on F2	1.077

Final R indices [I>2((I)]	R1 = 0.0394, wR2 = 0.0686

R indices (all data)	R1 = 0.0856, wR2 = 0.0835

Absolute structure parameter	0.00(2)

Extinction coefficient	0.00036(7)

Largest diff. peak and hole	0.328 and -0.311 e.Å-3

Ratio of min/max apparent transmission  	0.866793

Table D2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 43.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	724(1)	7205(1)	2144(1)	30(1)

Co(2)	265(1)	8104(1)	1191(1)	33(1)

C(1)	-788(2)	7540(2)	3755(5)	27(1)

C(2)	-878(2)	6998(2)	4451(5)	28(1)

C(3)	-405(2)	6940(2)	5458(4)	28(1)

C(4)	-303(3)	6508(3)	6443(6)	49(2)

C(5)	171(3)	6582(3)	7345(6)	56(2)

C(6)	532(3)	7075(3)	7266(6)	51(2)

C(7)	430(3)	7506(3)	6284(5)	36(1)

C(8)	-25(2)	7430(2)	5379(4)	27(1)

C(9)	-213(2)	7825(2)	4183(4)	24(1)

O(9)	-296(2)	8433(2)	4552(4)	30(1)

C(10)	-1195(2)	7721(3)	2816(6)	36(1)

C(11)	-1681(2)	7367(3)	2511(6)	45(2)

C(12)	-1753(3)	6831(3)	3176(6)	51(2)

C(13)	-1364(2)	6647(3)	4154(6)	40(2)

C(14)	248(2)	7796(2)	3054(5)	22(1)

C(15)	779(2)	8026(2)	2797(5)	25(1)

C(16)	1234(2)	8419(2)	3467(5)	30(1)

O(16)	906(2)	8741(2)	4491(3)	34(1)

C(17)	1718(3)	8046(3)	4128(7)	49(2)

C(18)	1513(3)	8852(3)	2478(6)	51(2)

C(19)	941(2)	6739(3)	3524(6)	42(2)

O(19)	1068(2)	6417(2)	4371(5)	64(1)

C(20)	216(3)	6665(2)	1430(5)	39(1)

O(20)	-105(2)	6328(2)	989(4)	69(1)

C(21)	1392(3)	7206(3)	1140(7)	57(2)

O(21)	1821(2)	7256(2)	529(6)	104(2)

C(22)	-335(3)	7741(3)	250(5)	40(1)

O(22)	-701(2)	7502(2)	-325(4)	59(1)

C(23)	782(3)	8274(3)	-167(6)	58(2)

O(23)	1103(2)	8375(3)	-1009(5)	101(2)

C(24)	-52(3)	8829(3)	1460(6)	53(2)

O(24)	-246(2)	9287(2)	1632(5)	85(2)

________________________________________________________________________________

Table D3:  Bond lengths [Å] and angles [°] for 43.

______________________________________________________________________________________

Co(1)-C(19) 	1.783(7)

Co(1)-C(21) 	1.800(6)

Co(1)-C(20) 	1.810(6)

Co(1)-C(14) 	1.926(5)

Co(1)-C(15) 	1.959(4)

Co(1)-Co(2) 	2.4559(11)

Co(2)-C(24) 	1.799(7)

Co(2)-C(23) 	1.812(6)

Co(2)-C(22) 	1.829(6)

Co(2)-C(14) 	1.961(5)

Co(2)-C(15) 	1.966(5)

C(1)-C(10) 	1.363(7)

C(1)-C(2) 	1.413(6)

C(1)-C(9) 	1.504(6)

C(2)-C(13) 	1.381(7)

C(2)-C(3) 	1.460(6)

C(3)-C(4) 	1.393(7)

C(3)-C(8) 	1.396(6)

C(4)-C(5) 	1.398(8)

C(5)-C(6) 	1.376(8)

C(6)-C(7) 	1.389(8)

C(7)-C(8) 	1.368(7)

C(8)-C(9) 	1.534(6)

C(9)-O(9) 	1.426(5)

C(9)-C(14) 	1.521(6)

C(10)-C(11) 	1.387(8)

C(11)-C(12) 	1.381(8)

C(12)-C(13) 	1.365(8)

C(14)-C(15) 	1.326(6)

C(15)-C(16) 	1.505(6)

C(16)-O(16) 	1.446(5)

C(16)-C(18) 	1.513(7)

C(16)-C(17) 	1.520(8)

C(19)-O(19) 	1.142(6)

C(20)-O(20) 	1.133(6)

C(21)-O(21) 	1.142(6)

C(22)-O(22) 	1.133(6)

C(23)-O(23) 	1.123(6)

C(24)-O(24) 	1.133(7)

C(19)-Co(1)-C(21)	101.0(3)

C(19)-Co(1)-C(20)	94.3(2)

C(21)-Co(1)-C(20)	108.4(2)

C(19)-Co(1)-C(14)	101.7(2)

C(21)-Co(1)-C(14)	135.9(2)

C(20)-Co(1)-C(14)	107.1(2)

C(19)-Co(1)-C(15)	106.6(2)

C(21)-Co(1)-C(15)	97.2(2)

C(20)-Co(1)-C(15)	143.2(2)

C(14)-Co(1)-C(15)	39.89(17)

C(19)-Co(1)-Co(2)	152.79(16)

C(21)-Co(1)-Co(2)	98.1(2)

C(20)-Co(1)-Co(2)	98.00(17)

C(14)-Co(1)-Co(2)	51.45(14)

C(15)-Co(1)-Co(2)	51.40(14)

C(24)-Co(2)-C(23)	99.8(3)

C(24)-Co(2)-C(22)	100.7(3)

C(23)-Co(2)-C(22)	101.2(2)

C(24)-Co(2)-C(14)	100.1(2)

C(23)-Co(2)-C(14)	141.0(2)

C(22)-Co(2)-C(14)	107.6(2)

C(24)-Co(2)-C(15)	101.3(2)

C(23)-Co(2)-C(15)	103.6(2)

C(22)-Co(2)-C(15)	143.3(2)

C(14)-Co(2)-C(15)	39.46(18)

C(24)-Co(2)-Co(1)	148.9(2)

C(23)-Co(2)-Co(1)	100.8(2)

C(22)-Co(2)-Co(1)	97.84(17)

C(14)-Co(2)-Co(1)	50.20(14)

C(15)-Co(2)-Co(1)	51.15(13)

C(10)-C(1)-C(2)	119.4(5)

C(10)-C(1)-C(9)	129.8(5)

C(2)-C(1)-C(9)	110.7(4)

C(13)-C(2)-C(1)	120.3(5)

C(13)-C(2)-C(3)	132.1(5)

C(1)-C(2)-C(3)	107.6(4)

C(4)-C(3)-C(8)	119.3(5)

C(4)-C(3)-C(2)	130.9(5)

C(8)-C(3)-C(2)	109.7(4)

C(3)-C(4)-C(5)	118.9(6)

C(6)-C(5)-C(4)	120.7(6)

C(5)-C(6)-C(7)	120.3(6)

C(8)-C(7)-C(6)	119.3(6)

C(7)-C(8)-C(3)	121.3(5)

C(7)-C(8)-C(9)	129.3(5)

C(3)-C(8)-C(9)	109.4(4)

O(9)-C(9)-C(1)	111.5(4)

O(9)-C(9)-C(14)	108.5(4)

C(1)-C(9)-C(14)	111.3(4)

O(9)-C(9)-C(8)	113.3(4)

C(1)-C(9)-C(8)	101.9(4)

C(14)-C(9)-C(8)	110.4(4)

C(1)-C(10)-C(11)	120.3(5)

C(12)-C(11)-C(10)	119.4(6)

C(13)-C(12)-C(11)	121.7(6)

C(12)-C(13)-C(2)	118.9(5)

C(15)-C(14)-C(9)	137.4(4)

C(15)-C(14)-Co(1)	71.4(3)

C(9)-C(14)-Co(1)	138.4(3)

C(15)-C(14)-Co(2)	70.5(3)

C(9)-C(14)-Co(2)	132.9(3)

Co(1)-C(14)-Co(2)	78.35(17)

C(14)-C(15)-C(16)	139.3(4)

C(14)-C(15)-Co(1)	68.7(3)

C(16)-C(15)-Co(1)	137.8(3)

C(14)-C(15)-Co(2)	70.1(3)

C(16)-C(15)-Co(2)	134.5(4)

Co(1)-C(15)-Co(2)	77.45(16)

O(16)-C(16)-C(15)	104.6(4)

O(16)-C(16)-C(18)	109.7(4)

C(15)-C(16)-C(18)	112.2(4)

O(16)-C(16)-C(17)	110.1(4)

C(15)-C(16)-C(17)	110.5(4)

C(18)-C(16)-C(17)	109.6(5)

O(19)-C(19)-Co(1)	176.4(5)

O(20)-C(20)-Co(1)	179.6(6)

O(21)-C(21)-Co(1)	174.2(5)

O(22)-C(22)-Co(2)	178.2(5)

O(23)-C(23)-Co(2)	179.5(7)

O(24)-C(24)-Co(2)	179.3(6)

______________________________________________________________________________________

Table D4:  Anisotropic displacement parameters (Å2 x 103) for 43.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	24(1) 	29(1)	37(1) 	-14(1)	2(1) 	-2(1)

Co(2)	32(1) 	35(1)	31(1) 	3(1)	1(1) 	-12(1)

C(1)	19(3) 	27(3)	35(2) 	-4(2)	3(3) 	-3(2)

C(2)	24(3) 	27(3)	33(2) 	11(2)	7(2) 	-1(2)

C(3)	27(3) 	27(3)	29(3) 	-4(2)	3(2) 	-3(3)

C(4)	60(4) 	40(4)	48(4) 	14(3)	1(3) 	-13(4)

C(5)	70(5) 	62(5)	36(3) 	18(3)	-14(3) 	3(4)

C(6)	56(4) 	65(5)	31(3) 	-2(3)	-13(3) 	1(3)

C(7)	44(4) 	33(4)	32(3) 	-9(3)	-6(3) 	-1(3)

C(8)	29(3) 	31(3)	22(2) 	-6(2)	3(2) 	3(3)

C(9)	24(3) 	14(3)	33(3) 	1(2)	1(2) 	2(2)

O(9)	17(2) 	21(2)	52(2) 	-12(2)	7(2) 	1(2)

C(10)	23(3) 	39(4)	47(3) 	13(3)	-2(3) 	-3(3)

C(11)	21(3) 	52(4)	62(4) 	16(3)	-2(3) 	-2(3)

C(12)	26(3) 	57(4)	69(4) 	13(4)	-13(3) 	-25(3)

C(13)	30(4) 	34(4)	56(4) 	14(3)	-3(3) 	-10(3)

C(14)	12(2) 	22(3)	33(2) 	-2(2)	-4(2) 	0(2)

C(15)	23(3) 	22(3)	30(2) 	-9(2)	2(2) 	1(2)

C(16)	21(3) 	30(3)	39(3) 	-14(2)	5(2) 	-7(2)

O(16)	29(2) 	30(2)	44(2) 	-19(2)	8(2) 	-8(2)

C(17)	18(3) 	52(4)	76(5) 	-27(4)	-12(3) 	-5(3)

C(18)	45(4) 	50(4)	58(4) 	-15(4)	14(3) 	-22(4)

C(19)	38(4) 	30(4)	60(4) 	-23(3)	-8(3) 	10(3)

O(19)	70(3) 	44(3)	78(3) 	-5(2)	-29(3) 	26(2)

C(20)	45(4) 	33(3)	39(3) 	-5(3)	-11(3) 	2(3)

O(20)	82(4) 	46(3)	80(3) 	-6(2)	-32(3) 	-28(3)

C(21)	50(4) 	39(4)	82(4) 	-30(4)	26(4) 	0(3)

O(21)	66(3) 	91(4)	155(5) 	-55(4)	75(4) 	-14(3)

C(22)	51(4) 	39(4)	29(3) 	12(3)	-6(3) 	-5(3)

O(22)	59(3) 	63(3)	54(2) 	4(2)	-28(2) 	-18(3)

C(23)	70(5) 	64(5)	41(3) 	0(3)	9(3) 	-31(4)

O(23)	113(5) 	126(5)	64(3) 	-4(3)	39(3) 	-64(4)

C(24)	53(4) 	43(4)	63(4) 	10(4)	-13(3) 	-6(3)

O(24)	89(4) 	43(3)	122(4) 	8(3)	-6(3) 	15(3)

______________________________________________________________________________

Table D5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 10 3)

for 43.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(4)	-541(19)	6200(20)	6480(40)	21(14)

H(5)	260(30)	6350(30)	8090(60)	90(20)

H(6)	830(20)	7150(20)	7980(50)	56(17)

H(7)	641(18)	7824(19)	6280(40)	16(13)

H(9)	0(19)	8539(19)	4700(40)	0(14)

H(10)	-1170(20)	8070(20)	2470(40)	35(16)

H(11)	-1960(20)	7520(20)	1870(40)	37(15)

H(12)	-2070(20)	6650(20)	2870(50)	43(16)

H(13)	-1350(20)	6300(30)	4610(50)	55(18)

H(16)	1120(30)	9010(30)	5070(80)	120(30)

H(17A)	1930(20)	7760(30)	3310(50)	63(17)

H(17B)	2050(20)	8280(20)	4570(50)	60(18)

H(17C)	1550(30)	7760(30)	4670(60)	70(20)

H(18A)	1840(20)	9120(20)	2910(50)	47(14)

H(18B)	1740(30)	8610(30)	1670(60)	70(20)

H(18C)	1240(30)	9170(30)	2090(60)	60(20)

________________________________________________________________________________

Table D6:  Hydrogen bonds for 43 [Å and °].

____________________________________________________________________________

D-H...A	d(D-H)	d(H...A)	d(D...A)	<(DHA)

____________________________________________________________________________

O(9)-H(9)...O(16)	0.72(4)	2.10(4)	2.790(5)	161(5)

____________________________________________________________________________

Table E1:  Crystal data and structure refinement for 77.

Empirical formula 	C21 H19 Co3 O10

Formula weight 	608.15

Temperature 	299(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P1

Unit cell dimensions	a = 7.761(4) Å	(= 90.486(14)°.

b = 12.739(7) Å	(= 106.479(12)°.

c = 13.332(8) Å	(= 91.064(18)°.

Volume	1263.6(13) Å3

Z	2

Density (calculated)	1.598 Mg/m3

Absorption coefficient	1.996 mm-1

F(000)	612

Crystal size	.03 x 0.1 x .17 mm3

( range for data collection	1.59 to 25.00°.

Index ranges	-9(h(8, -15(k(15, -15(l(15

Reflections collected	9539

Independent reflections	6746 [R(int) = 0.0656]

Completeness to ( = 25.00°	99.6 %

Absorption correction	Empirical (SADABS)

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6746 / 69 / 425

Goodness-of-fit on F2	0.988

Final R indices [I>2((I)]	R1 = 0.0567, wR2 = 0.0872

R indices (all data)	R1 = 0.1439, wR2 = 0.1105

Absolute structure parameter	0.08(4)

Largest diff. peak and hole	0.492 and -0.424 e.Å-3

Ratio of min/max apparent transmission  	0.892549

Table E2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 77.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1A)	7365(4)	6609(2)	8596(2)	42(1)

Co(2A)	5101(4)	7277(2)	9394(2)	40(1)

Co(3A)	7000(4)	8518(2)	8752(2)	46(1)

C(1A)	2752(17)	7918(9)	5053(11)	110(20)

O(2A)	5850(20)	8266(13)	6149(11)	35(6)

C(2A)	4319(17)	7535(9)	5988(9)	50(30)

C(3A)	4700(20)	6433(10)	5613(13)	40(8)

C(4A)	3240(30)	6277(10)	4578(13)	63(12)

C(5A)	1440(30)	6156(14)	4833(16)	60(12)

C(6A)	1051(16)	7287(16)	5083(16)	36(14)

C(7A)	3130(20)	7375(13)	4087(9)	80(30)

C(8A)	2530(30)	9106(10)	5025(18)	87(16)

C(9A)	1590(30)	7470(19)	3063(11)	130(40)

C(10A)	4860(30)	7720(20)	3825(11)	83(16)

C(1B)	2492(10)	7713(7)	5009(7)	45(7)

O(2B)	5085(19)	8683(8)	6169(8)	71(5)

C(2B)	4205(12)	7645(7)	5965(6)	49(18)

C(3B)	5345(12)	6828(9)	5591(8)	47(6)

C(4B)	4116(15)	6459(7)	4532(8)	63(6)

C(5B)	2560(20)	5828(6)	4739(10)	60(8)

C(6B)	1387(13)	6689(11)	4990(9)	57(6)

C(7B)	3228(13)	7485(7)	4058(6)	53(16)

C(8B)	1437(19)	8715(11)	4991(11)	71(9)

C(9B)	1746(18)	7317(11)	3011(7)	70(13)

C(10B)	4562(19)	8302(11)	3845(8)	117(13)

C(11A)	3750(30)	7448(15)	7020(17)	43(2)

C(12A)	5360(30)	7444(17)	8034(18)	40(2)

O(13A)	7060(30)	7174(16)	11628(14)	85(2)

C(13A)	6320(30)	7215(17)	10768(18)	48(7)

O(14A)	9500(30)	8998(13)	10860(13)	77(2)

C(14A)	8650(40)	8852(19)	10000(20)	56(2)

O(15A)	10240(20)	6227(14)	10533(15)	81(6)

C(15A)	9120(30)	6405(17)	9774(19)	61(8)

O(16A)	9270(20)	9175(14)	7434(14)	89(6)

C(16A)	8370(30)	8899(18)	7900(20)	55(7)

O(17A)	4560(30)	10323(15)	8270(19)	161(10)

C(17A)	5530(40)	9596(16)	8451(19)	82(10)

O(18A)	2760(20)	5402(11)	9055(14)	76(6)

C(18A)	3690(40)	6119(19)	9250(20)	56(2)

O(19A)	5760(20)	4549(11)	7998(14)	88(7)

C(19A)	6340(30)	5316(14)	8264(18)	40(6)

O(20A)	2350(30)	8774(15)	9455(19)	110(2)

C(20A)	3470(40)	8190(20)	9460(20)	61(2)

O(21A)	9500(30)	6599(16)	7151(16)	103(2)

C(21A)	8730(40)	6624(19)	7790(20)	62(3)

Co(1C)	2590(4)	3387(2)	1359(2)	42(1)

Co(2C)	4898(4)	2722(2)	604(2)	45(1)

Co(3C)	3072(4)	1488(2)	1299(2)	46(1)

C(1C)	7376(13)	2804(6)	5030(8)	27(7)

O(2C)	4417(19)	3351(12)	3927(9)	84(6)

C(2C)	5782(14)	2549(8)	4034(7)	31(14)

C(3C)	5122(18)	1451(9)	4273(9)	48(7)

C(4C)	6481(19)	1170(7)	5304(9)	66(7)

C(5C)	8280(20)	986(9)	5075(11)	74(9)

C(6C)	8944(12)	2105(13)	4964(10)	57(7)

C(7C)	6803(13)	2225(9)	5913(7)	63(14)

C(8C)	7860(30)	3971(7)	5194(12)	82(11)

C(9C)	8299(19)	2191(12)	6963(7)	57(13)

C(10C)	5124(18)	2631(17)	6175(9)	128(14)

C(1D)	7057(16)	2855(8)	5095(10)	89(18)

O(2D)	3927(16)	2832(13)	3970(10)	38(6)

C(2D)	5718(16)	2432(8)	4054(8)	80(30)

C(3D)	5820(20)	1228(8)	4188(12)	34(7)

C(4D)	7290(20)	1101(9)	5218(13)	70(11)

C(5D)	9070(20)	1437(16)	5031(16)	51(10)

C(6D)	8967(15)	2635(15)	5023(15)	80(19)

C(7D)	6915(19)	2004(12)	5902(9)	81(18)

C(8D)	6760(30)	3994(9)	5357(15)	80(13)

C(9D)	8350(30)	2130(18)	6973(10)	160(40)

C(10D)	5100(20)	1890(20)	6142(11)	70(14)

C(11C)	6090(30)	2716(15)	2996(17)	43(2)

C(12C)	4620(30)	2572(17)	2015(18)	40(2)

O(13C)	2920(30)	2735(17)	-1680(14)	85(2)

C(13C)	3680(40)	2730(20)	-830(20)	62(8)

O(14C)	430(30)	973(13)	-733(14)	77(2)

C(14C)	1530(40)	1195(19)	20(20)	56(2)

O(15C)	-270(30)	3617(15)	-636(14)	92(7)

C(15C)	810(30)	3589(14)	100(20)	52(7)

O(16C)	1050(20)	935(14)	2758(16)	92(6)

C(16C)	1880(40)	1150(20)	2170(20)	78(10)

O(17C)	5400(30)	-284(12)	1675(14)	85(6)

C(17C)	4510(30)	359(18)	1525(19)	61(8)

O(18C)	7200(30)	4596(13)	929(15)	107(8)

C(18C)	6310(40)	3881(19)	850(20)	56(2)

O(19C)	4220(30)	5483(13)	1928(15)	91(7)

C(19C)	3520(40)	4620(20)	1720(20)	77(9)

O(20C)	7730(30)	1254(15)	590(19)	110(2)

C(20C)	6630(40)	1840(20)	610(20)	61(2)

O(21C)	280(30)	3470(16)	2779(16)	103(2)

C(21C)	1270(40)	3413(19)	2330(20)	62(3)

________________________________________________________________________________

Table E3:   Bond lengths [Å] and angles [°] for 77.

_____________________________________________________________________________________

Co(1A)-C(21A) 	1.71(3)

Co(1A)-C(15A) 	1.79(2)

Co(1A)-C(19A) 	1.812(18)

Co(1A)-C(12A) 	1.88(2)

Co(1A)-Co(2A) 	2.458(5)

Co(1A)-Co(3A) 	2.467(4)

Co(2A)-C(20A) 	1.76(3)

Co(2A)-C(18A) 	1.80(3)

Co(2A)-C(13A) 	1.81(2)

Co(2A)-C(12A) 	1.89(2)

Co(2A)-Co(3A) 	2.460(5)

Co(3A)-C(17A) 	1.78(3)

Co(3A)-C(16A) 	1.83(3)

Co(3A)-C(14A) 	1.84(3)

Co(3A)-C(12A) 	1.90(2)

C(1A)-C(8A) 	1.5259

C(1A)-C(6A) 	1.5435

C(1A)-C(7A) 	1.5579

C(1A)-C(2A) 	1.5633

O(2A)-C(2A) 	1.4638

C(2A)-C(3A) 	1.5469

C(2A)-C(11A) 	1.56(2)

C(3A)-C(4A) 	1.5267

C(4A)-C(5A) 	1.5310

C(4A)-C(7A) 	1.5435

C(5A)-C(6A) 	1.5301

C(7A)-C(10A) 	1.5386

C(7A)-C(9A) 	1.5463

C(1B)-C(8B) 	1.5259

C(1B)-C(6B) 	1.5435

C(1B)-C(7B) 	1.5579

C(1B)-C(2B) 	1.5633

O(2B)-C(2B) 	1.4638

C(2B)-C(3B) 	1.5469

C(2B)-C(11A) 	1.56(2)

C(3B)-C(4B) 	1.5267

C(4B)-C(5B) 	1.5310

C(4B)-C(7B) 	1.5435

C(5B)-C(6B) 	1.5301

C(7B)-C(10B) 	1.5386

C(7B)-C(9B) 	1.5463

C(11A)-C(12A) 	1.56(3)

O(13A)-C(13A) 	1.13(3)

O(14A)-C(14A) 	1.15(3)

O(15A)-C(15A) 	1.16(2)

O(16A)-C(16A) 	1.11(2)

O(17A)-C(17A) 	1.19(3)

O(18A)-C(18A) 	1.14(2)

O(19A)-C(19A) 	1.082(19)

O(20A)-C(20A) 	1.15(3)

O(21A)-C(21A) 	1.17(3)

Co(1C)-C(19C) 	1.72(3)

Co(1C)-C(21C) 	1.87(3)

Co(1C)-C(15C) 	1.87(3)

Co(1C)-C(12C) 	1.90(2)

Co(1C)-Co(2C) 	2.450(5)

Co(1C)-Co(3C) 	2.460(4)

Co(2C)-C(20C) 	1.76(3)

Co(2C)-C(18C) 	1.79(2)

Co(2C)-C(13C) 	1.88(3)

Co(2C)-C(12C) 	1.97(2)

Co(2C)-Co(3C) 	2.455(5)

Co(3C)-C(16C) 	1.73(3)

Co(3C)-C(17C) 	1.81(2)

Co(3C)-C(14C) 	1.81(3)

Co(3C)-C(12C) 	1.88(2)

C(1C)-C(8C) 	1.5259

C(1C)-C(6C) 	1.5435

C(1C)-C(7C) 	1.5579

C(1C)-C(2C) 	1.5633

O(2C)-C(2C) 	1.4638

C(2C)-C(11C) 	1.49(2)

C(2C)-C(3C) 	1.5469

C(3C)-C(4C) 	1.5267

C(4C)-C(5C) 	1.5310

C(4C)-C(7C) 	1.5435

C(5C)-C(6C) 	1.5301

C(7C)-C(10C) 	1.5386

C(7C)-C(9C) 	1.5463

C(1D)-C(8D) 	1.5259

C(1D)-C(6D) 	1.5435

C(1D)-C(7D) 	1.5579

C(1D)-C(2D) 	1.5633

O(2D)-C(2D) 	1.4638

C(2D)-C(3D) 	1.5469

C(2D)-C(11C) 	1.56(2)

C(3D)-C(4D) 	1.5267

C(4D)-C(5D) 	1.5310

C(4D)-C(7D) 	1.5435

C(5D)-C(6D) 	1.5301

C(7D)-C(10D) 	1.5386

C(7D)-C(9D) 	1.5463

C(11C)-C(12C) 	1.48(3)

O(13C)-C(13C) 	1.12(3)

O(14C)-C(14C) 	1.15(3)

O(15C)-C(15C) 	1.10(3)

O(16C)-C(16C) 	1.18(3)

O(17C)-C(17C) 	1.07(2)

O(18C)-C(18C) 	1.12(2)

O(19C)-C(19C) 	1.21(2)

O(20C)-C(20C) 	1.15(3)

O(21C)-C(21C) 	1.10(3)

C(21A)-Co(1A)-C(15A)	95.8(11)

C(21A)-Co(1A)-C(19A)	99.0(11)

C(15A)-Co(1A)-C(19A)	103.7(11)

C(21A)-Co(1A)-C(12A)	109.6(11)

C(15A)-Co(1A)-C(12A)	141.9(10)

C(19A)-Co(1A)-C(12A)	100.0(10)

C(21A)-Co(1A)-Co(2A)	156.4(9)

C(15A)-Co(1A)-Co(2A)	98.0(8)

C(19A)-Co(1A)-Co(2A)	96.2(7)

C(12A)-Co(1A)-Co(2A)	49.6(8)

C(21A)-Co(1A)-Co(3A)	98.9(8)

C(15A)-Co(1A)-Co(3A)	99.7(7)

C(19A)-Co(1A)-Co(3A)	148.8(7)

C(12A)-Co(1A)-Co(3A)	49.7(7)

Co(2A)-Co(1A)-Co(3A)	59.95(13)

C(20A)-Co(2A)-C(18A)	97.2(13)

C(20A)-Co(2A)-C(13A)	99.4(12)

C(18A)-Co(2A)-C(13A)	100.4(11)

C(20A)-Co(2A)-C(12A)	104.2(11)

C(18A)-Co(2A)-C(12A)	103.0(10)

C(13A)-Co(2A)-C(12A)	144.0(10)

C(20A)-Co(2A)-Co(1A)	151.3(9)

C(18A)-Co(2A)-Co(1A)	99.1(9)

C(13A)-Co(2A)-Co(1A)	100.6(8)

C(12A)-Co(2A)-Co(1A)	49.0(7)

C(20A)-Co(2A)-Co(3A)	95.8(8)

C(18A)-Co(2A)-Co(3A)	152.2(9)

C(13A)-Co(2A)-Co(3A)	101.5(7)

C(12A)-Co(2A)-Co(3A)	49.8(7)

Co(1A)-Co(2A)-Co(3A)	60.20(13)

C(17A)-Co(3A)-C(16A)	95.8(11)

C(17A)-Co(3A)-C(14A)	106.1(11)

C(16A)-Co(3A)-C(14A)	97.6(11)

C(17A)-Co(3A)-C(12A)	98.4(11)

C(16A)-Co(3A)-C(12A)	106.9(10)

C(14A)-Co(3A)-C(12A)	143.2(10)

C(17A)-Co(3A)-Co(2A)	99.8(7)

C(16A)-Co(3A)-Co(2A)	153.3(7)

C(14A)-Co(3A)-Co(2A)	98.7(8)

C(12A)-Co(3A)-Co(2A)	49.4(7)

C(17A)-Co(3A)-Co(1A)	147.1(7)

C(16A)-Co(3A)-Co(1A)	95.9(8)

C(14A)-Co(3A)-Co(1A)	102.6(8)

C(12A)-Co(3A)-Co(1A)	48.8(7)

Co(2A)-Co(3A)-Co(1A)	59.85(13)

C(8A)-C(1A)-C(6A)	114.4

C(8A)-C(1A)-C(7A)	117.6

C(6A)-C(1A)-C(7A)	99.3

C(8A)-C(1A)-C(2A)	114.0

C(6A)-C(1A)-C(2A)	106.7

C(7A)-C(1A)-C(2A)	103.1

O(2A)-C(2A)-C(3A)	112.8

O(2A)-C(2A)-C(11A)	109.7(10)

C(3A)-C(2A)-C(11A)	110.2(11)

O(2A)-C(2A)-C(1A)	109.1

C(3A)-C(2A)-C(1A)	102.8

C(11A)-C(2A)-C(1A)	112.1(11)

C(4A)-C(3A)-C(2A)	103.3

C(3A)-C(4A)-C(5A)	107.4

C(3A)-C(4A)-C(7A)	102.7

C(5A)-C(4A)-C(7A)	103.2

C(6A)-C(5A)-C(4A)	102.5

C(5A)-C(6A)-C(1A)	104.4

C(10A)-C(7A)-C(4A)	113.6

C(10A)-C(7A)-C(9A)	106.1

C(4A)-C(7A)-C(9A)	113.6

C(10A)-C(7A)-C(1A)	116.6

C(4A)-C(7A)-C(1A)	92.9

C(9A)-C(7A)-C(1A)	114.0

C(8B)-C(1B)-C(6B)	114.4

C(8B)-C(1B)-C(7B)	117.6

C(6B)-C(1B)-C(7B)	99.3

C(8B)-C(1B)-C(2B)	114.0

C(6B)-C(1B)-C(2B)	106.7

C(7B)-C(1B)-C(2B)	103.1

O(2B)-C(2B)-C(3B)	112.8

O(2B)-C(2B)-C(1B)	109.1

C(3B)-C(2B)-C(1B)	102.8

O(2B)-C(2B)-C(11A)	101.0(9)

C(3B)-C(2B)-C(11A)	118.3(9)

C(1B)-C(2B)-C(11A)	113.0(9)

C(4B)-C(3B)-C(2B)	103.3

C(3B)-C(4B)-C(5B)	107.4

C(3B)-C(4B)-C(7B)	102.7

C(5B)-C(4B)-C(7B)	103.2

C(6B)-C(5B)-C(4B)	102.5

C(5B)-C(6B)-C(1B)	104.4

C(10B)-C(7B)-C(4B)	113.6

C(10B)-C(7B)-C(9B)	106.1

C(4B)-C(7B)-C(9B)	113.6

C(10B)-C(7B)-C(1B)	116.6

C(4B)-C(7B)-C(1B)	92.9

C(9B)-C(7B)-C(1B)	114.0

C(12A)-C(11A)-C(2A)	114.1(17)

C(12A)-C(11A)-C(2B)	117.0(16)

C(2A)-C(11A)-C(2B)	6.1(6)

C(11A)-C(12A)-Co(1A)	136.9(17)

C(11A)-C(12A)-Co(2A)	123.7(17)

Co(1A)-C(12A)-Co(2A)	81.4(9)

C(11A)-C(12A)-Co(3A)	132.4(16)

Co(1A)-C(12A)-Co(3A)	81.5(9)

Co(2A)-C(12A)-Co(3A)	80.8(9)

O(13A)-C(13A)-Co(2A)	179(2)

O(14A)-C(14A)-Co(3A)	169(2)

O(15A)-C(15A)-Co(1A)	177(2)

O(16A)-C(16A)-Co(3A)	175(2)

O(17A)-C(17A)-Co(3A)	179(2)

O(18A)-C(18A)-Co(2A)	173(2)

O(19A)-C(19A)-Co(1A)	175(2)

O(20A)-C(20A)-Co(2A)	176(3)

O(21A)-C(21A)-Co(1A)	173(2)

C(19C)-Co(1C)-C(21C)	93.2(13)

C(19C)-Co(1C)-C(15C)	104.5(11)

C(21C)-Co(1C)-C(15C)	102.1(11)

C(19C)-Co(1C)-C(12C)	99.0(11)

C(21C)-Co(1C)-C(12C)	103.8(11)

C(15C)-Co(1C)-C(12C)	143.7(10)

C(19C)-Co(1C)-Co(2C)	98.0(10)

C(21C)-Co(1C)-Co(2C)	154.4(8)

C(15C)-Co(1C)-Co(2C)	97.2(8)

C(12C)-Co(1C)-Co(2C)	51.8(8)

C(19C)-Co(1C)-Co(3C)	147.6(9)

C(21C)-Co(1C)-Co(3C)	99.3(8)

C(15C)-Co(1C)-Co(3C)	102.0(6)

C(12C)-Co(1C)-Co(3C)	49.0(7)

Co(2C)-Co(1C)-Co(3C)	60.01(13)

C(20C)-Co(2C)-C(18C)	95.7(13)

C(20C)-Co(2C)-C(13C)	100.7(12)

C(18C)-Co(2C)-C(13C)	105.7(12)

C(20C)-Co(2C)-C(12C)	102.7(11)

C(18C)-Co(2C)-C(12C)	97.9(10)

C(13C)-Co(2C)-C(12C)	144.7(10)

C(20C)-Co(2C)-Co(1C)	150.9(9)

C(18C)-Co(2C)-Co(1C)	96.7(9)

C(13C)-Co(2C)-Co(1C)	101.1(9)

C(12C)-Co(2C)-Co(1C)	49.5(7)

C(20C)-Co(2C)-Co(3C)	96.2(8)

C(18C)-Co(2C)-Co(3C)	146.3(9)

C(13C)-Co(2C)-Co(3C)	102.8(8)

C(12C)-Co(2C)-Co(3C)	48.7(6)

Co(1C)-Co(2C)-Co(3C)	60.18(14)

C(16C)-Co(3C)-C(17C)	96.6(12)

C(16C)-Co(3C)-C(14C)	104.6(12)

C(17C)-Co(3C)-C(14C)	102.5(11)

C(16C)-Co(3C)-C(12C)	102.7(12)

C(17C)-Co(3C)-C(12C)	102.8(10)

C(14C)-Co(3C)-C(12C)	140.0(10)

C(16C)-Co(3C)-Co(2C)	152.0(9)

C(17C)-Co(3C)-Co(2C)	100.4(8)

C(14C)-Co(3C)-Co(2C)	93.3(8)

C(12C)-Co(3C)-Co(2C)	51.9(7)

C(16C)-Co(3C)-Co(1C)	95.8(9)

C(17C)-Co(3C)-Co(1C)	152.0(7)

C(14C)-Co(3C)-Co(1C)	98.5(8)

C(12C)-Co(3C)-Co(1C)	49.8(7)

Co(2C)-Co(3C)-Co(1C)	59.81(13)

C(8C)-C(1C)-C(6C)	114.4

C(8C)-C(1C)-C(7C)	117.6

C(6C)-C(1C)-C(7C)	99.3

C(8C)-C(1C)-C(2C)	114.0

C(6C)-C(1C)-C(2C)	106.7

C(7C)-C(1C)-C(2C)	103.1

O(2C)-C(2C)-C(11C)	96.2(10)

O(2C)-C(2C)-C(3C)	112.8

C(11C)-C(2C)-C(3C)	118.4(9)

O(2C)-C(2C)-C(1C)	109.1

C(11C)-C(2C)-C(1C)	117.6(10)

C(3C)-C(2C)-C(1C)	102.8

C(4C)-C(3C)-C(2C)	103.3

C(3C)-C(4C)-C(5C)	107.4

C(3C)-C(4C)-C(7C)	102.7

C(5C)-C(4C)-C(7C)	103.2

C(6C)-C(5C)-C(4C)	102.5

C(5C)-C(6C)-C(1C)	104.4

C(10C)-C(7C)-C(4C)	113.6

C(10C)-C(7C)-C(9C)	106.1

C(4C)-C(7C)-C(9C)	113.6

C(10C)-C(7C)-C(1C)	116.6

C(4C)-C(7C)-C(1C)	92.9

C(9C)-C(7C)-C(1C)	114.0

C(8D)-C(1D)-C(6D)	114.4

C(8D)-C(1D)-C(7D)	117.6

C(6D)-C(1D)-C(7D)	99.3

C(8D)-C(1D)-C(2D)	114.0

C(6D)-C(1D)-C(2D)	106.7

C(7D)-C(1D)-C(2D)	103.1

O(2D)-C(2D)-C(3D)	112.8

O(2D)-C(2D)-C(1D)	109.1

C(3D)-C(2D)-C(1D)	102.8

O(2D)-C(2D)-C(11C)	105.1(10)

C(3D)-C(2D)-C(11C)	108.8(10)

C(1D)-C(2D)-C(11C)	118.5(10)

C(4D)-C(3D)-C(2D)	103.3

C(3D)-C(4D)-C(5D)	107.4

C(3D)-C(4D)-C(7D)	102.7

C(5D)-C(4D)-C(7D)	103.2

C(6D)-C(5D)-C(4D)	102.5

C(5D)-C(6D)-C(1D)	104.4

C(10D)-C(7D)-C(4D)	113.6

C(10D)-C(7D)-C(9D)	106.1

C(4D)-C(7D)-C(9D)	113.6

C(10D)-C(7D)-C(1D)	116.6

C(4D)-C(7D)-C(1D)	92.9

C(9D)-C(7D)-C(1D)	114.0

C(12C)-C(11C)-C(2C)	121.1(17)

C(12C)-C(11C)-C(2D)	118.5(16)

C(2C)-C(11C)-C(2D)	5.3(6)

C(11C)-C(12C)-Co(3C)	138.1(17)

C(11C)-C(12C)-Co(1C)	132.9(18)

Co(3C)-C(12C)-Co(1C)	81.2(9)

C(11C)-C(12C)-Co(2C)	124.5(17)

Co(3C)-C(12C)-Co(2C)	79.4(9)

Co(1C)-C(12C)-Co(2C)	78.6(9)

O(13C)-C(13C)-Co(2C)	179(3)

O(14C)-C(14C)-Co(3C)	173(3)

O(15C)-C(15C)-Co(1C)	173.8(19)

O(16C)-C(16C)-Co(3C)	179(3)

O(17C)-C(17C)-Co(3C)	178(2)

O(18C)-C(18C)-Co(2C)	175(2)

O(19C)-C(19C)-Co(1C)	176(3)

O(20C)-C(20C)-Co(2C)	178(3)

O(21C)-C(21C)-Co(1C)	169(3)

_____________________________________________________________________________________

Table E4:   Anisotropic displacement parameters (Å2 x 103) for 77.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1A)	38(2) 	41(2)	45(2) 	1(2)	12(2) 	8(2)

Co(2A)	39(2) 	49(2)	34(2) 	-2(2)	14(2) 	8(2)

Co(3A)	46(2) 	40(2)	45(2) 	0(2)	5(2) 	-4(2)

C(11A)	37(5) 	47(5)	45(4) 	12(4)	9(4) 	17(4)

C(12A)	30(4) 	52(4)	36(4) 	16(3)	4(3) 	2(3)

O(13A)	89(4) 	118(5)	37(4) 	8(3)	1(3) 	-3(3)

C(13A)	42(17) 	66(15)	45(17) 	18(14)	26(13) 	1(12)

O(14A)	81(4) 	81(3)	50(4) 	1(3)	-10(3) 	-22(3)

C(14A)	53(6) 	51(4)	61(6) 	7(4)	13(5) 	-5(4)

O(15A)	72(13) 	80(9)	75(13) 	-7(9)	-8(10) 	35(9)

C(15A)	52(16) 	79(15)	48(16) 	-6(12)	5(12) 	49(11)

O(16A)	84(12) 	128(13)	53(10) 	3(8)	21(8) 	-48(9)

C(16A)	44(14) 	68(14)	54(17) 	-12(12)	19(11) 	-27(11)

O(17A)	170(20) 	80(14)	210(20) 	61(14)	2(18) 	58(14)

C(17A)	150(20) 	34(13)	64(19) 	15(12)	26(17) 	-28(14)

O(18A)	48(11) 	57(10)	130(18) 	-14(10)	36(11) 	-1(8)

C(18A)	64(5) 	66(4)	45(6) 	8(4)	28(5) 	9(4)

O(19A)	107(16) 	50(10)	103(16) 	-21(10)	26(12) 	-34(10)

C(19A)	54(16) 	30(11)	45(15) 	-3(10)	29(12) 	-2(10)

O(20A)	69(4) 	105(4)	158(6) 	-9(4)	34(4) 	42(3)

C(20A)	49(5) 	79(5)	51(6) 	-2(4)	11(4) 	-5(4)

O(21A)	72(5) 	166(6)	89(5) 	15(4)	51(4) 	23(4)

C(21A)	54(5) 	77(5)	49(7) 	7(4)	2(5) 	13(4)

Co(1C)	36(2) 	52(2)	37(2) 	5(2)	10(2) 	5(2)

Co(2C)	39(2) 	52(2)	44(3) 	9(2)	10(2) 	4(2)

Co(3C)	52(3) 	45(2)	39(2) 	6(2)	9(2) 	-2(2)

C(11C)	37(5) 	47(5)	45(4) 	12(4)	9(4) 	17(4)

C(12C)	30(4) 	52(4)	36(4) 	16(3)	4(3) 	2(3)

O(13C)	89(4) 	118(5)	37(4) 	8(3)	1(3) 	-3(3)

C(13C)	60(20) 	72(17)	60(20) 	-11(16)	16(16) 	10(14)

O(14C)	81(4) 	81(3)	50(4) 	1(3)	-10(3) 	-22(3)

C(14C)	53(6) 	51(4)	61(6) 	7(4)	13(5) 	-5(4)

O(15C)	80(14) 	130(14)	39(10) 	-22(9)	-28(9) 	26(10)

C(15C)	74(19) 	36(12)	57(17) 	-13(12)	38(15) 	-13(12)

O(16C)	84(13) 	109(11)	87(13) 	-3(9)	36(10) 	-46(9)

C(16C)	61(18) 	71(16)	80(20) 	24(14)	-17(14) 	7(13)

O(17C)	102(16) 	61(12)	103(14) 	2(10)	44(13) 	33(10)

C(17C)	40(14) 	82(19)	54(17) 	-30(14)	1(12) 	21(12)

O(18C)	122(17) 	87(13)	120(18) 	29(12)	48(14) 	-40(12)

C(18C)	64(5) 	66(4)	45(6) 	8(4)	28(5) 	9(4)

O(19C)	102(16) 	75(12)	109(17) 	-37(12)	51(13) 	5(11)

C(19C)	51(18) 	100(20)	70(20) 	-19(16)	2(14) 	16(15)

O(20C)	69(4) 	105(4)	158(6) 	-9(4)	34(4) 	42(3)

C(20C)	49(5) 	79(5)	51(6) 	-2(4)	11(4) 	-5(4)

O(21C)	72(5) 	166(6)	89(5) 	15(4)	51(4) 	23(4)

C(21C)	54(5) 	77(5)	49(7) 	7(4)	2(5) 	13(4)

______________________________________________________________________________

Table E5:   Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 10 3)

for 77.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(2AA)	6786	7954	5980	52

H(3AA)	4595	5907	6105	48

H(3AB)	5874	6413	5512	48

H(4AA)	3454	5702	4164	76

H(5AA)	1549	5711	5425	72

H(5AB)	514	5878	4246	72

H(6AA)	9	7536	4570	44

H(6AB)	869	7334	5765	44

H(8AA)	1554	9287	4434	131

H(8AB)	3621	9440	4969	131

H(8AC)	2291	9340	5657	131

H(9AA)	472	7256	3185	191

H(9AB)	1819	7026	2532	191

H(9AC)	1514	8185	2836	191

H(10A)	5860	7679	4441	124

H(10B)	4745	8435	3589	124

H(10C)	5050	7276	3285	124

H(2BA)	6164	8683	6021	107

H(3BA)	5629	6254	6067	56

H(3BB)	6436	7142	5518	56

H(4BA)	4730	6073	4121	76

H(5BA)	2978	5368	5320	72

H(5BB)	1909	5425	4133	72

H(6BA)	253	6712	4462	68

H(6BB)	1188	6574	5659	68

H(8BA)	409	8706	4386	106

H(8BB)	2194	9313	4965	106

H(8BC)	1047	8757	5611	106

H(9BA)	878	6808	3102	105

H(9BB)	2277	7070	2487	105

H(9BC)	1164	7969	2794	105

H(10D)	5512	8434	4476	175

H(10E)	3945	8941	3618	175

H(10F)	5059	8042	3311	175

H(11A)	2992	8033	7061	52

H(11B)	3043	6807	6989	52

H(2CA)	3397	3072	4040	126

H(3CA)	5142	954	3731	57

H(3CB)	3928	1477	4347	57

H(4CA)	6100	585	5644	79

H(5CA)	8109	585	4441	89

H(5CB)	9101	635	5642	89

H(6CA)	10011	2276	5517	69

H(6CB)	9187	2184	4301	69

H(8CA)	8846	4072	5816	123

H(8CB)	6842	4346	5265	123

H(8CC)	8207	4230	4603	123

H(9CA)	9380	1937	6842	86

H(9CB)	7926	1730	7432	86

H(9CC)	8519	2884	7268	86

H(10G)	4152	2668	5544	192

H(10H)	5383	3318	6489	192

H(10I)	4790	2164	6653	192

H(2DA)	3160	2300	4031	57

H(3DA)	6147	899	3621	40

H(3DB)	4691	934	4229	40

H(4DA)	7315	407	5497	84

H(5DA)	9162	1166	4373	62

H(5DB)	10077	1209	5584	62

H(6DA)	9861	2942	5609	96

H(6DB)	9129	2906	4385	96

H(8DA)	7622	4202	6002	120

H(8DB)	5568	4059	5425	120

H(8DC)	6901	4437	4805	120

H(9DA)	9519	2200	6865	246

H(9DB)	8311	1523	7388	246

H(9DC)	8114	2745	7329	246

H(10J)	4153	1812	5498	105

H(10K)	4899	2509	6509	105

H(10L)	5095	1287	6567	105

H(11C)	6563	3427	2999	52

H(11D)	7045	2250	2951	52

________________________________________________________________________________

Table F1:  Crystal data and structure refinement for 112.

Empirical formula 	C31 H22 O

Formula weight 	410.49

Temperature 	197(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	P2(1)2(1)2(1)

Unit cell dimensions	a = 5.9605(15) Å	(= 90°.

b = 12.804(3) Å	(= 90°.

c = 28.760(8) Å	(= 90°.

Volume	2194.9(10) Å3

Z	4

Density (calculated)	1.242 Mg/m3

Absorption coefficient	0.073 mm-1

F(000)	864

Crystal size	.04 x .05 x .40 mm3

( range for data collection	1.42 to 25.00°.

Index ranges	-7≤h≤7, -16≤k≤15, -35≤l≤34

Reflections collected	16498

Independent reflections	3849 [R(int) = 0.0927]

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3835 / 0 / 378

Goodness-of-fit on F2	1.015

Final R indices [I>2((I)]	R1 = 0.0514, wR2 = 0.0909

R indices (all data)	R1 = 0.0960, wR2 = 0.1048

Absolute structure parameter	1.14(275)

Extinction coefficient	0.0229(17)

Largest diff. peak and hole	0.193 and -0.171 e.Å-3

Ratio of min/max apparent transmission  		0.549239

Table F2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 112.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

O(1)	7798(3)	7110(2)	1122(1)	43(1)

C(1)	8559(5)	6338(2)	1312(1)	31(1)

C(2)	10216(4)	6310(2)	1705(1)	29(1)

C(3)	10506(5)	5203(2)	1817(1)	33(1)

C(4)	9328(5)	4605(3)	1520(1)	33(1)

C(5)	8081(4)	5216(2)	1184(1)	29(1)

C(6)	6800(4)	4862(2)	831(1)	28(1)

C(7)	11254(4)	7155(2)	1889(1)	29(1)

C(8)	5348(5)	5515(2)	523(1)	30(1)

C(9)	5539(6)	5424(2)	41(1)	38(1)

C(10)	4132(6)	5978(3)	-249(1)	45(1)

C(11)	2482(6)	6607(3)	-66(1)	48(1)

C(12)	2276(6)	6689(3)	409(1)	51(1)

C(13)	3703(5)	6156(3)	701(1)	44(1)

C(14)	6694(5)	3714(2)	733(1)	31(1)

C(15)	8497(6)	3178(3)	553(1)	45(1)

C(16)	8335(7)	2110(3)	455(1)	56(1)

C(17)	6349(8)	1596(3)	550(1)	58(1)

C(18)	4553(7)	2135(3)	724(1)	54(1)

C(19)	4715(6)	3183(3)	811(1)	41(1)

C(20)	10692(5)	8245(2)	1744(1)	31(1)

C(21)	8654(5)	8702(3)	1864(1)	41(1)

C(22)	8225(7)	9729(3)	1733(1)	54(1)

C(23)	9814(7)	10283(3)	1485(1)	59(1)

C(24)	11792(7)	9831(3)	1372(1)	56(1)

C(25)	12257(5)	8811(3)	1500(1)	42(1)

C(26)	13037(4)	7088(2)	2249(1)	29(1)

C(27)	13122(5)	7850(3)	2595(1)	40(1)

C(28)	14762(6)	7828(3)	2932(1)	50(1)

C(29)	16379(6)	7051(3)	2929(1)	46(1)

C(30)	16336(5)	6303(3)	2592(1)	39(1)

C(31)	14705(5)	6318(3)	2249(1)	34(1)

________________________________________________________________________________

Table F3:  Bond lengths [Å] and angles [°] for 112.

___________________________________________________________________________________

O(1)-C(1) 	1.217(3)

C(1)-C(2) 	1.502(4)

C(1)-C(5) 	1.510(4)

C(2)-C(7) 	1.354(4)

C(2)-C(3) 	1.464(4)

C(3)-C(4) 	1.344(4)

C(4)-C(5) 	1.448(4)

C(5)-C(6) 	1.349(4)

C(6)-C(8) 	1.495(4)

C(6)-C(14) 	1.498(4)

C(7)-C(26) 	1.486(4)

C(7)-C(20) 	1.495(4)

C(8)-C(13) 	1.378(4)

C(8)-C(9) 	1.394(4)

C(9)-C(10) 	1.379(4)

C(10)-C(11) 	1.375(5)

C(11)-C(12) 	1.377(5)

C(12)-C(13) 	1.376(5)

C(14)-C(15) 	1.376(4)

C(14)-C(19) 	1.380(4)

C(15)-C(16) 	1.399(5)

C(16)-C(17) 	1.382(5)

C(17)-C(18) 	1.369(5)

C(18)-C(19) 	1.369(5)

C(20)-C(25) 	1.374(4)

C(20)-C(21) 	1.391(4)

C(21)-C(22) 	1.391(5)

C(22)-C(23) 	1.382(6)

C(23)-C(24) 	1.353(6)

C(24)-C(25) 	1.386(5)

C(26)-C(27) 	1.395(4)

C(26)-C(31) 	1.401(4)

C(27)-C(28) 	1.377(4)

C(28)-C(29) 	1.385(5)

C(29)-C(30) 	1.363(5)

C(30)-C(31) 	1.387(4)

O(1)-C(1)-C(2)	127.1(3)

O(1)-C(1)-C(5)	126.4(3)

C(2)-C(1)-C(5)	106.5(3)

C(7)-C(2)-C(3)	129.4(3)

C(7)-C(2)-C(1)	125.1(3)

C(3)-C(2)-C(1)	105.5(3)

C(4)-C(3)-C(2)	110.5(3)

C(3)-C(4)-C(5)	112.6(3)

C(6)-C(5)-C(4)	127.7(3)

C(6)-C(5)-C(1)	127.5(3)

C(4)-C(5)-C(1)	104.8(3)

C(5)-C(6)-C(8)	125.9(3)

C(5)-C(6)-C(14)	119.7(3)

C(8)-C(6)-C(14)	114.4(2)

C(2)-C(7)-C(26)	123.5(3)

C(2)-C(7)-C(20)	122.4(2)

C(26)-C(7)-C(20)	114.1(2)

C(13)-C(8)-C(9)	118.6(3)

C(13)-C(8)-C(6)	121.6(3)

C(9)-C(8)-C(6)	119.7(3)

C(10)-C(9)-C(8)	120.5(3)

C(11)-C(10)-C(9)	120.4(4)

C(10)-C(11)-C(12)	119.2(3)

C(13)-C(12)-C(11)	120.8(4)

C(12)-C(13)-C(8)	120.6(3)

C(15)-C(14)-C(19)	118.8(3)

C(15)-C(14)-C(6)	121.8(3)

C(19)-C(14)-C(6)	119.3(3)

C(14)-C(15)-C(16)	120.7(4)

C(17)-C(16)-C(15)	119.0(4)

C(18)-C(17)-C(16)	120.2(4)

C(17)-C(18)-C(19)	120.4(4)

C(18)-C(19)-C(14)	120.9(4)

C(25)-C(20)-C(21)	119.9(3)

C(25)-C(20)-C(7)	118.8(3)

C(21)-C(20)-C(7)	121.3(3)

C(20)-C(21)-C(22)	119.4(4)

C(23)-C(22)-C(21)	119.9(4)

C(24)-C(23)-C(22)	120.1(4)

C(23)-C(24)-C(25)	120.9(4)

C(20)-C(25)-C(24)	119.8(3)

C(27)-C(26)-C(31)	117.8(3)

C(27)-C(26)-C(7)	118.9(3)

C(31)-C(26)-C(7)	123.2(3)

C(28)-C(27)-C(26)	120.9(3)

C(27)-C(28)-C(29)	120.4(4)

C(30)-C(29)-C(28)	119.7(3)

C(29)-C(30)-C(31)	120.7(3)

C(30)-C(31)-C(26)	120.5(3)

_________________________________________________________________________________

Table F4:  Anisotropic displacement parameters (Å2 x 103) for 112.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

O(1)	58(1) 	30(1)	41(1) 	4(1)	-6(1) 	0(1)

C(1)	34(2) 	28(2)	32(2) 	4(2)	5(1) 	3(2)

C(2)	31(1) 	28(2)	27(2) 	-2(2)	4(1) 	0(1)

C(3)	37(2) 	29(2)	34(2) 	5(2)	-1(2) 	-1(2)

C(4)	40(2) 	24(2)	36(2) 	5(2)	1(2) 	-4(2)

C(5)	31(1) 	25(2)	31(2) 	2(2)	2(1) 	-2(1)

C(6)	31(1) 	25(2)	29(2) 	0(1)	7(1) 	1(1)

C(7)	30(1) 	30(2)	25(2) 	3(2)	7(1) 	2(1)

C(8)	34(2) 	24(2)	31(2) 	-3(1)	2(1) 	-5(2)

C(9)	49(2) 	29(2)	37(2) 	-3(2)	-1(2) 	2(2)

C(10)	65(2) 	38(2)	34(2) 	4(2)	-6(2) 	-3(2)

C(11)	48(2) 	50(2)	46(3) 	17(2)	-4(2) 	2(2)

C(12)	42(2) 	53(2)	59(3) 	24(2)	15(2) 	16(2)

C(13)	42(2) 	51(2)	40(2) 	11(2)	11(2) 	15(2)

C(14)	39(2) 	27(2)	26(2) 	2(2)	-2(2) 	4(2)

C(15)	43(2) 	45(2)	46(2) 	-7(2)	-1(2) 	9(2)

C(16)	70(2) 	45(3)	52(2) 	-17(2)	-12(2) 	21(2)

C(17)	87(3) 	24(2)	63(3) 	1(2)	-26(2) 	-1(2)

C(18)	68(2) 	32(2)	62(3) 	12(2)	-14(2) 	-10(2)

C(19)	46(2) 	29(2)	48(2) 	7(2)	-2(2) 	2(2)

C(20)	37(2) 	25(2)	30(2) 	-1(2)	-7(1) 	-3(1)

C(21)	42(2) 	33(2)	49(2) 	-3(2)	-2(2) 	9(2)

C(22)	58(2) 	41(2)	62(3) 	-13(2)	-18(2) 	13(2)

C(23)	84(3) 	24(2)	68(3) 	4(2)	-39(3) 	-2(2)

C(24)	66(2) 	37(2)	65(3) 	14(2)	-19(2) 	-14(2)

C(25)	43(2) 	40(2)	43(2) 	7(2)	-3(2) 	-6(2)

C(26)	30(1) 	29(2)	30(2) 	4(2)	5(1) 	-6(2)

C(27)	46(2) 	38(2)	36(2) 	-2(2)	-7(2) 	10(2)

C(28)	57(2) 	55(3)	38(2) 	-8(2)	-12(2) 	12(2)

C(29)	42(2) 	57(3)	40(2) 	6(2)	-11(2) 	5(2)

C(30)	36(2) 	41(2)	40(2) 	4(2)	3(2) 	6(2)

C(31)	34(2) 	33(2)	35(2) 	1(2)	7(2) 	-1(2)

______________________________________________________________________________

Table F5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 112.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(3)	11375(43)	4926(21)	2100(10)	38(8)

H(4)	9184(44)	3868(25)	1531(10)	40(9)

H(9)	6790(45)	5018(21)	-84(9)	36(8)

H(10)	4290(49)	5942(24)	-561(11)	43(10)

H(11)	1563(54)	7037(26)	-302(11)	66(10)

H(12)	1056(52)	7134(26)	525(10)	58(10)

H(13)	3516(53)	6147(25)	1039(11)	61(11)

H(15)	9815(51)	3546(23)	481(10)	47(10)

H(16)	9647(53)	1794(24)	296(11)	54(10)

H(17)	6220(67)	887(34)	454(13)	95(14)

H(18)	3294(65)	1732(31)	783(13)	79(13)

H(19)	3462(55)	3550(25)	904(10)	53(10)

H(21)	7560(59)	8291(29)	2032(12)	77(13)

H(22)	6814(57)	10025(25)	1842(11)	60(10)

H(23)	9434(58)	10988(31)	1400(12)	76(12)

H(24)	12946(66)	10165(31)	1173(13)	93(14)

H(25)	13781(45)	8482(21)	1421(9)	35(8)

H(27)	11891(41)	8398(19)	2610(8)	21(7)

H(28)	14778(50)	8345(24)	3156(11)	49(10)

H(29)	17486(43)	7068(21)	3159(9)	34(8)

H(30)	17462(47)	5752(23)	2581(9)	43(9)

H(31)	14582(38)	5750(21)	2008(9)	24(7)

________________________________________________________________________________

Table G1:  Crystal data and structure refinement for 120.

Empirical formula 	C24 H11 Co3 O9

Formula weight 	620.12

Temperature 	173(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)/n

Unit cell dimensions	a = 8.702(6) Å	((= 90°.

b = 30.56(2) Å	(= 98.679(12)°.

c = 26.752(19) Å	(= 90°.

Volume	7032(9) Å3

Z	12

Density (calculated)	1.757 Mg/m3

Absorption coefficient	2.151 mm-1

F(000)	3696

Crystal size	0.35 x 0.08 x 0.03 mm3

( range for data collection	1.54 to 20.25°.

Index ranges	-8(h(8, -29(k(29, -26(l(26

Reflections collected	31554

Independent reflections	6790 [R(int) = 0.1742]

Completeness to ( = 20.25°	99.7 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6790 / 198 / 839

Goodness-of-fit on F2	1.147

Final R indices [I>2((I)]	R1 = 0.1098, wR2 = 0.2429

R indices (all data)	R1 = 0.1650, wR2 = 0.2754

Extinction coefficient	0.0106(7)

Largest diff. peak and hole	1.867 and -1.048 e.Å-3

Ratio of min/max apparent transmission	0.752301

Table G2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 120.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	3286(3)	2063(1)	5564(1)	17(1)

Co(2)	3626(3)	2791(1)	5958(1)	19(1)

Co(3)	5843(3)	2288(1)	6018(1)	19(1)

C(1)	6630(20)	1610(7)	7305(8)	28(5)

C(2)	8010(20)	1352(7)	7357(8)	30(5)

C(3)	7970(20)	930(7)	7155(8)	32(5)

C(4)	6640(20)	757(7)	6885(8)	28(5)

C(5)	3120(20)	524(6)	6323(7)	20(5)

C(6)	1530(20)	520(7)	6141(8)	26(5)

C(7)	560(20)	870(7)	6203(8)	29(5)

C(8)	1190(20)	1236(7)	6476(7)	20(4)

C(9)	3640(20)	1612(6)	6956(8)	22(5)

C(10)	5300(20)	1428(6)	7031(7)	15(4)

C(11)	5280(20)	1022(7)	6825(8)	20(4)

C(12)	3670(20)	908(6)	6577(7)	16(4)

C(13)	2730(20)	1266(6)	6640(7)	12(4)

C(14)	3412(19)	2079(6)	6752(7)	8(5)

C(15)	3860(19)	2223(6)	6249(7)	12(5)

O(16)	3875(17)	1129(6)	5403(6)	50(5)

C(16)	3680(20)	1508(8)	5492(9)	33(6)

O(17)	-115(14)	1952(5)	5479(6)	46(5)

C(17)	1230(30)	1995(7)	5530(8)	31(6)

O(18)	3653(15)	2398(5)	4555(6)	34(4)

C(18)	3490(20)	2261(7)	4953(10)	30(6)

O(19)	305(16)	2925(5)	5947(6)	42(4)

C(19)	1590(20)	2874(7)	5949(8)	22(5)

O(20)	4631(16)	3358(5)	6819(6)	39(4)

C(20)	4270(20)	3121(7)	6495(8)	19(5)

O(21)	4353(15)	3357(5)	5116(5)	35(4)

C(21)	4070(20)	3143(7)	5447(8)	18(5)

O(22)	7258(15)	1426(5)	6010(5)	32(4)

C(22)	6710(20)	1768(8)	6032(8)	25(6)

O(23)	7736(17)	2641(5)	6927(7)	51(5)

C(23)	6980(30)	2497(8)	6588(10)	37(7)

O(24)	7260(16)	2677(5)	5168(6)	41(4)

C(24)	6750(20)	2524(7)	5492(9)	25(6)

Co(1A)	-1035(3)	4151(1)	4021(1)	19(1)

Co(2A)	1078(3)	3620(1)	3998(1)	18(1)

Co(3A)	1615(3)	4318(1)	4453(1)	18(1)

C(1A)	3480(20)	5222(7)	3618(8)	22(5)

C(2A)	3980(20)	5593(8)	3887(9)	36(6)

C(3A)	2970(20)	5922(7)	3981(8)	24(5)

C(4A)	1420(20)	5893(7)	3756(8)	28(5)

C(5A)	-2050(20)	5632(7)	3188(8)	24(5)

C(6A)	-3370(20)	5461(7)	2902(8)	29(5)

C(7A)	-3320(20)	5053(7)	2660(9)	33(6)

C(8A)	-1870(20)	4833(7)	2697(8)	23(4)

C(9A)	1110(20)	4838(7)	3073(8)	21(5)

C(10A)	1920(20)	5191(7)	3416(9)	32(6)

C(11A)	930(20)	5534(6)	3488(7)	16(4)

C(12A)	-660(20)	5408(7)	3228(8)	21(4)

C(13A)	-590(20)	5009(7)	2993(7)	18(4)

C(14A)	1300(20)	4362(7)	3253(8)	25(6)

C(15A)	860(20)	4201(6)	3774(7)	14(5)

O(16A)	-2359(16)	5015(5)	4137(6)	39(4)

C(16A)	-1850(30)	4675(9)	4079(9)	37(6)

O(17A)	-3095(17)	3884(5)	3100(6)	44(4)

C(17A)	-2320(20)	3991(7)	3472(9)	23(5)

O(18A)	-2285(17)	3694(5)	4861(6)	45(5)

C(18A)	-1860(20)	3874(7)	4546(9)	26(6)

O(19A)	-470(15)	3076(5)	3159(5)	30(4)

C(19A)	150(20)	3308(7)	3473(8)	21(5)

O(20A)	584(16)	2987(5)	4782(6)	39(4)

C(20A)	820(20)	3245(7)	4507(8)	20(5)

O(21A)	4299(15)	3506(5)	3822(6)	44(5)

C(21A)	3040(30)	3543(7)	3890(9)	35(6)

O(22A)	1202(15)	5241(5)	4664(5)	29(4)

C(22A)	1340(20)	4861(7)	4567(7)	14(5)

O(23A)	4971(15)	4397(5)	4454(7)	53(5)

C(23A)	3620(20)	4349(7)	4460(8)	25(6)

O(24A)	1449(16)	3959(5)	5474(6)	45(5)

C(24A)	1520(20)	4097(7)	5070(9)	25(6)

Co(1B)	-2154(3)	6940(1)	1152(1)	19(1)

Co(2B)	-1865(3)	7035(1)	2072(1)	18(1)

Co(3B)	356(3)	6787(1)	1681(1)	17(1)

C(1B)	1040(20)	5528(7)	1986(8)	28(5)

C(2B)	2580(20)	5414(7)	1914(9)	28(5)

C(3B)	2930(20)	5325(7)	1436(9)	36(6)

C(4B)	1890(20)	5344(7)	1031(9)	29(5)

C(5B)	-1320(30)	5482(7)	187(9)	35(5)

C(6B)	-2800(30)	5556(8)	-83(10)	46(6)

C(7B)	-3990(30)	5678(8)	167(9)	48(7)

C(8B)	-3740(20)	5731(7)	679(8)	28(5)

C(9B)	-1770(20)	5672(7)	1517(7)	20(4)

C(10B)	-30(20)	5562(7)	1534(8)	22(5)

C(11B)	320(20)	5462(7)	1066(8)	22(4)

C(12B)	-1080(20)	5531(6)	688(8)	21(4)

C(13B)	-2290(20)	5655(6)	947(8)	21(4)

C(14B)	-2194(19)	6081(6)	1798(7)	16(5)

C(15B)	-1630(20)	6527(6)	1674(7)	13(5)

O(16B)	-1482(17)	6581(5)	188(6)	41(4)

C(16B)	-1730(20)	6705(7)	566(9)	23(6)

O(17B)	-5517(17)	6853(7)	892(7)	80(7)

C(17B)	-4190(30)	6876(7)	995(9)	33(6)

O(18B)	-1889(15)	7887(5)	968(5)	36(4)

C(18B)	-1960(20)	7499(9)	1029(9)	36(6)

O(19B)	-5226(16)	7035(6)	2103(6)	53(5)

C(19B)	-3930(30)	7034(7)	2086(9)	33(6)

O(20B)	-976(16)	7964(5)	2255(6)	43(5)

C(20B)	-1320(20)	7605(8)	2177(8)	22(5)

O(21B)	-819(17)	6659(5)	3074(5)	44(5)

C(21B)	-1240(20)	6810(7)	2673(8)	18(5)

O(22B)	1734(19)	6349(5)	868(6)	50(5)

C(22B)	1220(20)	6510(7)	1198(8)	18(5)

O(23B)	2224(15)	6409(5)	2583(6)	34(4)

C(23B)	1490(20)	6538(7)	2226(9)	27(6)

O(24B)	1908(16)	7647(5)	1672(6)	39(4)

C(24B)	1320(20)	7323(8)	1678(8)	24(6)

________________________________________________________________________________

Table G3:  Bond lengths [Å] and angles [°] for 120.

______________________________________________________________________________________

Co(1)-C(16) 	1.75(3)

Co(1)-C(18) 	1.78(3)

Co(1)-C(17) 	1.79(2)

Co(1)-C(15) 	1.891(19)

Co(1)-Co(2) 	2.458(4)

Co(1)-Co(3) 	2.466(4)

Co(2)-C(20) 	1.78(2)

Co(2)-C(19) 	1.79(2)

Co(2)-C(21) 	1.83(2)

Co(2)-C(15) 	1.899(19)

Co(2)-Co(3) 	2.452(4)

Co(3)-C(22) 	1.75(2)

Co(3)-C(23) 	1.80(3)

Co(3)-C(24) 	1.86(2)

Co(3)-C(15) 	1.930(17)

C(1)-C(10) 	1.39(3)

C(1)-C(2) 	1.43(3)

C(2)-C(3) 	1.40(3)

C(3)-C(4) 	1.38(3)

C(4)-C(11) 	1.42(3)

C(5)-C(6) 	1.40(3)

C(5)-C(12) 	1.40(3)

C(6)-C(7) 	1.39(3)

C(7)-C(8) 	1.40(3)

C(8)-C(13) 	1.35(2)

C(9)-C(13) 	1.50(3)

C(9)-C(14) 	1.53(3)

C(9)-C(10) 	1.53(3)

C(10)-C(11) 	1.35(3)

C(11)-C(12) 	1.50(3)

C(12)-C(13) 	1.39(3)

C(14)-C(15) 	1.52(2)

O(16)-C(16) 	1.20(3)

O(17)-C(17) 	1.16(2)

O(18)-C(18) 	1.17(2)

O(19)-C(19) 	1.13(2)

O(20)-C(20) 	1.14(2)

O(21)-C(21) 	1.16(2)

O(22)-C(22) 	1.16(2)

O(23)-C(23) 	1.13(3)

O(24)-C(24) 	1.14(2)

Co(1A)-C(16A) 	1.77(3)

Co(1A)-C(17A) 	1.78(2)

Co(1A)-C(18A) 	1.87(2)

Co(1A)-C(15A) 	1.875(17)

Co(1A)-Co(2A) 	2.460(4)

Co(1A)-Co(3A) 	2.471(4)

Co(2A)-C(19A) 	1.78(2)

Co(2A)-C(21A) 	1.79(2)

Co(2A)-C(20A) 	1.82(2)

Co(2A)-C(15A) 	1.874(19)

Co(2A)-Co(3A) 	2.465(4)

Co(3A)-C(22A) 	1.71(2)

Co(3A)-C(23A) 	1.75(2)

Co(3A)-C(24A) 	1.80(2)

Co(3A)-C(15A) 	1.870(19)

C(1A)-C(2A) 	1.38(3)

C(1A)-C(10A) 	1.38(3)

C(2A)-C(3A) 	1.38(3)

C(3A)-C(4A) 	1.40(3)

C(4A)-C(11A) 	1.34(3)

C(5A)-C(12A) 	1.38(3)

C(5A)-C(6A) 	1.38(3)

C(6A)-C(7A) 	1.41(3)

C(7A)-C(8A) 	1.42(3)

C(8A)-C(13A) 	1.37(3)

C(9A)-C(10A) 	1.52(3)

C(9A)-C(14A) 	1.53(3)

C(9A)-C(13A) 	1.55(3)

C(10A)-C(11A) 	1.39(3)

C(11A)-C(12A) 	1.50(3)

C(12A)-C(13A) 	1.38(3)

C(14A)-C(15A) 	1.58(3)

O(16A)-C(16A) 	1.15(3)

O(17A)-C(17A) 	1.16(2)

O(18A)-C(18A) 	1.11(2)

O(19A)-C(19A) 	1.17(2)

O(20A)-C(20A) 	1.12(2)

O(21A)-C(21A) 	1.14(2)

O(22A)-C(22A) 	1.20(2)

O(23A)-C(23A) 	1.18(2)

O(24A)-C(24A) 	1.17(2)

Co(1B)-C(18B) 	1.75(3)

Co(1B)-C(17B) 	1.77(2)

Co(1B)-C(16B) 	1.81(2)

Co(1B)-C(15B) 	1.886(19)

Co(1B)-Co(2B) 	2.453(4)

Co(1B)-Co(3B) 	2.461(4)

Co(2B)-C(21B) 	1.76(2)

Co(2B)-C(19B) 	1.80(2)

Co(2B)-C(20B) 	1.82(2)

Co(2B)-C(15B) 	1.911(19)

Co(2B)-Co(3B) 	2.453(4)

Co(3B)-C(23B) 	1.80(2)

Co(3B)-C(22B) 	1.80(2)

Co(3B)-C(24B) 	1.84(2)

Co(3B)-C(15B) 	1.903(17)

C(1B)-C(10B) 	1.41(3)

C(1B)-C(2B) 	1.43(3)

C(2B)-C(3B) 	1.39(3)

C(3B)-C(4B) 	1.31(3)

C(4B)-C(11B) 	1.43(3)

C(5B)-C(12B) 	1.33(3)

C(5B)-C(6B) 	1.40(3)

C(6B)-C(7B) 	1.36(3)

C(7B)-C(8B) 	1.36(3)

C(8B)-C(13B) 	1.37(3)

C(9B)-C(13B) 	1.53(3)

C(9B)-C(14B) 	1.53(3)

C(9B)-C(10B) 	1.55(3)

C(10B)-C(11B) 	1.37(3)

C(11B)-C(12B) 	1.47(3)

C(12B)-C(13B) 	1.40(3)

C(14B)-C(15B) 	1.50(3)

O(16B)-C(16B) 	1.13(2)

O(17B)-C(17B) 	1.15(2)

O(18B)-C(18B) 	1.20(3)

O(19B)-C(19B) 	1.14(2)

O(20B)-C(20B) 	1.15(2)

O(21B)-C(21B) 	1.17(2)

O(22B)-C(22B) 	1.16(2)

O(23B)-C(23B) 	1.14(2)

O(24B)-C(24B) 	1.12(2)

C(16)-Co(1)-C(18)	100.4(10)

C(16)-Co(1)-C(17)	95.3(10)

C(18)-Co(1)-C(17)	103.4(10)

C(16)-Co(1)-C(15)	109.3(9)

C(18)-Co(1)-C(15)	139.0(9)

C(17)-Co(1)-C(15)	101.3(9)

C(16)-Co(1)-Co(2)	155.8(8)

C(18)-Co(1)-Co(2)	93.7(7)

C(17)-Co(1)-Co(2)	100.5(7)

C(15)-Co(1)-Co(2)	49.7(6)

C(16)-Co(1)-Co(3)	98.5(7)

C(18)-Co(1)-Co(3)	98.5(7)

C(17)-Co(1)-Co(3)	151.5(7)

C(15)-Co(1)-Co(3)	50.5(5)

Co(2)-Co(1)-Co(3)	59.74(11)

C(20)-Co(2)-C(19)	96.9(9)

C(20)-Co(2)-C(21)	101.2(9)

C(19)-Co(2)-C(21)	103.1(9)

C(20)-Co(2)-C(15)	100.7(9)

C(19)-Co(2)-C(15)	100.4(8)

C(21)-Co(2)-C(15)	145.6(8)

C(20)-Co(2)-Co(3)	98.9(6)

C(19)-Co(2)-Co(3)	149.2(7)

C(21)-Co(2)-Co(3)	99.6(6)

C(15)-Co(2)-Co(3)	50.7(5)

C(20)-Co(2)-Co(1)	149.7(7)

C(19)-Co(2)-Co(1)	93.9(7)

C(21)-Co(2)-Co(1)	103.8(6)

C(15)-Co(2)-Co(1)	49.4(6)

Co(3)-Co(2)-Co(1)	60.30(11)

C(22)-Co(3)-C(23)	97.0(10)

C(22)-Co(3)-C(24)	98.0(9)

C(23)-Co(3)-C(24)	105.1(10)

C(22)-Co(3)-C(15)	107.6(9)

C(23)-Co(3)-C(15)	99.6(9)

C(24)-Co(3)-C(15)	141.7(9)

C(22)-Co(3)-Co(2)	154.0(7)

C(23)-Co(3)-Co(2)	99.2(7)

C(24)-Co(3)-Co(2)	97.2(6)

C(15)-Co(3)-Co(2)	49.6(6)

C(22)-Co(3)-Co(1)	96.4(7)

C(23)-Co(3)-Co(1)	148.6(7)

C(24)-Co(3)-Co(1)	100.9(6)

C(15)-Co(3)-Co(1)	49.1(6)

Co(2)-Co(3)-Co(1)	59.96(11)

C(10)-C(1)-C(2)	117(2)

C(3)-C(2)-C(1)	120(2)

C(4)-C(3)-C(2)	122(2)

C(3)-C(4)-C(11)	118(2)

C(6)-C(5)-C(12)	114.9(18)

C(7)-C(6)-C(5)	123(2)

C(6)-C(7)-C(8)	118.9(19)

C(13)-C(8)-C(7)	120.9(19)

C(13)-C(9)-C(14)	115.4(16)

C(13)-C(9)-C(10)	102.7(16)

C(14)-C(9)-C(10)	117.3(15)

C(11)-C(10)-C(1)	122.4(18)

C(11)-C(10)-C(9)	109.4(16)

C(1)-C(10)-C(9)	128.0(19)

C(10)-C(11)-C(4)	121.2(19)

C(10)-C(11)-C(12)	110.1(16)

C(4)-C(11)-C(12)	128.5(19)

C(13)-C(12)-C(5)	123.7(17)

C(13)-C(12)-C(11)	106.9(17)

C(5)-C(12)-C(11)	129.4(17)

C(8)-C(13)-C(12)	118.7(18)

C(8)-C(13)-C(9)	130.1(18)

C(12)-C(13)-C(9)	110.6(16)

C(15)-C(14)-C(9)	123.2(15)

C(14)-C(15)-Co(1)	135.9(13)

C(14)-C(15)-Co(2)	127.0(12)

Co(1)-C(15)-Co(2)	80.9(8)

C(14)-C(15)-Co(3)	132.4(13)

Co(1)-C(15)-Co(3)	80.4(7)

Co(2)-C(15)-Co(3)	79.6(7)

O(16)-C(16)-Co(1)	174(2)

O(17)-C(17)-Co(1)	176(2)

O(18)-C(18)-Co(1)	179(2)

O(19)-C(19)-Co(2)	179(2)

O(20)-C(20)-Co(2)	175.0(19)

O(21)-C(21)-Co(2)	178.1(19)

O(22)-C(22)-Co(3)	175.8(19)

O(23)-C(23)-Co(3)	176(2)

O(24)-C(24)-Co(3)	177.9(19)

C(16A)-Co(1A)-C(17A)	96.4(10)

C(16A)-Co(1A)-C(18A)	98.0(10)

C(17A)-Co(1A)-C(18A)	103.3(9)

C(16A)-Co(1A)-C(15A)	110.0(9)

C(17A)-Co(1A)-C(15A)	102.1(9)

C(18A)-Co(1A)-C(15A)	139.4(9)

C(16A)-Co(1A)-Co(2A)	155.6(7)

C(17A)-Co(1A)-Co(2A)	100.2(7)

C(18A)-Co(1A)-Co(2A)	95.4(6)

C(15A)-Co(1A)-Co(2A)	49.0(6)

C(16A)-Co(1A)-Co(3A)	97.5(7)

C(17A)-Co(1A)-Co(3A)	150.6(6)

C(18A)-Co(1A)-Co(3A)	100.3(6)

C(15A)-Co(1A)-Co(3A)	48.6(6)

Co(2A)-Co(1A)-Co(3A)	59.99(11)

C(19A)-Co(2A)-C(21A)	97.6(9)

C(19A)-Co(2A)-C(20A)	99.2(9)

C(21A)-Co(2A)-C(20A)	105.4(9)

C(19A)-Co(2A)-C(15A)	104.0(9)

C(21A)-Co(2A)-C(15A)	97.2(9)

C(20A)-Co(2A)-C(15A)	144.9(9)

C(19A)-Co(2A)-Co(1A)	97.0(6)

C(21A)-Co(2A)-Co(1A)	145.7(7)

C(20A)-Co(2A)-Co(1A)	102.6(6)

C(15A)-Co(2A)-Co(1A)	49.0(5)

C(19A)-Co(2A)-Co(3A)	151.6(7)

C(21A)-Co(2A)-Co(3A)	94.5(7)

C(20A)-Co(2A)-Co(3A)	102.2(7)

C(15A)-Co(2A)-Co(3A)	48.8(6)

Co(1A)-Co(2A)-Co(3A)	60.23(11)

C(22A)-Co(3A)-C(23A)	96.3(9)

C(22A)-Co(3A)-C(24A)	100.0(9)

C(23A)-Co(3A)-C(24A)	101.2(9)

C(22A)-Co(3A)-C(15A)	108.8(9)

C(23A)-Co(3A)-C(15A)	103.1(9)

C(24A)-Co(3A)-C(15A)	139.6(9)

C(22A)-Co(3A)-Co(2A)	155.1(6)

C(23A)-Co(3A)-Co(2A)	99.7(7)

C(24A)-Co(3A)-Co(2A)	95.5(7)

C(15A)-Co(3A)-Co(2A)	48.9(6)

C(22A)-Co(3A)-Co(1A)	98.0(6)

C(23A)-Co(3A)-Co(1A)	151.4(7)

C(24A)-Co(3A)-Co(1A)	100.5(7)

C(15A)-Co(3A)-Co(1A)	48.8(5)

Co(2A)-Co(3A)-Co(1A)	59.78(11)

C(2A)-C(1A)-C(10A)	118.2(19)

C(1A)-C(2A)-C(3A)	122.4(19)

C(2A)-C(3A)-C(4A)	118(2)

C(11A)-C(4A)-C(3A)	119.1(19)

C(12A)-C(5A)-C(6A)	120(2)

C(5A)-C(6A)-C(7A)	120.3(19)

C(6A)-C(7A)-C(8A)	118.7(19)

C(13A)-C(8A)-C(7A)	119(2)

C(10A)-C(9A)-C(14A)	117.5(18)

C(10A)-C(9A)-C(13A)	101.1(16)

C(14A)-C(9A)-C(13A)	115.0(16)

C(1A)-C(10A)-C(11A)	119(2)

C(1A)-C(10A)-C(9A)	128.6(18)

C(11A)-C(10A)-C(9A)	112.0(17)

C(4A)-C(11A)-C(10A)	122.6(18)

C(4A)-C(11A)-C(12A)	130.4(18)

C(10A)-C(11A)-C(12A)	106.9(18)

C(13A)-C(12A)-C(5A)	120.1(19)

C(13A)-C(12A)-C(11A)	109.7(16)

C(5A)-C(12A)-C(11A)	130(2)

C(8A)-C(13A)-C(12A)	121.6(18)

C(8A)-C(13A)-C(9A)	128.2(19)

C(12A)-C(13A)-C(9A)	109.9(17)

C(9A)-C(14A)-C(15A)	122.8(16)

C(14A)-C(15A)-Co(3A)	134.5(14)

C(14A)-C(15A)-Co(2A)	123.5(13)

Co(3A)-C(15A)-Co(2A)	82.4(8)

C(14A)-C(15A)-Co(1A)	133.0(13)

Co(3A)-C(15A)-Co(1A)	82.6(8)

Co(2A)-C(15A)-Co(1A)	82.0(7)

O(16A)-C(16A)-Co(1A)	177(2)

O(17A)-C(17A)-Co(1A)	176.2(18)

O(18A)-C(18A)-Co(1A)	176(2)

O(19A)-C(19A)-Co(2A)	174.2(19)

O(20A)-C(20A)-Co(2A)	173(2)

O(21A)-C(21A)-Co(2A)	178(2)

O(22A)-C(22A)-Co(3A)	177.3(18)

O(23A)-C(23A)-Co(3A)	175.8(19)

O(24A)-C(24A)-Co(3A)	179(2)

C(18B)-Co(1B)-C(17B)	100.5(10)

C(18B)-Co(1B)-C(16B)	100.6(10)

C(17B)-Co(1B)-C(16B)	94.6(10)

C(18B)-Co(1B)-C(15B)	140.6(10)

C(17B)-Co(1B)-C(15B)	102.9(9)

C(16B)-Co(1B)-C(15B)	108.5(9)

C(18B)-Co(1B)-Co(2B)	94.3(8)

C(17B)-Co(1B)-Co(2B)	101.4(7)

C(16B)-Co(1B)-Co(2B)	155.6(7)

C(15B)-Co(1B)-Co(2B)	50.2(6)

C(18B)-Co(1B)-Co(3B)	101.0(7)

C(17B)-Co(1B)-Co(3B)	152.4(7)

C(16B)-Co(1B)-Co(3B)	98.1(6)

C(15B)-Co(1B)-Co(3B)	49.8(5)

Co(2B)-Co(1B)-Co(3B)	59.89(11)

C(21B)-Co(2B)-C(19B)	98.8(9)

C(21B)-Co(2B)-C(20B)	101.4(9)

C(19B)-Co(2B)-C(20B)	103.8(9)

C(21B)-Co(2B)-C(15B)	98.5(9)

C(19B)-Co(2B)-C(15B)	101.5(9)

C(20B)-Co(2B)-C(15B)	144.8(9)

C(21B)-Co(2B)-Co(3B)	96.6(6)

C(19B)-Co(2B)-Co(3B)	149.3(7)

C(20B)-Co(2B)-Co(3B)	98.9(6)

C(15B)-Co(2B)-Co(3B)	49.8(5)

C(21B)-Co(2B)-Co(1B)	147.3(7)

C(19B)-Co(2B)-Co(1B)	93.9(7)

C(20B)-Co(2B)-Co(1B)	104.6(7)

C(15B)-Co(2B)-Co(1B)	49.3(6)

Co(3B)-Co(2B)-Co(1B)	60.20(11)

C(23B)-Co(3B)-C(22B)	98.4(9)

C(23B)-Co(3B)-C(24B)	100.6(10)

C(22B)-Co(3B)-C(24B)	100.1(9)

C(23B)-Co(3B)-C(15B)	102.4(9)

C(22B)-Co(3B)-C(15B)	105.9(8)

C(24B)-Co(3B)-C(15B)	142.0(9)

C(23B)-Co(3B)-Co(2B)	98.8(7)

C(22B)-Co(3B)-Co(2B)	153.2(6)

C(24B)-Co(3B)-Co(2B)	96.8(6)

C(15B)-Co(3B)-Co(2B)	50.1(6)

C(23B)-Co(3B)-Co(1B)	151.0(7)

C(22B)-Co(3B)-Co(1B)	96.2(6)

C(24B)-Co(3B)-Co(1B)	101.4(7)

C(15B)-Co(3B)-Co(1B)	49.2(6)

Co(2B)-Co(3B)-Co(1B)	59.91(12)

C(10B)-C(1B)-C(2B)	114(2)

C(3B)-C(2B)-C(1B)	121(2)

C(4B)-C(3B)-C(2B)	122(2)

C(3B)-C(4B)-C(11B)	121(2)

C(12B)-C(5B)-C(6B)	120(2)

C(7B)-C(6B)-C(5B)	120(2)

C(6B)-C(7B)-C(8B)	120(2)

C(7B)-C(8B)-C(13B)	120(2)

C(13B)-C(9B)-C(14B)	117.4(17)

C(13B)-C(9B)-C(10B)	99.5(15)

C(14B)-C(9B)-C(10B)	118.1(16)

C(11B)-C(10B)-C(1B)	124.0(19)

C(11B)-C(10B)-C(9B)	111.9(17)

C(1B)-C(10B)-C(9B)	123.9(18)

C(10B)-C(11B)-C(4B)	117.5(19)

C(10B)-C(11B)-C(12B)	108.8(17)

C(4B)-C(11B)-C(12B)	134(2)

C(5B)-C(12B)-C(13B)	120.4(19)

C(5B)-C(12B)-C(11B)	132(2)

C(13B)-C(12B)-C(11B)	107.9(18)

C(8B)-C(13B)-C(12B)	119(2)

C(8B)-C(13B)-C(9B)	129.0(19)

C(12B)-C(13B)-C(9B)	111.6(17)

C(15B)-C(14B)-C(9B)	121.5(16)

C(14B)-C(15B)-Co(1B)	136.1(14)

C(14B)-C(15B)-Co(3B)	134.7(14)

Co(1B)-C(15B)-Co(3B)	81.0(7)

C(14B)-C(15B)-Co(2B)	123.4(13)

Co(1B)-C(15B)-Co(2B)	80.5(8)

Co(3B)-C(15B)-Co(2B)	80.1(7)

O(16B)-C(16B)-Co(1B)	176(2)

O(17B)-C(17B)-Co(1B)	177(2)

O(18B)-C(18B)-Co(1B)	176(2)

O(19B)-C(19B)-Co(2B)	179(2)

O(20B)-C(20B)-Co(2B)	178.2(19)

O(21B)-C(21B)-Co(2B)	180(2)

O(22B)-C(22B)-Co(3B)	176.1(19)

O(23B)-C(23B)-Co(3B)	175(2)

O(24B)-C(24B)-Co(3B)	179(2)

______________________________________________________________________________________

Table G4:  Anisotropic displacement parameters (Å2 x 103) for 120.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	14(2) 	26(2)	11(2) 	-1(1)	1(1) 	1(1)

Co(2)	15(2) 	24(2)	17(2) 	-1(1)	-1(1) 	1(1)

Co(3)	12(2) 	29(2)	16(2) 	5(1)	1(1) 	5(1)

C(1)	18(8) 	37(12)	33(15) 	1(10)	12(9) 	-11(7)

C(2)	24(6) 	40(8)	23(8) 	11(6)	0(6) 	-4(6)

C(3)	22(8) 	36(12)	39(17) 	17(10)	7(9) 	-2(9)

C(4)	17(8) 	34(12)	37(16) 	5(10)	14(9) 	3(7)

C(5)	33(8) 	10(10)	17(14) 	1(8)	10(9) 	6(8)

C(6)	34(6) 	24(7)	20(8) 	-3(6)	4(6) 	-3(6)

C(7)	20(9) 	28(13)	38(16) 	-1(10)	-2(10) 	-9(7)

C(8)	15(5) 	26(7)	20(8) 	-5(6)	6(6) 	0(5)

C(9)	20(7) 	21(11)	25(15) 	-5(9)	3(9) 	-5(7)

C(10)	19(5) 	16(7)	11(8) 	10(6)	3(6) 	-1(5)

C(11)	23(5) 	21(7)	15(8) 	7(6)	6(6) 	2(5)

C(12)	27(7) 	14(10)	8(13) 	6(8)	6(8) 	3(6)

C(13)	16(5) 	12(7)	9(8) 	1(6)	3(6) 	-1(5)

C(14)	7(7) 	10(8)	5(8) 	-3(6)	-1(6) 	-1(6)

C(15)	13(6) 	14(7)	10(7) 	-6(5)	7(5) 	1(5)

O(16)	47(10) 	55(14)	52(13) 	-6(10)	25(9) 	-3(9)

O(17)	4(8) 	56(12)	79(14) 	4(10)	8(8) 	-5(7)

O(18)	33(9) 	44(11)	24(11) 	3(8)	7(8) 	10(7)

O(19)	34(10) 	57(12)	36(11) 	-18(9)	9(8) 	8(8)

O(20)	41(9) 	42(11)	39(11) 	-21(9)	16(8) 	-15(8)

O(21)	33(9) 	42(11)	32(11) 	16(8)	13(8) 	1(7)

O(22)	31(8) 	46(12)	19(10) 	4(8)	0(7) 	5(8)

O(23)	40(10) 	43(12)	68(14) 	-4(10)	3(10) 	-14(8)

O(24)	33(9) 	53(12)	39(11) 	30(9)	13(8) 	15(8)

Co(1A)	11(1) 	26(2)	20(2) 	1(1)	4(1) 	3(1)

Co(2A)	13(2) 	24(2)	14(2) 	-1(1)	0(1) 	2(1)

Co(3A)	13(2) 	21(2)	21(2) 	-3(1)	5(1) 	1(1)

C(1A)	15(7) 	21(12)	31(15) 	16(9)	7(9) 	5(8)

C(2A)	11(9) 	40(15)	57(19) 	1(11)	3(10) 	-8(8)

C(3A)	32(9) 	21(12)	20(14) 	8(9)	5(9) 	-7(8)

C(4A)	23(8) 	17(12)	44(17) 	-2(10)	9(9) 	11(8)

C(5A)	24(8) 	27(13)	21(14) 	4(9)	5(9) 	11(8)

C(6A)	15(8) 	35(13)	38(17) 	14(10)	5(9) 	5(9)

C(7A)	22(8) 	33(14)	41(17) 	12(10)	-7(10) 	-6(9)

C(8A)	32(6) 	18(7)	18(8) 	10(6)	0(6) 	-2(5)

C(9A)	24(7) 	27(12)	14(13) 	-4(9)	10(8) 	4(7)

C(10A)	21(7) 	25(13)	49(17) 	-14(10)	6(10) 	5(8)

C(11A)	21(7) 	10(10)	18(14) 	13(8)	7(8) 	6(6)

C(12A)	16(5) 	22(7)	29(8) 	4(6)	13(6) 	0(5)

C(13A)	22(7) 	22(11)	11(13) 	10(8)	6(8) 	3(7)

C(14A)	14(11) 	26(16)	34(16) 	4(12)	1(10) 	11(10)

C(15A)	16(7) 	17(8)	12(8) 	-4(6)	8(6) 	-1(6)

O(16A)	41(9) 	33(11)	45(12) 	14(8)	15(8) 	5(8)

O(17A)	53(10) 	52(12)	20(11) 	-10(8)	-11(9) 	-6(9)

O(18A)	47(10) 	56(13)	35(11) 	16(9)	17(9) 	-6(8)

O(19A)	34(8) 	32(10)	21(10) 	-10(8)	-1(7) 	-17(7)

O(20A)	37(9) 	43(11)	37(11) 	14(9)	2(8) 	5(8)

O(21A)	17(8) 	59(13)	60(13) 	-14(9)	12(8) 	5(7)

O(22A)	39(9) 	25(11)	25(10) 	14(7)	18(7) 	8(7)

O(23A)	14(8) 	55(13)	87(15) 	6(10)	-1(8) 	-5(8)

O(24A)	36(9) 	53(12)	48(13) 	13(9)	12(9) 	14(8)

Co(1B)	14(2) 	23(2)	20(2) 	3(1)	1(1) 	-5(1)

Co(2B)	16(2) 	23(2)	16(2) 	0(1)	2(1) 	0(1)

Co(3B)	11(1) 	19(2)	20(2) 	0(1)	2(1) 	-2(1)

C(1B)	37(9) 	27(15)	19(9) 	12(11)	-1(7) 	-2(10)

C(2B)	36(9) 	14(14)	30(11) 	17(11)	-8(9) 	4(10)

C(3B)	20(9) 	41(17)	46(13) 	5(13)	6(8) 	-11(10)

C(4B)	30(8) 	27(15)	31(11) 	4(11)	9(8) 	9(10)

C(5B)	60(10) 	23(14)	22(8) 	1(11)	5(8) 	14(12)

C(6B)	57(8) 	44(9)	33(8) 	1(7)	-3(6) 	3(7)

C(7B)	53(12) 	61(19)	21(10) 	3(14)	-21(9) 	20(13)

C(8B)	26(8) 	30(15)	24(9) 	3(11)	-6(7) 	-1(10)

C(9B)	25(8) 	18(13)	17(8) 	1(10)	6(6) 	-8(9)

C(10B)	25(8) 	24(14)	15(8) 	1(10)	3(6) 	-3(9)

C(11B)	22(5) 	26(8)	21(6) 	-2(6)	8(5) 	-12(6)

C(12B)	28(8) 	16(13)	19(7) 	9(10)	5(6) 	-6(9)

C(13B)	27(8) 	15(13)	18(9) 	11(10)	-2(6) 	-5(9)

C(14B)	5(10) 	35(15)	7(13) 	-6(11)	-3(9) 	4(10)

C(15B)	15(7) 	16(8)	9(8) 	1(6)	5(6) 	-8(6)

O(16B)	50(10) 	39(11)	37(12) 	-17(9)	16(9) 	-3(8)

O(17B)	22(10) 	140(20)	71(16) 	20(13)	-22(9) 	-18(10)

O(18B)	37(9) 	47(12)	22(10) 	14(8)	-3(7) 	2(8)

O(19B)	17(9) 	93(15)	55(13) 	9(10)	26(8) 	-3(8)

O(20B)	41(10) 	14(10)	68(13) 	-13(9)	-14(8) 	-2(8)

O(21B)	49(10) 	72(13)	9(10) 	8(9)	1(8) 	13(9)

O(22B)	76(12) 	40(12)	43(12) 	-5(9)	43(10) 	-11(9)

O(23B)	34(6) 	32(7)	31(7) 	6(6)	-16(6) 	-2(5)

O(24B)	30(8) 	42(12)	42(12) 	-6(9)	-1(8) 	-10(8)

______________________________________________________________________________

Table G5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 10 3)

for 120.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1)	6623	1893	7451	34

H(2)	8961	1467	7529	36

H(3)	8893	757	7204	38

H(4)	6624	471	6745	34

H(5)	3786	284	6279	23

H(6)	1091	267	5968	31

H(7)	-507	862	6062	35

H(8)	519	1466	6546	24

H(9)	3283	1609	7294	26

H(14A)	2293	2148	6737	9

H(14B)	3978	2274	7014	9

H(1A)	4186	4994	3573	26

H(2A)	5055	5624	4012	44

H(3A)	3328	6161	4194	29

H(4A)	714	6124	3791	33

H(5A)	-2098	5904	3357	29

H(6A)	-4322	5619	2869	35

H(7A)	-4229	4928	2476	40

H(8A)	-1781	4567	2519	28

H(9A)	1497	4859	2741	25

H(14C)	2413	4287	3257	30

H(14D)	704	4179	2987	30

H(1B)	758	5578	2311	34

H(2B)	3381	5399	2199	34

H(3B)	3970	5247	1402	43

H(4B)	2180	5280	710	35

H(5B)	-493	5397	14	42

H(6B)	-2982	5520	-440	55

H(7B)	-4993	5728	-17	57

H(8B)	-4565	5820	850	33

H(9B)	-2257	5417	1667	24

H(14E)	-3343	6094	1755	20

H(14F)	-1832	6030	2162	20

________________________________________________________________________________

Table H1:  Crystal data and structure refinement for 121.

Empirical formula 	C48 H42 Si2

Formula weight 	675.00

Temperature 	173(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)/c

Unit cell dimensions	a = 13.467(6) Å	(= 90°.

b = 16.297(7) Å	(= 95.692(8)°.

c = 8.923(4) Å	(= 90°.

Volume	1948.7(14) Å3

Z	2

Density (calculated)	1.150 Mg/m3

Absorption coefficient	0.123 mm-1

F(000)	716

Crystal size	.1 x .3 x .5 mm3

( range for data collection	1.97 to 25.00°.

Index ranges	-16(h(15, -19(k(19, -9(l(10

Reflections collected	14547

Independent reflections	3424 [R(int) = 0.0522]

Completeness to ( = 25.00°	99.9 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3424 / 36 / 296

Goodness-of-fit on F2	1.020

Final R indices [I>2((I)]	R1 = 0.0651, wR2 = 0.1168

R indices (all data)	R1 = 0.1189, wR2 = 0.1388

Extinction coefficient	0.0054(7)

Largest diff. peak and hole	0.343 and -0.305 e.Å-3

Ratio of min/max apparent transmission  	0.916917

Table H2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 121.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Si(1)	8381(1)	5469(1)	2177(2)	47(1)

Si(2)	11374(2)	4126(2)	8668(2)	57(1)

C(1)	11951(11)	4437(14)	3090(30)	55(3)

C(2)	12877(13)	4148(19)	2750(50)	60(4)

C(3)	13721(13)	4590(20)	3180(50)	62(4)

C(4)	13694(14)	5283(17)	4070(50)	58(3)

C(5)	13112(19)	6868(11)	6100(30)	55(4)

C(6)	12650(30)	7485(17)	6820(50)	72(6)

C(7)	11630(30)	7480(30)	6900(100)	75(7)

C(8)	11030(30)	6890(70)	6100(200)	69(2)

C(9)	11021(9)	5587(11)	4446(15)	41(2)

C(10)	11906(10)	5155(11)	3900(20)	39(3)

C(11)	12780(16)	5550(30)	4490(80)	44(3)

C(12)	12531(14)	6233(9)	5440(30)	39(3)

C(13)	11472(13)	6320(12)	5250(20)	41(3)

C(14)	10093(5)	5349(5)	4150(8)	46(1)

C(15)	9185(4)	5099(3)	3920(6)	44(1)

C(16)	9212(6)	6115(5)	1058(10)	84(3)

C(17)	7848(9)	4606(7)	1062(11)	66(2)

C(18)	7391(10)	6129(8)	2820(13)	67(2)

C(19)	6625(9)	6353(6)	1553(15)	45(2)

C(20)	6749(6)	7106(6)	864(13)	51(2)

C(21)	6003(5)	7412(4)	-174(9)	57(2)

C(22)	5132(5)	6964(5)	-525(9)	65(3)

C(23)	5008(8)	6211(6)	164(11)	77(3)

C(24)	5754(11)	5906(6)	1203(13)	61(2)

C(25)	7773(11)	5559(14)	6590(30)	55(3)

C(26)	6839(13)	5747(19)	7040(50)	60(4)

C(27)	6029(13)	5260(20)	6630(50)	62(4)

C(28)	6127(14)	4530(18)	5880(50)	58(3)

C(29)	6889(18)	2915(11)	4080(30)	55(4)

C(30)	7410(30)	2333(18)	3360(50)	72(6)

C(31)	8410(30)	2410(30)	3240(100)	75(7)

C(32)	8920(30)	3110(70)	3800(200)	69(2)

C(33)	8772(10)	4512(11)	5135(16)	41(2)

C(34)	7857(10)	4856(11)	5747(19)	39(3)

C(35)	7061(15)	4310(30)	5480(80)	44(3)

C(36)	7407(14)	3580(9)	4740(30)	39(3)

C(37)	8396(13)	3742(12)	4370(20)	41(3)

C(38)	9594(6)	4358(5)	6318(9)	46(1)

C(39)	10282(5)	4263(4)	7286(7)	63(2)

C(40)	11015(5)	3433(4)	10175(7)	66(2)

C(41)	11837(8)	5145(6)	9402(11)	66(2)

C(42)	12347(10)	3609(8)	7638(12)	67(2)

C(43)	13378(9)	3433(6)	8480(15)	45(2)

C(44)	14117(11)	4016(6)	8344(12)	61(2)

C(45)	15005(9)	3980(6)	9278(10)	77(3)

C(46)	15155(5)	3361(5)	10348(9)	65(3)

C(47)	14416(5)	2778(4)	10484(9)	57(2)

C(48)	13527(5)	2814(6)	9550(13)	51(2)

Table H3:  Bond lengths [Å] and angles [°] for 121.

______________________________________________________________________________________

Si(1)-C(17) 	1.828(12)

Si(1)-C(18) 	1.849(14)

Si(1)-C(16) 	1.891(8)

Si(1)-C(15) 	1.903(6)

Si(2)-C(39) 	1.837(7)

Si(2)-C(40) 	1.856(7)

Si(2)-C(41) 	1.869(11)

Si(2)-C(42) 	1.873(13)

C(1)-C(10) 	1.381(10)

C(1)-C(2) 	1.394(11)

C(1)-H(1) 	0.9500

C(2)-C(3) 	1.367(11)

C(2)-H(2) 	0.9500

C(3)-C(4) 	1.387(12)

C(3)-H(3) 	0.9500

C(4)-C(11) 	1.389(10)

C(4)-H(4) 	0.9500

C(5)-C(6) 	1.377(11)

C(5)-C(12) 	1.390(10)

C(5)-H(5) 	0.9500

C(6)-C(7) 	1.375(11)

C(6)-H(6) 	0.9500

C(7)-C(8) 	1.39(3)

C(7)-H(7) 	0.9500

C(8)-C(13) 	1.39(2)

C(8)-H(8) 	0.9500

C(9)-C(14) 	1.310(15)

C(9)-C(13) 	1.493(10)

C(9)-C(10) 	1.506(10)

C(10)-C(11) 	1.395(15)

C(11)-C(12) 	1.462(11)

C(12)-C(13) 	1.427(12)

C(14)-C(15) 	1.287(9)

C(15)-C(33) 	1.587(18)

C(16)-H(16A) 	0.9800

C(16)-H(16B) 	0.9800

C(16)-H(16C) 	0.9800

C(17)-H(17A) 	0.9800

C(17)-H(17B) 	0.9800

C(17)-H(17C) 	0.9800

C(18)-C(19) 	1.498(15)

C(18)-H(18A) 	0.9900

C(18)-H(18B) 	0.9900

C(19)-C(20) 	1.3900

C(19)-C(24) 	1.3900

C(20)-C(21) 	1.3900

C(20)-H(20) 	0.9500

C(21)-C(22) 	1.3900

C(21)-H(21) 	0.9500

C(22)-C(23) 	1.3900

C(22)-H(22) 	0.9500

C(23)-C(24) 	1.3900

C(23)-H(23) 	0.9500

C(24)-H(24) 	0.9500

C(25)-C(34) 	1.380(10)

C(25)-C(26) 	1.392(11)

C(25)-H(25) 	0.9500

C(26)-C(27) 	1.364(11)

C(26)-H(26) 	0.9500

C(27)-C(28) 	1.384(12)

C(27)-H(27) 	0.9500

C(28)-C(35) 	1.389(10)

C(28)-H(28) 	0.9500

C(29)-C(30) 	1.377(11)

C(29)-C(36) 	1.387(10)

C(29)-H(29) 	0.9500

C(30)-C(31) 	1.374(12)

C(30)-H(30) 	0.9500

C(31)-C(32) 	1.39(3)

C(31)-H(31) 	0.9500

C(32)-C(37) 	1.39(2)

C(32)-H(32) 	0.9500

C(33)-C(38) 	1.473(12)

C(33)-C(37) 	1.492(10)

C(33)-C(34) 	1.505(10)

C(34)-C(35) 	1.394(14)

C(35)-C(36) 	1.461(11)

C(36)-C(37) 	1.428(12)

C(38)-C(39) 	1.213(10)

C(40)-H(40A) 	0.9800

C(40)-H(40B) 	0.9800

C(40)-H(40C) 	0.9800

C(41)-H(41A) 	0.9800

C(41)-H(41B) 	0.9800

C(41)-H(41C) 	0.9800

C(42)-C(43) 	1.538(16)

C(42)-H(42A) 	0.9900

C(42)-H(42B) 	0.9900

C(43)-C(44) 	1.3900

C(43)-C(48) 	1.3900

C(44)-C(45) 	1.3900

C(44)-H(44) 	0.9500

C(45)-C(46) 	1.3900

C(45)-H(45) 	0.9500

C(46)-C(47) 	1.3900

C(46)-H(46) 	0.9500

C(47)-C(48) 	1.3900

C(47)-H(47) 	0.9500

C(48)-H(48) 	0.9500

C(17)-Si(1)-C(18)	111.1(6)

C(17)-Si(1)-C(16)	111.2(4)

C(18)-Si(1)-C(16)	108.8(4)

C(17)-Si(1)-C(15)	111.2(4)

C(18)-Si(1)-C(15)	107.5(4)

C(16)-Si(1)-C(15)	106.9(3)

C(39)-Si(2)-C(40)	108.2(3)

C(39)-Si(2)-C(41)	110.1(4)

C(40)-Si(2)-C(41)	112.9(4)

C(39)-Si(2)-C(42)	106.1(5)

C(40)-Si(2)-C(42)	109.1(4)

C(41)-Si(2)-C(42)	110.3(5)

C(10)-C(1)-C(2)	119.1(11)

C(10)-C(1)-H(1)	120.5

C(2)-C(1)-H(1)	120.5

C(3)-C(2)-C(1)	120.0(13)

C(3)-C(2)-H(2)	120.0

C(1)-C(2)-H(2)	120.0

C(2)-C(3)-C(4)	121.4(12)

C(2)-C(3)-H(3)	119.3

C(4)-C(3)-H(3)	119.3

C(3)-C(4)-C(11)	118.8(12)

C(3)-C(4)-H(4)	120.6

C(11)-C(4)-H(4)	120.6

C(6)-C(5)-C(12)	118.6(13)

C(6)-C(5)-H(5)	120.7

C(12)-C(5)-H(5)	120.7

C(7)-C(6)-C(5)	121.3(13)

C(7)-C(6)-H(6)	119.3

C(5)-C(6)-H(6)	119.4

C(6)-C(7)-C(8)	120.6(15)

C(6)-C(7)-H(7)	119.7

C(8)-C(7)-H(7)	119.6

C(13)-C(8)-C(7)	118.9(13)

C(13)-C(8)-H(8)	120.6

C(7)-C(8)-H(8)	120.4

C(14)-C(9)-C(13)	132.0(12)

C(14)-C(9)-C(10)	124.5(12)

C(13)-C(9)-C(10)	103.4(8)

C(1)-C(10)-C(11)	120.5(10)

C(1)-C(10)-C(9)	129.9(11)

C(11)-C(10)-C(9)	109.3(8)

C(4)-C(11)-C(10)	119.6(14)

C(4)-C(11)-C(12)	130.7(13)

C(10)-C(11)-C(12)	109.6(9)

C(5)-C(12)-C(13)	119.3(11)

C(5)-C(12)-C(11)	131.4(12)

C(13)-C(12)-C(11)	106.9(13)

C(8)-C(13)-C(12)	118(3)

C(8)-C(13)-C(9)	129.4(13)

C(12)-C(13)-C(9)	109.4(9)

C(15)-C(14)-C(9)	177.3(10)

C(14)-C(15)-C(33)	118.3(7)

C(14)-C(15)-Si(1)	119.0(5)

C(33)-C(15)-Si(1)	122.7(5)

Si(1)-C(16)-H(16A)	109.5

Si(1)-C(16)-H(16B)	109.5

H(16A)-C(16)-H(16B)	109.5

Si(1)-C(16)-H(16C)	109.5

H(16A)-C(16)-H(16C)	109.5

H(16B)-C(16)-H(16C)	109.5

Si(1)-C(17)-H(17A)	109.5

Si(1)-C(17)-H(17B)	109.5

H(17A)-C(17)-H(17B)	109.5

Si(1)-C(17)-H(17C)	109.5

H(17A)-C(17)-H(17C)	109.5

H(17B)-C(17)-H(17C)	109.5

C(19)-C(18)-Si(1)	111.8(10)

C(19)-C(18)-H(18A)	109.3

Si(1)-C(18)-H(18A)	109.3

C(19)-C(18)-H(18B)	109.3

Si(1)-C(18)-H(18B)	109.3

H(18A)-C(18)-H(18B)	107.9

C(20)-C(19)-C(24)	120.0

C(20)-C(19)-C(18)	116.4(7)

C(24)-C(19)-C(18)	123.0(7)

C(21)-C(20)-C(19)	120.0

C(21)-C(20)-H(20)	120.0

C(19)-C(20)-H(20)	120.0

C(20)-C(21)-C(22)	120.0

C(20)-C(21)-H(21)	120.0

C(22)-C(21)-H(21)	120.0

C(21)-C(22)-C(23)	120.0

C(21)-C(22)-H(22)	120.0

C(23)-C(22)-H(22)	120.0

C(24)-C(23)-C(22)	120.0

C(24)-C(23)-H(23)	120.0

C(22)-C(23)-H(23)	120.0

C(23)-C(24)-C(19)	120.0

C(23)-C(24)-H(24)	120.0

C(19)-C(24)-H(24)	120.0

C(34)-C(25)-C(26)	117.7(12)

C(34)-C(25)-H(25)	121.2

C(26)-C(25)-H(25)	121.2

C(27)-C(26)-C(25)	121.3(12)

C(27)-C(26)-H(26)	119.4

C(25)-C(26)-H(26)	119.4

C(26)-C(27)-C(28)	120.9(13)

C(26)-C(27)-H(27)	119.5

C(28)-C(27)-H(27)	119.5

C(27)-C(28)-C(35)	118.7(12)

C(27)-C(28)-H(28)	120.6

C(35)-C(28)-H(28)	120.6

C(30)-C(29)-C(36)	118.7(13)

C(30)-C(29)-H(29)	120.7

C(36)-C(29)-H(29)	120.6

C(31)-C(30)-C(29)	121.5(13)

C(31)-C(30)-H(30)	119.3

C(29)-C(30)-H(30)	119.3

C(30)-C(31)-C(32)	120.4(15)

C(30)-C(31)-H(31)	119.8

C(32)-C(31)-H(31)	119.7

C(37)-C(32)-C(31)	119.0(13)

C(37)-C(32)-H(32)	120.6

C(31)-C(32)-H(32)	120.4

C(38)-C(33)-C(37)	112.4(12)

C(38)-C(33)-C(34)	112.8(11)

C(37)-C(33)-C(34)	103.1(9)

C(38)-C(33)-C(15)	107.6(10)

C(37)-C(33)-C(15)	108.7(12)

C(34)-C(33)-C(15)	112.2(12)

C(25)-C(34)-C(35)	121.3(12)

C(25)-C(34)-C(33)	128.4(11)

C(35)-C(34)-C(33)	110.1(9)

C(28)-C(35)-C(34)	119.5(12)

C(28)-C(35)-C(36)	131.6(12)

C(34)-C(35)-C(36)	108.9(9)

C(29)-C(36)-C(37)	119.2(11)

C(29)-C(36)-C(35)	131.2(12)

C(37)-C(36)-C(35)	107.4(11)

C(32)-C(37)-C(36)	119(3)

C(32)-C(37)-C(33)	129.5(13)

C(36)-C(37)-C(33)	109.4(9)

C(39)-C(38)-C(33)	177.4(11)

C(38)-C(39)-Si(2)	176.7(6)

Si(2)-C(40)-H(40A)	109.5

Si(2)-C(40)-H(40B)	109.5

H(40A)-C(40)-H(40B)	109.5

Si(2)-C(40)-H(40C)	109.5

H(40A)-C(40)-H(40C)	109.5

H(40B)-C(40)-H(40C)	109.5

Si(2)-C(41)-H(41A)	109.5

Si(2)-C(41)-H(41B)	109.5

H(41A)-C(41)-H(41B)	109.5

Si(2)-C(41)-H(41C)	109.5

H(41A)-C(41)-H(41C)	109.5

H(41B)-C(41)-H(41C)	109.5

C(43)-C(42)-Si(2)	119.0(10)

C(43)-C(42)-H(42A)	107.6

Si(2)-C(42)-H(42A)	107.6

C(43)-C(42)-H(42B)	107.6

Si(2)-C(42)-H(42B)	107.6

H(42A)-C(42)-H(42B)	107.0

C(44)-C(43)-C(48)	120.0

C(44)-C(43)-C(42)	116.7(7)

C(48)-C(43)-C(42)	122.1(7)

C(43)-C(44)-C(45)	120.0

C(43)-C(44)-H(44)	120.0

C(45)-C(44)-H(44)	120.0

C(46)-C(45)-C(44)	120.0

C(46)-C(45)-H(45)	120.0

C(44)-C(45)-H(45)	120.0

C(45)-C(46)-C(47)	120.0

C(45)-C(46)-H(46)	120.0

C(47)-C(46)-H(46)	120.0

C(48)-C(47)-C(46)	120.0

C(48)-C(47)-H(47)	120.0

C(46)-C(47)-H(47)	120.0

C(47)-C(48)-C(43)	120.0

C(47)-C(48)-H(48)	120.0

C(43)-C(48)-H(48)	120.0

_____________________________________________________________________________________

Table H4:  Anisotropic displacement parameters (Å2 x 103) for 121.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Si(1)	41(1) 	58(1)	42(1) 	1(1)	2(1) 	-3(1)

Si(2)	50(1) 	75(2)	42(1) 	4(1)	-13(1) 	-6(1)

C(1)	52(7) 	62(2)	51(10) 	-2(4)	5(7) 	-5(5)

C(2)	63(10) 	61(7)	57(10) 	0(4)	15(11) 	7(8)

C(3)	45(8) 	79(11)	62(10) 	4(5)	9(10) 	10(7)

C(4)	39(6) 	69(11)	64(3) 	10(8)	2(7) 	-4(4)

C(5)	59(2) 	50(9)	53(6) 	16(7)	-13(3) 	-4(5)

C(6)	83(4) 	62(11)	65(9) 	-5(11)	-22(4) 	2(7)

C(7)	90(4) 	65(10)	66(11) 	-15(11)	-6(5) 	20(5)

C(8)	66(3) 	70(4)	71(8) 	-10(2)	10(5) 	5(3)

C(9)	24(5) 	57(4)	39(7) 	4(5)	-11(4) 	3(4)

C(10)	37(6) 	53(2)	26(7) 	7(4)	-6(5) 	5(4)

C(11)	36(5) 	48(11)	47(3) 	13(8)	6(8) 	-8(5)

C(12)	49(3) 	31(6)	38(5) 	25(5)	4(2) 	-5(4)

C(13)	49(4) 	49(3)	24(9) 	8(5)	-7(5) 	5(3)

C(14)	46(4) 	55(4)	36(4) 	-1(3)	0(2) 	-2(3)

C(15)	39(3) 	51(4)	40(3) 	-6(3)	2(3) 	-4(3)

C(16)	69(6) 	93(6)	90(7) 	26(5)	13(5) 	-29(5)

C(17)	77(6) 	70(6)	48(5) 	13(3)	-16(4) 	1(4)

C(18)	74(7) 	81(7)	44(6) 	4(4)	-5(4) 	9(4)

C(19)	60(2) 	22(5)	52(2) 	-7(3)	3(2) 	11(3)

C(20)	27(5) 	61(3)	63(7) 	11(3)	-11(4) 	25(4)

C(21)	36(6) 	57(4)	81(6) 	6(4)	19(5) 	-5(4)

C(22)	66(5) 	77(8)	53(4) 	12(5)	2(4) 	25(4)

C(23)	55(3) 	101(6)	71(8) 	-15(5)	-8(4) 	3(3)

C(24)	62(4) 	59(3)	58(7) 	-17(4)	-6(4) 	-13(2)

C(25)	52(7) 	62(2)	51(10) 	-2(4)	5(7) 	-5(5)

C(26)	63(10) 	61(7)	57(10) 	0(4)	15(11) 	7(8)

C(27)	45(8) 	79(11)	62(10) 	4(5)	9(10) 	10(7)

C(28)	39(6) 	69(11)	64(3) 	10(8)	2(7) 	-4(4)

C(29)	59(2) 	50(9)	53(6) 	16(7)	-13(3) 	-4(5)

C(30)	83(4) 	62(11)	65(9) 	-5(11)	-22(4) 	2(7)

C(31)	90(4) 	65(10)	66(11) 	-15(11)	-6(5) 	20(5)

C(32)	66(3) 	70(4)	71(8) 	-10(2)	10(5) 	5(3)

C(33)	24(5) 	57(4)	39(7) 	4(5)	-11(4) 	3(4)

C(34)	37(6) 	53(2)	26(7) 	7(4)	-6(5) 	5(4)

C(35)	36(5) 	48(11)	47(3) 	13(8)	6(8) 	-8(5)

C(36)	49(3) 	31(6)	38(5) 	25(5)	4(2) 	-5(4)

C(37)	49(4) 	49(3)	24(9) 	8(5)	-7(5) 	5(3)

C(38)	46(4) 	55(4)	36(4) 	-1(3)	0(2) 	-2(3)

C(39)	61(5) 	78(5)	49(4) 	12(4)	-6(3) 	-4(4)

C(40)	63(5) 	79(5)	52(4) 	5(4)	-15(3) 	-13(4)

C(41)	77(6) 	70(6)	48(5) 	13(3)	-16(4) 	1(4)

C(42)	74(7) 	81(7)	44(6) 	4(4)	-5(4) 	9(4)

C(43)	60(2) 	22(5)	52(2) 	-7(3)	3(2) 	11(3)

C(44)	62(4) 	59(3)	58(7) 	-17(4)	-6(4) 	-13(2)

C(45)	55(3) 	101(6)	71(8) 	-15(5)	-8(4) 	3(3)

C(46)	66(5) 	77(8)	53(4) 	12(5)	2(4) 	25(4)

C(47)	36(6) 	57(4)	81(6) 	6(4)	19(5) 	-5(4)

C(48)	27(5) 	61(3)	63(7) 	11(3)	-11(4) 	25(4)

Table H5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 10 3)

for 121.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1)	11358	4144	2766	66

H(2)	12921	3645	2225	72

H(3)	14338	4418	2852	74

H(4)	14290	5571	4399	69

H(5)	13813	6877	6044	66

H(6)	13038	7922	7274	86

H(7)	11340	7889	7477	90

H(8)	10336	6881	6212	83

H(16A)	8825	6319	146	125

H(16B)	9769	5780	776	125

H(16C)	9473	6580	1672	125

H(17A)	7439	4814	174	100

H(17B)	7433	4277	1675	100

H(17C)	8388	4265	741	100

H(18A)	7061	5837	3609	81

H(18B)	7695	6636	3272	81

H(20)	7344	7412	1104	62

H(21)	6088	7927	-645	69

H(22)	4622	7173	-1234	78

H(23)	4412	5906	-75	92

H(24)	5669	5391	1673	73

H(25)	8333	5903	6849	66

H(26)	6765	6221	7637	72

H(27)	5389	5435	6872	74

H(28)	5567	4183	5649	69

H(29)	6190	2863	4128	66

H(30)	7062	1868	2926	86

H(31)	8763	1981	2797	90

H(32)	9621	3162	3701	83

H(40A)	10510	3702	10724	99

H(40B)	11604	3309	10873	99

H(40C)	10741	2923	9724	99

H(41A)	11324	5407	9945	100

H(41B)	11985	5494	8559	100

H(41C)	12444	5067	10088	100

H(42A)	12066	3079	7254	81

H(42B)	12451	3950	6750	81

H(44)	14015	4440	7613	73

H(45)	15510	4379	9186	92

H(46)	15762	3336	10987	78

H(47)	14518	2355	11215	69

H(48)	13022	2416	9642	62

________________________________________________________________________________

Table I1:  Crystal data and structure refinement for 124.

Empirical formula 	C60 H42 Co4 O14 Si2

Formula weight 	1278.84

Temperature 	173(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 10.516(5) Å	(= 86.312(8)°.

b = 12.051(6) Å	(= 76.860(8)°.

c = 12.382(6) Å	(= 66.034(8)°.

Volume	1395.6(12) Å3

Z	1

Density (calculated)	1.522 Mg/m3

Absorption coefficient	1.278 mm-1

F(000)	650

Crystal size	0.45 x 0.40 x 0.30 mm3

( range for data collection	1.69 to 27.50°.

Index ranges	-13(h(12, -15(k(14, -16(l(15

Reflections collected	12858

Independent reflections	6305 [R(int) = 0.0315]

Completeness to ( = 27.50°	98.3 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6305 / 0 / 446

Goodness-of-fit on F2	1.009

Final R indices [I>2((I)]	R1 = 0.0323, wR2 = 0.0673

R indices (all data)	R1 = 0.0536, wR2 = 0.0759

Extinction coefficient	0.0005(4)

Largest diff. peak and hole	0.357 and -0.313 e.Å-3

Ratio of min/max apparent transmission	0.842652

Table I2:  Atomic coordinates ( x 104) and equivalent  isotropic displacement parameters (Å2 x 103)

for 124.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	3188(1)	2096(1)	1667(1)	22(1)

Co(2)	1797(1)	4130(1)	2580(1)	20(1)

Si(1)	374(1)	2038(1)	3799(1)	23(1)

C(1)	-2273(3)	4553(2)	2014(2)	27(1)

C(2)	-3551(3)	4399(3)	2344(2)	35(1)

C(3)	-3694(3)	3434(3)	1925(2)	38(1)

C(4)	-2615(3)	2618(3)	1143(2)	34(1)

C(5)	193(3)	1258(2)	-880(2)	35(1)

C(6)	1408(3)	953(2)	-1726(2)	39(1)

C(7)	2320(3)	1533(2)	-1812(2)	33(1)

C(8)	2054(3)	2434(2)	-1031(2)	25(1)

O(9)	416(2)	4792(1)	443(1)	19(1)

C(9)	332(2)	3659(2)	771(2)	18(1)

C(10)	-1177(2)	3733(2)	1247(2)	21(1)

C(11)	-1353(3)	2785(2)	786(2)	25(1)

C(12)	-97(3)	2170(2)	-107(2)	25(1)

C(13)	860(2)	2721(2)	-179(2)	20(1)

C(14)	1228(2)	3245(2)	1641(2)	18(1)

C(15)	1236(2)	2731(2)	2635(2)	21(1)

C(16)	-173(4)	966(3)	3208(3)	40(1)

C(17)	1639(3)	1251(3)	4711(2)	37(1)

C(18)	-1241(3)	3305(2)	4615(2)	28(1)

C(19)	-2209(3)	2880(2)	5469(2)	27(1)

C(20)	-1984(3)	2606(2)	6537(2)	31(1)

C(21)	-2868(3)	2207(2)	7315(2)	34(1)

C(22)	-3989(3)	2062(3)	7039(2)	37(1)

C(23)	-4223(3)	2313(3)	5981(2)	45(1)

C(24)	-3344(3)	2723(3)	5209(2)	40(1)

O(25)	3199(2)	-61(2)	687(2)	48(1)

C(25)	3221(3)	761(2)	1061(2)	31(1)

O(26)	4866(2)	2877(2)	-237(2)	42(1)

C(26)	4246(3)	2558(2)	493(2)	29(1)

O(27)	5081(2)	973(2)	3232(2)	52(1)

C(27)	4361(3)	1395(2)	2628(2)	33(1)

O(28)	3028(2)	5551(2)	970(2)	42(1)

C(28)	2552(3)	5017(2)	1580(2)	27(1)

O(29)	3312(2)	3751(2)	4396(2)	44(1)

C(29)	2714(3)	3904(2)	3710(2)	27(1)

O(30)	-926(2)	6122(2)	3527(2)	42(1)

C(30)	129(3)	5345(2)	3163(2)	26(1)

________________________________________________________________________________

Table I3:  Bond lengths [Å] and angles [°] for 124.

_____________________________________________________________________________________

Co(1)-C(25) 	1.804(3)

Co(1)-C(26) 	1.823(3)

Co(1)-C(27) 	1.828(3)

Co(1)-C(14) 	1.968(2)

Co(1)-C(15) 	1.990(2)

Co(1)-Co(2) 	2.4727(11)

Co(2)-C(30) 	1.794(3)

Co(2)-C(29) 	1.820(2)

Co(2)-C(28) 	1.838(3)

Co(2)-C(14) 	1.959(2)

Co(2)-C(15) 	1.993(2)

Si(1)-C(16) 	1.858(3)

Si(1)-C(15) 	1.860(2)

Si(1)-C(17) 	1.862(3)

Si(1)-C(18) 	1.883(3)

C(1)-C(10) 	1.380(3)

C(1)-C(2) 	1.396(3)

C(2)-C(3) 	1.378(4)

C(3)-C(4) 	1.381(4)

C(4)-C(11) 	1.391(3)

C(5)-C(6) 	1.388(4)

C(5)-C(12) 	1.395(3)

C(6)-C(7) 	1.381(4)

C(7)-C(8) 	1.399(3)

C(8)-C(13) 	1.380(3)

O(9)-C(9) 	1.430(3)

O(9)-O(9)#1 	1.494(3)

C(9)-C(14) 	1.520(3)

C(9)-C(13) 	1.527(3)

C(9)-C(10) 	1.530(3)

C(10)-C(11) 	1.403(3)

C(11)-C(12) 	1.470(3)

C(12)-C(13) 	1.398(3)

C(14)-C(15) 	1.342(3)

C(18)-C(19) 	1.510(3)

C(19)-C(24) 	1.389(4)

C(19)-C(20) 	1.392(3)

C(20)-C(21) 	1.386(4)

C(21)-C(22) 	1.376(4)

C(22)-C(23) 	1.380(4)

C(23)-C(24) 	1.386(4)

O(25)-C(25) 	1.131(3)

O(26)-C(26) 	1.132(3)

O(27)-C(27) 	1.135(3)

O(28)-C(28) 	1.124(3)

O(29)-C(29) 	1.131(3)

O(30)-C(30) 	1.137(3)

C(25)-Co(1)-C(26)	99.89(11)

C(25)-Co(1)-C(27)	100.33(12)

C(26)-Co(1)-C(27)	105.94(12)

C(25)-Co(1)-C(14)	100.08(10)

C(26)-Co(1)-C(14)	102.46(11)

C(27)-Co(1)-C(14)	141.31(10)

C(25)-Co(1)-C(15)	100.43(10)

C(26)-Co(1)-C(15)	139.69(11)

C(27)-Co(1)-C(15)	104.15(11)

C(14)-Co(1)-C(15)	39.65(9)

C(25)-Co(1)-Co(2)	149.15(9)

C(26)-Co(1)-Co(2)	96.98(8)

C(27)-Co(1)-Co(2)	99.59(8)

C(14)-Co(1)-Co(2)	50.82(6)

C(15)-Co(1)-Co(2)	51.67(6)

C(30)-Co(2)-C(29)	100.44(11)

C(30)-Co(2)-C(28)	97.91(11)

C(29)-Co(2)-C(28)	104.31(11)

C(30)-Co(2)-C(14)	102.18(10)

C(29)-Co(2)-C(14)	141.35(10)

C(28)-Co(2)-C(14)	103.12(10)

C(30)-Co(2)-C(15)	101.77(10)

C(29)-Co(2)-C(15)	104.94(10)

C(28)-Co(2)-C(15)	140.84(9)

C(14)-Co(2)-C(15)	39.70(9)

C(30)-Co(2)-Co(1)	151.14(7)

C(29)-Co(2)-Co(1)	97.78(8)

C(28)-Co(2)-Co(1)	99.05(8)

C(14)-Co(2)-Co(1)	51.12(7)

C(15)-Co(2)-Co(1)	51.58(7)

C(16)-Si(1)-C(15)	108.49(12)

C(16)-Si(1)-C(17)	111.36(16)

C(15)-Si(1)-C(17)	109.69(13)

C(16)-Si(1)-C(18)	110.14(15)

C(15)-Si(1)-C(18)	107.58(11)

C(17)-Si(1)-C(18)	109.49(14)

C(10)-C(1)-C(2)	118.4(2)

C(3)-C(2)-C(1)	120.4(3)

C(2)-C(3)-C(4)	121.8(3)

C(3)-C(4)-C(11)	118.2(2)

C(6)-C(5)-C(12)	118.6(2)

C(7)-C(6)-C(5)	121.3(2)

C(6)-C(7)-C(8)	120.6(3)

C(13)-C(8)-C(7)	118.1(2)

C(9)-O(9)-O(9)#1	104.49(15)

O(9)-C(9)-C(14)	102.98(15)

O(9)-C(9)-C(13)	114.33(17)

C(14)-C(9)-C(13)	112.33(18)

O(9)-C(9)-C(10)	115.05(18)

C(14)-C(9)-C(10)	110.74(17)

C(13)-C(9)-C(10)	101.75(16)

C(1)-C(10)-C(11)	120.9(2)

C(1)-C(10)-C(9)	129.5(2)

C(11)-C(10)-C(9)	109.58(19)

C(4)-C(11)-C(10)	120.2(2)

C(4)-C(11)-C(12)	131.0(2)

C(10)-C(11)-C(12)	108.65(19)

C(5)-C(12)-C(13)	119.6(2)

C(5)-C(12)-C(11)	131.3(2)

C(13)-C(12)-C(11)	108.89(19)

C(8)-C(13)-C(12)	121.7(2)

C(8)-C(13)-C(9)	128.38(19)

C(12)-C(13)-C(9)	109.85(19)

C(15)-C(14)-C(9)	141.1(2)

C(15)-C(14)-Co(2)	71.50(12)

C(9)-C(14)-Co(2)	132.29(15)

C(15)-C(14)-Co(1)	71.09(13)

C(9)-C(14)-Co(1)	135.54(15)

Co(2)-C(14)-Co(1)	78.06(8)

C(14)-C(15)-Si(1)	148.78(18)

C(14)-C(15)-Co(1)	69.27(13)

Si(1)-C(15)-Co(1)	131.47(12)

C(14)-C(15)-Co(2)	68.80(13)

Si(1)-C(15)-Co(2)	132.29(11)

Co(1)-C(15)-Co(2)	76.75(8)

C(19)-C(18)-Si(1)	114.21(17)

C(24)-C(19)-C(20)	117.4(2)

C(24)-C(19)-C(18)	121.1(2)

C(20)-C(19)-C(18)	121.5(2)

C(21)-C(20)-C(19)	121.3(2)

C(22)-C(21)-C(20)	120.2(3)

C(21)-C(22)-C(23)	119.5(3)

C(22)-C(23)-C(24)	120.0(3)

C(23)-C(24)-C(19)	121.5(3)

O(25)-C(25)-Co(1)	178.0(2)

O(26)-C(26)-Co(1)	177.8(2)

O(27)-C(27)-Co(1)	179.1(2)

O(28)-C(28)-Co(2)	179.3(2)

O(29)-C(29)-Co(2)	178.5(2)

O(30)-C(30)-Co(2)	179.4(2)

_____________________________________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x,-y+1,-z

Table I4:  Anisotropic displacement parameters (Å2 x 103) for 124.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	18(1) 	22(1)	22(1) 	0(1)	-3(1) 	-4(1)

Co(2)	20(1) 	20(1)	20(1) 	1(1)	-4(1) 	-9(1)

Si(1)	28(1) 	21(1)	21(1) 	4(1)	-2(1) 	-12(1)

C(1)	25(1) 	30(1)	26(1) 	5(1)	-7(1) 	-10(1)

C(2)	23(1) 	46(2)	30(1) 	7(1)	-2(1) 	-10(1)

C(3)	24(1) 	54(2)	44(2) 	15(1)	-11(1) 	-23(1)

C(4)	32(2) 	37(2)	42(2) 	13(1)	-15(1) 	-22(1)

C(5)	43(2) 	27(1)	43(2) 	1(1)	-19(1) 	-18(1)

C(6)	49(2) 	30(1)	38(2) 	-10(1)	-14(1) 	-13(1)

C(7)	35(2) 	31(1)	26(1) 	-6(1)	-3(1) 	-7(1)

C(8)	25(1) 	26(1)	25(1) 	1(1)	-6(1) 	-10(1)

O(9)	24(1) 	18(1)	20(1) 	6(1)	-12(1) 	-11(1)

C(9)	19(1) 	17(1)	21(1) 	3(1)	-4(1) 	-9(1)

C(10)	18(1) 	25(1)	23(1) 	8(1)	-7(1) 	-11(1)

C(11)	25(1) 	25(1)	29(1) 	10(1)	-12(1) 	-14(1)

C(12)	29(1) 	22(1)	29(1) 	5(1)	-13(1) 	-12(1)

C(13)	23(1) 	19(1)	20(1) 	4(1)	-8(1) 	-8(1)

C(14)	16(1) 	16(1)	20(1) 	-1(1)	-2(1) 	-6(1)

C(15)	20(1) 	19(1)	22(1) 	0(1)	-4(1) 	-8(1)

C(16)	55(2) 	34(2)	39(2) 	0(1)	-4(2) 	-30(2)

C(17)	38(2) 	37(2)	31(2) 	14(1)	-8(1) 	-12(2)

C(18)	30(1) 	27(1)	24(1) 	4(1)	-1(1) 	-12(1)

C(19)	25(1) 	25(1)	25(1) 	0(1)	2(1) 	-8(1)

C(20)	31(1) 	32(1)	29(1) 	1(1)	-3(1) 	-14(1)

C(21)	39(2) 	38(2)	24(1) 	5(1)	-3(1) 	-17(1)

C(22)	28(2) 	44(2)	34(2) 	10(1)	2(1) 	-15(1)

C(23)	33(2) 	65(2)	43(2) 	14(2)	-10(1) 	-25(2)

C(24)	32(2) 	61(2)	27(1) 	12(1)	-8(1) 	-20(1)

O(25)	69(2) 	25(1)	46(1) 	-5(1)	-11(1) 	-16(1)

C(25)	31(1) 	24(1)	28(1) 	3(1)	-3(1) 	-4(1)

O(26)	36(1) 	59(1)	32(1) 	-3(1)	4(1) 	-24(1)

C(26)	22(1) 	34(1)	28(1) 	-7(1)	-4(1) 	-7(1)

O(27)	41(1) 	51(1)	47(1) 	2(1)	-24(1) 	4(1)

C(27)	26(1) 	29(1)	34(1) 	-2(1)	-5(1) 	-2(1)

O(28)	50(1) 	48(1)	39(1) 	14(1)	-9(1) 	-33(1)

C(28)	25(1) 	28(1)	29(1) 	2(1)	-8(1) 	-13(1)

O(29)	41(1) 	52(1)	35(1) 	-2(1)	-19(1) 	-10(1)

C(29)	24(1) 	26(1)	29(1) 	-3(1)	-3(1) 	-8(1)

O(30)	30(1) 	32(1)	52(1) 	-11(1)	-3(1) 	-5(1)

C(30)	32(1) 	25(1)	28(1) 	0(1)	-8(1) 	-16(1)

______________________________________________________________________________

Table I5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 10 3)

for 124.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1)	-2150(30)	5200(20)	2276(19)	26(6)

H(2)	-4300(30)	4970(20)	2840(20)	33(7)

H(3)	-4530(30)	3370(30)	2150(20)	44(8)

H(4)	-2680(30)	1940(20)	840(20)	39(8)

H(5)	-450(30)	870(30)	-820(20)	46(8)

H(6)	1620(30)	320(30)	-2250(20)	46(8)

H(7)	3080(30)	1370(20)	-2400(20)	29(7)

H(8)	2690(20)	2840(20)	-1114(18)	19(6)

H(16C)	610(40)	330(30)	2790(30)	74(11)

H(16B)	-820(40)	1390(30)	2720(30)	76(12)

H(16A)	-650(40)	620(40)	3740(30)	88(13)

H(17C)	1100(30)	1060(30)	5380(30)	50(9)

H(17B)	2030(30)	1740(30)	4960(30)	59(10)

H(17A)	2330(40)	580(30)	4410(30)	59(10)

H(18B)	-920(30)	3810(20)	4923(19)	28(6)

H(18A)	-1780(30)	3860(20)	4050(20)	39(7)

H(20)	-1200(30)	2710(20)	6720(20)	34(7)

H(21)	-2690(30)	2040(20)	8020(20)	40(8)

H(22)	-4570(30)	1820(20)	7560(20)	38(8)

H(23)	-4980(30)	2220(30)	5790(20)	58(9)

H(24)	-3530(30)	2870(20)	4520(20)	38(8)

________________________________________________________________________________

Table J1:  Crystal data and structure refinement for 125.

Empirical formula 	C50 H34 Co4 O14 Si2

Formula weight 	1150.67

Temperature 	173(2) K

Wavelength 	0.71073 Å

Crystal system 	Orthorhombic

Space group 	Pbca

Unit cell dimensions	a = 22.17(4) Å	(= 90°.

b = 13.24(3) Å	(= 90°.

c = 16.93(3) Å	( = 90°.

Volume	4969(17) Å3

Z	4

Density (calculated)	1.538 Mg/m3

Absorption coefficient	1.426 mm-1

F(000)	2328

Crystal size	0.20 x 0.10 x 0.02 mm3

( range for data collection	1.84 to 22.50°.

Index ranges	-23(h(23, -13(k(14, -18(l(17

Reflections collected	26564

Independent reflections	3244 [R(int) = 0.1512]

Completeness to ( = 22.50°	100.0 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	3244 / 0 / 323

Goodness-of-fit on F2	1.129

Final R indices [I>2((I)]	R1 = 0.0847, wR2 = 0.1172

R indices (all data)	R1 = 0.1315, wR2 = 0.1306

Extinction coefficient	0.00021(8)

Largest diff. peak and hole	0.383 and -0.344 e.Å-3

Ratio of min/max apparent transmission 	0.563115

Table J2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 125.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	3526(1)	7009(1)	1380(1)	42(1)

Co(2)	3410(1)	5170(1)	1419(1)	55(1)

C(1)	4757(4)	7337(8)	-398(5)	48(3)

C(2)	5002(5)	8277(9)	-571(7)	73(3)

C(3)	5395(5)	8717(10)	-29(9)	86(4)

C(4)	5534(4)	8274(11)	664(8)	82(4)

C(5)	5761(4)	6724(11)	2170(7)	82(5)

C(6)	5767(6)	5940(14)	2691(8)	114(7)

C(7)	5449(5)	5054(12)	2573(6)	92(5)

C(8)	5072(4)	4954(9)	1904(6)	61(3)

O(9)	4676(2)	5052(5)	115(3)	42(2)

C(9)	4662(3)	5902(7)	641(4)	39(2)

C(10)	4896(3)	6877(7)	299(5)	42(2)

C(11)	5300(4)	7324(9)	848(6)	54(3)

C(12)	5381(3)	6620(10)	1502(6)	60(3)

C(13)	5049(3)	5767(8)	1396(6)	46(3)

C(14)	3991(3)	5989(7)	833(4)	38(2)

C(15)	3458(3)	6070(8)	476(5)	54(3)

Si(1)	3028(2)	6349(8)	-483(4)	47(2)

C(16)	3366(7)	5507(15)	-1215(10)	70(6)

C(17)	2221(8)	6114(16)	-320(12)	41(6)

C(18)	3109(7)	7655(13)	-857(9)	58(6)

C(19)	2653(11)	8250(19)	-1102(12)	99(8)

Si(1A)	2973(3)	5675(9)	-377(5)	39(2)

C(16A)	3248(9)	6510(17)	-1185(12)	54(7)

C(17A)	2177(12)	5930(20)	-110(16)	48(9)

C(18A)	3099(13)	4400(20)	-761(17)	94(10)

C(19A)	2770(20)	3860(30)	-990(20)	155(16)

O(20)	4308(3)	7368(6)	2752(4)	90(3)

C(20)	4003(4)	7232(8)	2228(5)	49(3)

O(21)	3789(4)	8876(7)	528(6)	131(4)

C(21)	3691(5)	8171(10)	859(7)	80(4)

O(22)	2290(3)	7450(6)	1918(4)	83(3)

C(22)	2764(4)	7289(8)	1709(5)	52(3)

O(23)	3825(4)	4986(7)	3070(5)	111(3)

C(23)	3683(4)	5026(8)	2425(7)	68(3)

O(24)	3723(4)	3205(7)	745(7)	165(6)

C(24)	3604(5)	3977(10)	1003(8)	104(5)

O(25)	2107(3)	4881(7)	1674(5)	110(3)

C(25)	2604(4)	4997(9)	1562(6)	76(3)

________________________________________________________________________________

Table J3:  Bond lengths [Å] and angles [°] for 125.

_____________________________________________________________________________________

Co(1)-C(20) 	1.808(10)

Co(1)-C(21) 	1.811(13)

Co(1)-C(22) 	1.817(10)

Co(1)-C(14) 	1.935(8)

Co(1)-C(15) 	1.977(9)

Co(1)-Co(2) 	2.448(5)

Co(2)-C(24) 	1.782(14)

Co(2)-C(25) 	1.817(10)

Co(2)-C(23) 	1.818(12)

Co(2)-C(14) 	1.954(8)

Co(2)-C(15) 	1.995(10)

C(1)-C(10) 	1.364(12)

C(1)-C(2) 	1.389(13)

C(2)-C(3) 	1.393(14)

C(3)-C(4) 	1.347(15)

C(4)-C(11) 	1.396(15)

C(5)-C(6) 	1.363(18)

C(5)-C(12) 	1.417(13)

C(6)-C(7) 	1.383(18)

C(7)-C(8) 	1.412(13)

C(8)-C(13) 	1.379(13)

O(9)-C(9) 	1.436(9)

O(9)-O(9)#1 	1.494(9)

C(9)-C(10) 	1.507(12)

C(9)-C(14) 	1.526(10)

C(9)-C(13) 	1.550(11)

C(10)-C(11) 	1.420(11)

C(11)-C(12) 	1.458(14)

C(12)-C(13) 	1.360(13)

C(14)-C(15) 	1.332(10)

C(15)-Si(1A) 	1.875(11)

C(15)-Si(1) 	1.919(10)

Si(1)-C(16) 	1.827(19)

Si(1)-C(17) 	1.837(19)

Si(1)-C(18) 	1.85(2)

C(18)-C(19) 	1.35(3)

Si(1A)-C(18A) 	1.83(3)

Si(1A)-C(17A) 	1.85(3)

Si(1A)-C(16A) 	1.86(2)

C(18A)-C(19A) 	1.09(5)

O(20)-C(20) 	1.129(9)

O(21)-C(21) 	1.110(12)

O(22)-C(22) 	1.129(9)

O(23)-C(23) 	1.138(12)

O(24)-C(24) 	1.143(13)

O(25)-C(25) 	1.128(10)

C(20)-Co(1)-C(21)	97.4(5)

C(20)-Co(1)-C(22)	105.4(4)

C(21)-Co(1)-C(22)	99.4(4)

C(20)-Co(1)-C(14)	100.5(4)

C(21)-Co(1)-C(14)	104.6(4)

C(22)-Co(1)-C(14)	141.7(4)

C(20)-Co(1)-C(15)	139.7(4)

C(21)-Co(1)-C(15)	100.0(5)

C(22)-Co(1)-C(15)	107.2(4)

C(14)-Co(1)-C(15)	39.8(3)

C(20)-Co(1)-Co(2)	101.7(3)

C(21)-Co(1)-Co(2)	151.6(4)

C(22)-Co(1)-Co(2)	95.6(3)

C(14)-Co(1)-Co(2)	51.3(3)

C(15)-Co(1)-Co(2)	52.3(3)

C(24)-Co(2)-C(25)	100.3(5)

C(24)-Co(2)-C(23)	101.4(6)

C(25)-Co(2)-C(23)	100.9(4)

C(24)-Co(2)-C(14)	97.5(4)

C(25)-Co(2)-C(14)	141.8(5)

C(23)-Co(2)-C(14)	108.3(4)

C(24)-Co(2)-C(15)	101.5(6)

C(25)-Co(2)-C(15)	103.5(4)

C(23)-Co(2)-C(15)	142.7(4)

C(14)-Co(2)-C(15)	39.4(3)

C(24)-Co(2)-Co(1)	147.6(4)

C(25)-Co(2)-Co(1)	103.4(4)

C(23)-Co(2)-Co(1)	95.5(4)

C(14)-Co(2)-Co(1)	50.6(2)

C(15)-Co(2)-Co(1)	51.6(3)

C(10)-C(1)-C(2)	119.6(10)

C(1)-C(2)-C(3)	118.8(11)

C(4)-C(3)-C(2)	122.2(12)

C(3)-C(4)-C(11)	120.1(11)

C(6)-C(5)-C(12)	116.7(14)

C(5)-C(6)-C(7)	123.2(14)

C(6)-C(7)-C(8)	119.8(14)

C(13)-C(8)-C(7)	116.7(12)

C(9)-O(9)-O(9)#1	104.8(6)

O(9)-C(9)-C(10)	115.1(6)

O(9)-C(9)-C(14)	102.3(6)

C(10)-C(9)-C(14)	110.6(7)

O(9)-C(9)-C(13)	114.2(7)

C(10)-C(9)-C(13)	103.0(7)

C(14)-C(9)-C(13)	111.9(6)

C(1)-C(10)-C(11)	121.5(10)

C(1)-C(10)-C(9)	129.6(8)

C(11)-C(10)-C(9)	108.8(9)

C(4)-C(11)-C(10)	117.6(11)

C(4)-C(11)-C(12)	134.4(10)

C(10)-C(11)-C(12)	108.0(10)

C(13)-C(12)-C(5)	120.5(12)

C(13)-C(12)-C(11)	111.3(8)

C(5)-C(12)-C(11)	128.2(11)

C(12)-C(13)-C(8)	123.1(10)

C(12)-C(13)-C(9)	108.2(9)

C(8)-C(13)-C(9)	128.7(9)

C(15)-C(14)-C(9)	140.7(7)

C(15)-C(14)-Co(1)	71.8(5)

C(9)-C(14)-Co(1)	132.4(6)

C(15)-C(14)-Co(2)	72.0(5)

C(9)-C(14)-Co(2)	135.1(7)

Co(1)-C(14)-Co(2)	78.0(3)

C(14)-C(15)-Si(1A)	146.7(8)

C(14)-C(15)-Si(1)	147.2(7)

Si(1A)-C(15)-Si(1)	28.0(2)

C(14)-C(15)-Co(1)	68.4(5)

Si(1A)-C(15)-Co(1)	144.6(6)

Si(1)-C(15)-Co(1)	124.9(6)

C(14)-C(15)-Co(2)	68.6(5)

Si(1A)-C(15)-Co(2)	114.8(6)

Si(1)-C(15)-Co(2)	140.0(6)

Co(1)-C(15)-Co(2)	76.1(3)

C(16)-Si(1)-C(17)	113.5(10)

C(16)-Si(1)-C(18)	107.4(9)

C(17)-Si(1)-C(18)	107.7(9)

C(16)-Si(1)-C(15)	104.7(7)

C(17)-Si(1)-C(15)	108.9(8)

C(18)-Si(1)-C(15)	114.9(7)

C(19)-C(18)-Si(1)	125.4(15)

C(18A)-Si(1A)-C(17A)	113.6(14)

C(18A)-Si(1A)-C(16A)	103.7(11)

C(17A)-Si(1A)-C(16A)	112.6(12)

C(18A)-Si(1A)-C(15)	116.3(11)

C(17A)-Si(1A)-C(15)	107.9(10)

C(16A)-Si(1A)-C(15)	102.3(9)

C(19A)-C(18A)-Si(1A)	129(3)

O(20)-C(20)-Co(1)	178.9(8)

O(21)-C(21)-Co(1)	178.7(14)

O(22)-C(22)-Co(1)	179.0(10)

O(23)-C(23)-Co(2)	175.2(10)

O(24)-C(24)-Co(2)	178.8(12)

O(25)-C(25)-Co(2)	177.9(11)

_____________________________________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,-y+1,-z

Table J4:   Anisotropic displacement parameters (Å2 x 103) for 125.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	29(1) 	64(1)	32(1) 	3(1)	5(1) 	11(1)

Co(2)	33(1) 	63(1)	67(1) 	-17(1)	20(1) 	-1(1)

C(1)	36(5) 	69(8)	40(6) 	-4(6)	16(4) 	-9(5)

C(2)	58(7) 	80(10)	82(9) 	-7(8)	33(6) 	-3(7)

C(3)	67(8) 	80(11)	110(11) 	-33(10)	51(8) 	-34(7)

C(4)	43(6) 	111(13)	91(10) 	-68(9)	25(7) 	-26(7)

C(5)	33(6) 	152(15)	63(8) 	-61(9)	-2(6) 	10(7)

C(6)	57(8) 	220(20)	70(10) 	-78(13)	-28(8) 	60(11)

C(7)	79(9) 	158(15)	40(7) 	-22(9)	-12(6) 	70(9)

C(8)	51(6) 	81(9)	52(7) 	-16(7)	1(5) 	31(6)

O(9)	15(2) 	69(5)	41(3) 	-20(3)	8(2) 	0(3)

C(9)	23(4) 	66(8)	27(5) 	-17(5)	0(4) 	4(4)

C(10)	28(5) 	53(7)	44(6) 	-20(6)	10(4) 	-9(4)

C(11)	31(5) 	89(10)	42(7) 	-40(6)	11(5) 	-13(6)

C(12)	24(5) 	118(10)	37(6) 	-44(7)	0(5) 	5(6)

C(13)	20(4) 	78(8)	41(6) 	-20(6)	1(5) 	13(5)

C(14)	29(5) 	55(7)	30(5) 	-9(5)	4(4) 	7(4)

C(15)	22(4) 	101(8)	38(5) 	-14(6)	2(4) 	4(5)

Si(1)	27(3) 	79(6)	34(4) 	-12(4)	-7(2) 	10(4)

Si(1A)	32(3) 	50(7)	34(4) 	0(4)	-5(3) 	-6(4)

O(20)	65(5) 	142(8)	62(5) 	-45(5)	-18(4) 	33(5)

C(20)	46(6) 	68(8)	33(6) 	-3(5)	8(5) 	20(5)

O(21)	137(8) 	109(8)	148(9) 	69(7)	101(7) 	62(7)

C(21)	61(7) 	98(11)	82(9) 	37(8)	42(6) 	17(7)

O(22)	35(4) 	132(7)	80(5) 	-1(5)	19(4) 	27(4)

C(22)	48(6) 	67(8)	40(6) 	9(5)	10(5) 	12(5)

O(23)	113(7) 	139(9)	80(6) 	64(7)	21(5) 	42(6)

C(23)	68(7) 	67(8)	68(8) 	26(7)	29(6) 	26(6)

O(24)	123(8) 	89(8)	285(14) 	-103(9)	131(8) 	-53(6)

C(24)	60(7) 	84(11)	167(13) 	-46(10)	63(8) 	-46(8)

O(25)	35(4) 	173(9)	123(7) 	-39(6)	38(4) 	-19(5)

C(25)	51(6) 	104(10)	73(8) 	-32(7)	18(6) 	-9(6)

______________________________________________________________________________

Table J5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 10 3)

for 125.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1)	4494	7017	-764	58

H(2)	4903	8614	-1049	88

H(3)	5572	9351	-153	103

H(4)	5791	8609	1028	98

H(5)	6000	7311	2250	99

H(6)	6001	6005	3159	137

H(7)	5483	4515	2940	111

H(8)	4847	4356	1809	74

H(16C)	3166	5603	-1725	105

H(16B)	3316	4804	-1044	105

H(16A)	3796	5661	-1267	105

H(17C)	1998	6252	-808	62

H(17B)	2074	6558	101	62

H(17A)	2161	5408	-166	62

H(18A)	3505	7929	-878	69

H(19B)	2250	8005	-1091	119

H(19A)	2734	8914	-1286	119

H(16F)	3027	6358	-1673	80

H(16E)	3680	6393	-1270	80

H(16D)	3182	7218	-1039	80

H(17F)	2139	6623	84	72

H(17E)	2049	5457	304	72

H(17D)	1921	5840	-577	72

H(18B)	3507	4178	-760	112

H(19D)	2355	4035	-1009	186

H(19C)	2900	3218	-1173	186

________________________________________________________________________________

Table K1:  Crystal data and structure refinement for 130.

Empirical formula 	C68 H80 Co8 O28 Si4

Formula weight 	1929.12

Temperature 	153(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	Pc

Unit cell dimensions	a = 11.5638(3) Å	(= 90°.

b = 11.6426(2) Å	(= 91.52(1)°.

c = 31.5342(4) Å	(= 90°.

Volume	4244.05(14) Å3

Z	8

Density (calculated)	1.510 Mg/m3

Absorption coefficient	1.652 mm-1

F(000)	1968

Crystal size	0.08 x 0.20 x 0.20 mm3

( range for data collection	1.29 to 24.00°.

Index ranges	-13(h(14, -13(k(14, -40(l(39

Reflections collected	28830

Independent reflections	12353 [R(int) = 0.0806]

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	12321 / 20 / 1162

Goodness-of-fit on F2	0.995

Final R indices [I>2((I)]	R1 = 0.0507, wR2 = 0.0632

R indices (all data)	R1 = 0.0932, wR2 = 0.0720

Absolute structure parameter	0.042(11)

Extinction coefficient	0.00014(3)

Largest diff. peak and hole	0.466 and -0.403 e.Å-3

Max. and Min. effective transmission	0.893893 and 0.778849

Table K2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 130.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	7348(1)	2806(1)	1316(1)	22(1)

Co(2)	5420(1)	3530(1)	1078(1)	23(1)

Si(1)	5188(2)	1826(2)	2002(1)	27(1)

C(1)	5878(6)	958(7)	774(2)	17(2)

O(1)	6065(6)	1330(5)	348(2)	33(2)

C(2)	4663(7)	465(8)	774(3)	24(2)

C(3)	4510(7)	-632(7)	514(3)	25(2)

C(4)	5372(7)	-1556(8)	648(3)	31(2)

C(5)	6599(8)	-1089(8)	624(3)	34(3)

C(6)	6782(8)	-11(7)	886(3)	27(2)

C(7)	6008(6)	1929(6)	1082(2)	17(2)

C(8)	5777(6)	2248(6)	1478(2)	21(2)

C(9)	5901(7)	468(7)	2180(3)	41(2)

C(10)	3611(7)	1592(7)	1934(3)	42(3)

C(11)	5478(7)	3004(7)	2398(2)	43(2)

C(12)	8131(7)	3144(6)	843(3)	24(2)

O(12)	8620(5)	3364(5)	544(2)	47(2)

C(13)	7680(7)	3926(7)	1718(3)	29(2)

O(13)	7863(5)	4634(5)	1958(2)	38(2)

C(14)	8288(8)	1695(8)	1533(3)	33(2)

O(14)	8876(5)	1016(5)	1663(2)	47(2)

C(15)	5445(6)	4852(7)	1389(3)	28(2)

O(15)	5479(5)	5699(5)	1568(2)	45(2)

C(16)	3871(8)	3354(6)	1022(3)	28(2)

O(16)	2905(5)	3232(5)	985(2)	43(2)

C(17)	5749(7)	4024(7)	544(3)	37(2)

O(17)	5981(5)	4313(5)	208(2)	52(2)

Co(1B)	10464(1)	5809(1)	1103(1)	20(1)

Co(2B)	12326(1)	6636(1)	1361(1)	21(1)

Si(1B)	10009(2)	7634(2)	1972(1)	25(1)

C(1B)	10978(6)	8363(6)	735(2)	19(2)

O(1B)	11775(4)	8111(4)	415(2)	17(1)

C(2B)	9752(7)	8500(7)	552(2)	24(2)

C(3B)	9664(8)	9476(8)	237(3)	29(2)

C(4B)	10082(8)	10605(8)	440(3)	34(3)

C(5B)	11312(8)	10494(8)	622(3)	33(2)

C(6B)	11374(8)	9506(7)	944(3)	22(2)

C(7B)	11000(6)	7436(6)	1074(2)	17(2)

C(8B)	10715(6)	7189(6)	1472(2)	15(2)

C(9B)	10729(7)	8959(7)	2186(3)	38(2)

C(10B)	8457(7)	7956(7)	1838(3)	38(2)

C(11B)	10153(7)	6472(7)	2376(2)	42(2)

C(12B)	10875(6)	5155(7)	609(3)	26(2)

O(12B)	11130(5)	4686(5)	297(2)	36(2)

C(13B)	10473(7)	4579(8)	1457(3)	31(2)

O(13B)	10516(5)	3791(5)	1675(2)	41(2)

C(14B)	8935(7)	5949(6)	994(2)	24(2)

O(14B)	7966(5)	6059(5)	928(2)	42(2)

C(15B)	12702(7)	5580(8)	1767(3)	35(2)

O(15B)	12979(5)	4953(6)	2026(2)	55(2)

C(16B)	13198(7)	7801(7)	1567(2)	27(2)

O(16B)	13755(5)	8519(5)	1697(2)	45(2)

C(17B)	13135(7)	6271(7)	892(3)	26(2)

O(17B)	13638(5)	6006(4)	599(2)	33(2)

Co(1C)	9116(1)	2675(1)	3963(1)	22(1)

Co(2C)	9800(1)	4595(1)	3736(1)	20(1)

Si(1C)	10792(2)	2434(2)	3047(1)	28(1)

C(1C)	11757(6)	3188(6)	4276(2)	20(2)

O(1C)	11391(5)	3407(5)	4700(2)	28(2)

C(2C)	12672(7)	4059(8)	4154(3)	27(2)

C(3C)	13810(7)	3920(8)	4405(3)	30(2)

C(4C)	14282(8)	2711(8)	4380(3)	27(2)

C(5C)	13383(7)	1856(7)	4523(3)	21(2)

C(6C)	12242(7)	1974(7)	4270(3)	21(2)

C(7C)	10689(6)	3270(6)	3967(2)	16(2)

C(8C)	10401(6)	3064(6)	3574(2)	21(2)

C(9C)	11164(7)	895(7)	3127(3)	45(3)

C(10C)	12072(7)	3256(7)	2862(3)	48(3)

C(11C)	9548(7)	2558(7)	2656(2)	45(3)

C(12C)	8617(7)	3043(7)	4497(3)	36(2)

O(12C)	8312(5)	3307(5)	4822(2)	51(2)

C(13C)	7753(8)	2659(7)	3640(3)	39(3)

O(13C)	6909(6)	2646(5)	3457(2)	49(2)

C(14C)	9323(7)	1163(8)	4021(2)	27(2)

O(14C)	9440(5)	172(5)	4059(2)	41(2)

C(15C)	8657(8)	4853(7)	3340(3)	28(2)

O(15C)	7957(5)	5004(5)	3089(2)	39(2)

C(16C)	10861(8)	5530(7)	3525(2)	31(2)

O(16C)	11545(5)	6160(5)	3395(2)	38(2)

C(17C)	9466(7)	5385(7)	4212(3)	27(2)

O(17C)	9280(5)	5871(5)	4518(2)	43(2)

Co(1D)	6835(1)	2340(1)	-1084(1)	20(1)

Co(2D)	6048(1)	484(1)	-1348(1)	22(1)

Si(1D)	4938(2)	2817(2)	-1960(1)	24(1)

C(1D)	4305(6)	1728(6)	-732(2)	15(2)

O(1D)	4627(5)	922(5)	-401(2)	23(1)

C(2D)	3159(7)	1293(8)	-919(3)	22(2)

C(3D)	2179(8)	1335(8)	-604(3)	33(2)

C(4D)	2040(8)	2540(7)	-424(3)	31(2)

C(5D)	3161(8)	2969(8)	-221(3)	34(2)

C(6D)	4152(7)	2935(7)	-545(2)	18(2)

C(7D)	5220(6)	1762(6)	-1065(2)	19(2)

C(8D)	5435(6)	2070(6)	-1462(2)	19(2)

C(9D)	4568(7)	4349(6)	-1826(2)	35(2)

C(10D)	3606(6)	2065(7)	-2170(2)	38(2)

C(11D)	6087(6)	2753(7)	-2357(2)	33(2)

C(12D)	7490(7)	1878(7)	-578(3)	27(2)

O(12D)	7928(5)	1623(5)	-269(2)	38(2)

C(13D)	8078(7)	2401(6)	-1423(3)	27(2)

O(13D)	8871(5)	2374(4)	-1634(2)	40(2)

C(14D)	6652(6)	3859(8)	-974(3)	24(2)

O(14D)	6555(5)	4807(5)	-905(2)	40(2)

C(15D)	7179(7)	181(7)	-1727(3)	30(2)

O(15D)	7872(5)	-20(5)	-1962(2)	41(2)

C(16D)	4909(7)	-407(7)	-1585(3)	33(2)

O(16D)	4226(6)	-953(5)	-1738(2)	51(2)

C(17D)	6407(6)	-388(6)	-873(3)	18(2)

O(17D)	6646(5)	-888(5)	-579(2)	34(2)

________________________________________________________________________________

Table K3:  Bond lengths [Å] and angles [°] for 130.

___________________________________________________________________________________

Co(1)-C(12) 	1.808(8)

Co(1)-C(14) 	1.812(10)

Co(1)-C(13) 	1.852(9)

Co(1)-C(7) 	1.983(7)

Co(1)-C(8) 	2.008(7)

Co(1)-Co(2) 	2.481(2)

Co(2)-C(16) 	1.808(9)

Co(2)-C(15) 	1.825(9)

Co(2)-C(17) 	1.830(10)

Co(2)-C(7) 	1.984(7)

Co(2)-C(8) 	1.989(7)

Si(1)-C(10) 	1.850(8)

Si(1)-C(9) 	1.863(8)

Si(1)-C(8) 	1.871(7)

Si(1)-C(11) 	1.878(8)

C(1)-O(1) 	1.434(9)

C(1)-C(7) 	1.494(10)

C(1)-C(2) 	1.518(10)

C(1)-C(6) 	1.572(10)

C(2)-C(3) 	1.525(11)

C(3)-C(4) 	1.519(11)

C(4)-C(5) 	1.523(11)

C(5)-C(6) 	1.514(11)

C(7)-C(8) 	1.335(9)

C(12)-O(12) 	1.141(8)

C(13)-O(13) 	1.134(9)

C(14)-O(14) 	1.113(9)

C(15)-O(15) 	1.136(9)

C(16)-O(16) 	1.129(9)

C(17)-O(17) 	1.149(9)

Co(1B)-C(14B) 	1.799(9)

Co(1B)-C(12B) 	1.807(9)

Co(1B)-C(13B) 	1.817(9)

Co(1B)-C(7B) 	1.996(7)

Co(1B)-C(8B) 	2.000(7)

Co(1B)-Co(2B) 	2.477(2)

Co(2B)-C(16B) 	1.802(9)

Co(2B)-C(15B) 	1.819(10)

Co(2B)-C(17B) 	1.822(8)

Co(2B)-C(7B) 	1.991(7)

Co(2B)-C(8B) 	2.010(7)

Si(1B)-C(11B) 	1.864(8)

Si(1B)-C(8B) 	1.867(7)

Si(1B)-C(9B) 	1.870(8)

Si(1B)-C(10B) 	1.871(8)

C(1B)-O(1B) 	1.416(8)

C(1B)-C(7B) 	1.518(10)

C(1B)-C(2B) 	1.525(10)

C(1B)-C(6B) 	1.547(11)

C(2B)-C(3B) 	1.511(10)

C(3B)-C(4B) 	1.534(12)

C(4B)-C(5B) 	1.525(12)

C(5B)-C(6B) 	1.534(11)

C(7B)-C(8B) 	1.337(9)

C(12B)-O(12B) 	1.170(8)

C(13B)-O(13B) 	1.147(9)

C(14B)-O(14B) 	1.142(9)

C(15B)-O(15B) 	1.135(9)

C(16B)-O(16B) 	1.126(8)

C(17B)-O(17B) 	1.147(8)

Co(1C)-C(14C) 	1.786(9)

Co(1C)-C(12C) 	1.846(10)

Co(1C)-C(13C) 	1.854(11)

Co(1C)-C(7C) 	1.947(7)

Co(1C)-C(8C) 	2.003(6)

Co(1C)-Co(2C) 	2.4834(14)

Co(2C)-C(16C) 	1.781(9)

Co(2C)-C(17C) 	1.812(9)

Co(2C)-C(15C) 	1.819(9)

Co(2C)-C(7C) 	1.982(7)

Co(2C)-C(8C) 	1.985(7)

Si(1C)-C(9C) 	1.858(8)

Si(1C)-C(10C) 	1.868(8)

Si(1C)-C(11C) 	1.876(8)

Si(1C)-C(8C) 	1.883(7)

C(1C)-O(1C) 	1.434(8)

C(1C)-C(6C) 	1.521(10)

C(1C)-C(2C) 	1.522(10)

C(1C)-C(7C) 	1.557(10)

C(2C)-C(3C) 	1.528(11)

C(3C)-C(4C) 	1.513(12)

C(4C)-C(5C) 	1.517(11)

C(5C)-C(6C) 	1.530(11)

C(7C)-C(8C) 	1.295(9)

C(12C)-O(12C) 	1.134(9)

C(13C)-O(13C) 	1.120(10)

C(14C)-O(14C) 	1.168(9)

C(15C)-O(15C) 	1.129(9)

C(16C)-O(16C) 	1.161(9)

C(17C)-O(17C) 	1.145(8)

Co(1D)-C(13D) 	1.815(8)

Co(1D)-C(14D) 	1.816(9)

Co(1D)-C(12D) 	1.830(10)

Co(1D)-C(7D) 	1.987(7)

Co(1D)-C(8D) 	2.010(7)

Co(1D)-Co(2D) 	2.4797(15)

Co(2D)-C(16D) 	1.821(9)

Co(2D)-C(15D) 	1.827(8)

Co(2D)-C(17D) 	1.849(9)

Co(2D)-C(7D) 	1.993(7)

Co(2D)-C(8D) 	2.007(7)

Si(1D)-C(11D) 	1.851(7)

Si(1D)-C(8D) 	1.871(8)

Si(1D)-C(10D) 	1.877(8)

Si(1D)-C(9D) 	1.885(8)

C(1D)-O(1D) 	1.445(8)

C(1D)-C(7D) 	1.510(9)

C(1D)-C(2D) 	1.523(10)

C(1D)-C(6D) 	1.536(10)

C(2D)-C(3D) 	1.528(10)

C(3D)-C(4D) 	1.523(11)

C(4D)-C(5D) 	1.514(12)

C(5D)-C(6D) 	1.554(10)

C(7D)-C(8D) 	1.332(9)

C(12D)-O(12D) 	1.124(9)

C(13D)-O(13D) 	1.147(7)

C(14D)-O(14D) 	1.131(8)

C(15D)-O(15D) 	1.132(8)

C(16D)-O(16D) 	1.114(9)

C(17D)-O(17D) 	1.122(8)

C(12)-Co(1)-C(14)	99.1(4)

C(12)-Co(1)-C(13)	108.2(3)

C(14)-Co(1)-C(13)	97.7(4)

C(12)-Co(1)-C(7)	102.1(3)

C(14)-Co(1)-C(7)	103.1(3)

C(13)-Co(1)-C(7)	139.7(3)

C(12)-Co(1)-C(8)	139.1(3)

C(14)-Co(1)-C(8)	102.2(3)

C(13)-Co(1)-C(8)	103.1(3)

C(7)-Co(1)-C(8)	39.1(3)

C(12)-Co(1)-Co(2)	98.1(3)

C(14)-Co(1)-Co(2)	151.8(3)

C(13)-Co(1)-Co(2)	97.8(2)

C(7)-Co(1)-Co(2)	51.3(2)

C(8)-Co(1)-Co(2)	51.3(2)

C(16)-Co(2)-C(15)	98.6(3)

C(16)-Co(2)-C(17)	100.1(4)

C(15)-Co(2)-C(17)	103.3(4)

C(16)-Co(2)-C(7)	103.4(3)

C(15)-Co(2)-C(7)	142.0(3)

C(17)-Co(2)-C(7)	102.8(3)

C(16)-Co(2)-C(8)	99.5(3)

C(15)-Co(2)-C(8)	107.0(3)

C(17)-Co(2)-C(8)	140.8(3)

C(7)-Co(2)-C(8)	39.3(3)

C(16)-Co(2)-Co(1)	150.6(2)

C(15)-Co(2)-Co(1)	97.1(2)

C(17)-Co(2)-Co(1)	100.3(3)

C(7)-Co(2)-Co(1)	51.3(2)

C(8)-Co(2)-Co(1)	52.0(2)

C(10)-Si(1)-C(9)	109.7(4)

C(10)-Si(1)-C(8)	108.4(4)

C(9)-Si(1)-C(8)	108.7(3)

C(10)-Si(1)-C(11)	110.1(4)

C(9)-Si(1)-C(11)	110.5(4)

C(8)-Si(1)-C(11)	109.5(3)

O(1)-C(1)-C(7)	111.5(6)

O(1)-C(1)-C(2)	106.0(7)

C(7)-C(1)-C(2)	111.3(6)

O(1)-C(1)-C(6)	108.1(6)

C(7)-C(1)-C(6)	110.1(6)

C(2)-C(1)-C(6)	109.8(7)

C(1)-C(2)-C(3)	114.3(7)

C(4)-C(3)-C(2)	112.2(7)

C(3)-C(4)-C(5)	109.8(8)

C(6)-C(5)-C(4)	112.8(7)

C(5)-C(6)-C(1)	113.0(8)

C(8)-C(7)-C(1)	143.0(7)

C(8)-C(7)-Co(1)	71.5(5)

C(1)-C(7)-Co(1)	134.0(5)

C(8)-C(7)-Co(2)	70.6(4)

C(1)-C(7)-Co(2)	132.7(5)

Co(1)-C(7)-Co(2)	77.4(3)

C(7)-C(8)-Si(1)	147.0(6)

C(7)-C(8)-Co(2)	70.2(4)

Si(1)-C(8)-Co(2)	133.1(4)

C(7)-C(8)-Co(1)	69.4(4)

Si(1)-C(8)-Co(1)	131.5(4)

Co(2)-C(8)-Co(1)	76.7(3)

O(12)-C(12)-Co(1)	179.5(7)

O(13)-C(13)-Co(1)	178.0(8)

O(14)-C(14)-Co(1)	179.1(8)

O(15)-C(15)-Co(2)	176.9(7)

O(16)-C(16)-Co(2)	179.2(8)

O(17)-C(17)-Co(2)	178.1(8)

C(14B)-Co(1B)-C(12B)	98.9(3)

C(14B)-Co(1B)-C(13B)	100.2(3)

C(12B)-Co(1B)-C(13B)	101.5(3)

C(14B)-Co(1B)-C(7B)	102.1(3)

C(12B)-Co(1B)-C(7B)	105.8(3)

C(13B)-Co(1B)-C(7B)	141.2(3)

C(14B)-Co(1B)-C(8B)	99.5(3)

C(12B)-Co(1B)-C(8B)	143.3(3)

C(13B)-Co(1B)-C(8B)	106.0(3)

C(7B)-Co(1B)-C(8B)	39.1(3)

C(14B)-Co(1B)-Co(2B)	150.3(2)

C(12B)-Co(1B)-Co(2B)	101.6(2)

C(13B)-Co(1B)-Co(2B)	96.5(3)

C(7B)-Co(1B)-Co(2B)	51.5(2)

C(8B)-Co(1B)-Co(2B)	52.0(2)

C(16B)-Co(2B)-C(15B)	97.7(4)

C(16B)-Co(2B)-C(17B)	100.0(3)

C(15B)-Co(2B)-C(17B)	107.2(4)

C(16B)-Co(2B)-C(7B)	103.2(3)

C(15B)-Co(2B)-C(7B)	143.4(3)

C(17B)-Co(2B)-C(7B)	98.4(3)

C(16B)-Co(2B)-C(8B)	102.0(3)

C(15B)-Co(2B)-C(8B)	107.4(3)

C(17B)-Co(2B)-C(8B)	135.6(3)

C(7B)-Co(2B)-C(8B)	39.0(3)

C(16B)-Co(2B)-Co(1B)	152.2(3)

C(15B)-Co(2B)-Co(1B)	99.1(3)

C(17B)-Co(2B)-Co(1B)	95.9(3)

C(7B)-Co(2B)-Co(1B)	51.7(2)

C(8B)-Co(2B)-Co(1B)	51.7(2)

C(11B)-Si(1B)-C(8B)	110.1(3)

C(11B)-Si(1B)-C(9B)	108.7(4)

C(8B)-Si(1B)-C(9B)	109.5(3)

C(11B)-Si(1B)-C(10B)	111.5(4)

C(8B)-Si(1B)-C(10B)	107.7(3)

C(9B)-Si(1B)-C(10B)	109.3(4)

O(1B)-C(1B)-C(7B)	110.9(6)

O(1B)-C(1B)-C(2B)	111.5(6)

C(7B)-C(1B)-C(2B)	109.8(6)

O(1B)-C(1B)-C(6B)	106.9(6)

C(7B)-C(1B)-C(6B)	108.3(6)

C(2B)-C(1B)-C(6B)	109.4(7)

C(3B)-C(2B)-C(1B)	112.0(7)

C(2B)-C(3B)-C(4B)	110.7(7)

C(5B)-C(4B)-C(3B)	111.4(8)

C(4B)-C(5B)-C(6B)	109.8(8)

C(5B)-C(6B)-C(1B)	110.9(7)

C(8B)-C(7B)-C(1B)	144.4(7)

C(8B)-C(7B)-Co(2B)	71.2(4)

C(1B)-C(7B)-Co(2B)	130.6(5)

C(8B)-C(7B)-Co(1B)	70.7(4)

C(1B)-C(7B)-Co(1B)	135.0(5)

Co(2B)-C(7B)-Co(1B)	76.8(3)

C(7B)-C(8B)-Si(1B)	148.9(6)

C(7B)-C(8B)-Co(1B)	70.3(4)

Si(1B)-C(8B)-Co(1B)	130.9(4)

C(7B)-C(8B)-Co(2B)	69.7(4)

Si(1B)-C(8B)-Co(2B)	131.6(4)

Co(1B)-C(8B)-Co(2B)	76.3(2)

O(12B)-C(12B)-Co(1B)	177.1(7)

O(13B)-C(13B)-Co(1B)	177.6(7)

O(14B)-C(14B)-Co(1B)	178.7(7)

O(15B)-C(15B)-Co(2B)	176.8(8)

O(16B)-C(16B)-Co(2B)	179.0(8)

O(17B)-C(17B)-Co(2B)	177.9(7)

C(14C)-Co(1C)-C(12C)	100.3(3)

C(14C)-Co(1C)-C(13C)	99.0(4)

C(12C)-Co(1C)-C(13C)	102.9(4)

C(14C)-Co(1C)-C(7C)	103.1(3)

C(12C)-Co(1C)-C(7C)	103.1(4)

C(13C)-Co(1C)-C(7C)	142.0(3)

C(14C)-Co(1C)-C(8C)	100.7(3)

C(12C)-Co(1C)-C(8C)	139.6(4)

C(13C)-Co(1C)-C(8C)	107.5(4)

C(7C)-Co(1C)-C(8C)	38.3(3)

C(14C)-Co(1C)-Co(2C)	150.9(2)

C(12C)-Co(1C)-Co(2C)	99.5(3)

C(13C)-Co(1C)-Co(2C)	97.1(3)

C(7C)-Co(1C)-Co(2C)	51.4(2)

C(8C)-Co(1C)-Co(2C)	51.2(2)

C(16C)-Co(2C)-C(17C)	99.4(4)

C(16C)-Co(2C)-C(15C)	98.0(4)

C(17C)-Co(2C)-C(15C)	108.5(4)

C(16C)-Co(2C)-C(7C)	104.9(3)

C(17C)-Co(2C)-C(7C)	102.1(3)

C(15C)-Co(2C)-C(7C)	137.8(3)

C(16C)-Co(2C)-C(8C)	101.8(3)

C(17C)-Co(2C)-C(8C)	138.8(3)

C(15C)-Co(2C)-C(8C)	103.0(4)

C(7C)-Co(2C)-C(8C)	38.1(3)

C(16C)-Co(2C)-Co(1C)	152.3(3)

C(17C)-Co(2C)-Co(1C)	98.1(3)

C(15C)-Co(2C)-Co(1C)	96.6(3)

C(7C)-Co(2C)-Co(1C)	50.2(2)

C(8C)-Co(2C)-Co(1C)	51.8(2)

C(9C)-Si(1C)-C(10C)	110.7(4)

C(9C)-Si(1C)-C(11C)	109.5(4)

C(10C)-Si(1C)-C(11C)	110.8(4)

C(9C)-Si(1C)-C(8C)	108.4(4)

C(10C)-Si(1C)-C(8C)	106.7(3)

C(11C)-Si(1C)-C(8C)	110.7(4)

O(1C)-C(1C)-C(6C)	107.2(6)

O(1C)-C(1C)-C(2C)	110.0(6)

C(6C)-C(1C)-C(2C)	110.9(7)

O(1C)-C(1C)-C(7C)	108.9(6)

C(6C)-C(1C)-C(7C)	109.6(6)

C(2C)-C(1C)-C(7C)	110.1(6)

C(1C)-C(2C)-C(3C)	113.1(7)

C(4C)-C(3C)-C(2C)	112.2(8)

C(3C)-C(4C)-C(5C)	110.1(7)

C(4C)-C(5C)-C(6C)	111.9(7)

C(1C)-C(6C)-C(5C)	112.9(7)

C(8C)-C(7C)-C(1C)	140.1(7)

C(8C)-C(7C)-Co(1C)	73.2(5)

C(1C)-C(7C)-Co(1C)	135.0(5)

C(8C)-C(7C)-Co(2C)	71.1(5)

C(1C)-C(7C)-Co(2C)	132.4(6)

Co(1C)-C(7C)-Co(2C)	78.4(3)

C(7C)-C(8C)-Si(1C)	148.7(6)

C(7C)-C(8C)-Co(2C)	70.8(4)

Si(1C)-C(8C)-Co(2C)	132.1(4)

C(7C)-C(8C)-Co(1C)	68.5(4)

Si(1C)-C(8C)-Co(1C)	130.7(4)

Co(2C)-C(8C)-Co(1C)	77.0(2)

O(12C)-C(12C)-Co(1C)	177.7(8)

O(13C)-C(13C)-Co(1C)	177.6(9)

O(14C)-C(14C)-Co(1C)	178.9(8)

O(15C)-C(15C)-Co(2C)	178.9(8)

O(16C)-C(16C)-Co(2C)	178.3(7)

O(17C)-C(17C)-Co(2C)	178.2(7)

C(13D)-Co(1D)-C(14D)	100.0(3)

C(13D)-Co(1D)-C(12D)	102.1(3)

C(14D)-Co(1D)-C(12D)	99.6(4)

C(13D)-Co(1D)-C(7D)	142.2(3)

C(14D)-Co(1D)-C(7D)	102.1(3)

C(12D)-Co(1D)-C(7D)	104.0(3)

C(13D)-Co(1D)-C(8D)	107.2(3)

C(14D)-Co(1D)-C(8D)	99.8(3)

C(12D)-Co(1D)-C(8D)	141.2(3)

C(7D)-Co(1D)-C(8D)	38.9(3)

C(13D)-Co(1D)-Co(2D)	97.2(3)

C(14D)-Co(1D)-Co(2D)	150.4(3)

C(12D)-Co(1D)-Co(2D)	100.2(2)

C(7D)-Co(1D)-Co(2D)	51.6(2)

C(8D)-Co(1D)-Co(2D)	51.8(2)

C(16D)-Co(2D)-C(15D)	98.3(4)

C(16D)-Co(2D)-C(17D)	99.4(3)

C(15D)-Co(2D)-C(17D)	105.9(3)

C(16D)-Co(2D)-C(7D)	104.9(3)

C(15D)-Co(2D)-C(7D)	142.9(3)

C(17D)-Co(2D)-C(7D)	98.4(3)

C(16D)-Co(2D)-C(8D)	101.7(3)

C(15D)-Co(2D)-C(8D)	108.5(3)

C(17D)-Co(2D)-C(8D)	136.2(3)

C(7D)-Co(2D)-C(8D)	38.9(3)

C(16D)-Co(2D)-Co(1D)	152.7(3)

C(15D)-Co(2D)-Co(1D)	97.2(3)

C(17D)-Co(2D)-Co(1D)	97.7(2)

C(7D)-Co(2D)-Co(1D)	51.4(2)

C(8D)-Co(2D)-Co(1D)	51.9(2)

C(11D)-Si(1D)-C(8D)	109.8(3)

C(11D)-Si(1D)-C(10D)	109.8(3)

C(8D)-Si(1D)-C(10D)	108.1(3)

C(11D)-Si(1D)-C(9D)	111.2(3)

C(8D)-Si(1D)-C(9D)	108.6(3)

C(10D)-Si(1D)-C(9D)	109.4(4)

O(1D)-C(1D)-C(7D)	110.3(6)

O(1D)-C(1D)-C(2D)	105.5(6)

C(7D)-C(1D)-C(2D)	111.0(6)

O(1D)-C(1D)-C(6D)	110.3(6)

C(7D)-C(1D)-C(6D)	109.5(6)

C(2D)-C(1D)-C(6D)	110.2(6)

C(1D)-C(2D)-C(3D)	113.0(7)

C(4D)-C(3D)-C(2D)	111.1(7)

C(5D)-C(4D)-C(3D)	111.3(8)

C(4D)-C(5D)-C(6D)	110.7(7)

C(1D)-C(6D)-C(5D)	111.7(6)

C(8D)-C(7D)-C(1D)	144.2(7)

C(8D)-C(7D)-Co(1D)	71.4(4)

C(1D)-C(7D)-Co(1D)	134.9(5)

C(8D)-C(7D)-Co(2D)	71.1(4)

C(1D)-C(7D)-Co(2D)	130.3(5)

Co(1D)-C(7D)-Co(2D)	77.1(2)

C(7D)-C(8D)-Si(1D)	148.5(6)

C(7D)-C(8D)-Co(2D)	70.0(4)

Si(1D)-C(8D)-Co(2D)	132.6(4)

C(7D)-C(8D)-Co(1D)	69.6(4)

Si(1D)-C(8D)-Co(1D)	130.5(4)

Co(2D)-C(8D)-Co(1D)	76.3(3)

O(12D)-C(12D)-Co(1D)	177.3(7)

O(13D)-C(13D)-Co(1D)	176.1(7)

O(14D)-C(14D)-Co(1D)	178.9(7)

O(15D)-C(15D)-Co(2D)	179.2(8)

O(16D)-C(16D)-Co(2D)	178.3(8)

O(17D)-C(17D)-Co(2D)	177.7(7)

_____________________________________________________________________________________

# Table K4:  Anisotropic displacement parameters (Å2 x 103) for 130.  The anisotropic

displacement factor exponent takes the form: -2(2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	18(1) 	23(1)	26(1) 	-2(1)	-4(1) 	-2(1)

Co(2)	22(1) 	23(1)	23(1) 	1(1)	-7(1) 	0(1)

Si(1)	32(2) 	31(2)	17(1) 	1(1)	3(1) 	1(1)

C(1)	8(5) 	29(5)	13(5) 	3(4)	-6(3) 	-11(4)

O(1)	34(4) 	42(4)	23(4) 	1(3)	3(3) 	-16(3)

C(2)	15(5) 	26(5)	32(6) 	-4(5)	-2(4) 	-2(4)

C(3)	13(5) 	36(6)	25(5) 	-3(4)	-3(4) 	-2(4)

C(4)	32(6) 	31(6)	29(6) 	-4(5)	6(4) 	-9(5)

C(5)	21(6) 	45(7)	37(7) 	-16(5)	5(5) 	1(5)

C(6)	34(6) 	22(5)	27(6) 	-11(4)	0(5) 	-2(4)

C(7)	12(5) 	23(5)	16(5) 	7(4)	-4(4) 	0(4)

C(8)	13(5) 	23(5)	26(5) 	-4(4)	-8(4) 	0(4)

C(9)	54(7) 	36(6)	34(6) 	10(5)	4(5) 	-3(5)

C(10)	32(6) 	55(6)	42(6) 	-9(5)	15(5) 	-16(5)

C(11)	54(6) 	45(6)	30(6) 	-2(5)	-1(5) 	-7(5)

C(12)	20(5) 	13(5)	37(6) 	-11(4)	-5(4) 	-8(4)

O(12)	51(4) 	50(4)	42(4) 	-6(4)	11(3) 	-16(4)

C(13)	19(5) 	27(6)	40(6) 	3(5)	-4(4) 	6(4)

O(13)	36(4) 	31(4)	46(4) 	-14(3)	-11(3) 	-3(3)

C(14)	33(6) 	29(6)	38(6) 	-1(5)	-10(5) 	-10(5)

O(14)	41(4) 	41(4)	58(5) 	-2(4)	-34(3) 	16(3)

C(15)	8(5) 	28(6)	48(6) 	13(5)	-15(4) 	3(4)

O(15)	47(4) 	23(4)	64(5) 	-19(4)	-15(3) 	6(3)

C(16)	36(6) 	14(5)	33(5) 	2(4)	2(5) 	-2(5)

O(16)	24(4) 	46(4)	59(4) 	-1(3)	-7(3) 	-2(3)

C(17)	27(6) 	35(6)	49(7) 	-2(5)	-19(5) 	1(4)

O(17)	67(5) 	60(5)	29(4) 	18(4)	-9(4) 	-10(4)

Co(1B)	19(1) 	19(1)	21(1) 	-2(1)	1(1) 	-3(1)

Co(2B)	17(1) 	25(1)	22(1) 	4(1)	-1(1) 	-1(1)

Si(1B)	27(1) 	31(1)	16(1) 	0(1)	2(1) 	2(1)

C(1B)	18(5) 	16(5)	25(5) 	4(4)	3(4) 	-5(4)

O(1B)	14(3) 	24(3)	14(3) 	-4(3)	7(2) 	-2(2)

C(2B)	24(5) 	38(6)	11(5) 	6(4)	7(4) 	4(4)

C(3B)	22(6) 	38(6)	27(6) 	7(5)	-6(4) 	4(5)

C(4B)	46(7) 	15(6)	42(7) 	16(5)	2(5) 	0(5)

C(5B)	37(6) 	14(5)	47(7) 	3(5)	2(5) 	0(5)

C(6B)	19(6) 	13(5)	35(6) 	-1(4)	4(5) 	0(4)

C(7B)	10(4) 	20(5)	22(5) 	-9(4)	1(3) 	-1(4)

C(8B)	15(5) 	7(4)	24(5) 	2(4)	-6(4) 	-1(3)

C(9B)	44(6) 	35(6)	35(6) 	-8(5)	-2(5) 	4(5)

C(10B)	32(6) 	37(6)	47(6) 	-9(5)	12(4) 	-1(5)

C(11B)	45(6) 	59(6)	21(5) 	5(5)	9(4) 	-2(5)

C(12B)	12(5) 	36(6)	30(5) 	19(4)	-2(4) 	3(4)

O(12B)	49(4) 	35(4)	25(4) 	-6(3)	11(3) 	2(3)

C(13B)	32(6) 	34(6)	26(6) 	-9(5)	3(4) 	-12(5)

O(13B)	23(4) 	48(4)	53(4) 	27(4)	5(3) 	-1(3)

C(14B)	30(6) 	12(5)	29(5) 	-1(4)	7(4) 	1(4)

O(14B)	22(4) 	33(4)	70(5) 	0(3)	-6(3) 	2(3)

C(15B)	34(6) 	42(7)	29(6) 	-2(5)	3(4) 	-10(5)

O(15B)	48(5) 	62(5)	53(5) 	40(4)	-11(3) 	8(4)

C(16B)	27(6) 	33(6)	20(5) 	7(4)	-1(4) 	-1(5)

O(16B)	50(5) 	42(4)	41(4) 	-6(3)	-17(3) 	-23(4)

C(17B)	23(5) 	26(5)	30(6) 	-1(4)	-4(4) 	-7(4)

O(17B)	31(4) 	39(4)	29(4) 	10(3)	0(3) 	11(3)

Co(1C)	19(1) 	23(1)	22(1) 	4(1)	-1(1) 	-1(1)

Co(2C)	21(1) 	20(1)	20(1) 	3(1)	-3(1) 	2(1)

Si(1C)	29(2) 	34(2)	21(1) 	-7(1)	-1(1) 	0(1)

C(1C)	25(5) 	17(5)	18(5) 	2(4)	-3(4) 	3(4)

O(1C)	30(4) 	47(4)	6(3) 	-10(3)	4(3) 	7(3)

C(2C)	29(6) 	19(6)	33(6) 	8(5)	-9(4) 	6(5)

C(3C)	20(6) 	36(6)	34(6) 	12(5)	-15(4) 	-10(5)

C(4C)	25(6) 	22(5)	33(6) 	-10(5)	-6(5) 	1(5)

C(5C)	24(5) 	19(5)	18(5) 	2(4)	-6(4) 	5(4)

C(6C)	23(5) 	21(5)	19(5) 	-1(4)	0(4) 	3(4)

C(7C)	11(5) 	16(5)	22(5) 	8(4)	3(4) 	1(4)

C(8C)	23(5) 	17(5)	23(5) 	0(4)	13(4) 	-2(4)

C(9C)	42(6) 	45(6)	49(7) 	-28(5)	-3(5) 	6(5)

C(10C)	57(7) 	49(6)	40(6) 	-18(5)	33(5) 	-15(5)

C(11C)	56(6) 	55(7)	23(5) 	-7(5)	-17(4) 	10(5)

C(12C)	28(6) 	29(6)	51(7) 	21(5)	-11(5) 	7(4)

O(12C)	65(5) 	71(5)	18(4) 	1(3)	14(3) 	15(4)

C(13C)	43(7) 	18(5)	59(7) 	1(5)	13(5) 	-14(5)

O(13C)	40(5) 	40(4)	66(5) 	11(4)	-30(4) 	-8(4)

C(14C)	12(5) 	46(6)	23(5) 	-6(5)	-1(4) 	-13(5)

O(14C)	39(4) 	28(4)	57(4) 	4(3)	-1(3) 	1(3)

C(15C)	38(6) 	17(5)	29(6) 	9(4)	-13(5) 	2(4)

O(15C)	42(4) 	32(4)	41(4) 	5(3)	-13(3) 	5(3)

C(16C)	45(6) 	21(5)	28(5) 	-6(4)	-6(4) 	12(5)

O(16C)	33(4) 	41(4)	39(4) 	13(3)	-9(3) 	-17(3)

C(17C)	20(5) 	36(6)	26(6) 	13(5)	-4(4) 	8(4)

O(17C)	42(4) 	52(4)	34(4) 	-6(3)	1(3) 	9(3)

Co(1D)	18(1) 	20(1)	22(1) 	0(1)	0(1) 	-2(1)

Co(2D)	20(1) 	21(1)	24(1) 	-2(1)	1(1) 	1(1)

Si(1D)	26(1) 	28(1)	19(1) 	3(1)	-2(1) 	4(1)

C(1D)	15(5) 	16(5)	16(5) 	9(4)	0(4) 	2(4)

O(1D)	22(4) 	28(4)	18(4) 	4(3)	-9(3) 	2(3)

C(2D)	26(6) 	23(6)	16(5) 	3(5)	-1(4) 	-1(4)

C(3D)	18(5) 	39(6)	42(6) 	1(5)	7(4) 	1(5)

C(4D)	29(6) 	27(6)	39(6) 	4(5)	14(5) 	3(5)

C(5D)	24(6) 	45(7)	33(6) 	-5(5)	6(5) 	1(5)

C(6D)	24(5) 	18(5)	11(5) 	2(4)	2(4) 	2(4)

C(7D)	15(5) 	18(5)	24(5) 	-1(4)	0(4) 	-3(4)

C(8D)	20(5) 	18(5)	20(5) 	-3(4)	-12(4) 	-6(4)

C(9D)	51(6) 	32(6)	22(5) 	15(4)	-10(4) 	18(5)

C(10D)	25(5) 	61(6)	26(5) 	10(5)	-11(4) 	-2(5)

C(11D)	36(6) 	41(6)	21(5) 	4(4)	1(4) 	-5(4)

C(12D)	30(6) 	24(5)	28(6) 	-6(4)	7(5) 	-6(4)

O(12D)	33(4) 	55(4)	25(4) 	6(3)	-10(3) 	-3(3)

C(13D)	17(5) 	18(5)	46(6) 	11(4)	-5(4) 	4(4)

O(13D)	40(4) 	33(4)	49(4) 	-4(3)	13(3) 	-4(3)

C(14D)	6(5) 	35(6)	32(6) 	-3(5)	-3(4) 	-4(4)

O(14D)	36(4) 	23(4)	60(5) 	-5(3)	1(3) 	-1(3)

C(15D)	28(6) 	29(5)	32(6) 	1(4)	-15(4) 	11(4)

O(15D)	40(4) 	49(4)	35(4) 	-16(3)	13(3) 	8(3)

C(16D)	25(6) 	32(6)	43(6) 	-2(5)	5(5) 	3(5)

O(16D)	43(5) 	45(5)	64(5) 	-20(4)	-9(4) 	-11(4)

C(17D)	18(5) 	6(4)	32(5) 	-11(4)	-2(4) 	5(4)

O(17D)	37(4) 	35(4)	31(4) 	14(3)	-2(3) 	17(3)

______________________________________________________________________________

Table K5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 130.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1A)	6584(60)	1576(62)	281(23)	13(26)

H(2A)	4068(60)	1082(58)	653(21)	32(23)

H(2B)	4470(50)	222(48)	1032(19)	2(19)

H(3A)	3620(61)	-972(55)	524(20)	28(21)

H(3B)	4503(57)	-390(60)	182(24)	44(23)

H(4A)	5292(50)	-2404(54)	519(19)	16(18)

H(4B)	5203(52)	-1742(50)	948(20)	20(20)

H(5A)	7148(55)	-1571(53)	675(19)	7(21)

H(5B)	6838(47)	-1007(46)	336(18)	0(16)

H(6A)	7510(55)	397(53)	845(19)	18(20)

H(6B)	6607(51)	-72(51)	1188(21)	16(20)

H(9A)	5868(36)	-93(15)	1948(6)	62

H(9B)	5500(26)	159(23)	2425(10)	62

H(9C)	6711(13)	623(9)	2260(14)	62

H(10A)	3221(8)	2334(8)	1899(15)	64

H(10B)	3320(10)	1201(36)	2184(7)	64

H(10C)	3459(7)	1118(34)	1682(9)	64

H(11B)	5165(35)	3730(10)	2287(7)	65

H(11C)	6314(8)	3081(27)	2449(11)	65

H(11A)	5105(34)	2817(20)	2665(5)	65

H(1BA)	11585(46)	7595(46)	200(17)	0(17)

H(2BA)	9281(47)	8584(44)	802(18)	3(16)

H(2BB)	9548(57)	7659(60)	386(22)	38(22)

H(3BA)	8826(52)	9591(49)	109(18)	13(18)

H(3BB)	10108(61)	9306(55)	-25(23)	31(21)

H(4BA)	10068(54)	11107(54)	293(20)	0(21)

H(4BB)	9500(50)	10822(48)	701(19)	13(18)

H(5BA)	11396(61)	11213(59)	733(22)	29(24)

H(5BB)	11883(51)	10376(47)	394(18)	8(17)

H(6BA)	10829(76)	9846(72)	1195(29)	87(33)

H(6BB)	12069(62)	9393(58)	1036(22)	20(24)

H(9BA)	11531(14)	8782(11)	2269(13)	57

H(9BB)	10314(24)	9232(23)	2433(9)	57

H(9BC)	10717(34)	9556(14)	1967(5)	57

H(10D)	8023(10)	7236(7)	1810(14)	58

H(10E)	8403(7)	8379(34)	1569(8)	58

H(10F)	8130(12)	8423(33)	2064(7)	58

H(11G)	10972(8)	6360(29)	2453(11)	63

H(11H)	9831(38)	5756(12)	2259(6)	63

H(11I)	9730(36)	6689(20)	2629(6)	63

H(1CA)	11346(67)	3861(63)	4866(24)	30(29)

H(2CA)	12904(50)	4002(50)	3822(21)	18(19)

H(2CB)	12474(52)	4785(53)	4143(19)	5(20)

H(3CA)	14349(58)	4476(58)	4321(20)	24(21)

H(3CB)	13644(44)	4060(44)	4716(18)	0(16)

H(4CA)	14366(59)	2417(58)	4082(23)	39(24)

H(4CB)	14939(83)	2694(85)	4523(31)	91(42)

H(5CA)	13322(50)	1988(50)	4815(20)	12(19)

H(5CB)	13696(56)	1050(59)	4493(20)	30(22)

H(6CA)	12376(52)	1773(52)	3946(21)	26(20)

H(6CB)	11654(53)	1521(52)	4413(20)	19(19)

H(9CC)	11515(40)	593(13)	2870(6)	68

H(9CA)	10460(9)	460(10)	3185(16)	68

H(9CB)	11713(33)	820(8)	3368(10)	68

H(10G)	12291(30)	2972(32)	2583(8)	72

H(10H)	12721(15)	3154(36)	3065(9)	72

H(10I)	11875(15)	4073(10)	2842(16)	72

H(11D)	9693(20)	2070(32)	2409(7)	68

H(11F)	9467(26)	3358(10)	2564(11)	68

H(11E)	8835(10)	2309(39)	2790(5)	68

H(1DA)	5114(61)	1133(60)	-224(21)	17(25)

H(2DA)	3031(49)	1722(51)	-1149(18)	0(18)

H(2DB)	3218(52)	551(55)	-1078(20)	17(19)

H(3DA)	2459(51)	743(54)	-351(20)	20(19)

H(3DB)	1434(57)	1035(53)	-783(19)	18(20)

H(4DA)	1476(54)	2566(52)	-144(20)	27(18)

H(4DB)	1777(62)	3029(64)	-652(23)	41(27)

H(5DA)	3007(62)	3764(62)	-130(22)	34(24)

H(5DB)	3554(74)	2653(76)	85(29)	93(35)

H(6DA)	5015(53)	3117(48)	-384(18)	11(18)

H(6DB)	3880(48)	3379(49)	-781(19)	0(17)

H(9DA)	5282(7)	4787(11)	-1774(14)	53

H(9DC)	4103(33)	4364(7)	-1571(8)	53

H(9DB)	4127(33)	4694(13)	-2063(6)	53

H(10J)	3788(11)	1258(11)	-2226(13)	56

H(10K)	3338(22)	2435(23)	-2434(8)	56

H(10L)	2998(14)	2110(33)	-1960(6)	56

H(11F)	6280(28)	1949(7)	-2414(11)	49

H(11D)	6777(15)	3155(34)	-2247(6)	49

H(11E)	5812(16)	3121(35)	-2620(5)	49

________________________________________________________________________________

Table L1:  Crystal data and structure refinement for 135.

Empirical formula 	C21 H28 Co2 O7 Si

Formula weight 	538.38

Temperature 	148(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 15.1555(4) Å	(= 90°.

b = 11.7868(7) Å	(= 94.730(2)°.

c = 14.1365(8) Å	(= 90°.

Volume	2516.7(2) Å3

Z	4

Density (calculated)	1.421 Mg/m3

Absorption coefficient	1.401 mm-1

F(000)	1112

Crystal size	0.05 x 0.10 x 0.25 mm3

( range for data collection	1.35 to 25.00°.

Index ranges	-17(h(19, -15(k(15, -18(l(16

Reflections collected	18660

Independent reflections	4430 [R(int) = 0.0778]

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4407 / 0 / 362

Goodness-of-fit on F2	0.950

Final R indices [I>2((I)]	R1 = 0.0397, wR2 = 0.0590

R indices (all data)	R1 = 0.1000, wR2 = 0.0710

Extinction coefficient	0.00064(14)

Largest diff. peak and hole	0.300 and -0.315 e.Å-3

Max. and Min. effective transmission	0.870320 and 0.753886

Table L2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 135.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	7868(1)	5872(1)	580(1)	22(1)

Co(2)	7067(1)	5844(1)	2036(1)	21(1)

Si(1)	8897(1)	4055(1)	2251(1)	24(1)

O(1)	5907(2)	4709(2)	-124(2)	29(1)

C(1)	6406(2)	3956(3)	522(2)	21(1)

C(2)	5758(2)	3436(3)	1170(3)	23(1)

C(3)	6134(3)	2436(3)	1763(3)	25(1)

C(4)	6448(2)	1498(3)	1126(3)	21(1)

C(5)	7158(2)	2016(3)	549(3)	23(1)

C(6)	6807(3)	3009(3)	-57(3)	21(1)

C(7)	6719(2)	369(3)	1634(3)	26(1)

C(8)	6944(3)	-524(3)	910(3)	41(1)

C(9)	5945(3)	-93(4)	2143(4)	46(1)

C(10)	7515(3)	513(4)	2355(4)	48(1)

C(11)	7124(2)	4653(3)	1058(2)	18(1)

C(12)	7891(2)	4672(3)	1588(2)	19(1)

C(13)	9465(3)	3092(4)	1463(3)	38(1)

C(14)	8544(3)	3300(4)	3310(3)	38(1)

C(15)	9688(3)	5194(3)	2659(3)	32(1)

C(16)	8517(3)	5156(3)	-236(3)	29(1)

O(16)	8954(2)	4698(2)	-730(2)	46(1)

C(17)	7055(3)	6629(3)	-211(3)	28(1)

O(17)	6569(2)	7134(2)	-695(2)	40(1)

C(18)	8662(3)	6978(3)	936(3)	32(1)

O(18)	9150(2)	7685(2)	1133(2)	53(1)

C(19)	6072(3)	6589(3)	1582(3)	25(1)

O(19)	5448(2)	7054(2)	1300(2)	36(1)

C(20)	7751(2)	6864(3)	2710(3)	30(1)

O(20)	8184(2)	7507(2)	3141(2)	44(1)

C(21)	6647(2)	5088(3)	2998(3)	28(1)

O(21)	6380(2)	4591(2)	3602(2)	43(1)

________________________________________________________________________________

Table L3:  Bond lengths [Å] and angles [°] for 135.

___________________________________________________________________________________

Co(1)-C(16) 	1.788(4)

Co(1)-C(18) 	1.817(4)

Co(1)-C(17) 	1.827(4)

Co(1)-C(11) 	1.980(3)

Co(1)-C(12) 	2.007(3)

Co(1)-Co(2) 	2.4734(7)

Co(2)-C(21) 	1.787(4)

Co(2)-C(20) 	1.807(4)

Co(2)-C(19) 	1.815(4)

Co(2)-C(11) 	1.977(3)

Co(2)-C(12) 	2.000(3)

Si(1)-C(13) 	1.851(4)

Si(1)-C(15) 	1.859(4)

Si(1)-C(14) 	1.857(4)

Si(1)-C(12) 	1.869(4)

O(1)-C(1) 	1.442(4)

C(1)-C(11) 	1.515(5)

C(1)-C(2) 	1.526(5)

C(1)-C(6) 	1.539(4)

C(2)-C(3) 	1.529(5)

C(3)-C(4) 	1.527(5)

C(4)-C(5) 	1.529(5)

C(4)-C(7) 	1.551(5)

C(5)-C(6) 	1.521(5)

C(7)-C(8) 	1.526(5)

C(7)-C(10) 	1.523(6)

C(7)-C(9) 	1.527(5)

C(11)-C(12) 	1.331(4)

C(16)-O(16) 	1.139(4)

C(17)-O(17) 	1.131(4)

C(18)-O(18) 	1.133(4)

C(19)-O(19) 	1.138(4)

C(20)-O(20) 	1.144(4)

C(21)-O(21) 	1.138(4)

C(16)-Co(1)-C(18)	97.4(2)

C(16)-Co(1)-C(17)	102.4(2)

C(18)-Co(1)-C(17)	102.6(2)

C(16)-Co(1)-C(11)	103.69(15)

C(18)-Co(1)-C(11)	144.1(2)

C(17)-Co(1)-C(11)	100.9(2)

C(16)-Co(1)-C(12)	98.43(15)

C(18)-Co(1)-C(12)	109.7(2)

C(17)-Co(1)-C(12)	138.65(15)

C(11)-Co(1)-C(12)	38.99(12)

C(16)-Co(1)-Co(2)	149.76(12)

C(18)-Co(1)-Co(2)	97.99(12)

C(17)-Co(1)-Co(2)	99.42(11)

C(11)-Co(1)-Co(2)	51.26(9)

C(12)-Co(1)-Co(2)	51.76(9)

C(21)-Co(2)-C(20)	98.9(2)

C(21)-Co(2)-C(19)	99.9(2)

C(20)-Co(2)-C(19)	106.8(2)

C(21)-Co(2)-C(11)	102.5(2)

C(20)-Co(2)-C(11)	141.74(15)

C(19)-Co(2)-C(11)	100.3(2)

C(21)-Co(2)-C(12)	99.59(15)

C(20)-Co(2)-C(12)	106.29(15)

C(19)-Co(2)-C(12)	138.1(2)

C(11)-Co(2)-C(12)	39.09(12)

C(21)-Co(2)-Co(1)	150.43(12)

C(20)-Co(2)-Co(1)	97.50(12)

C(19)-Co(2)-Co(1)	98.63(12)

C(11)-Co(2)-Co(1)	51.37(9)

C(12)-Co(2)-Co(1)	52.00(10)

C(13)-Si(1)-C(15)	108.0(2)

C(13)-Si(1)-C(14)	111.7(2)

C(15)-Si(1)-C(14)	108.5(2)

C(13)-Si(1)-C(12)	109.7(2)

C(15)-Si(1)-C(12)	110.7(2)

C(14)-Si(1)-C(12)	108.2(2)

O(1)-C(1)-C(11)	107.5(3)

O(1)-C(1)-C(2)	107.3(3)

C(11)-C(1)-C(2)	112.9(3)

O(1)-C(1)-C(6)	108.6(3)

C(11)-C(1)-C(6)	111.1(3)

C(2)-C(1)-C(6)	109.3(3)

C(1)-C(2)-C(3)	114.2(3)

C(4)-C(3)-C(2)	110.7(3)

C(3)-C(4)-C(5)	107.0(3)

C(3)-C(4)-C(7)	115.5(3)

C(5)-C(4)-C(7)	114.7(3)

C(6)-C(5)-C(4)	112.3(3)

C(5)-C(6)-C(1)	113.1(3)

C(8)-C(7)-C(10)	108.5(4)

C(8)-C(7)-C(9)	107.0(3)

C(10)-C(7)-C(9)	108.7(4)

C(8)-C(7)-C(4)	110.2(3)

C(10)-C(7)-C(4)	112.3(3)

C(9)-C(7)-C(4)	109.9(3)

C(12)-C(11)-C(1)	148.1(3)

C(12)-C(11)-Co(2)	71.4(2)

C(1)-C(11)-Co(2)	131.6(2)

C(12)-C(11)-Co(1)	71.6(2)

C(1)-C(11)-Co(1)	128.9(2)

Co(2)-C(11)-Co(1)	77.37(12)

C(11)-C(12)-Si(1)	156.1(3)

C(11)-C(12)-Co(2)	69.5(2)

Si(1)-C(12)-Co(2)	127.9(2)

C(11)-C(12)-Co(1)	69.4(2)

Si(1)-C(12)-Co(1)	126.6(2)

Co(2)-C(12)-Co(1)	76.24(11)

O(16)-C(16)-Co(1)	177.6(4)

O(17)-C(17)-Co(1)	177.4(3)

O(18)-C(18)-Co(1)	178.0(4)

O(19)-C(19)-Co(2)	179.9(3)

O(20)-C(20)-Co(2)	179.6(4)

O(21)-C(21)-Co(2)	178.9(3)

Table L4:  Anisotropic displacement parameters (Å2 x 103) for 135.  The anisotropic

displacement factor exponent takes the form: -2(2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	21(1) 	23(1)	22(1) 	1(1)	3(1) 	-2(1)

Co(2)	20(1) 	22(1)	21(1) 	-4(1)	2(1) 	1(1)

Si(1)	18(1) 	24(1)	29(1) 	2(1)	-2(1) 	-1(1)

O(1)	27(2) 	22(1)	35(2) 	5(1)	-12(1) 	2(1)

C(1)	20(2) 	21(2)	20(2) 	0(2)	1(2) 	-1(2)

C(2)	18(2) 	21(2)	31(3) 	-5(2)	1(2) 	4(2)

C(3)	24(2) 	25(2)	27(3) 	0(2)	8(2) 	-4(2)

C(4)	19(2) 	19(2)	23(2) 	-2(2)	-2(2) 	-2(2)

C(5)	21(2) 	24(2)	24(3) 	-8(2)	3(2) 	-1(2)

C(6)	24(2) 	23(2)	14(2) 	0(2)	-1(2) 	-1(2)

C(7)	30(2) 	20(2)	27(3) 	-4(2)	-1(2) 	-2(2)

C(8)	65(4) 	23(2)	35(3) 	3(2)	3(2) 	6(2)

C(9)	58(3) 	29(3)	53(4) 	11(2)	18(3) 	-3(2)

C(10)	63(4) 	33(3)	43(3) 	8(2)	-20(3) 	2(3)

C(11)	17(2) 	18(2)	20(2) 	-2(2)	5(2) 	4(2)

C(12)	20(2) 	15(2)	23(2) 	-2(2)	8(2) 	0(2)

C(13)	26(3) 	40(3)	48(3) 	-8(2)	-2(2) 	12(2)

C(14)	25(3) 	47(3)	42(3) 	17(2)	-5(2) 	-4(2)

C(15)	21(3) 	32(3)	42(3) 	2(2)	-7(2) 	-1(2)

C(16)	27(3) 	35(2)	25(3) 	5(2)	0(2) 	-7(2)

O(16)	39(2) 	61(2)	40(2) 	-9(2)	16(2) 	5(2)

C(17)	30(3) 	30(2)	24(3) 	2(2)	9(2) 	-1(2)

O(17)	33(2) 	49(2)	39(2) 	18(2)	1(2) 	4(2)

C(18)	30(3) 	37(2)	29(3) 	4(2)	2(2) 	-4(2)

O(18)	46(2) 	44(2)	67(2) 	-2(2)	-4(2) 	-26(2)

C(19)	30(3) 	24(2)	23(3) 	-4(2)	8(2) 	-4(2)

O(19)	27(2) 	37(2)	41(2) 	-1(1)	-4(1) 	6(1)

C(20)	27(3) 	31(2)	31(3) 	-7(2)	5(2) 	4(2)

O(20)	31(2) 	47(2)	54(2) 	-28(2)	2(2) 	-6(1)

C(21)	25(2) 	35(2)	22(3) 	-7(2)	-3(2) 	3(2)

O(21)	40(2) 	57(2)	32(2) 	11(2)	6(2) 	-2(1)

______________________________________________________________________________

Table L5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 135.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1A)	5425(2)	4428(2)	-277(2)	34

H(1B)	5839(2)	5346(2)	142(2)	34

H(1C)	6185(2)	4819(2)	-614(2)	34

H(2A)	5256(21)	3182(25)	749(23)	28

H(2B)	5572(21)	3972(27)	1531(23)	28

H(3A)	6619(22)	2635(26)	2247(23)	30

H(3B)	5703(21)	2166(26)	2144(22)	30

H(4A)	5963(21)	1299(24)	699(22)	25

H(5A)	7665(21)	2249(26)	951(23)	27

H(5B)	7390(20)	1452(25)	164(23)	27

H(6B)	7278(21)	3314(24)	-377(22)	25

H(6A)	6332(20)	2747(25)	-566(22)	25

H(8C)	7482(26)	-354(32)	629(30)	62

H(8A)	6471(26)	-594(32)	443(30)	62

H(8B)	7044(25)	-1260(32)	1202(27)	62

H(9A)	5798(27)	396(34)	2709(29)	69

H(9C)	6105(25)	-849(35)	2404(29)	69

H(9B)	5357(27)	-103(33)	1702(30)	69

H(10C)	7425(29)	994(34)	2837(30)	71

H(10B)	8041(27)	715(34)	2032(31)	71

H(10A)	7629(26)	-243(35)	2639(29)	71

H(13B)	10014(26)	2885(31)	1768(28)	57

H(13C)	9556(26)	3344(31)	845(29)	57

H(13A)	9183(25)	2388(32)	1319(27)	57

H(14C)	8982(26)	2938(31)	3649(28)	57

H(14B)	8039(25)	2803(31)	3151(27)	57

H(14A)	8363(26)	3772(31)	3781(28)	57

H(15A)	10174(23)	4878(30)	2990(26)	49

H(15B)	9440(24)	5715(30)	3100(26)	49

H(15C)	9853(23)	5649(30)	2129(26)	49

________________________________________________________________________________

Table M1:  Crystal data and structure refinement for 136.

Empirical formula 	C21 H28 Co2 O7 Si

Formula weight 	538.38

Temperature 	148(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21

Unit cell dimensions	a = 8.617(6) Å	(= 90°.

b = 16.526(9) Å	(= 94.938(15)°.

c = 8.767(6) Å	(= 90°.

Volume	1243.8(14) Å3

Z	2

Density (calculated)	1.438 Mg/m3

Absorption coefficient	1.418 mm-1

F(000)	556

Crystal size	0.04 x 0.22 x 0.34 mm3

( range for data collection	2.33 to 25.00°.

Index ranges	-11(h(11, -21(k(21, -11(l(11

Reflections collected	10317

Independent reflections	4295 [R(int) = 0.0358]

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4293 / 1 / 365

Goodness-of-fit on F2	0.974

Final R indices [I>2((I)]	R1 = 0.0381, wR2 = 0.0699

R indices (all data)	R1 = 0.0570, wR2 = 0.0751

Absolute structure parameter	0.00(2)

Extinction coefficient	0.0010(7)

Largest diff. peak and hole	0.323 and -0.333 e.Å-3

Max. and Min. effective transmission	0.828674 and 0.653084

Table M2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 136.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	-3575(1)	-2665(1)	-4793(1)	23(1)

Co(2)	-3615(1)	-3808(1)	-6629(1)	22(1)

Si(1)	-6867(1)	-3863(1)	-4475(1)	27(1)

C(1)	-5725(5)	-2343(2)	-7915(5)	24(1)

O(1)	-4554(5)	-2176(2)	-8943(5)	45(1)

C(2)	-7087(6)	-2798(3)	-8777(5)	28(1)

C(3)	-7995(7)	-2276(3)	-9966(6)	29(1)

C(4)	-8623(6)	-1509(2)	-9256(5)	23(1)

C(5)	-7247(6)	-1041(3)	-8504(6)	32(1)

C(6)	-6339(7)	-1547(3)	-7283(6)	31(1)

C(7)	-9734(5)	-989(2)	-10358(5)	25(1)

C(8)	-8884(9)	-655(5)	-11681(9)	65(2)

C(9)	-10396(10)	-287(4)	-9488(8)	65(2)

C(10)	-11092(9)	-1486(4)	-11026(9)	56(2)

C(11)	-5008(5)	-2868(2)	-6638(5)	22(1)

C(12)	-5361(5)	-3364(2)	-5530(5)	20(1)

C(13)	-8429(8)	-3116(4)	-4194(7)	51(2)

C(14)	-7704(9)	-4732(4)	-5618(8)	52(2)

C(15)	-5984(8)	-4223(5)	-2590(7)	54(2)

C(16)	-4600(6)	-1931(3)	-3745(6)	32(1)

O(16)	-5271(5)	-1473(2)	-3091(5)	49(1)

C(17)	-2106(6)	-2026(3)	-5547(6)	32(1)

O(17)	-1209(5)	-1610(2)	-6024(5)	52(1)

C(18)	-2616(6)	-3209(3)	-3161(6)	32(1)

O(18)	-2043(5)	-3552(2)	-2151(4)	48(1)

C(19)	-2081(6)	-3451(2)	-7778(5)	31(1)

O(19)	-1107(4)	-3239(2)	-8469(4)	48(1)

C(20)	-2671(6)	-4580(3)	-5427(5)	33(1)

O(20)	-2027(5)	-5068(2)	-4698(4)	52(1)

C(21)	-4690(6)	-4461(3)	-7998(6)	28(1)

O(21)	-5353(4)	-4874(2)	-8853(4)	41(1)

________________________________________________________________________________

Table M3:  Bond lengths [Å] and angles [°] for 136.

___________________________________________________________________________________

Co(1)-C(16) 	1.799(5)

Co(1)-C(17) 	1.816(6)

Co(1)-C(18) 	1.826(5)

Co(1)-C(11) 	1.977(4)

Co(1)-C(12) 	1.987(4)

Co(1)-Co(2) 	2.4803(13)

Co(2)-C(20) 	1.803(5)

Co(2)-C(21) 	1.808(5)

Co(2)-C(19) 	1.828(5)

Co(2)-C(11) 	1.963(4)

Co(2)-C(12) 	1.995(4)

Si(1)-C(12) 	1.851(5)

Si(1)-C(15) 	1.857(6)

Si(1)-C(13) 	1.858(7)

Si(1)-C(14) 	1.860(6)

C(1)-O(1) 	1.437(6)

C(1)-C(11) 	1.507(6)

C(1)-C(2) 	1.537(7)

C(1)-C(6) 	1.538(6)

C(2)-C(3) 	1.517(6)

C(3)-C(4) 	1.531(6)

C(4)-C(5) 	1.518(7)

C(4)-C(7) 	1.559(6)

C(5)-C(6) 	1.521(7)

C(7)-C(10) 	1.506(8)

C(7)-C(9) 	1.526(8)

C(7)-C(8) 	1.528(7)

C(11)-C(12) 	1.326(6)

C(16)-O(16) 	1.137(5)

C(17)-O(17) 	1.141(6)

C(18)-O(18) 	1.129(6)

C(19)-O(19) 	1.132(5)

C(20)-O(20) 	1.143(5)

C(21)-O(21) 	1.131(5)

C(16)-Co(1)-C(17)	100.5(2)

C(16)-Co(1)-C(18)	98.1(2)

C(17)-Co(1)-C(18)	106.8(2)

C(16)-Co(1)-C(11)	103.4(2)

C(17)-Co(1)-C(11)	101.9(2)

C(18)-Co(1)-C(11)	140.0(2)

C(16)-Co(1)-C(12)	99.1(2)

C(17)-Co(1)-C(12)	139.8(2)

C(18)-Co(1)-C(12)	104.7(2)

C(11)-Co(1)-C(12)	39.1(2)

C(16)-Co(1)-Co(2)	149.9(2)

C(17)-Co(1)-Co(2)	100.27(14)

C(18)-Co(1)-Co(2)	96.50(14)

C(11)-Co(1)-Co(2)	50.74(11)

C(12)-Co(1)-Co(2)	51.61(13)

C(20)-Co(2)-C(21)	98.4(2)

C(20)-Co(2)-C(19)	103.8(2)

C(21)-Co(2)-C(19)	100.4(2)

C(20)-Co(2)-C(11)	143.8(2)

C(21)-Co(2)-C(11)	101.0(2)

C(19)-Co(2)-C(11)	102.3(2)

C(20)-Co(2)-C(12)	107.4(2)

C(21)-Co(2)-C(12)	100.1(2)

C(19)-Co(2)-C(12)	139.3(2)

C(11)-Co(2)-C(12)	39.1(2)

C(20)-Co(2)-Co(1)	100.34(15)

C(21)-Co(2)-Co(1)	149.6(2)

C(19)-Co(2)-Co(1)	98.11(14)

C(11)-Co(2)-Co(1)	51.24(13)

C(12)-Co(2)-Co(1)	51.34(12)

C(12)-Si(1)-C(15)	109.7(3)

C(12)-Si(1)-C(13)	108.5(3)

C(15)-Si(1)-C(13)	109.9(3)

C(12)-Si(1)-C(14)	109.3(3)

C(15)-Si(1)-C(14)	110.0(3)

C(13)-Si(1)-C(14)	109.4(3)

O(1)-C(1)-C(11)	108.1(4)

O(1)-C(1)-C(2)	109.5(4)

C(11)-C(1)-C(2)	109.3(3)

O(1)-C(1)-C(6)	110.1(4)

C(11)-C(1)-C(6)	110.9(3)

C(2)-C(1)-C(6)	108.9(4)

C(3)-C(2)-C(1)	112.8(4)

C(2)-C(3)-C(4)	111.7(4)

C(5)-C(4)-C(3)	107.9(4)

C(5)-C(4)-C(7)	113.8(3)

C(3)-C(4)-C(7)	115.1(4)

C(4)-C(5)-C(6)	111.2(4)

C(5)-C(6)-C(1)	112.9(4)

C(10)-C(7)-C(9)	107.3(6)

C(10)-C(7)-C(8)	108.0(5)

C(9)-C(7)-C(8)	109.2(5)

C(10)-C(7)-C(4)	110.8(4)

C(9)-C(7)-C(4)	110.2(4)

C(8)-C(7)-C(4)	111.1(4)

C(12)-C(11)-C(1)	142.7(4)

C(12)-C(11)-Co(2)	71.7(2)

C(1)-C(11)-Co(2)	132.1(3)

C(12)-C(11)-Co(1)	70.9(3)

C(1)-C(11)-Co(1)	134.2(3)

Co(2)-C(11)-Co(1)	78.0(2)

C(11)-C(12)-Si(1)	148.9(4)

C(11)-C(12)-Co(1)	70.0(3)

Si(1)-C(12)-Co(1)	130.8(2)

C(11)-C(12)-Co(2)	69.1(3)

Si(1)-C(12)-Co(2)	131.9(2)

Co(1)-C(12)-Co(2)	77.1(2)

O(16)-C(16)-Co(1)	178.8(5)

O(17)-C(17)-Co(1)	178.4(4)

O(18)-C(18)-Co(1)	178.9(5)

O(19)-C(19)-Co(2)	178.5(5)

O(20)-C(20)-Co(2)	177.5(5)

O(21)-C(21)-Co(2)	179.4(4)

Table M4:  Anisotropic displacement parameters (Å2 x 103) for 136.  The anisotropic

displacement factor exponent takes the form: -2(2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	22(1) 	24(1)	23(1) 	-1(1)	2(1) 	0(1)

Co(2)	22(1) 	23(1)	22(1) 	0(1)	5(1) 	3(1)

Si(1)	23(1) 	34(1)	24(1) 	0(1)	5(1) 	-5(1)

C(1)	26(3) 	28(2)	21(2) 	3(2)	10(2) 	0(2)

O(1)	32(2) 	62(3)	44(2) 	26(2)	13(2) 	9(2)

C(2)	39(3) 	18(2)	28(3) 	-4(2)	2(2) 	8(2)

C(3)	36(3) 	27(2)	23(3) 	-1(2)	1(2) 	6(2)

C(4)	25(3) 	20(2)	23(3) 	5(2)	7(2) 	2(2)

C(5)	33(3) 	27(2)	34(3) 	1(2)	-5(2) 	4(2)

C(6)	33(3) 	19(2)	37(3) 	-3(2)	-9(3) 	0(2)

C(7)	20(3) 	28(2)	29(3) 	6(2)	5(2) 	0(2)

C(8)	42(4) 	93(5)	61(5) 	50(4)	14(4) 	15(4)

C(9)	66(6) 	64(4)	63(5) 	-9(3)	-8(4) 	46(4)

C(10)	44(5) 	46(3)	75(5) 	21(3)	-23(4) 	-8(3)

C(11)	21(3) 	21(2)	25(2) 	-4(2)	5(2) 	1(2)

C(12)	20(2) 	19(2)	20(2) 	-4(2)	2(2) 	-1(2)

C(13)	32(4) 	66(4)	56(4) 	-6(3)	19(3) 	1(3)

C(14)	57(5) 	46(3)	54(4) 	-8(3)	12(3) 	-20(3)

C(15)	47(4) 	83(4)	32(3) 	28(3)	-1(3) 	-18(4)

C(16)	29(3) 	33(2)	31(3) 	-1(2)	-3(2) 	-7(2)

O(16)	44(3) 	47(2)	58(3) 	-25(2)	14(2) 	1(2)

C(17)	33(3) 	28(2)	35(3) 	-6(2)	5(2) 	4(2)

O(17)	50(3) 	41(2)	67(3) 	-4(2)	22(2) 	-14(2)

C(18)	32(3) 	29(2)	35(3) 	-8(2)	-1(2) 	0(2)

O(18)	58(3) 	49(2)	35(2) 	7(2)	-14(2) 	5(2)

C(19)	32(3) 	28(2)	33(3) 	0(2)	8(2) 	5(2)

O(19)	50(3) 	48(2)	51(2) 	-2(2)	28(2) 	-8(2)

C(20)	37(3) 	34(2)	29(3) 	0(2)	9(2) 	10(2)

O(20)	72(3) 	46(2)	39(2) 	12(2)	11(2) 	25(2)

C(21)	24(3) 	28(2)	31(3) 	3(2)	4(2) 	8(2)

O(21)	51(3) 	34(2)	37(2) 	-10(2)	-3(2) 	0(2)

______________________________________________________________________________

Table M5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 136.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(11A)	-4357(109)	-1894(43)	-9128(96)	68

H(4A)	-6671(59)	-3180(29)	-9071(57)	34

H(4B)	-7840(57)	-3023(26)	-8046(53)	34

H(5A)	-8882(56)	-2578(29)	-10391(48)	34

H(5B)	-7379(61)	-2158(27)	-10709(57)	34

H(9A)	-9347(55)	-1683(24)	-8409(52)	27

H(8A)	-7622(58)	-477(27)	-8057(54)	38

H(8B)	-6578(60)	-881(29)	-9284(57)	38

H(7A)	-5564(64)	-1264(27)	-6815(59)	37

H(7B)	-7073(59)	-1742(26)	-6437(57)	37

H(2A)	-7872(101)	-452(40)	-11550(87)	97

H(2B)	-9584(98)	-336(41)	-12236(86)	97

H(2C)	-8690(94)	-1059(45)	-12314(87)	97

H(3A)	-9457(97)	21(44)	-9375(82)	97

H(3B)	-10893(94)	-516(43)	-8715(93)	97

H(3C)	-11138(96)	63(45)	-10048(84)	97

H(1A)	-10543(89)	-1884(40)	-11599(80)	85

H(1B)	-11854(80)	-1170(36)	-11638(80)	85

H(1C)	-11533(89)	-1671(45)	-10377(88)	85

H(18A)	-9419(82)	-3310(36)	-3887(70)	76

H(18B)	-8809(84)	-2993(39)	-4933(77)	76

H(18C)	-8029(72)	-2579(40)	-3784(68)	76

H(6A)	-8680(83)	-4933(40)	-5067(70)	77

H(6B)	-6922(86)	-5109(38)	-5741(73)	77

H(6C)	-8020(81)	-4538(38)	-6544(78)	77

H(13A)	-6559(80)	-4603(40)	-2211(75)	81

H(13B)	-5708(75)	-3732(43)	-1986(75)	81

H(13C)	-5115(87)	-4546(38)	-2545(77)	81

________________________________________________________________________________

Table N1:  Crystal data and structure refinement for 142.

Empirical formula 	C46 H40 O2 Si2

Formula weight 	680.96

Temperature 	148(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 9.406(4) Å	(= 79.557(9)°.

b = 9.501(4) Å	(= 81.686(9)°.

c = 12.006(5) Å	(= 61.650(8)°.

Volume	926.5(7) Å3

Z	1

Density (calculated)	1.220 Mg/m3

Absorption coefficient	0.134 mm-1

F(000)	360

Crystal size	0.12 x 0.14 x 0.20 mm3

( range for data collection	1.73 to 23.32°.

Index ranges	-10(h(10, -10(k(10, -13(l(12

Reflections collected	6091

Independent reflections	2661 [R(int) = 0.0668]

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	2661 / 0 / 307

Goodness-of-fit on F2	0.994

Final R indices [I>2((I)]	R1 = 0.0593, wR2 = 0.1278

R indices (all data)	R1 = 0.1026, wR2 = 0.1464

Extinction coefficient	0.0229(46)

Largest diff. peak and hole	0.355 and -0.255 e.Å-3

Max. and Min effective transmission	0.982099 and 0.620956

Table N2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 142.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Si(1)	4154(1)	9106(1)	2649(1)	21(1)

O(1)	2638(3)	7139(3)	-601(2)	29(1)

C(1)	1640(4)	8576(4)	-82(3)	20(1)

C(2)	1116(5)	10079(5)	-966(3)	22(1)

C(3)	-139(5)	11590(5)	-472(3)	20(1)

C(4)	2525(4)	8703(4)	807(3)	21(1)

C(5)	3207(4)	8851(4)	1512(3)	23(1)

C(6)	6325(4)	7517(4)	2663(3)	22(1)

C(7)	7006(5)	6358(5)	1913(3)	26(1)

C(8)	8621(5)	5182(5)	1947(4)	34(1)

C(9)	9566(6)	5136(6)	2744(4)	34(1)

C(10)	8923(5)	6261(5)	3500(4)	32(1)

C(11)	7332(5)	7424(5)	3453(4)	28(1)

C(12)	3118(4)	8798(4)	4056(3)	21(1)

C(13)	2174(5)	10014(5)	4745(4)	27(1)

C(14)	1463(5)	9688(5)	5793(4)	30(1)

C(15)	1653(5)	8160(5)	6161(4)	30(1)

C(16)	2548(5)	6935(6)	5495(4)	32(1)

C(17)	3265(5)	7255(5)	4466(4)	28(1)

C(18)	3989(4)	11185(4)	2370(3)	22(1)

C(19)	3495(5)	12178(5)	1340(3)	26(1)

C(20)	3383(5)	13708(5)	1150(4)	32(1)

C(21)	3748(5)	14294(5)	1985(4)	33(1)

C(22)	4250(5)	13337(5)	2999(4)	35(1)

C(23)	4367(5)	11802(5)	3197(4)	30(1)

________________________________________________________________________________

Table N3:  Bond lengths [Å] and angles [°] for 142.

___________________________________________________________________________________

Si(1)-C(5) 	1.842(4)

Si(1)-C(12) 	1.872(4)

Si(1)-C(18) 	1.876(4)

Si(1)-C(6) 	1.877(4)

O(1)-C(1) 	1.434(4)

C(1)-C(4) 	1.499(5)

C(1)-C(2) 	1.531(5)

C(1)-C(3)#1 	1.537(5)

C(2)-C(3) 	1.518(5)

C(3)-C(1)#1 	1.537(5)

C(4)-C(5) 	1.197(5)

C(6)-C(7) 	1.398(5)

C(6)-C(11) 	1.398(5)

C(7)-C(8) 	1.395(6)

C(8)-C(9) 	1.380(6)

C(9)-C(10) 	1.382(6)

C(10)-C(11) 	1.377(6)

C(12)-C(13) 	1.403(5)

C(12)-C(17) 	1.406(5)

C(13)-C(14) 	1.392(6)

C(14)-C(15) 	1.370(6)

C(15)-C(16) 	1.384(6)

C(16)-C(17) 	1.375(6)

C(18)-C(19) 	1.401(5)

C(18)-C(23) 	1.402(5)

C(19)-C(20) 	1.385(6)

C(20)-C(21) 	1.384(6)

C(21)-C(22) 	1.374(6)

C(22)-C(23) 	1.388(6)

C(5)-Si(1)-C(12)	109.6(2)

C(5)-Si(1)-C(18)	108.6(2)

C(12)-Si(1)-C(18)	110.9(2)

C(5)-Si(1)-C(6)	108.6(2)

C(12)-Si(1)-C(6)	107.8(2)

C(18)-Si(1)-C(6)	111.3(2)

O(1)-C(1)-C(4)	110.2(3)

O(1)-C(1)-C(2)	111.2(3)

C(4)-C(1)-C(2)	110.0(3)

O(1)-C(1)-C(3)#1	106.1(3)

C(4)-C(1)-C(3)#1	109.8(3)

C(2)-C(1)-C(3)#1	109.5(3)

C(3)-C(2)-C(1)	112.3(3)

C(2)-C(3)-C(1)#1	112.2(3)

C(5)-C(4)-C(1)	178.2(4)

C(4)-C(5)-Si(1)	176.8(3)

C(7)-C(6)-C(11)	116.8(4)

C(7)-C(6)-Si(1)	122.5(3)

C(11)-C(6)-Si(1)	120.7(3)

C(8)-C(7)-C(6)	121.3(4)

C(9)-C(8)-C(7)	119.7(4)

C(8)-C(9)-C(10)	120.3(4)

C(11)-C(10)-C(9)	119.5(4)

C(10)-C(11)-C(6)	122.4(4)

C(13)-C(12)-C(17)	116.5(4)

C(13)-C(12)-Si(1)	124.6(3)

C(17)-C(12)-Si(1)	119.0(3)

C(14)-C(13)-C(12)	121.3(4)

C(15)-C(14)-C(13)	120.1(4)

C(14)-C(15)-C(16)	120.3(4)

C(17)-C(16)-C(15)	119.6(4)

C(16)-C(17)-C(12)	122.2(4)

C(19)-C(18)-C(23)	117.3(4)

C(19)-C(18)-Si(1)	122.1(3)

C(23)-C(18)-Si(1)	120.6(3)

C(20)-C(19)-C(18)	121.2(4)

C(21)-C(20)-C(19)	120.3(5)

C(22)-C(21)-C(20)	119.6(4)

C(21)-C(22)-C(23)	120.5(4)

C(22)-C(23)-C(18)	121.1(4)

____________________________________________________________________________________

Symmetry transformations used to generate equivalent atoms:  #1 -x,-y+2,-z

Table N4:  Anisotropic displacement parameters (Å2 x 103) for 142.  The anisotropic

displacement factor exponent takes the form: -2(2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Si(1)	25(1) 	21(1)	21(1) 	-2(1)	-6(1) 	-11(1)

O(1)	27(2) 	25(2)	35(2) 	-10(1)	-3(1) 	-10(1)

C(1)	22(2) 	20(2)	20(2) 	-5(2)	0(2) 	-10(2)

C(2)	22(2) 	28(3)	19(2) 	-3(2)	1(2) 	-16(2)

C(3)	27(2) 	21(2)	16(2) 	7(2)	-8(2) 	-15(2)

C(4)	21(2) 	16(2)	25(2) 	0(2)	-1(2) 	-7(2)

C(5)	26(2) 	23(2)	19(2) 	-4(2)	-1(2) 	-11(2)

C(6)	24(2) 	21(2)	22(2) 	0(2)	0(2) 	-14(2)

C(7)	29(3) 	31(3)	16(2) 	-4(2)	1(2) 	-12(2)

C(8)	40(3) 	30(3)	28(3) 	-8(2)	8(2) 	-14(2)

C(9)	19(3) 	35(3)	42(3) 	1(2)	4(2) 	-12(2)

C(10)	23(3) 	32(3)	43(3) 	-3(2)	-10(2) 	-13(2)

C(11)	30(3) 	22(2)	33(3) 	-4(2)	-6(2) 	-11(2)

C(12)	16(2) 	23(2)	23(2) 	-1(2)	-7(2) 	-7(2)

C(13)	26(2) 	25(3)	30(3) 	-4(2)	-7(2) 	-11(2)

C(14)	35(3) 	32(3)	24(3) 	-6(2)	2(2) 	-17(2)

C(15)	33(3) 	35(3)	26(3) 	-2(2)	-2(2) 	-18(2)

C(16)	35(3) 	28(3)	36(3) 	3(2)	-3(2) 	-20(2)

C(17)	33(3) 	27(3)	24(3) 	-6(2)	3(2) 	-16(2)

C(18)	18(2) 	18(2)	30(3) 	-3(2)	1(2) 	-9(2)

C(19)	33(3) 	21(2)	21(2) 	-4(2)	4(2) 	-11(2)

C(20)	37(3) 	26(3)	28(3) 	-2(2)	9(2) 	-13(2)

C(21)	27(3) 	22(3)	47(3) 	-7(2)	7(2) 	-11(2)

C(22)	37(3) 	26(3)	51(3) 	-6(3)	-15(3) 	-18(2)

C(23)	28(3) 	29(3)	30(3) 	-1(2)	-11(2) 	-11(2)

______________________________________________________________________________

Table N5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 142.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1)	3576(64)	7139(61)	-883(43)	81(20)

H(2A)	668(40)	9857(39)	-1556(29)	21(9)

H(2B)	2056(45)	10199(41)	-1310(29)	24(10)

H(3A)	394(39)	11750(38)	161(29)	20(9)

H(3B)	-462(38)	12439(41)	-1030(29)	12(9)

H(7)	6357(40)	6395(39)	1378(29)	18(9)

H(8)	9042(51)	4395(52)	1429(37)	56(14)

H(9)	10615(45)	4419(42)	2741(29)	18(10)

H(10)	9576(42)	6200(40)	4026(30)	23(10)

H(11)	6841(45)	8184(48)	3988(33)	39(12)

H(13)	1973(43)	11097(47)	4458(31)	29(11)

H(14)	850(41)	10480(43)	6231(30)	19(10)

H(15)	1169(52)	7906(51)	6932(38)	51(13)

H(16)	2545(44)	5973(48)	5708(31)	33(12)

H(17)	3869(50)	6470(51)	4045(36)	43(13)

H(19)	3256(39)	11774(40)	685(29)	23(9)

H(20)	3033(51)	14403(52)	470(38)	46(14)

H(21)	3666(44)	15344(49)	1875(31)	35(12)

H(22)	4455(42)	13661(43)	3548(31)	23(11)

H(23)	4791(39)	11118(40)	3866(29)	15(10)

________________________________________________________________________________

Table O1:  Crystal data and structure refinement for 144.

Empirical formula 	C59 H42 Cl2 Co4 O14 Si2

Formula weight 	1337.73

Temperature 	148(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 13.309(5) Å	(= 110.403(7)°.

b = 14.193(5) Å	(= 105.961(7)°.

c = 17.751(7) Å	(= 100.478(8)°.

Volume	2874.5(19) Å3

Z	2

Density (calculated)	1.546 Mg/m3

Absorption coefficient	1.334 mm-1

F(000)	1356

Crystal size	0.10 x 0.20 x 0.28 mm3

( range for data collection	1.32 to 21.50°.

Index ranges	-17(h(17, -18(k(18, -22(l(22

Reflections collected	19969

Independent reflections	19969 [R(int) = 0.0000]

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	19894 / 0 / 389

Goodness-of-fit on F2	0.915

Final R indices [I>2((I)]	R1 = 0.0856, wR2 = 0.1977

R indices (all data)	R1 = 0.1664, wR2 = 0.2335

Extinction coefficient	0.0060(11)

Largest diff. peak and hole	1.092 and -0.891 e.Å-3

Table O2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 144.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	3646(1)	7300(1)	5178(1)	26(1)

Co(2)	2042(1)	5708(1)	4217(1)	26(1)

Co(3)	4249(1)	8158(1)	716(1)	25(1)

Co(4)	2672(1)	6550(1)	-246(1)	23(1)

Si(1)	1209(2)	8021(2)	4582(2)	26(1)

Si(2)	1764(2)	8834(2)	217(2)	22(1)

C(1)	2994(8)	6805(8)	3175(7)	30(3)

O(1A)	3970(15)	6396(14)	3175(10)	37(6)

O(1B)	3402(16)	5867(15)	2888(11)	40(7)

C(2)	2009(9)	6321(9)	2376(6)	36(3)

C(3)	2228(9)	6355(8)	1575(7)	38(3)

C(4)	2808(8)	7487(8)	1743(6)	22(3)

O(4A)	1798(13)	7766(14)	1790(10)	40(6)

O(4B)	2328(14)	8328(13)	2093(10)	31(6)

C(5)	3766(9)	7934(9)	2494(7)	40(3)

C(6)	3609(10)	7911(9)	3323(7)	50(4)

C(7)	2738(8)	6861(8)	3978(7)	28(3)

C(8)	2188(8)	7234(7)	4450(6)	23(3)

C(9)	2952(7)	7546(7)	925(6)	17(3)

C(10)	2631(7)	8002(7)	410(6)	16(2)

O(11)	4859(5)	9545(6)	5815(5)	44(2)

C(11)	4354(8)	8703(8)	5571(7)	30(3)

O(12)	3614(6)	7309(6)	6835(5)	41(2)

C(12)	3606(8)	7308(7)	6181(6)	21(3)

O(13)	5445(6)	6447(6)	4931(5)	51(2)

C(13)	4726(10)	6752(9)	5007(8)	43(3)

C(14)	1598(9)	5450(8)	5045(7)	33(3)

O(14)	1251(6)	5215(6)	5487(5)	44(2)

O(15)	3314(6)	4236(6)	3755(5)	57(2)

C(15)	2820(9)	4819(8)	3970(7)	33(3)

O(16)	6(5)	4517(5)	2701(4)	36(2)

C(16)	816(8)	5010(7)	3323(6)	22(3)

C(17)	444(7)	7722(7)	5258(6)	13(2)

C(18)	948(9)	7528(8)	5958(6)	35(3)

C(19)	388(9)	7352(8)	6486(7)	46(3)

C(20)	-701(8)	7303(7)	6275(7)	35(3)

C(21)	-1220(10)	7448(8)	5565(7)	48(3)

C(22)	-663(8)	7649(7)	5045(7)	32(3)

C(23)	1966(8)	9475(8)	5154(7)	33(3)

C(24)	1907(8)	10091(8)	5929(6)	28(3)

C(25)	2449(9)	11179(9)	6373(8)	50(4)

C(26)	3092(9)	11625(9)	6012(7)	44(3)

C(27)	3190(9)	11053(9)	5264(7)	44(3)

C(28)	2624(8)	9951(8)	4815(7)	40(3)

C(29)	166(7)	7715(7)	3506(6)	22(3)

C(30)	181(8)	8368(8)	3087(6)	31(3)

C(31)	-581(8)	8068(8)	2279(7)	41(3)

C(32)	-1442(9)	7170(8)	1879(7)	46(3)

C(33)	-1485(8)	6471(8)	2274(7)	37(3)

C(34)	-696(7)	6748(8)	3088(6)	30(3)

O(35)	5388(5)	10144(5)	2286(4)	36(2)

C(35)	4904(8)	9399(8)	1657(7)	29(3)

O(36)	5816(6)	7054(6)	1200(5)	50(2)

C(36)	5190(9)	7486(8)	1004(7)	40(3)

C(37)	4623(9)	8515(9)	-110(8)	43(4)

O(37)	4860(6)	8753(6)	-586(5)	53(3)

O(38)	409(6)	5200(5)	-843(4)	43(2)

C(38)	1288(8)	5743(7)	-616(6)	21(3)

O(39)	3680(6)	4918(6)	-3(5)	49(2)

C(39)	3305(8)	5565(8)	-103(7)	33(3)

O(40)	2681(6)	6442(6)	-1944(5)	52(3)

C(40)	2662(9)	6490(9)	-1278(8)	41(3)

C(41)	1999(8)	9883(7)	1293(6)	25(3)

C(42)	3067(8)	10660(7)	1789(6)	31(3)

C(43)	3313(9)	11390(8)	2614(7)	41(3)

C(44)	2536(8)	11360(8)	2980(7)	38(3)

C(45)	1472(9)	10614(8)	2525(7)	41(3)

C(46)	1237(8)	9907(8)	1664(6)	31(3)

C(47)	265(8)	7967(8)	-337(6)	23(3)

C(48)	-179(8)	7352(8)	36(7)	37(3)

C(49)	-1285(8)	6709(8)	-371(7)	35(3)

C(50)	-1848(10)	6687(9)	-1115(7)	45(3)

C(51)	-1450(9)	7313(9)	-1484(8)	53(4)

C(52)	-374(8)	7947(8)	-1095(7)	36(3)

C(53)	2106(8)	9521(8)	-462(6)	27(3)

C(54)	2101(8)	10581(8)	-246(7)	32(3)

C(55)	2269(8)	11079(8)	-774(7)	36(3)

C(56)	2489(8)	10513(8)	-1513(7)	32(3)

C(57)	2463(7)	9489(8)	-1739(7)	31(3)

C(58)	2277(8)	9009(8)	-1197(6)	31(3)

C(1S)	5104(13)	4353(17)	2616(12)	139(8)

Cl(1S)	5200(4)	4931(5)	1791(4)	154(2)

Cl(2S)	6602(5)	5372(4)	3454(4)	143(2)

________________________________________________________________________________

Table O3:  Bond lengths [Å] and angles [°] for 144.

____________________________________________________________________________________

Co(1)-C(12) 	1.791(10)

Co(1)-C(13) 	1.801(13)

Co(1)-C(11) 	1.823(10)

Co(1)-C(7) 	1.943(10)

Co(1)-C(8) 	1.979(10)

Co(1)-Co(2) 	2.476(2)

Co(2)-C(16) 	1.748(10)

Co(2)-C(15) 	1.787(12)

Co(2)-C(14) 	1.849(11)

Co(2)-C(7) 	1.966(10)

Co(2)-C(8) 	2.020(10)

Co(3)-C(36) 	1.779(13)

Co(3)-C(35) 	1.800(10)

Co(3)-C(37) 	1.866(12)

Co(3)-C(9) 	1.975(9)

Co(3)-C(10) 	2.020(9)

Co(3)-Co(4) 	2.469(2)

Co(4)-C(38) 	1.783(9)

Co(4)-C(40) 	1.800(12)

Co(4)-C(39) 	1.814(12)

Co(4)-C(9) 	1.946(9)

Co(4)-C(10) 	2.002(9)

Si(1)-C(29) 	1.873(10)

Si(1)-C(8) 	1.875(11)

Si(1)-C(23) 	1.877(10)

Si(1)-C(17) 	1.879(9)

Si(2)-C(10) 	1.846(10)

Si(2)-C(41) 	1.867(10)

Si(2)-C(53) 	1.890(10)

Si(2)-C(47) 	1.909(9)

C(1)-C(2) 	1.474(13)

C(1)-O(1B) 	1.51(2)

C(1)-O(1A) 	1.52(2)

C(1)-C(6) 	1.526(13)

C(1)-C(7) 	1.533(14)

C(2)-C(3) 	1.543(12)

C(3)-C(4) 	1.534(12)

C(4)-C(5) 	1.409(13)

C(4)-O(4B) 	1.48(2)

C(4)-O(4A) 	1.48(2)

C(4)-C(9) 	1.544(13)

C(5)-C(6) 	1.553(13)

C(7)-C(8) 	1.298(14)

C(9)-C(10) 	1.317(12)

O(11)-C(11) 	1.120(10)

O(12)-C(12) 	1.159(10)

O(13)-C(13) 	1.142(13)

C(14)-O(14) 	1.125(10)

O(15)-C(15) 	1.175(12)

O(16)-C(16) 	1.184(10)

C(17)-C(18) 	1.385(12)

C(17)-C(22) 	1.390(13)

C(18)-C(19) 	1.407(12)

C(19)-C(20) 	1.375(14)

C(20)-C(21) 	1.363(14)

C(21)-C(22) 	1.403(12)

C(23)-C(24) 	1.381(13)

C(23)-C(28) 	1.394(11)

C(24)-C(25) 	1.401(13)

C(25)-C(26) 	1.391(12)

C(26)-C(27) 	1.349(15)

C(27)-C(28) 	1.422(13)

C(29)-C(30) 	1.377(12)

C(29)-C(34) 	1.414(11)

C(30)-C(31) 	1.372(13)

C(31)-C(32) 	1.353(12)

C(32)-C(33) 	1.402(12)

C(33)-C(34) 	1.401(13)

O(35)-C(35) 	1.147(10)

O(36)-C(36) 	1.168(12)

C(37)-O(37) 	1.111(11)

O(38)-C(38) 	1.150(9)

O(39)-C(39) 	1.163(12)

O(40)-C(40) 	1.167(11)

C(41)-C(46) 	1.352(12)

C(41)-C(42) 	1.440(11)

C(42)-C(43) 	1.372(13)

C(43)-C(44) 	1.366(13)

C(44)-C(45) 	1.418(12)

C(45)-C(46) 	1.412(13)

C(47)-C(52) 	1.367(13)

C(47)-C(48) 	1.407(11)

C(48)-C(49) 	1.410(12)

C(49)-C(50) 	1.314(14)

C(50)-C(51) 	1.387(12)

C(51)-C(52) 	1.375(13)

C(53)-C(58) 	1.357(13)

C(53)-C(54) 	1.419(14)

C(54)-C(55) 	1.396(12)

C(55)-C(56) 	1.419(14)

C(56)-C(57) 	1.358(13)

C(57)-C(58) 	1.406(11)

C(1S)-Cl(1S) 	1.93(2)

C(1S)-Cl(2S) 	2.02(2)

C(12)-Co(1)-C(13)	105.4(5)

C(12)-Co(1)-C(11)	98.1(5)

C(13)-Co(1)-C(11)	100.4(5)

C(12)-Co(1)-C(7)	143.1(4)

C(13)-Co(1)-C(7)	98.5(5)

C(11)-Co(1)-C(7)	104.8(4)

C(12)-Co(1)-C(8)	109.8(4)

C(13)-Co(1)-C(8)	136.5(5)

C(11)-Co(1)-C(8)	99.1(4)

C(7)-Co(1)-C(8)	38.7(4)

C(12)-Co(1)-Co(2)	97.0(3)

C(13)-Co(1)-Co(2)	99.1(3)

C(11)-Co(1)-Co(2)	151.1(3)

C(7)-Co(1)-Co(2)	51.1(3)

C(8)-Co(1)-Co(2)	52.5(3)

C(16)-Co(2)-C(15)	99.7(5)

C(16)-Co(2)-C(14)	99.1(4)

C(15)-Co(2)-C(14)	103.3(5)

C(16)-Co(2)-C(7)	104.1(4)

C(15)-Co(2)-C(7)	101.8(5)

C(14)-Co(2)-C(7)	142.1(4)

C(16)-Co(2)-C(8)	103.6(4)

C(15)-Co(2)-C(8)	137.4(4)

C(14)-Co(2)-C(8)	107.5(5)

C(7)-Co(2)-C(8)	38.0(4)

C(16)-Co(2)-Co(1)	152.5(3)

C(15)-Co(2)-Co(1)	95.9(3)

C(14)-Co(2)-Co(1)	99.1(3)

C(7)-Co(2)-Co(1)	50.3(3)

C(8)-Co(2)-Co(1)	51.0(3)

C(36)-Co(3)-C(35)	97.9(5)

C(36)-Co(3)-C(37)	103.6(5)

C(35)-Co(3)-C(37)	100.9(5)

C(36)-Co(3)-C(9)	104.0(4)

C(35)-Co(3)-C(9)	102.1(4)

C(37)-Co(3)-C(9)	140.9(4)

C(36)-Co(3)-C(10)	139.7(4)

C(35)-Co(3)-C(10)	103.8(4)

C(37)-Co(3)-C(10)	105.1(5)

C(9)-Co(3)-C(10)	38.5(3)

C(36)-Co(3)-Co(4)	95.8(3)

C(35)-Co(3)-Co(4)	151.8(3)

C(37)-Co(3)-Co(4)	99.7(3)

C(9)-Co(3)-Co(4)	50.4(3)

C(10)-Co(3)-Co(4)	51.8(3)

C(38)-Co(4)-C(40)	96.9(5)

C(38)-Co(4)-C(39)	96.2(4)

C(40)-Co(4)-C(39)	104.3(5)

C(38)-Co(4)-C(9)	104.1(4)

C(40)-Co(4)-C(9)	142.1(5)

C(39)-Co(4)-C(9)	104.4(5)

C(38)-Co(4)-C(10)	103.4(4)

C(40)-Co(4)-C(10)	105.8(5)

C(39)-Co(4)-C(10)	141.5(4)

C(9)-Co(4)-C(10)	38.9(3)

C(38)-Co(4)-Co(3)	153.8(3)

C(40)-Co(4)-Co(3)	99.6(3)

C(39)-Co(4)-Co(3)	99.2(3)

C(9)-Co(4)-Co(3)	51.5(3)

C(10)-Co(4)-Co(3)	52.4(2)

C(29)-Si(1)-C(8)	110.7(5)

C(29)-Si(1)-C(23)	109.8(5)

C(8)-Si(1)-C(23)	110.8(4)

C(29)-Si(1)-C(17)	107.5(4)

C(8)-Si(1)-C(17)	111.8(4)

C(23)-Si(1)-C(17)	106.2(4)

C(10)-Si(2)-C(41)	107.1(4)

C(10)-Si(2)-C(53)	114.0(4)

C(41)-Si(2)-C(53)	107.3(4)

C(10)-Si(2)-C(47)	108.4(4)

C(41)-Si(2)-C(47)	110.8(4)

C(53)-Si(2)-C(47)	109.2(4)

C(2)-C(1)-O(1B)	92.0(11)

C(2)-C(1)-O(1A)	118.3(11)

C(2)-C(1)-C(6)	110.7(10)

O(1B)-C(1)-C(6)	123.2(11)

O(1A)-C(1)-C(6)	94.2(10)

C(2)-C(1)-C(7)	113.2(8)

O(1B)-C(1)-C(7)	107.4(10)

O(1A)-C(1)-C(7)	109.2(10)

C(6)-C(1)-C(7)	109.4(9)

C(1)-C(2)-C(3)	114.2(9)

C(4)-C(3)-C(2)	111.2(9)

C(5)-C(4)-O(4B)	92.9(10)

C(5)-C(4)-O(4A)	119.4(11)

C(5)-C(4)-C(3)	110.0(9)

O(4B)-C(4)-C(3)	118.3(10)

O(4A)-C(4)-C(3)	89.2(9)

C(5)-C(4)-C(9)	116.2(8)

O(4B)-C(4)-C(9)	106.7(9)

O(4A)-C(4)-C(9)	107.3(9)

C(3)-C(4)-C(9)	111.8(8)

C(4)-C(5)-C(6)	116.0(9)

C(1)-C(6)-C(5)	112.0(10)

C(8)-C(7)-C(1)	143.8(11)

C(8)-C(7)-Co(1)	72.2(6)

C(1)-C(7)-Co(1)	133.6(7)

C(8)-C(7)-Co(2)	73.3(6)

C(1)-C(7)-Co(2)	129.2(8)

Co(1)-C(7)-Co(2)	78.6(4)

C(7)-C(8)-Si(1)	145.0(9)

C(7)-C(8)-Co(1)	69.2(6)

Si(1)-C(8)-Co(1)	135.9(5)

C(7)-C(8)-Co(2)	68.8(7)

Si(1)-C(8)-Co(2)	132.0(5)

Co(1)-C(8)-Co(2)	76.5(4)

C(10)-C(9)-C(4)	138.1(10)

C(10)-C(9)-Co(4)	72.8(6)

C(4)-C(9)-Co(4)	136.8(7)

C(10)-C(9)-Co(3)	72.6(6)

C(4)-C(9)-Co(3)	132.1(7)

Co(4)-C(9)-Co(3)	78.1(4)

C(9)-C(10)-Si(2)	142.3(8)

C(9)-C(10)-Co(4)	68.2(6)

Si(2)-C(10)-Co(4)	136.3(5)

C(9)-C(10)-Co(3)	68.9(6)

Si(2)-C(10)-Co(3)	135.3(5)

Co(4)-C(10)-Co(3)	75.8(3)

O(11)-C(11)-Co(1)	174.8(10)

O(12)-C(12)-Co(1)	177.8(9)

O(13)-C(13)-Co(1)	176.8(10)

O(14)-C(14)-Co(2)	173.6(9)

O(15)-C(15)-Co(2)	175.6(10)

O(16)-C(16)-Co(2)	177.6(9)

C(18)-C(17)-C(22)	118.2(9)

C(18)-C(17)-Si(1)	121.2(8)

C(22)-C(17)-Si(1)	120.5(8)

C(17)-C(18)-C(19)	121.1(10)

C(20)-C(19)-C(18)	119.7(11)

C(21)-C(20)-C(19)	119.7(11)

C(20)-C(21)-C(22)	121.1(11)

C(17)-C(22)-C(21)	120.0(10)

C(24)-C(23)-C(28)	118.5(9)

C(24)-C(23)-Si(1)	120.9(8)

C(28)-C(23)-Si(1)	120.5(8)

C(23)-C(24)-C(25)	122.9(10)

C(26)-C(25)-C(24)	116.8(11)

C(27)-C(26)-C(25)	122.5(11)

C(26)-C(27)-C(28)	120.0(11)

C(23)-C(28)-C(27)	119.3(10)

C(30)-C(29)-C(34)	117.3(9)

C(30)-C(29)-Si(1)	124.4(7)

C(34)-C(29)-Si(1)	118.3(8)

C(31)-C(30)-C(29)	121.1(9)

C(32)-C(31)-C(30)	122.9(11)

C(31)-C(32)-C(33)	117.8(11)

C(34)-C(33)-C(32)	120.0(9)

C(33)-C(34)-C(29)	120.6(10)

O(35)-C(35)-Co(3)	173.5(10)

O(36)-C(36)-Co(3)	179.3(8)

O(37)-C(37)-Co(3)	178.2(10)

O(38)-C(38)-Co(4)	177.6(9)

O(39)-C(39)-Co(4)	177.5(9)

O(40)-C(40)-Co(4)	178.1(11)

C(46)-C(41)-C(42)	117.7(9)

C(46)-C(41)-Si(2)	123.0(7)

C(42)-C(41)-Si(2)	119.1(8)

C(43)-C(42)-C(41)	121.5(10)

C(44)-C(43)-C(42)	119.1(10)

C(43)-C(44)-C(45)	122.0(11)

C(46)-C(45)-C(44)	117.0(10)

C(41)-C(46)-C(45)	122.6(9)

C(52)-C(47)-C(48)	120.2(9)

C(52)-C(47)-Si(2)	119.9(8)

C(48)-C(47)-Si(2)	119.9(7)

C(47)-C(48)-C(49)	120.2(10)

C(50)-C(49)-C(48)	117.0(11)

C(49)-C(50)-C(51)	124.1(11)

C(52)-C(51)-C(50)	119.4(11)

C(47)-C(52)-C(51)	118.8(11)

C(58)-C(53)-C(54)	118.0(10)

C(58)-C(53)-Si(2)	122.1(8)

C(54)-C(53)-Si(2)	119.7(8)

C(55)-C(54)-C(53)	120.7(10)

C(54)-C(55)-C(56)	118.4(10)

C(57)-C(56)-C(55)	121.2(10)

C(56)-C(57)-C(58)	118.7(10)

C(53)-C(58)-C(57)	122.9(10)

Cl(1S)-C(1S)-Cl(2S)	90.1(8)

_____________________________________________________________________________________

Table O5:  Anisotropic displacement parameters (Å2 x 103) for 144.  The anisotropic

displacement factor exponent takes the form: -2(2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	24(1) 	29(1)	24(1) 	13(1)	3(1) 	8(1)

Co(2)	33(1) 	21(1)	25(1) 	12(1)	7(1) 	10(1)

Co(3)	20(1) 	28(1)	26(1) 	11(1)	7(1) 	7(1)

Co(4)	26(1) 	21(1)	23(1) 	7(1)	11(1) 	10(1)

Si(1)	30(2) 	25(2)	21(2) 	7(2)	7(2) 	10(1)

Si(2)	20(2) 	29(2)	21(2) 	15(2)	8(2) 	9(1)

C(1S)	115(15) 	242(24)	122(14) 	94(16)	42(13) 	164(16)

Cl(1S)	156(5) 	272(7)	157(5) 	157(6)	100(4) 	144(5)

Cl(2S)	183(5) 	100(4)	161(5) 	41(4)	76(5) 	88(4)

______________________________________________________________________________

Table O6:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 144.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1AA)	4477(15)	6731(14)	3662(10)	55

H(1BA)	4000(16)	5970(15)	3270(11)	59

H(2A)	1461(9)	6691(9)	2471(6)	44

H(2B)	1684(9)	5575(9)	2257(6)	44

H(3A)	2691(9)	5901(8)	1424(7)	45

H(3B)	1523(9)	6071(8)	1078(7)	45

H(4AA)	1925(13)	8421(14)	1950(10)	60

H(4BA)	1712(14)	8213(13)	1727(10)	47

H(5B)	4094(9)	8678(9)	2611(7)	48

H(5A)	4300(9)	7556(9)	2376(7)	48

H(6B)	4338(10)	8161(9)	3790(7)	60

H(6A)	3195(10)	8401(9)	3515(7)	60

H(18)	1685(9)	7513(8)	6083(6)	42

H(19)	759(9)	7267(8)	6987(7)	55

H(20)	-1089(8)	7170(7)	6621(7)	42

H(21)	-1973(10)	7413(8)	5421(7)	57

H(22)	-1041(8)	7734(7)	4546(7)	38

H(24)	1481(8)	9761(8)	6171(6)	34

H(25)	2380(9)	11593(9)	6897(8)	61

H(26)	3478(9)	12360(9)	6302(7)	53

H(27)	3638(9)	11387(9)	5037(7)	52

H(28)	2694(8)	9544(8)	4290(7)	48

H(30)	728(8)	9039(8)	3362(6)	37

H(31)	-500(8)	8509(8)	1988(7)	49

H(32)	-2000(9)	7018(8)	1348(7)	55

H(33)	-2048(8)	5811(8)	1991(7)	45

H(34)	-741(7)	6281(8)	3361(6)	36

H(42)	3612(8)	10666(7)	1539(6)	37

H(43)	4014(9)	11909(8)	2927(7)	49

H(44)	2715(8)	11855(8)	3557(7)	46

H(45)	940(9)	10590(8)	2788(7)	49

H(46)	515(8)	9430(8)	1332(6)	38

H(48)	268(8)	7370(8)	563(7)	45

H(49)	-1608(8)	6311(8)	-118(7)	42

H(50)	-2574(10)	6211(9)	-1421(7)	54

H(51)	-1917(9)	7304(9)	-2000(8)	64

H(52)	-81(8)	8364(8)	-1348(7)	43

H(54)	1982(8)	10957(8)	265(7)	38

H(55)	2237(8)	11779(8)	-643(7)	43

H(56)	2657(8)	10857(8)	-1856(7)	39

H(57)	2568(7)	9103(8)	-2253(7)	37

H(58)	2270(8)	8295(8)	-1352(6)	37

H(1SA)	5079(13)	3602(17)	2414(12)	166

H(1SB)	4503(13)	4467(17)	2828(12)	166

________________________________________________________________________________

Table P1:  Crystal data and structure refinement for 145.

Empirical formula 	C58 H40 Co4 O14 Si2

Formula weight 	1252.80

Temperature 	148(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	C2/c

Unit cell dimensions	a = 17.529(19) Å	(= 90°.

b = 21.222(23) Å	(= 119.14(2)°.

c = 17.686(19) Å	(= 90°.

Volume	5746.8(107) Å3

Z	4

Density (calculated)	1.448 Mg/m3

Absorption coefficient	1.239 mm-1

F(000)	2544

Crystal size	.05 x 0.10 x .23 mm3

( range for data collection	1.64 to 23.26°.

Index ranges	-17(h(19, -22(k(23, -18(l(19

Reflections collected	18840

Independent reflections	4135 [R(int) = 0.0924]

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4135 / 1 / 373

Goodness-of-fit on F2	1.023

Final R indices [I>2((I)]	R1 = 0.0547, wR2 = 0.0941

R indices (all data)	R1 = 0.1197, wR2 = 0.1125

Extinction coefficient	0.00013(4)

Largest diff. peak and hole	0.314 and -0.360 e.Å-3

Max. and Min effective transmission	0.886841  0.839571

Table P2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 145.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	4557(1)	8101(1)	-258(1)	25(1)

Co(2)	6155(1)	8090(1)	725(1)	25(1)

Si(1)	5332(1)	6522(1)	322(1)	26(1)

O(1)	4909(3)	8653(2)	1695(3)	40(1)

C(1)	5085(3)	7986(3)	1725(3)	20(1)

C(2)	4294(4)	7635(3)	1678(4)	28(2)

C(3)	5901(4)	7796(4)	2586(4)	30(2)

C(4)	5211(3)	7833(3)	956(3)	18(1)

C(5)	5296(3)	7383(3)	487(3)	24(2)

O(6)	4512(3)	8081(2)	-1956(3)	47(1)

C(6)	4541(4)	8080(3)	-1282(4)	32(2)

O(7)	2765(3)	7661(2)	-851(3)	48(1)

C(7)	3476(4)	7817(3)	-616(3)	30(2)

O(8)	4213(3)	9445(2)	-61(3)	60(2)

C(8)	4355(4)	8928(4)	-123(4)	39(2)

O(9)	6366(3)	9422(2)	1229(3)	53(1)

C(9)	6280(4)	8905(3)	1024(4)	34(2)

O(10)	7752(3)	7681(2)	2274(3)	44(1)

C(10)	7136(4)	7830(3)	1663(4)	31(2)

O(11)	6777(3)	8027(3)	-560(3)	60(2)

C(11)	6537(4)	8035(3)	-62(4)	41(2)

C(12)	4184(4)	6198(3)	-257(4)	24(2)

C(13)	3896(4)	5852(3)	-1017(4)	38(2)

C(14)	3045(4)	5623(3)	-1462(4)	42(2)

C(15)	2475(4)	5725(3)	-1158(4)	43(2)

C(16)	2743(4)	6063(3)	-406(4)	41(2)

C(17)	3600(4)	6296(3)	46(4)	32(2)

C(18)	5874(4)	6321(3)	-327(3)	23(2)

C(19)	6413(4)	5805(3)	-136(4)	35(2)

C(20)	6786(4)	5629(3)	-646(4)	50(2)

C(21)	6600(4)	5970(3)	-1373(4)	39(2)

C(22)	6058(4)	6466(3)	-1598(4)	35(2)

C(23)	5703(4)	6643(3)	-1081(4)	37(2)

C(24)	6006(4)	6164(3)	1420(4)	26(2)

C(25)	5647(4)	5817(3)	1828(4)	50(2)

C(26)	6164(5)	5576(3)	2666(4)	53(2)

C(27)	7051(5)	5664(3)	3088(4)	45(2)

C(28)	7425(4)	5989(3)	2680(4)	43(2)

C(29)	6908(4)	6247(3)	1861(4)	36(2)

________________________________________________________________________________

Table P3:  Bond lengths [Å] and angles [°] for 145.

___________________________________________________________________________________

Co(1)-C(7) 	1.785(7)

Co(1)-C(6) 	1.797(7)

Co(1)-C(8) 	1.829(8)

Co(1)-C(4) 	1.963(5)

Co(1)-C(5) 	2.019(6)

Co(1)-Co(2) 	2.475(3)

Co(2)-C(9) 	1.789(7)

Co(2)-C(10) 	1.799(6)

Co(2)-C(11) 	1.817(7)

Co(2)-C(4) 	1.966(6)

Co(2)-C(5) 	2.020(6)

Si(1)-C(5) 	1.856(7)

Si(1)-C(18) 	1.862(6)

Si(1)-C(24) 	1.872(6)

Si(1)-C(12) 	1.888(6)

O(1)-C(1) 	1.445(7)

C(1)-C(4) 	1.515(8)

C(1)-C(2) 	1.541(8)

C(1)-C(3) 	1.552(7)

C(2)-C(3)#1 	1.536(8)

C(3)-C(2)#1 	1.536(8)

C(4)-C(5) 	1.321(7)

O(6)-C(6) 	1.169(7)

O(7)-C(7) 	1.154(7)

O(8)-C(8) 	1.142(8)

O(9)-C(9) 	1.144(7)

O(10)-C(10) 	1.140(6)

O(11)-C(11) 	1.147(7)

C(12)-C(17) 	1.383(8)

C(12)-C(13) 	1.394(8)

C(13)-C(14) 	1.392(8)

C(14)-C(15) 	1.363(8)

C(15)-C(16) 	1.377(8)

C(16)-C(17) 	1.404(8)

C(18)-C(19) 	1.376(8)

C(18)-C(23) 	1.395(8)

C(19)-C(20) 	1.399(8)

C(20)-C(21) 	1.369(8)

C(21)-C(22) 	1.343(8)

C(22)-C(23) 	1.385(8)

C(24)-C(25) 	1.379(8)

C(24)-C(29) 	1.392(8)

C(25)-C(26) 	1.405(8)

C(26)-C(27) 	1.371(9)

C(27)-C(28) 	1.372(9)

C(28)-C(29) 	1.394(7)

C(7)-Co(1)-C(6)	98.2(3)

C(7)-Co(1)-C(8)	97.5(3)

C(6)-Co(1)-C(8)	104.3(3)

C(7)-Co(1)-C(4)	104.1(2)

C(6)-Co(1)-C(4)	144.0(3)

C(8)-Co(1)-C(4)	100.5(3)

C(7)-Co(1)-C(5)	102.1(2)

C(6)-Co(1)-C(5)	109.2(3)

C(8)-Co(1)-C(5)	137.9(3)

C(4)-Co(1)-C(5)	38.7(2)

C(7)-Co(1)-Co(2)	152.7(2)

C(6)-Co(1)-Co(2)	99.5(2)

C(8)-Co(1)-Co(2)	98.1(2)

C(4)-Co(1)-Co(2)	51.0(2)

C(5)-Co(1)-Co(2)	52.2(2)

C(9)-Co(2)-C(10)	95.7(3)

C(9)-Co(2)-C(11)	104.5(3)

C(10)-Co(2)-C(11)	98.3(3)

C(9)-Co(2)-C(4)	101.7(3)

C(10)-Co(2)-C(4)	104.2(3)

C(11)-Co(2)-C(4)	143.4(3)

C(9)-Co(2)-C(5)	138.7(3)

C(10)-Co(2)-C(5)	104.2(2)

C(11)-Co(2)-C(5)	107.9(3)

C(4)-Co(2)-C(5)	38.7(2)

C(9)-Co(2)-Co(1)	97.7(2)

C(10)-Co(2)-Co(1)	153.8(2)

C(11)-Co(2)-Co(1)	100.1(2)

C(4)-Co(2)-Co(1)	50.9(2)

C(5)-Co(2)-Co(1)	52.2(2)

C(5)-Si(1)-C(18)	112.8(3)

C(5)-Si(1)-C(24)	106.8(3)

C(18)-Si(1)-C(24)	107.0(3)

C(5)-Si(1)-C(12)	109.6(3)

C(18)-Si(1)-C(12)	108.2(3)

C(24)-Si(1)-C(12)	112.5(3)

O(1)-C(1)-C(4)	107.4(4)

O(1)-C(1)-C(2)	107.6(5)

C(4)-C(1)-C(2)	111.6(4)

O(1)-C(1)-C(3)	111.7(5)

C(4)-C(1)-C(3)	110.9(5)

C(2)-C(1)-C(3)	107.6(5)

C(3)#1-C(2)-C(1)	114.4(5)

C(2)#1-C(3)-C(1)	114.2(5)

C(5)-C(4)-C(1)	146.1(5)

C(5)-C(4)-Co(1)	72.9(3)

C(1)-C(4)-Co(1)	131.1(4)

C(5)-C(4)-Co(2)	72.9(4)

C(1)-C(4)-Co(2)	129.2(4)

Co(1)-C(4)-Co(2)	78.1(2)

C(4)-C(5)-Si(1)	146.4(5)

C(4)-C(5)-Co(1)	68.4(3)

Si(1)-C(5)-Co(1)	134.5(3)

C(4)-C(5)-Co(2)	68.4(3)

Si(1)-C(5)-Co(2)	133.3(3)

Co(1)-C(5)-Co(2)	75.6(2)

O(6)-C(6)-Co(1)	178.0(5)

O(7)-C(7)-Co(1)	177.0(6)

O(8)-C(8)-Co(1)	178.2(6)

O(9)-C(9)-Co(2)	178.9(6)

O(10)-C(10)-Co(2)	177.7(6)

O(11)-C(11)-Co(2)	177.2(7)

C(17)-C(12)-C(13)	117.7(5)

C(17)-C(12)-Si(1)	122.0(4)

C(13)-C(12)-Si(1)	120.3(5)

C(14)-C(13)-C(12)	120.9(6)

C(15)-C(14)-C(13)	120.8(6)

C(14)-C(15)-C(16)	119.5(6)

C(15)-C(16)-C(17)	120.1(6)

C(12)-C(17)-C(16)	120.9(6)

C(19)-C(18)-C(23)	115.3(6)

C(19)-C(18)-Si(1)	121.7(5)

C(23)-C(18)-Si(1)	122.8(5)

C(18)-C(19)-C(20)	122.3(6)

C(21)-C(20)-C(19)	119.5(6)

C(22)-C(21)-C(20)	120.2(6)

C(21)-C(22)-C(23)	119.8(6)

C(22)-C(23)-C(18)	122.8(6)

C(25)-C(24)-C(29)	117.2(5)

C(25)-C(24)-Si(1)	122.7(5)

C(29)-C(24)-Si(1)	120.1(5)

C(24)-C(25)-C(26)	121.5(6)

C(27)-C(26)-C(25)	120.2(7)

C(26)-C(27)-C(28)	119.2(6)

C(27)-C(28)-C(29)	120.6(6)

C(24)-C(29)-C(28)	121.3(6)

___________________________________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,y,-z+1/2

Table P4:  Anisotropic displacement parameters (Å2 x 103) for 145.  The anisotropic

displacement factor exponent takes the form: -2(2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	22(1) 	33(1)	19(1) 	6(1)	9(1) 	1(1)

Co(2)	21(1) 	33(1)	21(1) 	4(1)	10(1) 	-2(1)

Si(1)	25(1) 	32(1)	20(1) 	1(1)	11(1) 	1(1)

O(1)	68(3) 	12(3)	48(3) 	-3(2)	35(3) 	4(2)

C(1)	26(3) 	24(4)	12(3) 	-2(3)	10(3) 	0(3)

C(2)	17(4) 	49(5)	16(4) 	-8(3)	8(3) 	-9(3)

C(3)	22(4) 	47(5)	19(4) 	3(3)	9(3) 	-2(4)

C(4)	14(3) 	23(4)	16(3) 	4(3)	7(3) 	1(2)

C(5)	16(3) 	32(4)	26(4) 	3(3)	14(3) 	0(3)

O(6)	50(3) 	64(3)	30(3) 	10(3)	23(2) 	4(3)

C(6)	28(4) 	31(4)	28(4) 	12(4)	7(3) 	7(3)

O(7)	29(3) 	67(4)	39(3) 	11(2)	8(2) 	-4(3)

C(7)	34(4) 	40(4)	8(3) 	7(3)	4(3) 	5(3)

O(8)	63(3) 	37(3)	59(3) 	5(3)	15(3) 	13(3)

C(8)	26(4) 	66(6)	18(4) 	4(4)	6(3) 	-2(4)

O(9)	38(3) 	35(3)	74(4) 	4(3)	18(3) 	-2(2)

C(9)	23(4) 	25(5)	43(4) 	12(4)	7(3) 	-2(3)

O(10)	24(3) 	53(3)	42(3) 	12(2)	7(2) 	0(2)

C(10)	31(4) 	36(4)	33(4) 	1(3)	22(3) 	-4(3)

O(11)	51(3) 	96(4)	44(3) 	-7(3)	33(3) 	-22(3)

C(11)	24(4) 	62(5)	34(4) 	9(4)	13(3) 	-13(4)

C(12)	26(4) 	20(4)	22(4) 	6(3)	9(3) 	3(3)

C(13)	41(4) 	42(5)	40(4) 	-1(4)	28(4) 	-2(3)

C(14)	42(5) 	52(5)	32(4) 	-16(3)	19(4) 	-20(4)

C(15)	26(4) 	33(5)	55(5) 	0(4)	8(4) 	-11(3)

C(16)	34(4) 	37(5)	54(5) 	-2(4)	23(4) 	3(3)

C(17)	29(4) 	36(4)	34(4) 	-15(3)	16(3) 	-4(3)

C(18)	28(4) 	25(4)	14(3) 	-1(3)	10(3) 	4(3)

C(19)	45(4) 	34(5)	36(4) 	0(3)	28(3) 	6(3)

C(20)	54(5) 	53(5)	48(5) 	0(4)	28(4) 	20(4)

C(21)	38(4) 	57(5)	29(4) 	-11(4)	22(3) 	-5(4)

C(22)	39(4) 	48(5)	30(4) 	-1(3)	25(3) 	-4(4)

C(23)	34(4) 	43(5)	33(4) 	-2(3)	15(3) 	11(3)

C(24)	31(4) 	25(4)	23(3) 	2(3)	13(3) 	5(3)

C(25)	36(4) 	72(6)	53(5) 	30(4)	30(4) 	25(4)

C(26)	67(6) 	66(6)	55(5) 	35(4)	52(5) 	30(4)

C(27)	59(5) 	51(5)	22(4) 	6(3)	17(4) 	22(4)

C(28)	35(4) 	45(5)	28(4) 	0(4)	0(3) 	-8(3)

C(29)	42(4) 	28(4)	30(4) 	2(3)	10(3) 	-7(3)

______________________________________________________________________________

Table P5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 145.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1)	5242(35)	8807(31)	2166(23)	73(30)

H(2B)	4461(26)	7108(22)	1734(26)	11(13)

H(2A)	3780(44)	7651(30)	1117(44)	77(24)

H(3B)	6229(41)	8160(30)	2706(39)	63(25)

H(3A)	6105(35)	7294(30)	2490(35)	56(20)

H(13)	4287(4)	5770(3)	-1234(4)	45

H(14)	2860(4)	5393(3)	-1983(4)	50

H(15)	1896(4)	5565(3)	-1464(4)	51

H(16)	2348(4)	6138(3)	-192(4)	49

H(17)	3781(4)	6525(3)	568(4)	39

H(19)	6536(4)	5560(3)	360(4)	42

H(20)	7165(4)	5276(3)	-489(4)	60

H(21)	6855(4)	5854(3)	-1720(4)	47

H(22)	5918(4)	6696(3)	-2111(4)	42

H(23)	5327(4)	6999(3)	-1247(4)	45

H(25)	5036(4)	5740(3)	1536(4)	60

H(26)	5899(5)	5351(3)	2941(4)	64

H(27)	7403(5)	5503(3)	3656(4)	54

H(28)	8041(4)	6037(3)	2958(4)	51

H(29)	7176(4)	6485(3)	1599(4)	43

________________________________________________________________________________

Table P6:  Torsion angles [°] for 145.

__________________________________________________________________________________

C(7)-Co(1)-Co(2)-C(9)	-126.3(5)

C(6)-Co(1)-Co(2)-C(9)	104.1(3)

C(8)-Co(1)-Co(2)-C(9)	-1.9(3)

C(4)-Co(1)-Co(2)-C(9)	-98.8(3)

C(5)-Co(1)-Co(2)-C(9)	-148.8(3)

C(7)-Co(1)-Co(2)-C(10)	-6.4(6)

C(6)-Co(1)-Co(2)-C(10)	-136.0(5)

C(8)-Co(1)-Co(2)-C(10)	118.0(5)

C(4)-Co(1)-Co(2)-C(10)	21.1(5)

C(5)-Co(1)-Co(2)-C(10)	-28.9(5)

C(7)-Co(1)-Co(2)-C(11)	127.4(5)

C(6)-Co(1)-Co(2)-C(11)	-2.2(3)

C(8)-Co(1)-Co(2)-C(11)	-108.2(3)

C(4)-Co(1)-Co(2)-C(11)	154.9(3)

C(5)-Co(1)-Co(2)-C(11)	104.9(3)

C(7)-Co(1)-Co(2)-C(4)	-27.5(5)

C(6)-Co(1)-Co(2)-C(4)	-157.0(3)

C(8)-Co(1)-Co(2)-C(4)	96.9(3)

C(4)-Co(1)-Co(2)-C(4)	0.0

C(5)-Co(1)-Co(2)-C(4)	-50.0(3)

C(7)-Co(1)-Co(2)-C(5)	22.5(5)

C(6)-Co(1)-Co(2)-C(5)	-107.0(3)

C(8)-Co(1)-Co(2)-C(5)	146.9(3)

C(4)-Co(1)-Co(2)-C(5)	50.0(3)

C(5)-Co(1)-Co(2)-C(5)	0.0

O(1)-C(1)-C(2)-C(3)#1	-59.3(7)

C(4)-C(1)-C(2)-C(3)#1	-176.9(5)

C(3)-C(1)-C(2)-C(3)#1	61.2(6)

O(1)-C(1)-C(3)-C(2)#1	87.7(7)

C(4)-C(1)-C(3)-C(2)#1	-152.5(6)

C(2)-C(1)-C(3)-C(2)#1	-30.2(7)

O(1)-C(1)-C(4)-C(5)	-170.3(8)

C(2)-C(1)-C(4)-C(5)	-52.6(10)

C(3)-C(1)-C(4)-C(5)	67.3(10)

O(1)-C(1)-C(4)-Co(1)	-43.5(7)

C(2)-C(1)-C(4)-Co(1)	74.2(6)

C(3)-C(1)-C(4)-Co(1)	-165.8(5)

O(1)-C(1)-C(4)-Co(2)	67.5(6)

C(2)-C(1)-C(4)-Co(2)	-174.8(4)

C(3)-C(1)-C(4)-Co(2)	-54.9(7)

C(7)-Co(1)-C(4)-C(5)	91.9(4)

C(6)-Co(1)-C(4)-C(5)	-34.6(6)

C(8)-Co(1)-C(4)-C(5)	-167.6(4)

C(5)-Co(1)-C(4)-C(5)	0.000(2)

Co(2)-Co(1)-C(4)-C(5)	-75.5(3)

C(7)-Co(1)-C(4)-C(1)	-60.3(6)

C(6)-Co(1)-C(4)-C(1)	173.2(5)

C(8)-Co(1)-C(4)-C(1)	40.3(6)

C(5)-Co(1)-C(4)-C(1)	-152.2(7)

Co(2)-Co(1)-C(4)-C(1)	132.3(6)

C(7)-Co(1)-C(4)-Co(2)	167.4(2)

C(6)-Co(1)-C(4)-Co(2)	40.9(5)

C(8)-Co(1)-C(4)-Co(2)	-92.0(3)

C(5)-Co(1)-C(4)-Co(2)	75.5(3)

Co(2)-Co(1)-C(4)-Co(2)	0.0

C(9)-Co(2)-C(4)-C(5)	166.0(3)

C(10)-Co(2)-C(4)-C(5)	-95.0(4)

C(11)-Co(2)-C(4)-C(5)	31.1(6)

C(5)-Co(2)-C(4)-C(5)	0.0

Co(1)-Co(2)-C(4)-C(5)	75.6(3)

C(9)-Co(2)-C(4)-C(1)	-43.6(5)

C(10)-Co(2)-C(4)-C(1)	55.4(5)

C(11)-Co(2)-C(4)-C(1)	-178.4(5)

C(5)-Co(2)-C(4)-C(1)	150.4(7)

Co(1)-Co(2)-C(4)-C(1)	-134.0(6)

C(9)-Co(2)-C(4)-Co(1)	90.4(2)

C(10)-Co(2)-C(4)-Co(1)	-170.6(2)

C(11)-Co(2)-C(4)-Co(1)	-44.4(5)

C(5)-Co(2)-C(4)-Co(1)	-75.6(3)

Co(1)-Co(2)-C(4)-Co(1)	0.0

C(1)-C(4)-C(5)-Si(1)	0.9(15)

Co(1)-C(4)-C(5)-Si(1)	-139.9(7)

Co(2)-C(4)-C(5)-Si(1)	137.6(7)

C(1)-C(4)-C(5)-Co(1)	140.9(9)

Co(1)-C(4)-C(5)-Co(1)	0.000(1)

Co(2)-C(4)-C(5)-Co(1)	-82.5(2)

C(1)-C(4)-C(5)-Co(2)	-136.7(9)

Co(1)-C(4)-C(5)-Co(2)	82.5(2)

Co(2)-C(4)-C(5)-Co(2)	0.0

C(18)-Si(1)-C(5)-C(4)	-159.6(7)

C(24)-Si(1)-C(5)-C(4)	-42.3(8)

C(12)-Si(1)-C(5)-C(4)	79.8(8)

C(18)-Si(1)-C(5)-Co(1)	77.4(5)

C(24)-Si(1)-C(5)-Co(1)	-165.3(4)

C(12)-Si(1)-C(5)-Co(1)	-43.2(5)

C(18)-Si(1)-C(5)-Co(2)	-39.2(5)

C(24)-Si(1)-C(5)-Co(2)	78.2(4)

C(12)-Si(1)-C(5)-Co(2)	-159.7(4)

C(7)-Co(1)-C(5)-C(4)	-97.5(4)

C(6)-Co(1)-C(5)-C(4)	159.3(4)

C(8)-Co(1)-C(5)-C(4)	18.4(5)

C(4)-Co(1)-C(5)-C(4)	0.000(3)

Co(2)-Co(1)-C(5)-C(4)	72.2(3)

C(7)-Co(1)-C(5)-Si(1)	52.6(5)

C(6)-Co(1)-C(5)-Si(1)	-50.6(5)

C(8)-Co(1)-C(5)-Si(1)	168.5(4)

C(4)-Co(1)-C(5)-Si(1)	150.1(6)

Co(2)-Co(1)-C(5)-Si(1)	-137.8(5)

C(7)-Co(1)-C(5)-Co(2)	-169.6(2)

C(6)-Co(1)-C(5)-Co(2)	87.1(3)

C(8)-Co(1)-C(5)-Co(2)	-53.7(4)

C(4)-Co(1)-C(5)-Co(2)	-72.2(3)

Co(2)-Co(1)-C(5)-Co(2)	0.0

C(9)-Co(2)-C(5)-C(4)	-21.0(5)

C(10)-Co(2)-C(5)-C(4)	95.2(4)

C(11)-Co(2)-C(5)-C(4)	-161.1(3)

C(4)-Co(2)-C(5)-C(4)	0.0

Co(1)-Co(2)-C(5)-C(4)	-72.1(3)

C(9)-Co(2)-C(5)-Si(1)	-170.2(4)

C(10)-Co(2)-C(5)-Si(1)	-54.0(5)

C(11)-Co(2)-C(5)-Si(1)	49.8(5)

C(4)-Co(2)-C(5)-Si(1)	-149.1(6)

Co(1)-Co(2)-C(5)-Si(1)	138.8(5)

C(9)-Co(2)-C(5)-Co(1)	51.0(4)

C(10)-Co(2)-C(5)-Co(1)	167.3(2)

C(11)-Co(2)-C(5)-Co(1)	-89.0(3)

C(4)-Co(2)-C(5)-Co(1)	72.1(3)

Co(1)-Co(2)-C(5)-Co(1)	0.0

C(7)-Co(1)-C(6)-O(6)	66.5(164)

C(8)-Co(1)-C(6)-O(6)	-33.4(164)

C(4)-Co(1)-C(6)-O(6)	-165.5(161)

C(5)-Co(1)-C(6)-O(6)	172.4(163)

Co(2)-Co(1)-C(6)-O(6)	-134.4(163)

C(6)-Co(1)-C(7)-O(7)	-94.7(99)

C(8)-Co(1)-C(7)-O(7)	11.0(99)

C(4)-Co(1)-C(7)-O(7)	113.8(98)

C(5)-Co(1)-C(7)-O(7)	153.5(98)

Co(2)-Co(1)-C(7)-O(7)	135.5(96)

C(7)-Co(1)-C(8)-O(8)	-60.5(201)

C(6)-Co(1)-C(8)-O(8)	39.9(201)

C(4)-Co(1)-C(8)-O(8)	-166.4(201)

C(5)-Co(1)-C(8)-O(8)	-178.0(1000)

Co(2)-Co(1)-C(8)-O(8)	141.9(201)

C(10)-Co(2)-C(9)-O(9)	-37.0(282)

C(11)-Co(2)-C(9)-O(9)	-137.0(281)

C(4)-Co(2)-C(9)-O(9)	68.9(281)

C(5)-Co(2)-C(9)-O(9)	82.1(281)

Co(1)-Co(2)-C(9)-O(9)	120.4(281)

C(9)-Co(2)-C(10)-O(10)	34.3(138)

C(11)-Co(2)-C(10)-O(10)	139.9(138)

C(4)-Co(2)-C(10)-O(10)	-69.3(139)

C(5)-Co(2)-C(10)-O(10)	-109.2(138)

Co(1)-Co(2)-C(10)-O(10)	-86.0(139)

C(9)-Co(2)-C(11)-O(11)	-11.7(113)

C(10)-Co(2)-C(11)-O(11)	-109.8(112)

C(4)-Co(2)-C(11)-O(11)	122.5(111)

C(5)-Co(2)-C(11)-O(11)	142.3(112)

Co(1)-Co(2)-C(11)-O(11)	89.0(112)

C(5)-Si(1)-C(12)-C(17)	-53.6(5)

C(18)-Si(1)-C(12)-C(17)	-177.0(5)

C(24)-Si(1)-C(12)-C(17)	65.0(6)

C(5)-Si(1)-C(12)-C(13)	126.0(5)

C(18)-Si(1)-C(12)-C(13)	2.7(5)

C(24)-Si(1)-C(12)-C(13)	-115.4(5)

C(17)-C(12)-C(13)-C(14)	1.2(9)

Si(1)-C(12)-C(13)-C(14)	-178.5(5)

C(12)-C(13)-C(14)-C(15)	-0.9(10)

C(13)-C(14)-C(15)-C(16)	0.4(10)

C(14)-C(15)-C(16)-C(17)	-0.3(10)

C(13)-C(12)-C(17)-C(16)	-1.0(9)

Si(1)-C(12)-C(17)-C(16)	178.6(5)

C(15)-C(16)-C(17)-C(12)	0.6(10)

C(5)-Si(1)-C(18)-C(19)	141.4(5)

C(24)-Si(1)-C(18)-C(19)	24.2(6)

C(12)-Si(1)-C(18)-C(19)	-97.3(5)

C(5)-Si(1)-C(18)-C(23)	-44.8(6)

C(24)-Si(1)-C(18)-C(23)	-161.9(5)

C(12)-Si(1)-C(18)-C(23)	76.6(5)

C(23)-C(18)-C(19)-C(20)	2.1(9)

Si(1)-C(18)-C(19)-C(20)	176.4(5)

C(18)-C(19)-C(20)-C(21)	-1.4(10)

C(19)-C(20)-C(21)-C(22)	-0.5(10)

C(20)-C(21)-C(22)-C(23)	1.6(10)

C(21)-C(22)-C(23)-C(18)	-0.8(10)

C(19)-C(18)-C(23)-C(22)	-1.0(9)

Si(1)-C(18)-C(23)-C(22)	-175.2(5)

C(5)-Si(1)-C(24)-C(25)	106.5(6)

C(18)-Si(1)-C(24)-C(25)	-132.4(5)

C(12)-Si(1)-C(24)-C(25)	-13.7(6)

C(5)-Si(1)-C(24)-C(29)	-73.1(5)

C(18)-Si(1)-C(24)-C(29)	48.0(5)

C(12)-Si(1)-C(24)-C(29)	166.7(5)

C(29)-C(24)-C(25)-C(26)	2.2(10)

Si(1)-C(24)-C(25)-C(26)	-177.4(5)

C(24)-C(25)-C(26)-C(27)	-2.2(11)

C(25)-C(26)-C(27)-C(28)	-0.3(11)

C(26)-C(27)-C(28)-C(29)	2.6(10)

C(25)-C(24)-C(29)-C(28)	0.1(9)

Si(1)-C(24)-C(29)-C(28)	179.7(5)

C(27)-C(28)-C(29)-C(24)	-2.5(10)

__________________________________________________________________________________

Symmetry transformations used to generate equivalent atoms:

#1 -x+1,y,-z+1/2

Table Q1:  Crystal data and structure refinement for 149.

Empirical formula 	C28 H28 Co4 O14 Si2

Formula weight 	880.40

Temperature 	148(2) K

Wavelength 	0.71073 Å

Crystal system 	Triclinic

Space group 	P-1

Unit cell dimensions	a = 15.1645(6) Å	(= 85.838(2)°.

b = 15.2359(9) Å	(= 65.577(3)°.

c = 17.8463(11) Å	(= 84.452(3)°.

Volume	3734.3(4) Å3

Z	4

Density (calculated)	1.566 Mg/m3

Absorption coefficient	1.870 mm-1

F(000)	1776

Crystal size	.02 x .10 x .12 mm3

( range for data collection	1.25 to 20.00°.

Index ranges	-15(h(15, -15(k(15, -18(l(18

Reflections collected	18212

Independent reflections	6972 [R(int) = 0.1871]

Absorption correction	None

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	6878 / 0 / 556

Goodness-of-fit on F2	0.960

Final R indices [I>2((I)]	R1 = 0.0737, wR2 = 0.0883

R indices (all data)	R1 = 0.2024, wR2 = 0.1194

Extinction coefficient	0.00020(6)

Largest diff. peak and hole	0.576 and -0.590 e.Å-3

Ratio of min to max apparent transmission	0.817396

Table Q2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 149.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1A)	-6407(2)	-1436(2)	8577(1)	27(1)

Co(2A)	-6784(2)	-2886(1)	9314(1)	26(1)

Co(3A)	-334(2)	-2418(2)	7937(1)	24(1)

Co(4A)	-561(2)	-4019(1)	8214(1)	25(1)

Si(1A)	-6596(3)	-1355(3)	10617(2)	32(2)

Si(2A)	-1541(4)	-2925(4)	10090(2)	40(2)

O(1A)	-4363(6)	-3045(6)	7839(4)	21(3)

C(1A)	-4539(10)	-2573(9)	8576(7)	13(4)

C(2A)	-4255(9)	-3257(9)	9121(7)	16(4)

C(3A)	-3182(9)	-3587(8)	8728(7)	17(4)

O(4A)	-2185(6)	-2933(5)	7360(4)	19(3)

C(4A)	-2433(10)	-2909(10)	8227(7)	20(4)

C(5A)	-2955(10)	-1992(9)	8483(7)	25(4)

C(6A)	-3910(9)	-1782(9)	8379(7)	16(4)

C(7A)	-5612(10)	-2282(9)	8971(7)	9(4)

C(8A)	-6270(10)	-1864(9)	9613(7)	18(4)

C(9A)	-1538(10)	-3020(9)	8400(7)	14(4)

C(10A)	-1216(10)	-3028(9)	8981(7)	16(4)

O(11A)	-5420(8)	225(8)	8237(6)	61(4)

C(11A)	-5790(11)	-413(11)	8344(8)	23(5)

O(12A)	-5767(8)	-2039(7)	6871(6)	57(4)

C(12A)	-6010(12)	-1809(11)	7538(9)	39(5)

O(13A)	-8410(9)	-648(8)	9076(7)	68(4)

C(13A)	-7640(15)	-942(12)	8897(10)	51(6)

O(14A)	-6423(8)	-3929(7)	7878(6)	61(4)

C(14A)	-6584(11)	-3532(11)	8444(9)	35(5)

O(15A)	-8892(8)	-2487(7)	10214(7)	72(4)

C(15A)	-8038(14)	-2664(11)	9848(9)	43(5)

O(16A)	-6389(7)	-4344(7)	10330(5)	39(3)

C(16A)	-6552(11)	-3756(11)	9947(8)	28(5)

C(17A)	-6469(11)	-119(10)	10444(8)	55(6)

C(18A)	-7864(10)	-1567(10)	11341(7)	47(5)

C(19A)	-5732(10)	-1831(10)	11072(8)	47(5)

O(20A)	1599(9)	-2359(8)	7953(7)	66(4)

C(20A)	866(14)	-2390(12)	7945(9)	42(6)

O(21A)	-16(7)	-2365(6)	6183(5)	43(3)

C(21A)	-137(11)	-2381(11)	6872(9)	34(5)

O(22A)	-981(8)	-556(8)	8309(7)	63(4)

C(22A)	-730(12)	-1277(13)	8144(9)	39(6)

O(23A)	-434(7)	-4629(7)	6644(6)	45(4)

C(23A)	-469(12)	-4378(11)	7268(9)	39(5)

O(24A)	1343(8)	-4478(7)	8279(7)	69(5)

C(24A)	621(13)	-4305(11)	8253(9)	31(5)

O(25A)	-1517(8)	-5456(7)	9366(6)	58(4)

C(25A)	-1165(11)	-4900(11)	8926(9)	35(5)

C(26A)	-1475(12)	-1767(11)	10288(9)	78(7)

C(27A)	-2787(11)	-3295(11)	10693(8)	63(6)

C(28A)	-668(10)	-3644(10)	10355(8)	51(5)

Co(1B)	-3180(2)	-854(2)	4638(1)	30(1)

Co(2B)	-1588(2)	-933(1)	4725(1)	27(1)

Co(3B)	-4267(2)	-6165(1)	6933(1)	23(1)

Co(4B)	-2490(2)	-6504(1)	6501(1)	22(1)

Si(1B)	-1436(4)	-2107(3)	3027(2)	40(2)

Si(2B)	-3100(3)	-6575(3)	4814(2)	25(1)

O(1B)	-3154(6)	-2296(6)	6346(4)	14(2)

C(1B)	-2749(10)	-2649(9)	5519(7)	16(4)

C(2B)	-3507(9)	-3134(9)	5410(7)	18(4)

C(3B)	-3834(9)	-3956(9)	6008(7)	20(4)

O(4B)	-2985(6)	-4269(6)	6927(4)	19(3)

C(4B)	-3028(10)	-4491(9)	6183(7)	13(4)

C(5B)	-2037(9)	-4297(9)	5471(7)	21(4)

C(6B)	-1838(9)	-3292(9)	5394(7)	21(4)

C(7B)	-2470(10)	-1888(9)	4895(7)	19(4)

C(8B)	-2019(10)	-1714(10)	4095(8)	27(4)

C(9B)	-3195(10)	-5481(10)	6228(7)	18(4)

C(10B)	-3216(10)	-6120(9)	5785(7)	15(4)

O(11B)	-4707(10)	-1638(9)	4375(6)	77(4)

C(11B)	-4133(15)	-1327(13)	4490(10)	69(6)

O(12B)	-4326(9)	-163(8)	6285(6)	79(5)

C(12B)	-3892(12)	-438(11)	5629(10)	43(6)

O(13B)	-2856(8)	577(7)	3363(6)	65(4)

C(13B)	-3017(12)	38(12)	3862(9)	42(5)

O(14B)	-2143(9)	-503(7)	6451(6)	69(4)

C(14B)	-1924(13)	-656(12)	5773(10)	52(6)

O(15B)	-870(8)	633(7)	3656(6)	54(4)

C(15B)	-1181(12)	21(12)	4112(9)	53(5)

O(16B)	358(9)	-1751(7)	4394(7)	76(5)

C(16B)	-404(14)	-1461(12)	4512(10)	48(6)

C(17B)	-927(11)	-1179(10)	2288(8)	63(6)

C(18B)	-462(13)	-2967(12)	2968(10)	95(7)

C(19B)	-2367(12)	-2601(11)	2787(9)	82(7)

O(20B)	-4786(7)	-5424(7)	8571(6)	39(3)

C(20B)	-4598(11)	-5733(11)	7953(9)	30(5)

O(21B)	-5962(8)	-5423(7)	6630(5)	40(3)

C(21B)	-5308(13)	-5705(11)	6754(9)	37(6)

O(22B)	-4894(8)	-7984(7)	7196(6)	51(4)

C(22B)	-4637(11)	-7282(12)	7108(8)	30(5)

O(23B)	-2218(7)	-5894(7)	7935(6)	40(3)

C(23B)	-2339(11)	-6154(11)	7388(9)	31(5)

O(24B)	-505(7)	-6291(6)	5259(5)	39(3)

C(24B)	-1290(12)	-6398(10)	5758(8)	33(5)

O(25B)	-2510(7)	-8439(7)	6705(6)	49(4)

C(25B)	-2501(12)	-7688(12)	6618(9)	36(5)

C(26B)	-4271(10)	-6347(9)	4726(7)	36(5)

C(27B)	-2142(10)	-5988(9)	3931(7)	36(5)

C(28B)	-2746(11)	-7779(9)	4786(8)	45(5)

________________________________________________________________________________

Table Q3:  Bond lengths [Å] and angles [°] for 149.

___________________________________________________________________________________

Co(1A)-C(13A) 	1.81(2)

Co(1A)-C(12A) 	1.81(2)

Co(1A)-C(11A) 	1.83(2)

Co(1A)-C(7A) 	1.969(13)

Co(1A)-C(8A) 	2.001(12)

Co(1A)-Co(2A) 	2.477(3)

Co(2A)-C(15A) 	1.75(2)

Co(2A)-C(16A) 	1.78(2)

Co(2A)-C(14A) 	1.80(2)

Co(2A)-C(7A) 	1.927(13)

Co(2A)-C(8A) 	2.003(14)

Co(3A)-C(21A) 	1.794(15)

Co(3A)-C(22A) 	1.80(2)

Co(3A)-C(20A) 	1.83(2)

Co(3A)-C(9A) 	1.955(13)

Co(3A)-C(10A) 	2.014(11)

Co(3A)-Co(4A) 	2.482(3)

Co(4A)-C(23A) 	1.76(2)

Co(4A)-C(25A) 	1.81(2)

Co(4A)-C(24A) 	1.83(2)

Co(4A)-C(9A) 	1.963(14)

Co(4A)-C(10A) 	2.007(14)

Si(1A)-C(8A) 	1.857(14)

Si(1A)-C(18A) 	1.864(13)

Si(1A)-C(19A) 	1.874(14)

Si(1A)-C(17A) 	1.901(15)

Si(2A)-C(28A) 	1.827(15)

Si(2A)-C(26A) 	1.84(2)

Si(2A)-C(10A) 	1.847(12)

Si(2A)-C(27A) 	1.865(15)

O(1A)-C(1A) 	1.460(13)

C(1A)-C(7A) 	1.52(2)

C(1A)-C(2A) 	1.53(2)

C(1A)-C(6A) 	1.54(2)

C(2A)-C(3A) 	1.53(2)

C(3A)-C(4A) 	1.55(2)

O(4A)-C(4A) 	1.435(13)

C(4A)-C(9A) 	1.50(2)

C(4A)-C(5A) 	1.54(2)

C(5A)-C(6A) 	1.54(2)

C(7A)-C(8A) 	1.32(2)

C(9A)-C(10A) 	1.32(2)

O(11A)-C(11A) 	1.13(2)

O(12A)-C(12A) 	1.162(15)

O(13A)-C(13A) 	1.13(2)

O(14A)-C(14A) 	1.14(2)

O(15A)-C(15A) 	1.20(2)

O(16A)-C(16A) 	1.158(14)

O(20A)-C(20A) 	1.12(2)

O(21A)-C(21A) 	1.165(13)

O(22A)-C(22A) 	1.14(2)

O(23A)-C(23A) 	1.18(2)

O(24A)-C(24A) 	1.12(2)

O(25A)-C(25A) 	1.123(14)

Co(1B)-C(12B) 	1.77(2)

Co(1B)-C(11B) 	1.79(2)

Co(1B)-C(13B) 	1.83(2)

Co(1B)-C(7B) 	1.957(14)

Co(1B)-C(8B) 	2.021(15)

Co(1B)-Co(2B) 	2.474(3)

Co(2B)-C(15B) 	1.75(2)

Co(2B)-C(16B) 	1.79(2)

Co(2B)-C(14B) 	1.80(2)

Co(2B)-C(7B) 	1.994(13)

Co(2B)-C(8B) 	2.015(14)

Co(3B)-C(21B) 	1.80(2)

Co(3B)-C(22B) 	1.81(2)

Co(3B)-C(20B) 	1.83(2)

Co(3B)-C(9B) 	1.938(13)

Co(3B)-C(10B) 	2.010(12)

Co(3B)-Co(4B) 	2.489(3)

Co(4B)-C(24B) 	1.77(2)

Co(4B)-C(25B) 	1.80(2)

Co(4B)-C(23B) 	1.81(2)

Co(4B)-C(9B) 	1.952(14)

Co(4B)-C(10B) 	2.030(13)

Si(1B)-C(18B) 	1.85(2)

Si(1B)-C(17B) 	1.853(13)

Si(1B)-C(8B) 	1.855(14)

Si(1B)-C(19B) 	1.87(2)

Si(2B)-C(10B) 	1.846(14)

Si(2B)-C(26B) 	1.845(14)

Si(2B)-C(28B) 	1.859(14)

Si(2B)-C(27B) 	1.884(12)

O(1B)-C(1B) 	1.464(13)

C(1B)-C(2B) 	1.51(2)

C(1B)-C(7B) 	1.51(2)

C(1B)-C(6B) 	1.56(2)

C(2B)-C(3B) 	1.563(14)

C(3B)-C(4B) 	1.53(2)

O(4B)-C(4B) 	1.423(13)

C(4B)-C(9B) 	1.54(2)

C(4B)-C(5B) 	1.55(2)

C(5B)-C(6B) 	1.57(2)

C(7B)-C(8B) 	1.323(14)

C(9B)-C(10B) 	1.31(2)

O(11B)-C(11B) 	1.12(2)

O(12B)-C(12B) 	1.17(2)

O(13B)-C(13B) 	1.131(14)

O(14B)-C(14B) 	1.15(2)

O(15B)-C(15B) 	1.19(2)

O(16B)-C(16B) 	1.13(2)

O(20B)-C(20B) 	1.144(14)

O(21B)-C(21B) 	1.14(2)

O(22B)-C(22B) 	1.15(2)

O(23B)-C(23B) 	1.167(15)

O(24B)-C(24B) 	1.174(14)

O(25B)-C(25B) 	1.14(2)

C(13A)-Co(1A)-C(12A)	108.0(8)

C(13A)-Co(1A)-C(11A)	97.6(8)

C(12A)-Co(1A)-C(11A)	99.1(6)

C(13A)-Co(1A)-C(7A)	141.0(7)

C(12A)-Co(1A)-C(7A)	99.5(6)

C(11A)-Co(1A)-C(7A)	104.9(6)

C(13A)-Co(1A)-C(8A)	105.9(7)

C(12A)-Co(1A)-C(8A)	137.4(7)

C(11A)-Co(1A)-C(8A)	101.2(6)

C(7A)-Co(1A)-C(8A)	38.9(5)

C(13A)-Co(1A)-Co(2A)	98.4(6)

C(12A)-Co(1A)-Co(2A)	97.9(5)

C(11A)-Co(1A)-Co(2A)	151.7(5)

C(7A)-Co(1A)-Co(2A)	49.8(4)

C(8A)-Co(1A)-Co(2A)	51.8(4)

C(15A)-Co(2A)-C(16A)	101.0(7)

C(15A)-Co(2A)-C(14A)	107.8(7)

C(16A)-Co(2A)-C(14A)	97.6(7)

C(15A)-Co(2A)-C(7A)	138.7(7)

C(16A)-Co(2A)-C(7A)	100.2(6)

C(14A)-Co(2A)-C(7A)	103.9(6)

C(15A)-Co(2A)-C(8A)	101.6(7)

C(16A)-Co(2A)-C(8A)	101.6(6)

C(14A)-Co(2A)-C(8A)	140.9(6)

C(7A)-Co(2A)-C(8A)	39.3(5)

C(15A)-Co(2A)-Co(1A)	98.0(5)

C(16A)-Co(2A)-Co(1A)	150.1(5)

C(14A)-Co(2A)-Co(1A)	98.2(5)

C(7A)-Co(2A)-Co(1A)	51.3(4)

C(8A)-Co(2A)-Co(1A)	51.8(3)

C(21A)-Co(3A)-C(22A)	98.2(7)

C(21A)-Co(3A)-C(20A)	106.0(7)

C(22A)-Co(3A)-C(20A)	97.5(8)

C(21A)-Co(3A)-C(9A)	98.8(6)

C(22A)-Co(3A)-C(9A)	104.0(7)

C(20A)-Co(3A)-C(9A)	144.3(6)

C(21A)-Co(3A)-C(10A)	136.2(6)

C(22A)-Co(3A)-C(10A)	102.0(6)

C(20A)-Co(3A)-C(10A)	109.3(6)

C(9A)-Co(3A)-C(10A)	38.7(4)

C(21A)-Co(3A)-Co(4A)	97.5(5)

C(22A)-Co(3A)-Co(4A)	152.2(5)

C(20A)-Co(3A)-Co(4A)	100.0(5)

C(9A)-Co(3A)-Co(4A)	50.8(4)

C(10A)-Co(3A)-Co(4A)	51.7(4)

C(23A)-Co(4A)-C(25A)	102.4(7)

C(23A)-Co(4A)-C(24A)	106.8(7)

C(25A)-Co(4A)-C(24A)	95.1(7)

C(23A)-Co(4A)-C(9A)	100.8(7)

C(25A)-Co(4A)-C(9A)	106.4(6)

C(24A)-Co(4A)-C(9A)	140.3(7)

C(23A)-Co(4A)-C(10A)	139.2(7)

C(25A)-Co(4A)-C(10A)	96.5(6)

C(24A)-Co(4A)-C(10A)	107.2(6)

C(9A)-Co(4A)-C(10A)	38.7(5)

C(23A)-Co(4A)-Co(3A)	103.1(5)

C(25A)-Co(4A)-Co(3A)	148.5(5)

C(24A)-Co(4A)-Co(3A)	95.0(5)

C(9A)-Co(4A)-Co(3A)	50.6(4)

C(10A)-Co(4A)-Co(3A)	52.0(3)

C(8A)-Si(1A)-C(18A)	110.8(7)

C(8A)-Si(1A)-C(19A)	109.0(7)

C(18A)-Si(1A)-C(19A)	109.6(6)

C(8A)-Si(1A)-C(17A)	109.3(6)

C(18A)-Si(1A)-C(17A)	109.8(7)

C(19A)-Si(1A)-C(17A)	108.2(7)

C(28A)-Si(2A)-C(26A)	110.4(7)

C(28A)-Si(2A)-C(10A)	107.5(7)

C(26A)-Si(2A)-C(10A)	109.1(6)

C(28A)-Si(2A)-C(27A)	109.4(7)

C(26A)-Si(2A)-C(27A)	111.1(8)

C(10A)-Si(2A)-C(27A)	109.3(7)

O(1A)-C(1A)-C(7A)	107.7(10)

O(1A)-C(1A)-C(2A)	104.3(11)

C(7A)-C(1A)-C(2A)	111.5(9)

O(1A)-C(1A)-C(6A)	111.9(9)

C(7A)-C(1A)-C(6A)	111.3(12)

C(2A)-C(1A)-C(6A)	109.9(11)

C(3A)-C(2A)-C(1A)	112.8(10)

C(2A)-C(3A)-C(4A)	117.9(11)

O(4A)-C(4A)-C(9A)	111.0(11)

O(4A)-C(4A)-C(5A)	105.3(11)

C(9A)-C(4A)-C(5A)	110.1(12)

O(4A)-C(4A)-C(3A)	111.7(11)

C(9A)-C(4A)-C(3A)	112.3(11)

C(5A)-C(4A)-C(3A)	106.0(11)

C(6A)-C(5A)-C(4A)	116.9(12)

C(5A)-C(6A)-C(1A)	113.8(11)

C(8A)-C(7A)-C(1A)	141.9(13)

C(8A)-C(7A)-Co(2A)	73.4(8)

C(1A)-C(7A)-Co(2A)	133.9(10)

C(8A)-C(7A)-Co(1A)	71.8(8)

C(1A)-C(7A)-Co(1A)	130.8(8)

Co(2A)-C(7A)-Co(1A)	78.9(5)

C(7A)-C(8A)-Si(1A)	149.1(11)

C(7A)-C(8A)-Co(1A)	69.2(7)

Si(1A)-C(8A)-Co(1A)	133.2(8)

C(7A)-C(8A)-Co(2A)	67.3(8)

Si(1A)-C(8A)-Co(2A)	131.4(7)

Co(1A)-C(8A)-Co(2A)	76.4(5)

C(10A)-C(9A)-C(4A)	144.3(13)

C(10A)-C(9A)-Co(3A)	73.1(8)

C(4A)-C(9A)-Co(3A)	131.7(9)

C(10A)-C(9A)-Co(4A)	72.5(9)

C(4A)-C(9A)-Co(4A)	130.5(10)

Co(3A)-C(9A)-Co(4A)	78.6(5)

C(9A)-C(10A)-Si(2A)	146.1(11)

C(9A)-C(10A)-Co(4A)	68.8(9)

Si(2A)-C(10A)-Co(4A)	132.3(7)

C(9A)-C(10A)-Co(3A)	68.3(7)

Si(2A)-C(10A)-Co(3A)	135.2(8)

Co(4A)-C(10A)-Co(3A)	76.3(4)

O(11A)-C(11A)-Co(1A)	176.9(13)

O(12A)-C(12A)-Co(1A)	178.9(15)

O(13A)-C(13A)-Co(1A)	177.7(19)

O(14A)-C(14A)-Co(2A)	177.3(14)

O(15A)-C(15A)-Co(2A)	178.1(15)

O(16A)-C(16A)-Co(2A)	177.1(14)

O(20A)-C(20A)-Co(3A)	178.9(17)

O(21A)-C(21A)-Co(3A)	179.2(14)

O(22A)-C(22A)-Co(3A)	177.1(16)

O(23A)-C(23A)-Co(4A)	178.1(15)

O(24A)-C(24A)-Co(4A)	179.8(8)

O(25A)-C(25A)-Co(4A)	178.2(15)

C(12B)-Co(1B)-C(11B)	97.6(8)

C(12B)-Co(1B)-C(13B)	109.3(7)

C(11B)-Co(1B)-C(13B)	95.8(8)

C(12B)-Co(1B)-C(7B)	101.9(6)

C(11B)-Co(1B)-C(7B)	102.9(7)

C(13B)-Co(1B)-C(7B)	140.9(6)

C(12B)-Co(1B)-C(8B)	138.7(7)

C(11B)-Co(1B)-C(8B)	103.1(8)

C(13B)-Co(1B)-C(8B)	103.7(6)

C(7B)-Co(1B)-C(8B)	38.8(4)

C(12B)-Co(1B)-Co(2B)	97.3(5)

C(11B)-Co(1B)-Co(2B)	153.1(7)

C(13B)-Co(1B)-Co(2B)	100.3(5)

C(7B)-Co(1B)-Co(2B)	51.9(4)

C(8B)-Co(1B)-Co(2B)	52.1(4)

C(15B)-Co(2B)-C(16B)	96.0(8)

C(15B)-Co(2B)-C(14B)	107.1(8)

C(16B)-Co(2B)-C(14B)	98.9(8)

C(15B)-Co(2B)-C(7B)	141.0(7)

C(16B)-Co(2B)-C(7B)	106.9(7)

C(14B)-Co(2B)-C(7B)	100.2(7)

C(15B)-Co(2B)-C(8B)	107.8(6)

C(16B)-Co(2B)-C(8B)	99.2(7)

C(14B)-Co(2B)-C(8B)	138.4(7)

C(7B)-Co(2B)-C(8B)	38.5(4)

C(15B)-Co(2B)-Co(1B)	96.0(6)

C(16B)-Co(2B)-Co(1B)	151.4(6)

C(14B)-Co(2B)-Co(1B)	102.2(6)

C(7B)-Co(2B)-Co(1B)	50.6(4)

C(8B)-Co(2B)-Co(1B)	52.3(4)

C(21B)-Co(3B)-C(22B)	94.6(7)

C(21B)-Co(3B)-C(20B)	98.8(7)

C(22B)-Co(3B)-C(20B)	106.1(6)

C(21B)-Co(3B)-C(9B)	106.0(6)

C(22B)-Co(3B)-C(9B)	140.9(7)

C(20B)-Co(3B)-C(9B)	103.1(6)

C(21B)-Co(3B)-C(10B)	101.1(6)

C(22B)-Co(3B)-C(10B)	105.6(6)

C(20B)-Co(3B)-C(10B)	140.8(6)

C(9B)-Co(3B)-C(10B)	38.7(5)

C(21B)-Co(3B)-Co(4B)	152.7(5)

C(22B)-Co(3B)-Co(4B)	98.6(5)

C(20B)-Co(3B)-Co(4B)	100.3(5)

C(9B)-Co(3B)-Co(4B)	50.5(4)

C(10B)-Co(3B)-Co(4B)	52.3(4)

C(24B)-Co(4B)-C(25B)	100.4(7)

C(24B)-Co(4B)-C(23B)	98.4(7)

C(25B)-Co(4B)-C(23B)	105.4(7)

C(24B)-Co(4B)-C(9B)	102.1(6)

C(25B)-Co(4B)-C(9B)	140.5(7)

C(23B)-Co(4B)-C(9B)	102.9(7)

C(24B)-Co(4B)-C(10B)	98.9(6)

C(25B)-Co(4B)-C(10B)	106.2(6)

C(23B)-Co(4B)-C(10B)	140.3(7)

C(9B)-Co(4B)-C(10B)	38.3(5)

C(24B)-Co(4B)-Co(3B)	149.1(5)

C(25B)-Co(4B)-Co(3B)	97.5(5)

C(23B)-Co(4B)-Co(3B)	100.9(5)

C(9B)-Co(4B)-Co(3B)	50.0(4)

C(10B)-Co(4B)-Co(3B)	51.6(4)

C(18B)-Si(1B)-C(17B)	110.4(8)

C(18B)-Si(1B)-C(8B)	108.3(7)

C(17B)-Si(1B)-C(8B)	110.4(7)

C(18B)-Si(1B)-C(19B)	109.2(9)

C(17B)-Si(1B)-C(19B)	109.8(7)

C(8B)-Si(1B)-C(19B)	108.8(7)

C(10B)-Si(2B)-C(26B)	108.3(6)

C(10B)-Si(2B)-C(28B)	111.0(6)

C(26B)-Si(2B)-C(28B)	110.9(7)

C(10B)-Si(2B)-C(27B)	108.4(6)

C(26B)-Si(2B)-C(27B)	108.7(6)

C(28B)-Si(2B)-C(27B)	109.4(6)

O(1B)-C(1B)-C(2B)	109.4(10)

O(1B)-C(1B)-C(7B)	108.6(11)

C(2B)-C(1B)-C(7B)	109.2(11)

O(1B)-C(1B)-C(6B)	110.2(10)

C(2B)-C(1B)-C(6B)	109.6(13)

C(7B)-C(1B)-C(6B)	109.9(11)

C(1B)-C(2B)-C(3B)	113.9(11)

C(4B)-C(3B)-C(2B)	115.4(11)

O(4B)-C(4B)-C(3B)	113.4(11)

O(4B)-C(4B)-C(9B)	109.2(10)

C(3B)-C(4B)-C(9B)	108.7(11)

O(4B)-C(4B)-C(5B)	107.0(11)

C(3B)-C(4B)-C(5B)	108.4(10)

C(9B)-C(4B)-C(5B)	110.2(11)

C(4B)-C(5B)-C(6B)	112.2(11)

C(1B)-C(6B)-C(5B)	114.1(11)

C(8B)-C(7B)-C(1B)	141.8(14)

C(8B)-C(7B)-Co(1B)	73.2(9)

C(1B)-C(7B)-Co(1B)	134.6(10)

C(8B)-C(7B)-Co(2B)	71.6(8)

C(1B)-C(7B)-Co(2B)	131.4(10)

Co(1B)-C(7B)-Co(2B)	77.5(5)

C(7B)-C(8B)-Si(1B)	149.5(12)

C(7B)-C(8B)-Co(2B)	69.9(8)

Si(1B)-C(8B)-Co(2B)	132.6(8)

C(7B)-C(8B)-Co(1B)	68.0(9)

Si(1B)-C(8B)-Co(1B)	130.9(8)

Co(2B)-C(8B)-Co(1B)	75.6(5)

C(10B)-C(9B)-C(4B)	142.6(12)

C(10B)-C(9B)-Co(3B)	73.6(9)

C(4B)-C(9B)-Co(3B)	132.3(10)

C(10B)-C(9B)-Co(4B)	74.1(9)

C(4B)-C(9B)-Co(4B)	129.7(10)

Co(3B)-C(9B)-Co(4B)	79.5(5)

C(9B)-C(10B)-Si(2B)	152.9(11)

C(9B)-C(10B)-Co(3B)	67.7(8)

Si(2B)-C(10B)-Co(3B)	132.0(7)

C(9B)-C(10B)-Co(4B)	67.6(8)

Si(2B)-C(10B)-Co(4B)	129.5(8)

Co(3B)-C(10B)-Co(4B)	76.0(4)

O(11B)-C(11B)-Co(1B)	177.6(20)

O(12B)-C(12B)-Co(1B)	177.2(16)

O(13B)-C(13B)-Co(1B)	175.8(16)

O(14B)-C(14B)-Co(2B)	178.1(16)

O(15B)-C(15B)-Co(2B)	175.8(15)

O(16B)-C(16B)-Co(2B)	175.9(18)

O(20B)-C(20B)-Co(3B)	176.5(14)

O(21B)-C(21B)-Co(3B)	178.8(16)

O(22B)-C(22B)-Co(3B)	176.8(14)

O(23B)-C(23B)-Co(4B)	176.6(13)

O(24B)-C(24B)-Co(4B)	177.2(14)

O(25B)-C(25B)-Co(4B)	178.9(14)

____________________________________________________________________________________

Table Q4:  Anisotropic displacement parameters (Å2 x 103) for 149.  The anisotropic

displacement factor exponent takes the form: -2(2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Co(1A)	27(2) 	28(2)	28(1) 	-1(1)	-15(1) 	3(1)

Co(2A)	21(2) 	19(2)	39(1) 	-4(1)	-12(1) 	-2(1)

Co(3A)	25(2) 	23(2)	30(1) 	0(1)	-15(1) 	-4(1)

Co(4A)	21(2) 	24(2)	29(1) 	3(1)	-11(1) 	-3(1)

Si(1A)	34(4) 	34(4)	27(3) 	-7(3)	-13(3) 	0(3)

Si(2A)	32(4) 	63(5)	26(3) 	-1(3)	-13(3) 	-5(3)

O(11A)	69(11) 	37(10)	88(9) 	10(7)	-37(8) 	-33(8)

O(12A)	72(11) 	52(10)	44(7) 	-15(7)	-27(7) 	33(7)

O(13A)	39(10) 	67(11)	101(10) 	-2(8)	-35(9) 	8(8)

O(14A)	76(11) 	56(11)	55(8) 	-28(7)	-27(7) 	-4(8)

O(15A)	14(9) 	46(10)	131(11) 	3(8)	-3(8) 	-15(7)

O(16A)	26(8) 	35(9)	53(7) 	30(6)	-16(6) 	-10(6)

O(20A)	37(10) 	67(11)	107(10) 	-11(8)	-44(8) 	3(8)

O(21A)	65(10) 	35(9)	38(7) 	9(6)	-27(7) 	-23(7)

O(22A)	49(10) 	29(10)	113(10) 	-19(8)	-33(8) 	3(8)

O(23A)	38(9) 	45(10)	48(7) 	8(7)	-14(6) 	-5(7)

O(24A)	26(10) 	67(11)	110(10) 	45(8)	-31(8) 	-9(8)

O(25A)	56(10) 	48(10)	83(8) 	47(8)	-43(7) 	-35(8)

Co(1B)	34(2) 	22(2)	36(1) 	7(1)	-17(1) 	-2(1)

Co(2B)	33(2) 	15(2)	31(1) 	7(1)	-13(1) 	-6(1)

Co(3B)	25(2) 	17(2)	28(1) 	0(1)	-11(1) 	-3(1)

Co(4B)	25(2) 	12(2)	32(1) 	3(1)	-15(1) 	2(1)

Si(1B)	54(5) 	37(4)	26(3) 	1(3)	-12(3) 	-5(3)

Si(2B)	27(4) 	21(4)	29(3) 	-6(2)	-11(3) 	-5(3)

O(12B)	104(13) 	62(11)	57(8) 	-15(8)	-24(8) 	29(8)

O(13B)	96(12) 	30(10)	70(8) 	23(7)	-40(8) 	-5(8)

O(14B)	122(13) 	28(9)	54(8) 	0(7)	-30(8) 	-24(8)

O(16B)	36(10) 	31(10)	144(12) 	13(8)	-24(9) 	2(8)

O(20B)	36(9) 	37(9)	44(7) 	-18(6)	-17(6) 	10(6)

O(21B)	42(9) 	42(9)	41(7) 	-4(6)	-22(7) 	6(7)

O(22B)	73(10) 	26(9)	62(8) 	17(7)	-37(7) 	-14(7)

O(23B)	41(9) 	32(9)	55(7) 	-6(6)	-28(7) 	1(6)

O(24B)	25(8) 	38(9)	47(7) 	2(6)	-10(6) 	11(6)

O(25B)	52(10) 	9(9)	71(8) 	0(7)	-12(7) 	1(7)

______________________________________________________________________________

Table Q5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 149.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1A)	-4519(6)	-2708(6)	7512(4)	31

H(2AA)	-4394(9)	-2994(9)	9653(7)	20

H(2AB)	-4658(9)	-3765(9)	9236(7)	20

H(3AA)	-3116(9)	-4067(8)	8359(7)	20

H(3AB)	-3000(9)	-3851(8)	9173(7)	20

H(4A)	-2694(6)	-2869(5)	7277(4)	29

H(5AA)	-3091(10)	-1927(9)	9069(7)	30

H(5AB)	-2502(10)	-1542(9)	8159(7)	30

H(6AA)	-3758(9)	-1570(9)	7804(7)	19

H(6AB)	-4291(9)	-1297(9)	8744(7)	19

H(17A)	-6640(11)	151(10)	10972(8)	82

H(17B)	-6905(11)	140(10)	10193(8)	82

H(17C)	-5797(11)	-12(10)	10076(8)	82

H(18A)	-8021(10)	-1294(10)	11866(7)	70

H(18B)	-7923(10)	-2205(10)	11434(7)	70

H(18C)	-8314(10)	-1314(10)	11103(7)	70

H(19A)	-5900(10)	-1565(10)	11602(8)	71

H(19B)	-5068(10)	-1706(10)	10697(8)	71

H(19C)	-5777(10)	-2471(10)	11156(8)	71

H(26A)	-1946(12)	-1389(11)	10143(9)	118

H(26B)	-819(12)	-1584(11)	9953(9)	118

H(26C)	-1624(12)	-1711(11)	10872(9)	118

H(27A)	-3256(11)	-2911(11)	10551(8)	95

H(27B)	-2950(11)	-3265(11)	11283(8)	95

H(27C)	-2808(11)	-3904(11)	10563(8)	95

H(28A)	-712(10)	-4257(10)	10248(8)	76

H(28B)	-814(10)	-3594(10)	10940(8)	76

H(28C)	-10(10)	-3468(10)	10020(8)	76

H(1B)	-3320(6)	-2713(6)	6699(4)	21

H(2BA)	-3246(9)	-3328(9)	4836(7)	22

H(2BB)	-4084(9)	-2721(9)	5497(7)	22

H(3BA)	-4347(9)	-3755(9)	6537(7)	24

H(3BB)	-4127(9)	-4351(9)	5772(7)	24

H(4B)	-2882(6)	-3733(6)	6901(4)	29

H(5BA)	-2028(9)	-4478(9)	4946(7)	25

H(5BB)	-1510(9)	-4653(9)	5569(7)	25

H(6BA)	-1590(9)	-3173(9)	5807(7)	25

H(6BB)	-1324(9)	-3169(9)	4842(7)	25

H(17D)	-1451(11)	-729(10)	2327(8)	94

H(17E)	-619(11)	-1396(10)	1728(8)	94

H(17F)	-443(11)	-920(10)	2420(8)	94

H(18D)	-742(13)	-3454(12)	3361(10)	142

H(18E)	22(13)	-2714(12)	3102(10)	142

H(18F)	-152(13)	-3190(12)	2409(10)	142

H(19D)	-2885(12)	-2148(11)	2818(9)	122

H(19E)	-2642(12)	-3084(11)	3185(9)	122

H(19F)	-2062(12)	-2829(11)	2230(9)	122

H(26D)	-4223(10)	-6584(9)	4213(7)	54

H(26E)	-4431(10)	-5708(9)	4721(7)	54

H(26F)	-4782(10)	-6628(9)	5195(7)	54

H(27D)	-2071(10)	-6221(9)	3410(7)	55

H(27E)	-1522(10)	-6082(9)	3985(7)	55

H(27F)	-2335(10)	-5355(9)	3939(7)	55

H(28D)	-2690(11)	-8004(9)	4266(8)	68

H(28E)	-3242(11)	-8084(9)	5248(8)	68

H(28F)	-2121(11)	-7883(9)	4829(8)	68

________________________________________________________________________________

Table Q6:  Torsion angles [°] for 149.

____________________________________________________________________________________

C(13A)-Co(1A)-Co(2A)-C(15A)	-5.2(8)

C(12A)-Co(1A)-Co(2A)-C(15A)	-114.8(8)

C(11A)-Co(1A)-Co(2A)-C(15A)	118.7(12)

C(7A)-Co(1A)-Co(2A)-C(15A)	149.3(7)

C(8A)-Co(1A)-Co(2A)-C(15A)	98.4(7)

C(13A)-Co(1A)-Co(2A)-C(16A)	-134.5(11)

C(12A)-Co(1A)-Co(2A)-C(16A)	115.9(11)

C(11A)-Co(1A)-Co(2A)-C(16A)	-10.6(14)

C(7A)-Co(1A)-Co(2A)-C(16A)	20.0(11)

C(8A)-Co(1A)-Co(2A)-C(16A)	-30.9(11)

C(13A)-Co(1A)-Co(2A)-C(14A)	104.1(8)

C(12A)-Co(1A)-Co(2A)-C(14A)	-5.5(8)

C(11A)-Co(1A)-Co(2A)-C(14A)	-131.9(12)

C(7A)-Co(1A)-Co(2A)-C(14A)	-101.3(7)

C(8A)-Co(1A)-Co(2A)-C(14A)	-152.2(7)

C(13A)-Co(1A)-Co(2A)-C(7A)	-154.6(8)

C(12A)-Co(1A)-Co(2A)-C(7A)	95.8(7)

C(11A)-Co(1A)-Co(2A)-C(7A)	-30.6(11)

C(7A)-Co(1A)-Co(2A)-C(7A)	0.0

C(8A)-Co(1A)-Co(2A)-C(7A)	-50.9(6)

C(13A)-Co(1A)-Co(2A)-C(8A)	-103.7(8)

C(12A)-Co(1A)-Co(2A)-C(8A)	146.7(7)

C(11A)-Co(1A)-Co(2A)-C(8A)	20.3(12)

C(7A)-Co(1A)-Co(2A)-C(8A)	50.9(6)

C(8A)-Co(1A)-Co(2A)-C(8A)	0.000(1)

C(21A)-Co(3A)-Co(4A)-C(23A)	-1.9(8)

C(22A)-Co(3A)-Co(4A)-C(23A)	122.0(13)

C(20A)-Co(3A)-Co(4A)-C(23A)	-109.7(8)

C(9A)-Co(3A)-Co(4A)-C(23A)	93.4(7)

C(10A)-Co(3A)-Co(4A)-C(23A)	143.6(8)

C(21A)-Co(3A)-Co(4A)-C(25A)	-145.1(11)

C(22A)-Co(3A)-Co(4A)-C(25A)	-21.2(15)

C(20A)-Co(3A)-Co(4A)-C(25A)	107.1(11)

C(9A)-Co(3A)-Co(4A)-C(25A)	-49.9(11)

C(10A)-Co(3A)-Co(4A)-C(25A)	0.3(11)

C(21A)-Co(3A)-Co(4A)-C(24A)	106.6(7)

C(22A)-Co(3A)-Co(4A)-C(24A)	-129.5(12)

C(20A)-Co(3A)-Co(4A)-C(24A)	-1.2(7)

C(9A)-Co(3A)-Co(4A)-C(24A)	-158.1(7)

C(10A)-Co(3A)-Co(4A)-C(24A)	-107.9(7)

C(21A)-Co(3A)-Co(4A)-C(9A)	-95.3(7)

C(22A)-Co(3A)-Co(4A)-C(9A)	28.7(12)

C(20A)-Co(3A)-Co(4A)-C(9A)	156.9(7)

C(9A)-Co(3A)-Co(4A)-C(9A)	0.0

C(10A)-Co(3A)-Co(4A)-C(9A)	50.2(6)

C(21A)-Co(3A)-Co(4A)-C(10A)	-145.5(7)

C(22A)-Co(3A)-Co(4A)-C(10A)	-21.6(13)

C(20A)-Co(3A)-Co(4A)-C(10A)	106.7(7)

C(9A)-Co(3A)-Co(4A)-C(10A)	-50.2(6)

C(10A)-Co(3A)-Co(4A)-C(10A)	0.0

O(1A)-C(1A)-C(2A)-C(3A)	62.2(13)

C(7A)-C(1A)-C(2A)-C(3A)	178.2(11)

C(6A)-C(1A)-C(2A)-C(3A)	-57.9(15)

C(1A)-C(2A)-C(3A)-C(4A)	38.1(17)

C(2A)-C(3A)-C(4A)-O(4A)	-97.0(14)

C(2A)-C(3A)-C(4A)-C(9A)	137.5(12)

C(2A)-C(3A)-C(4A)-C(5A)	17.2(16)

O(4A)-C(4A)-C(5A)-C(6A)	62.6(14)

C(9A)-C(4A)-C(5A)-C(6A)	-177.7(10)

C(3A)-C(4A)-C(5A)-C(6A)	-56.0(14)

C(4A)-C(5A)-C(6A)-C(1A)	37.3(16)

O(1A)-C(1A)-C(6A)-C(5A)	-94.3(12)

C(7A)-C(1A)-C(6A)-C(5A)	145.1(11)

C(2A)-C(1A)-C(6A)-C(5A)	21.1(15)

O(1A)-C(1A)-C(7A)-C(8A)	178.8(16)

C(2A)-C(1A)-C(7A)-C(8A)	64.9(23)

C(6A)-C(1A)-C(7A)-C(8A)	-58.2(22)

O(1A)-C(1A)-C(7A)-Co(2A)	53.0(15)

C(2A)-C(1A)-C(7A)-Co(2A)	-60.9(16)

C(6A)-C(1A)-C(7A)-Co(2A)	176.0(9)

O(1A)-C(1A)-C(7A)-Co(1A)	-65.6(15)

C(2A)-C(1A)-C(7A)-Co(1A)	-179.5(10)

C(6A)-C(1A)-C(7A)-Co(1A)	57.4(15)

C(15A)-Co(2A)-C(7A)-C(8A)	24.2(12)

C(16A)-Co(2A)-C(7A)-C(8A)	-95.9(9)

C(14A)-Co(2A)-C(7A)-C(8A)	163.5(8)

C(8A)-Co(2A)-C(7A)-C(8A)	0.000(1)

Co(1A)-Co(2A)-C(7A)-C(8A)	74.1(8)

C(15A)-Co(2A)-C(7A)-C(1A)	172.7(11)

C(16A)-Co(2A)-C(7A)-C(1A)	52.6(13)

C(14A)-Co(2A)-C(7A)-C(1A)	-48.0(13)

C(8A)-Co(2A)-C(7A)-C(1A)	148.5(16)

Co(1A)-Co(2A)-C(7A)-C(1A)	-137.3(13)

C(15A)-Co(2A)-C(7A)-Co(1A)	-50.0(10)

C(16A)-Co(2A)-C(7A)-Co(1A)	-170.0(5)

C(14A)-Co(2A)-C(7A)-Co(1A)	89.4(6)

C(8A)-Co(2A)-C(7A)-Co(1A)	-74.1(8)

Co(1A)-Co(2A)-C(7A)-Co(1A)	0.0

C(13A)-Co(1A)-C(7A)-C(8A)	-33.6(15)

C(12A)-Co(1A)-C(7A)-C(8A)	-168.3(9)

C(11A)-Co(1A)-C(7A)-C(8A)	89.5(9)

C(8A)-Co(1A)-C(7A)-C(8A)	0.000(4)

Co(2A)-Co(1A)-C(7A)-C(8A)	-76.0(8)

C(13A)-Co(1A)-C(7A)-C(1A)	-177.7(13)

C(12A)-Co(1A)-C(7A)-C(1A)	47.5(14)

C(11A)-Co(1A)-C(7A)-C(1A)	-54.6(13)

C(8A)-Co(1A)-C(7A)-C(1A)	-144.1(17)

Co(2A)-Co(1A)-C(7A)-C(1A)	139.9(14)

C(13A)-Co(1A)-C(7A)-Co(2A)	42.4(12)

C(12A)-Co(1A)-C(7A)-Co(2A)	-92.3(6)

C(11A)-Co(1A)-C(7A)-Co(2A)	165.5(5)

C(8A)-Co(1A)-C(7A)-Co(2A)	76.0(8)

Co(2A)-Co(1A)-C(7A)-Co(2A)	0.0

C(1A)-C(7A)-C(8A)-Si(1A)	-8.3(35)

Co(2A)-C(7A)-C(8A)-Si(1A)	134.1(20)

Co(1A)-C(7A)-C(8A)-Si(1A)	-142.4(20)

C(1A)-C(7A)-C(8A)-Co(1A)	134.0(19)

Co(2A)-C(7A)-C(8A)-Co(1A)	-83.5(4)

Co(1A)-C(7A)-C(8A)-Co(1A)	0.000(2)

C(1A)-C(7A)-C(8A)-Co(2A)	-142.5(19)

Co(2A)-C(7A)-C(8A)-Co(2A)	0.000(1)

Co(1A)-C(7A)-C(8A)-Co(2A)	83.5(4)

C(18A)-Si(1A)-C(8A)-C(7A)	-142.8(20)

C(19A)-Si(1A)-C(8A)-C(7A)	-22.1(23)

C(17A)-Si(1A)-C(8A)-C(7A)	96.0(21)

C(18A)-Si(1A)-C(8A)-Co(1A)	88.8(11)

C(19A)-Si(1A)-C(8A)-Co(1A)	-150.5(9)

C(17A)-Si(1A)-C(8A)-Co(1A)	-32.4(12)

C(18A)-Si(1A)-C(8A)-Co(2A)	-24.8(12)

C(19A)-Si(1A)-C(8A)-Co(2A)	95.9(11)

C(17A)-Si(1A)-C(8A)-Co(2A)	-146.0(9)

C(13A)-Co(1A)-C(8A)-C(7A)	158.8(10)

C(12A)-Co(1A)-C(8A)-C(7A)	17.1(13)

C(11A)-Co(1A)-C(8A)-C(7A)	-99.9(9)

C(7A)-Co(1A)-C(8A)-C(7A)	0.000(4)

Co(2A)-Co(1A)-C(8A)-C(7A)	70.5(8)

C(13A)-Co(1A)-C(8A)-Si(1A)	-46.8(12)

C(12A)-Co(1A)-C(8A)-Si(1A)	171.6(9)

C(11A)-Co(1A)-C(8A)-Si(1A)	54.6(11)

C(7A)-Co(1A)-C(8A)-Si(1A)	154.5(15)

Co(2A)-Co(1A)-C(8A)-Si(1A)	-135.0(12)

C(13A)-Co(1A)-C(8A)-Co(2A)	88.3(7)

C(12A)-Co(1A)-C(8A)-Co(2A)	-53.4(10)

C(11A)-Co(1A)-C(8A)-Co(2A)	-170.4(6)

C(7A)-Co(1A)-C(8A)-Co(2A)	-70.5(8)

Co(2A)-Co(1A)-C(8A)-Co(2A)	0.0

C(15A)-Co(2A)-C(8A)-C(7A)	-164.0(9)

C(16A)-Co(2A)-C(8A)-C(7A)	92.0(9)

C(14A)-Co(2A)-C(8A)-C(7A)	-25.9(13)

C(7A)-Co(2A)-C(8A)-C(7A)	0.000(1)

Co(1A)-Co(2A)-C(8A)-C(7A)	-72.9(7)

C(15A)-Co(2A)-C(8A)-Si(1A)	45.5(11)

C(16A)-Co(2A)-C(8A)-Si(1A)	-58.5(11)

C(14A)-Co(2A)-C(8A)-Si(1A)	-176.4(10)

C(7A)-Co(2A)-C(8A)-Si(1A)	-150.5(15)

Co(1A)-Co(2A)-C(8A)-Si(1A)	136.6(12)

C(15A)-Co(2A)-C(8A)-Co(1A)	-91.1(6)

C(16A)-Co(2A)-C(8A)-Co(1A)	164.9(5)

C(14A)-Co(2A)-C(8A)-Co(1A)	47.0(11)

C(7A)-Co(2A)-C(8A)-Co(1A)	72.9(7)

Co(1A)-Co(2A)-C(8A)-Co(1A)	0.0

O(4A)-C(4A)-C(9A)-C(10A)	176.0(19)

C(5A)-C(4A)-C(9A)-C(10A)	59.8(25)

C(3A)-C(4A)-C(9A)-C(10A)	-58.1(27)

O(4A)-C(4A)-C(9A)-Co(3A)	51.0(18)

C(5A)-C(4A)-C(9A)-Co(3A)	-65.2(16)

C(3A)-C(4A)-C(9A)-Co(3A)	176.9(10)

O(4A)-C(4A)-C(9A)-Co(4A)	-63.4(15)

C(5A)-C(4A)-C(9A)-Co(4A)	-179.6(8)

C(3A)-C(4A)-C(9A)-Co(4A)	62.5(15)

C(21A)-Co(3A)-C(9A)-C(10A)	167.5(9)

C(22A)-Co(3A)-C(9A)-C(10A)	-91.8(10)

C(20A)-Co(3A)-C(9A)-C(10A)	33.6(16)

C(10A)-Co(3A)-C(9A)-C(10A)	0.000(1)

Co(4A)-Co(3A)-C(9A)-C(10A)	74.9(9)

C(21A)-Co(3A)-C(9A)-C(4A)	-42.5(15)

C(22A)-Co(3A)-C(9A)-C(4A)	58.3(15)

C(20A)-Co(3A)-C(9A)-C(4A)	-176.4(13)

C(10A)-Co(3A)-C(9A)-C(4A)	150.0(19)

Co(4A)-Co(3A)-C(9A)-C(4A)	-135.0(15)

C(21A)-Co(3A)-C(9A)-Co(4A)	92.5(6)

C(22A)-Co(3A)-C(9A)-Co(4A)	-166.7(6)

C(20A)-Co(3A)-C(9A)-Co(4A)	-41.4(12)

C(10A)-Co(3A)-C(9A)-Co(4A)	-74.9(9)

Co(4A)-Co(3A)-C(9A)-Co(4A)	0.0

C(23A)-Co(4A)-C(9A)-C(10A)	-173.7(9)

C(25A)-Co(4A)-C(9A)-C(10A)	79.8(9)

C(24A)-Co(4A)-C(9A)-C(10A)	-40.1(12)

C(10A)-Co(4A)-C(9A)-C(10A)	0.000(4)

Co(3A)-Co(4A)-C(9A)-C(10A)	-75.6(8)

C(23A)-Co(4A)-C(9A)-C(4A)	38.1(12)

C(25A)-Co(4A)-C(9A)-C(4A)	-68.4(12)

C(24A)-Co(4A)-C(9A)-C(4A)	171.7(10)

C(10A)-Co(4A)-C(9A)-C(4A)	-148.2(15)

Co(3A)-Co(4A)-C(9A)-C(4A)	136.1(13)

C(23A)-Co(4A)-C(9A)-Co(3A)	-98.1(6)

C(25A)-Co(4A)-C(9A)-Co(3A)	155.4(5)

C(24A)-Co(4A)-C(9A)-Co(3A)	35.6(10)

C(10A)-Co(4A)-C(9A)-Co(3A)	75.6(8)

Co(3A)-Co(4A)-C(9A)-Co(3A)	0.0

C(4A)-C(9A)-C(10A)-Si(2A)	0.7(38)

Co(3A)-C(9A)-C(10A)-Si(2A)	141.0(19)

Co(4A)-C(9A)-C(10A)-Si(2A)	-135.9(19)

C(4A)-C(9A)-C(10A)-Co(4A)	136.6(22)

Co(3A)-C(9A)-C(10A)-Co(4A)	-83.1(4)

Co(4A)-C(9A)-C(10A)-Co(4A)	0.000(2)

C(4A)-C(9A)-C(10A)-Co(3A)	-140.3(23)

Co(3A)-C(9A)-C(10A)-Co(3A)	0.0

Co(4A)-C(9A)-C(10A)-Co(3A)	83.1(4)

C(28A)-Si(2A)-C(10A)-C(9A)	147.4(20)

C(26A)-Si(2A)-C(10A)-C(9A)	-92.9(21)

C(27A)-Si(2A)-C(10A)-C(9A)	28.8(22)

C(28A)-Si(2A)-C(10A)-Co(4A)	28.7(12)

C(26A)-Si(2A)-C(10A)-Co(4A)	148.4(10)

C(27A)-Si(2A)-C(10A)-Co(4A)	-89.9(11)

C(28A)-Si(2A)-C(10A)-Co(3A)	-88.7(12)

C(26A)-Si(2A)-C(10A)-Co(3A)	31.0(13)

C(27A)-Si(2A)-C(10A)-Co(3A)	152.7(10)

C(23A)-Co(4A)-C(10A)-C(9A)	9.5(13)

C(25A)-Co(4A)-C(10A)-C(9A)	-108.1(9)

C(24A)-Co(4A)-C(10A)-C(9A)	154.5(8)

C(9A)-Co(4A)-C(10A)-C(9A)	0.000(4)

Co(3A)-Co(4A)-C(10A)-C(9A)	71.7(7)

C(23A)-Co(4A)-C(10A)-Si(2A)	157.9(9)

C(25A)-Co(4A)-C(10A)-Si(2A)	40.3(11)

C(24A)-Co(4A)-C(10A)-Si(2A)	-57.1(11)

C(9A)-Co(4A)-C(10A)-Si(2A)	148.4(15)

Co(3A)-Co(4A)-C(10A)-Si(2A)	-139.9(12)

C(23A)-Co(4A)-C(10A)-Co(3A)	-62.2(10)

C(25A)-Co(4A)-C(10A)-Co(3A)	-179.8(6)

C(24A)-Co(4A)-C(10A)-Co(3A)	82.8(6)

C(9A)-Co(4A)-C(10A)-Co(3A)	-71.7(7)

Co(3A)-Co(4A)-C(10A)-Co(3A)	0.0

C(21A)-Co(3A)-C(10A)-C(9A)	-18.1(14)

C(22A)-Co(3A)-C(10A)-C(9A)	97.5(10)

C(20A)-Co(3A)-C(10A)-C(9A)	-160.0(10)

C(9A)-Co(3A)-C(10A)-C(9A)	0.000(1)

Co(4A)-Co(3A)-C(10A)-C(9A)	-72.4(8)

C(21A)-Co(3A)-C(10A)-Si(2A)	-168.2(10)

C(22A)-Co(3A)-C(10A)-Si(2A)	-52.6(12)

C(20A)-Co(3A)-C(10A)-Si(2A)	49.8(13)

C(9A)-Co(3A)-C(10A)-Si(2A)	-150.2(17)

Co(4A)-Co(3A)-C(10A)-Si(2A)	137.5(13)

C(21A)-Co(3A)-C(10A)-Co(4A)	54.3(10)

C(22A)-Co(3A)-C(10A)-Co(4A)	169.9(6)

C(20A)-Co(3A)-C(10A)-Co(4A)	-87.6(7)

C(9A)-Co(3A)-C(10A)-Co(4A)	72.4(8)

Co(4A)-Co(3A)-C(10A)-Co(4A)	0.0

C(13A)-Co(1A)-C(11A)-O(11A)	77.1(288)

C(12A)-Co(1A)-C(11A)-O(11A)	-173.2(287)

C(7A)-Co(1A)-C(11A)-O(11A)	-70.8(288)

C(8A)-Co(1A)-C(11A)-O(11A)	-30.9(289)

Co(2A)-Co(1A)-C(11A)-O(11A)	-47.0(294)

C(13A)-Co(1A)-C(12A)-O(12A)	21.4(803)

C(11A)-Co(1A)-C(12A)-O(12A)	-79.7(802)

C(7A)-Co(1A)-C(12A)-O(12A)	173.4(1000)

C(8A)-Co(1A)-C(12A)-O(12A)	162.6(797)

Co(2A)-Co(1A)-C(12A)-O(12A)	123.0(802)

C(12A)-Co(1A)-C(13A)-O(13A)	18.6(395)

C(11A)-Co(1A)-C(13A)-O(13A)	120.8(393)

C(7A)-Co(1A)-C(13A)-O(13A)	-114.0(390)

C(8A)-Co(1A)-C(13A)-O(13A)	-135.2(393)

Co(2A)-Co(1A)-C(13A)-O(13A)	-82.6(394)

C(15A)-Co(2A)-C(14A)-O(14A)	152.8(339)

C(16A)-Co(2A)-C(14A)-O(14A)	-103.0(340)

C(7A)-Co(2A)-C(14A)-O(14A)	-0.4(342)

C(8A)-Co(2A)-C(14A)-O(14A)	16.1(346)

Co(1A)-Co(2A)-C(14A)-O(14A)	51.6(341)

C(16A)-Co(2A)-C(15A)-O(15A)	126.4(439)

C(14A)-Co(2A)-C(15A)-O(15A)	-131.8(439)

C(7A)-Co(2A)-C(15A)-O(15A)	6.6(445)

C(8A)-Co(2A)-C(15A)-O(15A)	21.9(441)

Co(1A)-Co(2A)-C(15A)-O(15A)	-30.5(440)

C(15A)-Co(2A)-C(16A)-O(16A)	117.6(263)

C(14A)-Co(2A)-C(16A)-O(16A)	7.7(264)

C(7A)-Co(2A)-C(16A)-O(16A)	-98.0(264)

C(8A)-Co(2A)-C(16A)-O(16A)	-138.0(263)

Co(1A)-Co(2A)-C(16A)-O(16A)	-113.7(261)

C(21A)-Co(3A)-C(20A)-O(20A)	100.2(818)

C(22A)-Co(3A)-C(20A)-O(20A)	-0.6(819)

C(9A)-Co(3A)-C(20A)-O(20A)	-127.6(814)

C(10A)-Co(3A)-C(20A)-O(20A)	-106.2(818)

Co(4A)-Co(3A)-C(20A)-O(20A)	-159.0(817)

C(22A)-Co(3A)-C(21A)-O(21A)	-126.8(910)

C(20A)-Co(3A)-C(21A)-O(21A)	132.9(910)

C(9A)-Co(3A)-C(21A)-O(21A)	-21.1(911)

C(10A)-Co(3A)-C(21A)-O(21A)	-9.8(915)

Co(4A)-Co(3A)-C(21A)-O(21A)	30.3(911)

C(21A)-Co(3A)-C(22A)-O(22A)	-172.4(323)

C(20A)-Co(3A)-C(22A)-O(22A)	-64.9(323)

C(9A)-Co(3A)-C(22A)-O(22A)	86.4(324)

C(10A)-Co(3A)-C(22A)-O(22A)	46.7(324)

Co(4A)-Co(3A)-C(22A)-O(22A)	63.9(329)

C(25A)-Co(4A)-C(23A)-O(23A)	37.0(441)

C(24A)-Co(4A)-C(23A)-O(23A)	136.3(438)

C(9A)-Co(4A)-C(23A)-O(23A)	-72.6(440)

C(10A)-Co(4A)-C(23A)-O(23A)	-78.6(441)

Co(3A)-Co(4A)-C(23A)-O(23A)	-124.3(439)

C(23A)-Co(4A)-C(24A)-O(24A)	138.2(1000)

C(25A)-Co(4A)-C(24A)-O(24A)	-117.2(1000)

C(9A)-Co(4A)-C(24A)-O(24A)	6.2(1000)

C(10A)-Co(4A)-C(24A)-O(24A)	-18.7(1000)

Co(3A)-Co(4A)-C(24A)-O(24A)	33.0(1000)

C(23A)-Co(4A)-C(25A)-O(25A)	95.8(472)

C(24A)-Co(4A)-C(25A)-O(25A)	-12.6(473)

C(9A)-Co(4A)-C(25A)-O(25A)	-158.8(471)

C(10A)-Co(4A)-C(25A)-O(25A)	-120.6(472)

Co(3A)-Co(4A)-C(25A)-O(25A)	-120.9(469)

C(12B)-Co(1B)-Co(2B)-C(15B)	-102.7(8)

C(11B)-Co(1B)-Co(2B)-C(15B)	134.2(13)

C(13B)-Co(1B)-Co(2B)-C(15B)	8.5(8)

C(7B)-Co(1B)-Co(2B)-C(15B)	157.8(7)

C(8B)-Co(1B)-Co(2B)-C(15B)	108.0(7)

C(12B)-Co(1B)-Co(2B)-C(16B)	143.1(12)

C(11B)-Co(1B)-Co(2B)-C(16B)	19.9(16)

C(13B)-Co(1B)-Co(2B)-C(16B)	-105.7(12)

C(7B)-Co(1B)-Co(2B)-C(16B)	43.6(12)

C(8B)-Co(1B)-Co(2B)-C(16B)	-6.3(12)

C(12B)-Co(1B)-Co(2B)-C(14B)	6.2(8)

C(11B)-Co(1B)-Co(2B)-C(14B)	-116.9(13)

C(13B)-Co(1B)-Co(2B)-C(14B)	117.4(8)

C(7B)-Co(1B)-Co(2B)-C(14B)	-93.2(7)

C(8B)-Co(1B)-Co(2B)-C(14B)	-143.1(7)

C(12B)-Co(1B)-Co(2B)-C(7B)	99.5(7)

C(11B)-Co(1B)-Co(2B)-C(7B)	-23.6(13)

C(13B)-Co(1B)-Co(2B)-C(7B)	-149.3(7)

C(7B)-Co(1B)-Co(2B)-C(7B)	0.0

C(8B)-Co(1B)-Co(2B)-C(7B)	-49.9(6)

C(12B)-Co(1B)-Co(2B)-C(8B)	149.3(7)

C(11B)-Co(1B)-Co(2B)-C(8B)	26.2(12)

C(13B)-Co(1B)-Co(2B)-C(8B)	-99.4(7)

C(7B)-Co(1B)-Co(2B)-C(8B)	49.9(6)

C(8B)-Co(1B)-Co(2B)-C(8B)	0.0

C(21B)-Co(3B)-Co(4B)-C(24B)	5.4(16)

C(22B)-Co(3B)-Co(4B)-C(24B)	123.5(11)

C(20B)-Co(3B)-Co(4B)-C(24B)	-128.3(11)

C(9B)-Co(3B)-Co(4B)-C(24B)	-29.7(11)

C(10B)-Co(3B)-Co(4B)-C(24B)	20.4(11)

C(21B)-Co(3B)-Co(4B)-C(25B)	-119.7(13)

C(22B)-Co(3B)-Co(4B)-C(25B)	-1.6(7)

C(20B)-Co(3B)-Co(4B)-C(25B)	106.6(7)

C(9B)-Co(3B)-Co(4B)-C(25B)	-154.8(7)

C(10B)-Co(3B)-Co(4B)-C(25B)	-104.7(7)

C(21B)-Co(3B)-Co(4B)-C(23B)	133.0(13)

C(22B)-Co(3B)-Co(4B)-C(23B)	-109.0(7)

C(20B)-Co(3B)-Co(4B)-C(23B)	-0.8(7)

C(9B)-Co(3B)-Co(4B)-C(23B)	97.8(7)

C(10B)-Co(3B)-Co(4B)-C(23B)	147.9(7)

C(21B)-Co(3B)-Co(4B)-C(9B)	35.1(13)

C(22B)-Co(3B)-Co(4B)-C(9B)	153.2(7)

C(20B)-Co(3B)-Co(4B)-C(9B)	-98.6(7)

C(9B)-Co(3B)-Co(4B)-C(9B)	0.0

C(10B)-Co(3B)-Co(4B)-C(9B)	50.1(6)

C(21B)-Co(3B)-Co(4B)-C(10B)	-14.9(13)

C(22B)-Co(3B)-Co(4B)-C(10B)	103.1(7)

C(20B)-Co(3B)-Co(4B)-C(10B)	-148.7(7)

C(9B)-Co(3B)-Co(4B)-C(10B)	-50.1(6)

C(10B)-Co(3B)-Co(4B)-C(10B)	0.0

O(1B)-C(1B)-C(2B)-C(3B)	-63.0(16)

C(7B)-C(1B)-C(2B)-C(3B)	178.3(11)

C(6B)-C(1B)-C(2B)-C(3B)	57.9(14)

C(1B)-C(2B)-C(3B)-C(4B)	-37.5(17)

C(2B)-C(3B)-C(4B)-O(4B)	96.8(12)

C(2B)-C(3B)-C(4B)-C(9B)	-141.6(11)

C(2B)-C(3B)-C(4B)-C(5B)	-21.8(15)

O(4B)-C(4B)-C(5B)-C(6B)	-62.1(14)

C(3B)-C(4B)-C(5B)-C(6B)	60.5(14)

C(9B)-C(4B)-C(5B)-C(6B)	179.3(10)

O(1B)-C(1B)-C(6B)-C(5B)	102.0(12)

C(2B)-C(1B)-C(6B)-C(5B)	-18.4(14)

C(7B)-C(1B)-C(6B)-C(5B)	-138.3(11)

C(4B)-C(5B)-C(6B)-C(1B)	-40.4(15)

O(1B)-C(1B)-C(7B)-C(8B)	172.4(18)

C(2B)-C(1B)-C(7B)-C(8B)	-68.4(25)

C(6B)-C(1B)-C(7B)-C(8B)	51.8(25)

O(1B)-C(1B)-C(7B)-Co(1B)	-61.2(16)

C(2B)-C(1B)-C(7B)-Co(1B)	58.0(18)

C(6B)-C(1B)-C(7B)-Co(1B)	178.2(10)

O(1B)-C(1B)-C(7B)-Co(2B)	56.4(17)

C(2B)-C(1B)-C(7B)-Co(2B)	175.6(11)

C(6B)-C(1B)-C(7B)-Co(2B)	-64.2(17)

C(12B)-Co(1B)-C(7B)-C(8B)	-164.3(10)

C(11B)-Co(1B)-C(7B)-C(8B)	95.0(10)

C(13B)-Co(1B)-C(7B)-C(8B)	-21.6(14)

C(8B)-Co(1B)-C(7B)-C(8B)	0.000(1)

Co(2B)-Co(1B)-C(7B)-C(8B)	-74.3(8)

C(12B)-Co(1B)-C(7B)-C(1B)	47.1(15)

C(11B)-Co(1B)-C(7B)-C(1B)	-53.7(15)

C(13B)-Co(1B)-C(7B)-C(1B)	-170.2(13)

C(8B)-Co(1B)-C(7B)-C(1B)	-148.6(18)

Co(2B)-Co(1B)-C(7B)-C(1B)	137.1(15)

C(12B)-Co(1B)-C(7B)-Co(2B)	-90.0(6)

C(11B)-Co(1B)-C(7B)-Co(2B)	169.3(6)

C(13B)-Co(1B)-C(7B)-Co(2B)	52.7(11)

C(8B)-Co(1B)-C(7B)-Co(2B)	74.3(8)

Co(2B)-Co(1B)-C(7B)-Co(2B)	0.0

C(15B)-Co(2B)-C(7B)-C(8B)	39.6(15)

C(16B)-Co(2B)-C(7B)-C(8B)	-83.6(10)

C(14B)-Co(2B)-C(7B)-C(8B)	173.7(10)

C(8B)-Co(2B)-C(7B)-C(8B)	0.0

Co(1B)-Co(2B)-C(7B)-C(8B)	76.2(9)

C(15B)-Co(2B)-C(7B)-C(1B)	-176.3(13)

C(16B)-Co(2B)-C(7B)-C(1B)	60.5(15)

C(14B)-Co(2B)-C(7B)-C(1B)	-42.2(15)

C(8B)-Co(2B)-C(7B)-C(1B)	144.1(19)

Co(1B)-Co(2B)-C(7B)-C(1B)	-139.7(15)

C(15B)-Co(2B)-C(7B)-Co(1B)	-36.6(12)

C(16B)-Co(2B)-C(7B)-Co(1B)	-159.8(6)

C(14B)-Co(2B)-C(7B)-Co(1B)	97.5(7)

C(8B)-Co(2B)-C(7B)-Co(1B)	-76.2(9)

Co(1B)-Co(2B)-C(7B)-Co(1B)	0.0

C(1B)-C(7B)-C(8B)-Si(1B)	8.3(40)

Co(1B)-C(7B)-C(8B)-Si(1B)	-134.9(23)

Co(2B)-C(7B)-C(8B)-Si(1B)	143.0(24)

C(1B)-C(7B)-C(8B)-Co(2B)	-134.7(21)

Co(1B)-C(7B)-C(8B)-Co(2B)	82.1(4)

Co(2B)-C(7B)-C(8B)-Co(2B)	0.0

C(1B)-C(7B)-C(8B)-Co(1B)	143.2(21)

Co(1B)-C(7B)-C(8B)-Co(1B)	0.000(1)

Co(2B)-C(7B)-C(8B)-Co(1B)	-82.1(4)

C(18B)-Si(1B)-C(8B)-C(7B)	-55.6(26)

C(17B)-Si(1B)-C(8B)-C(7B)	-176.5(23)

C(19B)-Si(1B)-C(8B)-C(7B)	62.9(25)

C(18B)-Si(1B)-C(8B)-Co(2B)	74.3(12)

C(17B)-Si(1B)-C(8B)-Co(2B)	-46.7(13)

C(19B)-Si(1B)-C(8B)-Co(2B)	-167.2(10)

C(18B)-Si(1B)-C(8B)-Co(1B)	-175.2(10)

C(17B)-Si(1B)-C(8B)-Co(1B)	63.8(12)

C(19B)-Si(1B)-C(8B)-Co(1B)	-56.7(12)

C(15B)-Co(2B)-C(8B)-C(7B)	-155.1(10)

C(16B)-Co(2B)-C(8B)-C(7B)	105.5(10)

C(14B)-Co(2B)-C(8B)-C(7B)	-9.4(15)

C(7B)-Co(2B)-C(8B)-C(7B)	0.0

Co(1B)-Co(2B)-C(8B)-C(7B)	-71.5(9)

C(15B)-Co(2B)-C(8B)-Si(1B)	49.4(13)

C(16B)-Co(2B)-C(8B)-Si(1B)	-50.0(12)

C(14B)-Co(2B)-C(8B)-Si(1B)	-164.9(11)

C(7B)-Co(2B)-C(8B)-Si(1B)	-155.5(17)

Co(1B)-Co(2B)-C(8B)-Si(1B)	133.0(12)

C(15B)-Co(2B)-C(8B)-Co(1B)	-83.7(7)

C(16B)-Co(2B)-C(8B)-Co(1B)	177.0(6)

C(14B)-Co(2B)-C(8B)-Co(1B)	62.1(11)

C(7B)-Co(2B)-C(8B)-Co(1B)	71.5(9)

Co(1B)-Co(2B)-C(8B)-Co(1B)	0.0

C(12B)-Co(1B)-C(8B)-C(7B)	23.7(14)

C(11B)-Co(1B)-C(8B)-C(7B)	-94.4(10)

C(13B)-Co(1B)-C(8B)-C(7B)	166.2(9)

C(7B)-Co(1B)-C(8B)-C(7B)	0.000(2)

Co(2B)-Co(1B)-C(8B)-C(7B)	73.8(8)

C(12B)-Co(1B)-C(8B)-Si(1B)	175.3(9)

C(11B)-Co(1B)-C(8B)-Si(1B)	57.2(11)

C(13B)-Co(1B)-C(8B)-Si(1B)	-42.2(12)

C(7B)-Co(1B)-C(8B)-Si(1B)	151.6(15)

Co(2B)-Co(1B)-C(8B)-Si(1B)	-134.6(11)

C(12B)-Co(1B)-C(8B)-Co(2B)	-50.1(11)

C(11B)-Co(1B)-C(8B)-Co(2B)	-168.1(6)

C(13B)-Co(1B)-C(8B)-Co(2B)	92.4(6)

C(7B)-Co(1B)-C(8B)-Co(2B)	-73.8(8)

Co(2B)-Co(1B)-C(8B)-Co(2B)	0.0

O(4B)-C(4B)-C(9B)-C(10B)	-171.3(19)

C(3B)-C(4B)-C(9B)-C(10B)	64.6(24)

C(5B)-C(4B)-C(9B)-C(10B)	-54.0(26)

O(4B)-C(4B)-C(9B)-Co(3B)	64.4(16)

C(3B)-C(4B)-C(9B)-Co(3B)	-59.7(15)

C(5B)-C(4B)-C(9B)-Co(3B)	-178.3(10)

O(4B)-C(4B)-C(9B)-Co(4B)	-51.4(15)

C(3B)-C(4B)-C(9B)-Co(4B)	-175.5(9)

C(5B)-C(4B)-C(9B)-Co(4B)	65.9(14)

C(21B)-Co(3B)-C(9B)-C(10B)	-87.7(10)

C(22B)-Co(3B)-C(9B)-C(10B)	31.3(14)

C(20B)-Co(3B)-C(9B)-C(10B)	168.9(10)

C(10B)-Co(3B)-C(9B)-C(10B)	0.000(2)

Co(4B)-Co(3B)-C(9B)-C(10B)	76.3(9)

C(21B)-Co(3B)-C(9B)-C(4B)	60.7(14)

C(22B)-Co(3B)-C(9B)-C(4B)	179.8(11)

C(20B)-Co(3B)-C(9B)-C(4B)	-42.6(14)

C(10B)-Co(3B)-C(9B)-C(4B)	148.5(18)

Co(4B)-Co(3B)-C(9B)-C(4B)	-135.2(15)

C(21B)-Co(3B)-C(9B)-Co(4B)	-164.1(6)

C(22B)-Co(3B)-C(9B)-Co(4B)	-45.0(11)

C(20B)-Co(3B)-C(9B)-Co(4B)	92.6(6)

C(10B)-Co(3B)-C(9B)-Co(4B)	-76.3(9)

Co(4B)-Co(3B)-C(9B)-Co(4B)	0.0

C(24B)-Co(4B)-C(9B)-C(10B)	89.1(9)

C(25B)-Co(4B)-C(9B)-C(10B)	-34.3(13)

C(23B)-Co(4B)-C(9B)-C(10B)	-169.2(8)

C(10B)-Co(4B)-C(9B)-C(10B)	0.000(2)

Co(3B)-Co(4B)-C(9B)-C(10B)	-75.8(8)

C(24B)-Co(4B)-C(9B)-C(4B)	-57.7(12)

C(25B)-Co(4B)-C(9B)-C(4B)	178.9(11)

C(23B)-Co(4B)-C(9B)-C(4B)	44.0(12)

C(10B)-Co(4B)-C(9B)-C(4B)	-146.8(15)

Co(3B)-Co(4B)-C(9B)-C(4B)	137.4(13)

C(24B)-Co(4B)-C(9B)-Co(3B)	164.9(6)

C(25B)-Co(4B)-C(9B)-Co(3B)	41.5(10)

C(23B)-Co(4B)-C(9B)-Co(3B)	-93.4(6)

C(10B)-Co(4B)-C(9B)-Co(3B)	75.8(8)

Co(3B)-Co(4B)-C(9B)-Co(3B)	0.0

C(4B)-C(9B)-C(10B)-Si(2B)	1.2(43)

Co(3B)-C(9B)-C(10B)-Si(2B)	141.6(25)

Co(4B)-C(9B)-C(10B)-Si(2B)	-134.9(25)

C(4B)-C(9B)-C(10B)-Co(3B)	-140.4(22)

Co(3B)-C(9B)-C(10B)-Co(3B)	0.000(1)

Co(4B)-C(9B)-C(10B)-Co(3B)	83.5(3)

C(4B)-C(9B)-C(10B)-Co(4B)	136.0(22)

Co(3B)-C(9B)-C(10B)-Co(4B)	-83.5(3)

Co(4B)-C(9B)-C(10B)-Co(4B)	0.0

C(26B)-Si(2B)-C(10B)-C(9B)	-85.0(27)

C(28B)-Si(2B)-C(10B)-C(9B)	152.9(25)

C(27B)-Si(2B)-C(10B)-C(9B)	32.7(28)

C(26B)-Si(2B)-C(10B)-Co(3B)	44.4(11)

C(28B)-Si(2B)-C(10B)-Co(3B)	-77.6(11)

C(27B)-Si(2B)-C(10B)-Co(3B)	162.2(9)

C(26B)-Si(2B)-C(10B)-Co(4B)	153.1(8)

C(28B)-Si(2B)-C(10B)-Co(4B)	31.1(11)

C(27B)-Si(2B)-C(10B)-Co(4B)	-89.1(9)

C(21B)-Co(3B)-C(10B)-C(9B)	101.9(10)

C(22B)-Co(3B)-C(10B)-C(9B)	-160.1(10)

C(20B)-Co(3B)-C(10B)-C(9B)	-17.2(15)

C(9B)-Co(3B)-C(10B)-C(9B)	0.000(2)

Co(4B)-Co(3B)-C(10B)-C(9B)	-71.2(8)

C(21B)-Co(3B)-C(10B)-Si(2B)	-55.7(12)

C(22B)-Co(3B)-C(10B)-Si(2B)	42.3(12)

C(20B)-Co(3B)-C(10B)-Si(2B)	-174.8(9)

C(9B)-Co(3B)-C(10B)-Si(2B)	-157.6(16)

Co(4B)-Co(3B)-C(10B)-Si(2B)	131.2(12)

C(21B)-Co(3B)-C(10B)-Co(4B)	173.1(6)

C(22B)-Co(3B)-C(10B)-Co(4B)	-88.9(6)

C(20B)-Co(3B)-C(10B)-Co(4B)	54.0(11)

C(9B)-Co(3B)-C(10B)-Co(4B)	71.2(8)

Co(4B)-Co(3B)-C(10B)-Co(4B)	0.0

C(24B)-Co(4B)-C(10B)-C(9B)	-98.3(9)

C(25B)-Co(4B)-C(10B)-C(9B)	158.1(9)

C(23B)-Co(4B)-C(10B)-C(9B)	16.6(13)

C(9B)-Co(4B)-C(10B)-C(9B)	0.000(2)

Co(3B)-Co(4B)-C(10B)-C(9B)	71.3(8)

C(24B)-Co(4B)-C(10B)-Si(2B)	56.9(10)

C(25B)-Co(4B)-C(10B)-Si(2B)	-46.7(10)

C(23B)-Co(4B)-C(10B)-Si(2B)	171.8(8)

C(9B)-Co(4B)-C(10B)-Si(2B)	155.2(14)

Co(3B)-Co(4B)-C(10B)-Si(2B)	-133.5(10)

C(24B)-Co(4B)-C(10B)-Co(3B)	-169.6(6)

C(25B)-Co(4B)-C(10B)-Co(3B)	86.8(6)

C(23B)-Co(4B)-C(10B)-Co(3B)	-54.7(9)

C(9B)-Co(4B)-C(10B)-Co(3B)	-71.3(8)

Co(3B)-Co(4B)-C(10B)-Co(3B)	0.0

C(12B)-Co(1B)-C(11B)-O(11B)	-166.3(399)

C(13B)-Co(1B)-C(11B)-O(11B)	83.3(400)

C(7B)-Co(1B)-C(11B)-O(11B)	-62.1(400)

C(8B)-Co(1B)-C(11B)-O(11B)	-22.2(401)

Co(2B)-Co(1B)-C(11B)-O(11B)	-43.2(405)

C(11B)-Co(1B)-C(12B)-O(12B)	159.3(321)

C(13B)-Co(1B)-C(12B)-O(12B)	-101.8(321)

C(7B)-Co(1B)-C(12B)-O(12B)	54.3(322)

C(8B)-Co(1B)-C(12B)-O(12B)	39.3(326)

Co(2B)-Co(1B)-C(12B)-O(12B)	1.8(323)

C(12B)-Co(1B)-C(13B)-O(13B)	127.4(207)

C(11B)-Co(1B)-C(13B)-O(13B)	-132.5(207)

C(7B)-Co(1B)-C(13B)-O(13B)	-13.7(214)

C(8B)-Co(1B)-C(13B)-O(13B)	-27.4(209)

Co(2B)-Co(1B)-C(13B)-O(13B)	25.8(208)

C(15B)-Co(2B)-C(14B)-O(14B)	-173.3(1000)

C(16B)-Co(2B)-C(14B)-O(14B)	-74.2(515)

C(7B)-Co(2B)-C(14B)-O(14B)	34.9(515)

C(8B)-Co(2B)-C(14B)-O(14B)	40.8(519)

Co(1B)-Co(2B)-C(14B)-O(14B)	86.5(515)

C(16B)-Co(2B)-C(15B)-O(15B)	51.7(208)

C(14B)-Co(2B)-C(15B)-O(15B)	152.9(206)

C(7B)-Co(2B)-C(15B)-O(15B)	-74.7(210)

C(8B)-Co(2B)-C(15B)-O(15B)	-50.1(209)

Co(1B)-Co(2B)-C(15B)-O(15B)	-102.3(207)

C(15B)-Co(2B)-C(16B)-O(16B)	55.6(230)

C(14B)-Co(2B)-C(16B)-O(16B)	-52.8(230)

C(7B)-Co(2B)-C(16B)-O(16B)	-156.3(228)

C(8B)-Co(2B)-C(16B)-O(16B)	164.8(229)

Co(1B)-Co(2B)-C(16B)-O(16B)	169.8(221)

C(21B)-Co(3B)-C(20B)-O(20B)	-82.0(245)

C(22B)-Co(3B)-C(20B)-O(20B)	-179.3(1000)

C(9B)-Co(3B)-C(20B)-O(20B)	26.9(246)

C(10B)-Co(3B)-C(20B)-O(20B)	37.8(250)

Co(4B)-Co(3B)-C(20B)-O(20B)	78.5(245)

C(22B)-Co(3B)-C(21B)-O(21B)	-62.2(656)

C(20B)-Co(3B)-C(21B)-O(21B)	-169.3(655)

C(9B)-Co(3B)-C(21B)-O(21B)	84.2(656)

C(10B)-Co(3B)-C(21B)-O(21B)	44.7(656)

Co(4B)-Co(3B)-C(21B)-O(21B)	56.7(661)

C(21B)-Co(3B)-C(22B)-O(22B)	28.6(255)

C(20B)-Co(3B)-C(22B)-O(22B)	129.2(254)

C(9B)-Co(3B)-C(22B)-O(22B)	-93.9(255)

C(10B)-Co(3B)-C(22B)-O(22B)	-74.2(255)

Co(4B)-Co(3B)-C(22B)-O(22B)	-127.4(254)

C(24B)-Co(4B)-C(23B)-O(23B)	45.6(268)

C(25B)-Co(4B)-C(23B)-O(23B)	148.9(266)

C(9B)-Co(4B)-C(23B)-O(23B)	-59.0(268)

C(10B)-Co(4B)-C(23B)-O(23B)	-69.4(269)

Co(3B)-Co(4B)-C(23B)-O(23B)	-110.1(267)

C(25B)-Co(4B)-C(24B)-O(24B)	163.8(271)

C(23B)-Co(4B)-C(24B)-O(24B)	-88.8(271)

C(9B)-Co(4B)-C(24B)-O(24B)	16.5(273)

C(10B)-Co(4B)-C(24B)-O(24B)	55.3(272)

Co(3B)-Co(4B)-C(24B)-O(24B)	39.3(278)

C(24B)-Co(4B)-C(25B)-O(25B)	113.9(821)

C(23B)-Co(4B)-C(25B)-O(25B)	12.1(823)

C(9B)-Co(4B)-C(25B)-O(25B)	-122.2(819)

C(10B)-Co(4B)-C(25B)-O(25B)	-143.5(820)

Co(3B)-Co(4B)-C(25B)-O(25B)	-91.4(821)

_____________________________________________________________________________________

Table R1:  Crystal data and structure refinement for 150.

Empirical formula 	C22 H28 Co2 O8 Si2

Formula weight 	594.48

Temperature 	148(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P21/c

Unit cell dimensions	a = 12.7652(6) Å	(= 90°.

b = 11.3770(5) Å	(= 98.176(2)°.

c = 18.4035(4) Å	(= 90°.

Volume	2645.6(2) Å3

Z	4

Density (calculated)	1.493 Mg/m3

Absorption coefficient	1.387 mm-1

F(000)	1224

Crystal size	0.14 x 0.24 x 0.34 mm3

( range for data collection	1.61 to 25.00°.

Index ranges	-15(h(16, -12(k(14, -23(l(23

Reflections collected	19761

Independent reflections	4666 [R(int) = 0.0496]

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	4662 / 0 / 392

Goodness-of-fit on F2	0.929

Final R indices [I>2((I)]	R1 = 0.0289, wR2 = 0.0506

R indices (all data)	R1 = 0.0548, wR2 = 0.0553

Extinction coefficient	0.00043(11)

Largest diff. peak and hole	0.269 and -0.278 e.Å-3

Max. and Min effective transmission	0.745773 and 0.668449

Table R2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 150.  U(eq) is defined as one third of the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	2745(1)	5999(1)	1418(1)	18(1)

Co(2)	3900(1)	7019(1)	2416(1)	18(1)

Si(1)	2513(1)	9068(1)	1204(1)	19(1)

Si(2)	-2360(1)	7716(1)	5232(1)	20(1)

O(1)	1436(2)	5600(2)	2946(1)	28(1)

C(1)	1499(2)	6798(2)	2720(1)	18(1)

C(2)	418(2)	7197(2)	2333(1)	18(1)

C(3)	-435(2)	7154(2)	2837(1)	19(1)

O(4)	-67(2)	9090(2)	3290(1)	28(1)

C(4)	-129(2)	7877(2)	3532(1)	20(1)

C(5)	956(2)	7477(3)	3917(1)	24(1)

C(6)	1803(2)	7526(3)	3416(1)	23(1)

C(7)	2331(2)	6951(2)	2226(1)	16(1)

C(8)	2674(2)	7678(2)	1737(1)	16(1)

C(9)	3380(2)	8999(3)	474(2)	29(1)

C(10)	1098(2)	9237(3)	793(2)	26(1)

C(11)	2887(2)	10312(2)	1845(2)	27(1)

O(12)	668(1)	5810(2)	516(1)	29(1)

C(12)	1488(2)	5857(2)	860(1)	21(1)

C(13)	3609(2)	5994(2)	708(1)	28(1)

O(13)	4129(2)	5976(2)	258(1)	46(1)

O(14)	3031(2)	3646(2)	2099(1)	36(1)

C(14)	2907(2)	4538(2)	1824(1)	24(1)

O(15)	5761(2)	7141(2)	1630(1)	35(1)

C(15)	5051(2)	7094(2)	1938(1)	24(1)

C(16)	4131(2)	5844(2)	3093(1)	26(1)

O(16)	4252(2)	5129(2)	3526(1)	42(1)

O(17)	4389(2)	9060(2)	3381(1)	38(1)

C(17)	4199(2)	8266(2)	3008(1)	25(1)

C(18)	-904(2)	7790(2)	4056(1)	22(1)

C(19)	-1475(2)	7747(2)	4519(1)	21(1)

C(20)	-3732(2)	7564(3)	4760(2)	28(1)

C(21)	-2171(3)	9107(3)	5769(2)	29(1)

C(22)	-1974(3)	6468(3)	5861(2)	30(1)

________________________________________________________________________________

Table R3:  Bond lengths [Å] and angles [°] for 150.

____________________________________________________________________________________

Co(1)-C(12) 	1.785(3)

Co(1)-C(14) 	1.822(3)

Co(1)-C(13) 	1.827(3)

Co(1)-C(7) 	1.971(2)

Co(1)-C(8) 	2.005(2)

Co(1)-Co(2) 	2.4737(4)

Co(2)-C(17) 	1.797(3)

Co(2)-C(15) 	1.819(3)

Co(2)-C(16) 	1.823(3)

Co(2)-C(7) 	1.984(2)

Co(2)-C(8) 	2.003(2)

Si(1)-C(8) 	1.857(2)

Si(1)-C(9) 	1.859(3)

Si(1)-C(11) 	1.861(3)

Si(1)-C(10) 	1.866(3)

Si(2)-C(19) 	1.848(3)

Si(2)-C(20) 	1.849(3)

Si(2)-C(22) 	1.854(3)

Si(2)-C(21) 	1.864(3)

O(1)-C(1) 	1.431(3)

C(1)-C(7) 	1.504(3)

C(1)-C(6) 	1.528(3)

C(1)-C(2) 	1.528(3)

C(2)-C(3) 	1.528(3)

C(3)-C(4) 	1.524(3)

O(4)-C(4) 	1.456(3)

C(4)-C(18) 	1.479(3)

C(4)-C(5) 	1.533(3)

C(5)-C(6) 	1.518(4)

C(7)-C(8) 	1.341(3)

O(12)-C(12) 	1.145(3)

C(13)-O(13) 	1.132(3)

O(14)-C(14) 	1.135(3)

O(15)-C(15) 	1.137(3)

C(16)-O(16) 	1.134(3)

O(17)-C(17) 	1.140(3)

C(18)-C(19) 	1.200(3)

C(12)-Co(1)-C(14)	101.18(11)

C(12)-Co(1)-C(13)	99.95(11)

C(14)-Co(1)-C(13)	104.27(12)

C(12)-Co(1)-C(7)	99.66(10)

C(14)-Co(1)-C(7)	102.63(10)

C(13)-Co(1)-C(7)	142.69(11)

C(12)-Co(1)-C(8)	100.38(10)

C(14)-Co(1)-C(8)	139.16(10)

C(13)-Co(1)-C(8)	105.62(11)

C(7)-Co(1)-C(8)	39.41(9)

C(12)-Co(1)-Co(2)	149.44(8)

C(14)-Co(1)-Co(2)	95.90(7)

C(13)-Co(1)-Co(2)	100.14(8)

C(7)-Co(1)-Co(2)	51.52(7)

C(8)-Co(1)-Co(2)	51.86(6)

C(17)-Co(2)-C(15)	98.06(12)

C(17)-Co(2)-C(16)	99.43(11)

C(15)-Co(2)-C(16)	107.58(11)

C(17)-Co(2)-C(7)	105.05(11)

C(15)-Co(2)-C(7)	141.35(10)

C(16)-Co(2)-C(7)	98.78(11)

C(17)-Co(2)-C(8)	99.35(10)

C(15)-Co(2)-C(8)	107.08(10)

C(16)-Co(2)-C(8)	137.46(11)

C(7)-Co(2)-C(8)	39.30(9)

C(17)-Co(2)-Co(1)	150.88(8)

C(15)-Co(2)-Co(1)	95.73(8)

C(16)-Co(2)-Co(1)	100.65(8)

C(7)-Co(2)-Co(1)	51.05(6)

C(8)-Co(2)-Co(1)	51.92(6)

C(8)-Si(1)-C(9)	108.26(13)

C(8)-Si(1)-C(11)	108.21(11)

C(9)-Si(1)-C(11)	111.38(14)

C(8)-Si(1)-C(10)	109.29(12)

C(9)-Si(1)-C(10)	110.66(13)

C(11)-Si(1)-C(10)	108.99(13)

C(19)-Si(2)-C(20)	107.62(12)

C(19)-Si(2)-C(22)	108.84(13)

C(20)-Si(2)-C(22)	111.76(15)

C(19)-Si(2)-C(21)	108.33(13)

C(20)-Si(2)-C(21)	111.76(14)

C(22)-Si(2)-C(21)	108.44(14)

O(1)-C(1)-C(7)	111.0(2)

O(1)-C(1)-C(6)	106.9(2)

C(7)-C(1)-C(6)	109.1(2)

O(1)-C(1)-C(2)	109.5(2)

C(7)-C(1)-C(2)	110.7(2)

C(6)-C(1)-C(2)	109.5(2)

C(3)-C(2)-C(1)	112.5(2)

C(4)-C(3)-C(2)	111.9(2)

O(4)-C(4)-C(18)	109.5(2)

O(4)-C(4)-C(3)	105.9(2)

C(18)-C(4)-C(3)	113.3(2)

O(4)-C(4)-C(5)	109.8(2)

C(18)-C(4)-C(5)	108.8(2)

C(3)-C(4)-C(5)	109.5(2)

C(6)-C(5)-C(4)	112.5(2)

C(5)-C(6)-C(1)	111.8(2)

C(8)-C(7)-C(1)	143.4(2)

C(8)-C(7)-Co(1)	71.65(14)

C(1)-C(7)-Co(1)	132.9(2)

C(8)-C(7)-Co(2)	71.11(15)

C(1)-C(7)-Co(2)	132.9(2)

Co(1)-C(7)-Co(2)	77.42(9)

C(7)-C(8)-Si(1)	149.1(2)

C(7)-C(8)-Co(2)	69.59(13)

Si(1)-C(8)-Co(2)	131.79(13)

C(7)-C(8)-Co(1)	68.94(13)

Si(1)-C(8)-Co(1)	131.52(12)

Co(2)-C(8)-Co(1)	76.22(8)

O(12)-C(12)-Co(1)	177.0(2)

O(13)-C(13)-Co(1)	178.5(2)

O(14)-C(14)-Co(1)	177.5(2)

O(15)-C(15)-Co(2)	179.1(2)

O(16)-C(16)-Co(2)	177.9(3)

O(17)-C(17)-Co(2)	179.7(2)

C(19)-C(18)-C(4)	175.3(3)

C(18)-C(19)-Si(2)	178.7(2)

____________________________________________________________________________________

Table R4:  Anisotropic displacement parameters (Å2 x 103) for 150.  The anisotropic

displacement factor exponent takes the form: -2(2[ h2a*2U11 + ... + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	17(1) 	18(1)	20(1) 	-2(1)	6(1) 	-1(1)

Co(2)	14(1) 	21(1)	20(1) 	0(1)	3(1) 	1(1)

Si(1)	19(1) 	18(1)	21(1) 	2(1)	4(1) 	0(1)

Si(2)	18(1) 	23(1)	19(1) 	0(1)	6(1) 	1(1)

O(1)	32(1) 	21(1)	35(1) 	8(1)	15(1) 	4(1)

C(1)	15(1) 	20(2)	20(1) 	4(1)	4(1) 	3(1)

C(2)	16(2) 	20(2)	17(1) 	-1(1)	4(1) 	-2(1)

C(3)	15(2) 	22(2)	21(1) 	1(1)	5(1) 	1(1)

O(4)	31(1) 	22(1)	35(1) 	-5(1)	12(1) 	-2(1)

C(4)	16(2) 	21(1)	23(1) 	0(1)	8(1) 	1(1)

C(5)	20(2) 	35(2)	17(1) 	-7(1)	5(1) 	1(1)

C(6)	17(2) 	34(2)	19(1) 	-1(1)	2(1) 	3(1)

C(7)	15(1) 	15(1)	17(1) 	-3(1)	1(1) 	4(1)

C(8)	12(1) 	18(1)	17(1) 	-3(1)	1(1) 	-1(1)

C(9)	30(2) 	29(2)	30(2) 	7(1)	10(1) 	-2(2)

C(10)	23(2) 	26(2)	27(2) 	7(1)	-1(1) 	0(1)

C(11)	27(2) 	21(2)	31(2) 	1(1)	3(1) 	1(1)

O(12)	27(1) 	32(1)	27(1) 	2(1)	-2(1) 	-4(1)

C(12)	30(2) 	15(1)	19(1) 	1(1)	12(1) 	-2(1)

C(13)	29(2) 	25(2)	32(2) 	-12(1)	8(1) 	-9(1)

O(13)	47(1) 	54(1)	46(1) 	-19(1)	33(1) 	-18(1)

O(14)	41(1) 	22(1)	43(1) 	5(1)	-4(1) 	0(1)

C(14)	20(2) 	27(2)	25(2) 	-6(1)	3(1) 	0(1)

O(15)	21(1) 	50(1)	38(1) 	-3(1)	13(1) 	-4(1)

C(15)	23(2) 	25(2)	24(2) 	0(1)	0(1) 	-1(1)

C(16)	15(2) 	32(2)	32(2) 	-1(1)	2(1) 	-1(1)

O(16)	37(1) 	43(1)	44(1) 	22(1)	-2(1) 	0(1)

O(17)	38(1) 	36(1)	38(1) 	-15(1)	-6(1) 	-1(1)

C(17)	15(2) 	34(2)	26(2) 	6(1)	-2(1) 	2(1)

C(18)	19(2) 	22(2)	24(1) 	-4(1)	3(1) 	1(1)

C(19)	18(2) 	22(2)	22(1) 	-1(1)	3(1) 	1(1)

C(20)	22(2) 	33(2)	29(2) 	-2(1)	9(1) 	1(1)

C(21)	29(2) 	32(2)	28(2) 	-2(1)	9(1) 	-3(2)

C(22)	29(2) 	32(2)	30(2) 	3(1)	6(1) 	4(2)

______________________________________________________________________________

Table R5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 103)

for 150.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1A)	1218(26)	5256(27)	2694(16)	42

H(2A)	217(18)	6685(19)	1885(12)	21

H(2B)	482(18)	7971(20)	2171(11)	21

H(3A)	-555(18)	6354(20)	2997(12)	23

H(3B)	-1071(20)	7456(19)	2597(12)	23

H(4A)	167(26)	9372(26)	3578(15)	43

H(5A)	892(19)	6644(21)	4095(12)	28

H(5B)	1147(19)	7943(20)	4326(13)	28

H(6A)	1928(19)	8371(21)	3265(12)	28

H(6B)	2397(20)	7233(20)	3671(12)	28

H(9A)	3127(21)	8436(23)	104(14)	44

H(9B)	3410(20)	9740(24)	220(13)	44

H(9C)	4051(22)	8803(23)	655(14)	44

H(10A)	809(21)	8568(23)	542(13)	39

H(10B)	676(21)	9359(22)	1190(14)	39

H(10C)	1016(21)	9859(23)	475(13)	39

H(11A)	3654(22)	10308(21)	2042(13)	40

H(11B)	2698(20)	11036(23)	1605(13)	40

H(11C)	2549(21)	10267(22)	2255(14)	40

H(20A)	-3847(21)	6942(23)	4410(14)	42

H(20B)	-4187(23)	7463(22)	5093(15)	42

H(20C)	-3986(21)	8317(23)	4496(13)	42

H(21A)	-1554(22)	9072(24)	6046(14)	44

H(21B)	-2266(21)	9764(23)	5465(14)	44

H(21C)	-2657(22)	9186(23)	6088(14)	44

H(22A)	-1284(23)	6546(23)	6102(14)	45

H(22B)	-2445(22)	6436(23)	6210(14)	45

H(22C)	-1995(21)	5723(24)	5607(13)	45

________________________________________________________________________________

Table S1:  Crystal data and structure refinement for 151.

Empirical formula 	C28 H26 Co4 O13 Si2

Formula weight 	862.39

Temperature 	173(2) K

Wavelength 	0.71073 Å

Crystal system 	Monoclinic

Space group 	P2(1)/n

Unit cell dimensions	a = 16.825(5) Å	(= 90°.

b = 23.538(7) Å	(= 91.089(7)°.

c = 18.008(5) Å	( = 90°.

Volume	7130(4) Å3

Z	8

Density (calculated)	1.607 Mg/m3

Absorption coefficient	1.955 mm-1

F(000)	3472

Crystal size	0.25 x 0.15 x 0.10 mm3

( range for data collection	1.42 to 21.50°.

Index ranges	-16(h(17, -24(k(24, -10(l(18

Reflections collected	28401

Independent reflections	8189 [R(int) = 0.1945]

Completeness to ( = 21.50°	100.0 %

Absorption correction	SADABS

Refinement method	Full-matrix least-squares on F2

Data / restraints / parameters	8189 / 0 / 570

Goodness-of-fit on F2	1.026

Final R indices [I>2((I)]	R1 = 0.0904, wR2 = 0.1836

R indices (all data)	R1 = 0.1941, wR2 = 0.2226

Extinction coefficient	0.00084(10)

Largest diff. peak and hole	1.270 and -0.876 e.Å-3

Ratio of min/max apparent transmission  	0.184008

Table S2:  Atomic coordinates ( x 104) and equivalent isotropic displacement parameters (Å2 x 103)

for 151.  U(eq) is defined as one third of  the trace of the orthogonalized Uij tensor.

________________________________________________________________________________

x	y	z	U(eq)

________________________________________________________________________________

Co(1)	2284(1)	2102(1)	-1119(1)	18(1)

Co(2)	2326(1)	3128(1)	-836(1)	20(1)

Co(3)	-2465(1)	2181(1)	713(1)	19(1)

Co(4)	-2473(1)	3223(1)	544(1)	19(1)

Si(1)	2872(3)	2320(2)	736(3)	26(1)

Si(2)	-3044(3)	2527(2)	-1111(3)	21(1)

O(1)	555(15)	1915(11)	101(13)	209(11)

C(1)	744(10)	2535(7)	-307(9)	31(5)

C(2)	167(10)	2511(7)	-938(9)	42(5)

C(3)	-692(14)	2534(9)	-746(13)	76(8)

C(4)	-905(11)	2633(7)	-48(10)	33(5)

C(5)	-375(11)	2776(8)	525(10)	49(6)

C(6)	451(11)	2809(8)	363(10)	53(6)

C(7)	1613(9)	2538(6)	-478(8)	15(4)

C(8)	2298(9)	2492(6)	-130(8)	13(4)

C(9)	2519(10)	1605(6)	1074(9)	31(5)

C(10)	2634(10)	2885(7)	1439(9)	41(5)

C(11)	3947(10)	2309(8)	534(10)	50(6)

O(12)	1823(7)	955(5)	-656(6)	44(4)

C(12)	2002(10)	1391(7)	-837(9)	26(5)

O(13)	1451(7)	2152(5)	-2567(6)	42(4)

C(13)	1787(10)	2121(7)	-2011(10)	23(5)

O(14)	3992(7)	1970(5)	-1444(6)	42(3)

C(14)	3335(11)	2012(7)	-1326(9)	30(5)

O(15)	1577(7)	3480(4)	-2236(6)	43(4)

C(15)	1867(10)	3365(7)	-1665(10)	33(5)

O(16)	1989(7)	4081(5)	159(6)	42(4)

C(16)	2127(11)	3727(8)	-231(10)	32(5)

O(17)	4038(7)	3354(5)	-1050(7)	46(4)

C(17)	3382(11)	3272(7)	-964(9)	22(4)

C(18)	-1769(10)	2655(6)	107(8)	19(4)

C(19)	-2471(9)	2615(6)	-229(8)	21(4)

C(20)	-2729(10)	1827(6)	-1508(9)	31(5)

C(21)	-2785(10)	3123(7)	-1749(9)	37(5)

C(22)	-4140(9)	2529(6)	-955(9)	29(5)

O(23)	-1651(7)	2168(5)	2174(6)	39(3)

C(23)	-1954(11)	2184(7)	1591(11)	38(5)

O(24)	-2062(8)	1058(5)	125(7)	56(4)

C(24)	-2194(11)	1490(8)	340(10)	35(5)

O(25)	-4166(7)	1977(5)	1046(7)	46(4)

C(25)	-3520(12)	2048(7)	932(9)	33(5)

O(26)	-4193(7)	3408(5)	773(6)	41(4)

C(26)	-3549(11)	3345(7)	703(9)	24(5)

O(27)	-2087(8)	4227(5)	-330(7)	53(4)

C(27)	-2242(11)	3828(8)	-4(10)	33(5)

O(28)	-1646(7)	3524(5)	1946(6)	37(3)

C(28)	-1959(10)	3439(7)	1411(9)	22(4)

Co(1A)	4869(1)	483(1)	1639(1)	21(1)

Co(2A)	4902(1)	-562(1)	1763(1)	21(1)

Co(3A)	144(1)	-133(1)	3597(1)	20(1)

Co(4A)	-74(1)	-721(1)	2472(1)	19(1)

Si(1A)	5419(3)	90(2)	3453(3)	23(1)

Si(2A)	-330(3)	710(2)	2021(3)	31(1)

O(1A)	3171(15)	573(11)	2755(13)	57(8)

C(1A)	3307(9)	2(7)	2341(9)	21(4)

C(2A)	3087(17)	-402(12)	2922(15)	9(7)

C(2B)	2120(30)	175(18)	3070(20)	68(14)

C(3A)	2220(20)	-401(14)	3094(18)	27(9)

C(3B)	3010(20)	107(15)	2990(20)	38(10)

O(4A)	1902(14)	-801(10)	2841(13)	49(7)

C(4A)	1668(10)	-201(6)	2596(9)	22(4)

C(5A)	1891(14)	-36(9)	1846(12)	79(8)

C(6A)	2789(11)	-92(8)	1694(10)	50(6)

C(7A)	4168(8)	-25(6)	2209(7)	8(4)

C(8A)	4869(9)	21(6)	2550(8)	15(4)

C(9A)	5112(10)	775(6)	3899(9)	30(5)

C(10A)	5122(10)	-515(7)	4053(9)	36(5)

C(11A)	6501(9)	69(6)	3286(9)	28(5)

O(12A)	4428(8)	1579(5)	2288(6)	49(4)

C(12A)	4624(10)	1167(7)	2029(9)	24(5)

O(13A)	4037(7)	561(6)	187(7)	51(4)

C(13A)	4364(11)	538(7)	739(10)	30(5)

O(14A)	6586(7)	684(5)	1339(6)	43(4)

C(14A)	5924(11)	625(7)	1454(9)	28(5)

O(15A)	4618(7)	-1592(5)	2650(7)	45(4)

C(15A)	4703(10)	-1192(7)	2311(9)	23(5)

O(16A)	4115(7)	-909(5)	354(6)	47(4)

C(16A)	4431(11)	-775(7)	892(10)	34(5)

O(17A)	6616(7)	-665(5)	1524(6)	34(3)

C(17A)	5949(11)	-639(7)	1617(9)	27(5)

C(18A)	804(9)	-187(6)	2704(8)	16(4)

C(19A)	149(9)	102(6)	2528(7)	6(4)

C(20A)	165(10)	1384(7)	2332(9)	42(5)

C(21A)	-1404(10)	704(7)	2239(9)	41(5)

C(22A)	-210(12)	594(8)	1024(10)	66(7)

O(23A)	848(8)	884(5)	4282(7)	66(5)

C(23A)	581(11)	504(8)	4018(9)	31(5)

O(24A)	-1500(8)	-25(6)	4134(7)	62(4)

C(24A)	-898(12)	-63(8)	3937(10)	37(5)

O(25A)	910(7)	-1003(5)	4542(6)	45(4)

C(25A)	591(10)	-688(7)	4185(9)	25(5)

O(26A)	-1837(7)	-790(5)	2601(7)	42(4)

C(26A)	-1172(11)	-779(7)	2534(9)	32(5)

O(27A)	147(8)	-906(6)	884(7)	67(5)

C(27A)	59(11)	-820(7)	1519(10)	37(5)

O(28A)	508(8)	-1828(5)	2957(7)	57(4)

C(28A)	280(10)	-1410(8)	2776(9)	31(5)

________________________________________________________________________________

Table S3:  Bond lengths [Å] and angles [°] for 151.

_____________________________________________________

Co(1)-C(13) 	1.797(17)

Co(1)-C(12) 	1.813(18)

Co(1)-C(14) 	1.826(19)

Co(1)-C(7) 	1.927(15)

Co(1)-C(8) 	2.004(14)

Co(1)-Co(2) 	2.471(3)

Co(2)-C(15) 	1.759(18)

Co(2)-C(16) 	1.816(19)

Co(2)-C(17) 	1.827(18)

Co(2)-C(7) 	1.952(15)

Co(2)-C(8) 	1.965(14)

Co(3)-C(23) 	1.785(19)

Co(3)-C(24) 	1.819(19)

Co(3)-C(25) 	1.85(2)

Co(3)-C(18) 	1.963(16)

Co(3)-C(19) 	1.980(15)

Co(3)-Co(4) 	2.472(3)

Co(4)-C(27) 	1.779(19)

Co(4)-C(28) 	1.842(17)

Co(4)-C(26) 	1.860(18)

Co(4)-C(18) 	1.961(16)

Co(4)-C(19) 	1.997(15)

Si(1)-C(11) 	1.852(18)

Si(1)-C(8) 	1.864(15)

Si(1)-C(10) 	1.885(16)

Si(1)-C(9) 	1.887(15)

Si(2)-C(19) 	1.854(15)

Si(2)-C(21) 	1.870(16)

Si(2)-C(22) 	1.871(16)

Si(2)-C(20) 	1.875(15)

O(1)-C(1) 	1.67(3)

O(1)-H(1) 	0.8400

C(1)-C(6) 	1.46(2)

C(1)-C(2) 	1.48(2)

C(1)-C(7) 	1.50(2)

C(2)-C(3) 	1.49(3)

C(2)-H(2B) 	0.9900

C(2)-H(2A) 	0.9900

C(3)-C(4) 	1.33(2)

C(3)-H(3) 	0.9500

C(4)-C(5) 	1.39(2)

C(4)-C(18) 	1.49(2)

C(5)-C(6) 	1.43(2)

C(5)-H(5A) 	0.9900

C(5)-H(5B) 	0.9900

C(6)-H(6A) 	0.9900

C(6)-H(6B) 	0.9900

C(7)-C(8) 	1.307(18)

C(9)-H(9C) 	0.9800

C(9)-H(9B) 	0.9800

C(9)-H(9A) 	0.9800

C(10)-H(10C) 	0.9800

C(10)-H(10B) 	0.9800

C(10)-H(10A) 	0.9800

C(11)-H(11C) 	0.9800

C(11)-H(11B) 	0.9800

C(11)-H(11A) 	0.9800

O(12)-C(12) 	1.120(18)

O(13)-C(13) 	1.143(17)

O(14)-C(14) 	1.135(18)

O(15)-C(15) 	1.161(18)

O(16)-C(16) 	1.117(18)

O(17)-C(17) 	1.135(18)

C(18)-C(19) 	1.320(19)

C(20)-H(20C) 	0.9800

C(20)-H(20B) 	0.9800

C(20)-H(20A) 	0.9800

C(21)-H(21C) 	0.9800

C(21)-H(21B) 	0.9800

C(21)-H(21A) 	0.9800

C(22)-H(22C) 	0.9800

C(22)-H(22B) 	0.9800

C(22)-H(22A) 	0.9800

O(23)-C(23) 	1.159(18)

O(24)-C(24) 	1.114(19)

O(25)-C(25) 	1.122(19)

O(26)-C(26) 	1.104(18)

O(27)-C(27) 	1.141(18)

O(28)-C(28) 	1.106(16)

Co(1A)-C(12A) 	1.809(18)

Co(1A)-C(13A) 	1.821(18)

Co(1A)-C(14A) 	1.842(19)

Co(1A)-C(8A) 	1.968(15)

Co(1A)-C(7A) 	1.980(14)

Co(1A)-Co(2A) 	2.471(3)

Co(2A)-C(17A) 	1.795(19)

Co(2A)-C(16A) 	1.814(19)

Co(2A)-C(15A) 	1.815(18)

Co(2A)-C(7A) 	1.952(14)

Co(2A)-C(8A) 	1.975(15)

Co(3A)-C(23A) 	1.827(19)

Co(3A)-C(25A) 	1.834(18)

Co(3A)-C(24A) 	1.88(2)

Co(3A)-C(18A) 	1.975(15)

Co(3A)-C(19A) 	2.002(14)

Co(3A)-Co(4A) 	2.476(3)

Co(4A)-C(27A) 	1.750(19)

Co(4A)-C(28A) 	1.810(19)

Co(4A)-C(26A) 	1.858(19)

Co(4A)-C(19A) 	1.974(13)

Co(4A)-C(18A) 	1.978(15)

Si(1A)-C(11A) 	1.852(16)

Si(1A)-C(10A) 	1.861(16)

Si(1A)-C(8A) 	1.862(15)

Si(1A)-C(9A) 	1.879(15)

Si(2A)-C(22A) 	1.831(19)

Si(2A)-C(21A) 	1.857(17)

Si(2A)-C(20A) 	1.872(16)

Si(2A)-C(19A) 	1.873(14)

O(1A)-C(1A) 	1.56(3)

O(1A)-H(1A) 	0.8400

C(1A)-C(3B) 	1.30(4)

C(1A)-C(6A) 	1.46(2)

C(1A)-C(2A) 	1.47(3)

C(1A)-C(7A) 	1.47(2)

C(2A)-C(3A) 	1.50(4)

C(2A)-H(2AB) 	0.9900

C(2A)-H(2AA) 	0.9900

C(2B)-C(4A) 	1.44(4)

C(2B)-C(3B) 	1.52(5)

C(2B)-H(2BB) 	0.9900

C(2B)-H(2BA) 	0.9900

C(3A)-C(4A) 	1.36(3)

C(3A)-H(3A) 	0.9500

C(3B)-H(3B) 	0.9500

O(4A)-C(4A) 	1.53(3)

O(4A)-H(4A) 	0.8400

C(4A)-C(5A) 	1.46(2)

C(4A)-C(18A) 	1.47(2)

C(5A)-C(6A) 	1.55(3)

C(5A)-H(5C) 	0.9900

C(5A)-H(5D) 	0.9900

C(6A)-H(6D) 	0.9900

C(6A)-H(6C) 	0.9900

C(7A)-C(8A) 	1.324(18)

C(9A)-H(9F) 	0.9800

C(9A)-H(9E) 	0.9800

C(9A)-H(9D) 	0.9800

C(10A)-H(10F) 	0.9800

C(10A)-H(10E) 	0.9800

C(10A)-H(10D) 	0.9800

C(11A)-H(11F) 	0.9800

C(11A)-H(11E) 	0.9800

C(11A)-H(11D) 	0.9800

O(12A)-C(12A) 	1.127(17)

O(13A)-C(13A) 	1.128(17)

O(14A)-C(14A) 	1.146(18)

O(15A)-C(15A) 	1.133(17)

O(16A)-C(16A) 	1.141(18)

O(17A)-C(17A) 	1.140(18)

C(18A)-C(19A) 	1.327(18)

C(20A)-H(20F) 	0.9800

C(20A)-H(20E) 	0.9800

C(20A)-H(20D) 	0.9800

C(21A)-H(21F) 	0.9800

C(21A)-H(21E) 	0.9800

C(21A)-H(21D) 	0.9800

C(22A)-H(22F) 	0.9800

C(22A)-H(22E) 	0.9800

C(22A)-H(22D) 	0.9800

O(23A)-C(23A) 	1.106(18)

O(24A)-C(24A) 	1.08(2)

O(25A)-C(25A) 	1.115(17)

O(26A)-C(26A) 	1.127(18)

O(27A)-C(27A) 	1.174(18)

O(28A)-C(28A) 	1.102(18)

C(13)-Co(1)-C(12)	98.9(7)

C(13)-Co(1)-C(14)	104.9(8)

C(12)-Co(1)-C(14)	102.1(8)

C(13)-Co(1)-C(7)	104.7(7)

C(12)-Co(1)-C(7)	99.5(7)

C(14)-Co(1)-C(7)	139.8(7)

C(13)-Co(1)-C(8)	141.3(7)

C(12)-Co(1)-C(8)	100.0(6)

C(14)-Co(1)-C(8)	103.8(7)

C(7)-Co(1)-C(8)	38.8(5)

C(13)-Co(1)-Co(2)	99.8(5)

C(12)-Co(1)-Co(2)	148.3(5)

C(14)-Co(1)-Co(2)	97.5(5)

C(7)-Co(1)-Co(2)	50.9(4)

C(8)-Co(1)-Co(2)	50.8(4)

C(15)-Co(2)-C(16)	100.5(8)

C(15)-Co(2)-C(17)	104.2(7)

C(16)-Co(2)-C(17)	97.1(7)

C(15)-Co(2)-C(7)	104.0(7)

C(16)-Co(2)-C(7)	103.4(7)

C(17)-Co(2)-C(7)	141.1(7)

C(15)-Co(2)-C(8)	140.8(7)

C(16)-Co(2)-C(8)	101.3(7)

C(17)-Co(2)-C(8)	104.9(7)

C(7)-Co(2)-C(8)	39.0(5)

C(15)-Co(2)-Co(1)	97.1(6)

C(16)-Co(2)-Co(1)	151.4(6)

C(17)-Co(2)-Co(1)	100.3(5)

C(7)-Co(2)-Co(1)	50.0(4)

C(8)-Co(2)-Co(1)	52.2(4)

C(23)-Co(3)-C(24)	102.2(8)

C(23)-Co(3)-C(25)	105.0(8)

C(24)-Co(3)-C(25)	100.1(8)

C(23)-Co(3)-C(18)	102.0(7)

C(24)-Co(3)-C(18)	98.5(7)

C(25)-Co(3)-C(18)	142.9(7)

C(23)-Co(3)-C(19)	138.7(7)

C(24)-Co(3)-C(19)	98.2(7)

C(25)-Co(3)-C(19)	106.2(7)

C(18)-Co(3)-C(19)	39.1(6)

C(23)-Co(3)-Co(4)	96.1(6)

C(24)-Co(3)-Co(4)	147.4(6)

C(25)-Co(3)-Co(4)	100.9(5)

C(18)-Co(3)-Co(4)	50.9(4)

C(19)-Co(3)-Co(4)	51.9(4)

C(27)-Co(4)-C(28)	98.4(7)

C(27)-Co(4)-C(26)	100.7(8)

C(28)-Co(4)-C(26)	105.6(7)

C(27)-Co(4)-C(18)	100.6(7)

C(28)-Co(4)-C(18)	104.5(7)

C(26)-Co(4)-C(18)	139.8(7)

C(27)-Co(4)-C(19)	100.6(7)

C(28)-Co(4)-C(19)	141.4(7)

C(26)-Co(4)-C(19)	103.5(7)

C(18)-Co(4)-C(19)	39.0(6)

C(27)-Co(4)-Co(3)	149.5(6)

C(28)-Co(4)-Co(3)	99.7(5)

C(26)-Co(4)-Co(3)	97.9(5)

C(18)-Co(4)-Co(3)	51.0(5)

C(19)-Co(4)-Co(3)	51.3(4)

C(11)-Si(1)-C(8)	109.3(7)

C(11)-Si(1)-C(10)	111.2(8)

C(8)-Si(1)-C(10)	107.2(7)

C(11)-Si(1)-C(9)	111.4(8)

C(8)-Si(1)-C(9)	107.7(7)

C(10)-Si(1)-C(9)	109.9(8)

C(19)-Si(2)-C(21)	108.6(7)

C(19)-Si(2)-C(22)	111.6(7)

C(21)-Si(2)-C(22)	109.4(7)

C(19)-Si(2)-C(20)	106.2(7)

C(21)-Si(2)-C(20)	110.7(8)

C(22)-Si(2)-C(20)	110.3(7)

C(1)-O(1)-H(1)	109.5

C(6)-C(1)-C(2)	115.0(16)

C(6)-C(1)-C(7)	120.9(15)

C(2)-C(1)-C(7)	118.0(15)

C(6)-C(1)-O(1)	87.3(14)

C(2)-C(1)-O(1)	100.3(14)

C(7)-C(1)-O(1)	107.0(14)

C(1)-C(2)-C(3)	116.3(16)

C(1)-C(2)-H(2B)	108.2

C(3)-C(2)-H(2B)	108.2

C(1)-C(2)-H(2A)	108.2

C(3)-C(2)-H(2A)	108.2

H(2B)-C(2)-H(2A)	107.4

C(4)-C(3)-C(2)	120(2)

C(4)-C(3)-H(3)	119.9

C(2)-C(3)-H(3)	119.9

C(3)-C(4)-C(5)	124(2)

C(3)-C(4)-C(18)	117.6(17)

C(5)-C(4)-C(18)	117.9(16)

C(4)-C(5)-C(6)	118.3(17)

C(4)-C(5)-H(5A)	107.7

C(6)-C(5)-H(5A)	107.7

C(4)-C(5)-H(5B)	107.7

C(6)-C(5)-H(5B)	107.7

H(5A)-C(5)-H(5B)	107.1

C(5)-C(6)-C(1)	119.3(17)

C(5)-C(6)-H(6A)	107.5

C(1)-C(6)-H(6A)	107.5

C(5)-C(6)-H(6B)	107.5

C(1)-C(6)-H(6B)	107.5

H(6A)-C(6)-H(6B)	107.0

C(8)-C(7)-C(1)	139.1(15)

C(8)-C(7)-Co(1)	73.8(10)

C(1)-C(7)-Co(1)	134.8(11)

C(8)-C(7)-Co(2)	71.0(9)

C(1)-C(7)-Co(2)	132.8(11)

Co(1)-C(7)-Co(2)	79.1(6)

C(7)-C(8)-Si(1)	149.1(13)

C(7)-C(8)-Co(2)	70.0(9)

Si(1)-C(8)-Co(2)	133.6(8)

C(7)-C(8)-Co(1)	67.4(9)

Si(1)-C(8)-Co(1)	129.9(8)

Co(2)-C(8)-Co(1)	77.0(5)

Si(1)-C(9)-H(9C)	109.5

Si(1)-C(9)-H(9B)	109.5

H(9C)-C(9)-H(9B)	109.5

Si(1)-C(9)-H(9A)	109.5

H(9C)-C(9)-H(9A)	109.5

H(9B)-C(9)-H(9A)	109.5

Si(1)-C(10)-H(10C)	109.5

Si(1)-C(10)-H(10B)	109.5

H(10C)-C(10)-H(10B)	109.5

Si(1)-C(10)-H(10A)	109.5

H(10C)-C(10)-H(10A)	109.5

H(10B)-C(10)-H(10A)	109.5

Si(1)-C(11)-H(11C)	109.5

Si(1)-C(11)-H(11B)	109.5

H(11C)-C(11)-H(11B)	109.5

Si(1)-C(11)-H(11A)	109.5

H(11C)-C(11)-H(11A)	109.5

H(11B)-C(11)-H(11A)	109.5

O(12)-C(12)-Co(1)	179.2(17)

O(13)-C(13)-Co(1)	177.1(16)

O(14)-C(14)-Co(1)	178.1(17)

O(15)-C(15)-Co(2)	174.8(16)

O(16)-C(16)-Co(2)	177.3(17)

O(17)-C(17)-Co(2)	178.9(16)

C(19)-C(18)-C(4)	141.4(16)

C(19)-C(18)-Co(4)	72.0(10)

C(4)-C(18)-Co(4)	134.3(12)

C(19)-C(18)-Co(3)	71.1(10)

C(4)-C(18)-Co(3)	132.9(12)

Co(4)-C(18)-Co(3)	78.1(6)

C(18)-C(19)-Si(2)	147.9(14)

C(18)-C(19)-Co(3)	69.7(9)

Si(2)-C(19)-Co(3)	132.1(9)

C(18)-C(19)-Co(4)	69.1(9)

Si(2)-C(19)-Co(4)	132.1(9)

Co(3)-C(19)-Co(4)	76.9(5)

Si(2)-C(20)-H(20C)	109.5

Si(2)-C(20)-H(20B)	109.5

H(20C)-C(20)-H(20B)	109.5

Si(2)-C(20)-H(20A)	109.5

H(20C)-C(20)-H(20A)	109.5

H(20B)-C(20)-H(20A)	109.5

Si(2)-C(21)-H(21C)	109.5

Si(2)-C(21)-H(21B)	109.5

H(21C)-C(21)-H(21B)	109.5

Si(2)-C(21)-H(21A)	109.5

H(21C)-C(21)-H(21A)	109.5

H(21B)-C(21)-H(21A)	109.5

Si(2)-C(22)-H(22C)	109.5

Si(2)-C(22)-H(22B)	109.5

H(22C)-C(22)-H(22B)	109.5

Si(2)-C(22)-H(22A)	109.5

H(22C)-C(22)-H(22A)	109.5

H(22B)-C(22)-H(22A)	109.5

O(23)-C(23)-Co(3)	176.6(17)

O(24)-C(24)-Co(3)	176.7(18)

O(25)-C(25)-Co(3)	177.9(17)

O(26)-C(26)-Co(4)	177.3(16)

O(27)-C(27)-Co(4)	177.3(16)

O(28)-C(28)-Co(4)	174.4(15)

C(12A)-Co(1A)-C(13A)	100.1(7)

C(12A)-Co(1A)-C(14A)	97.8(7)

C(13A)-Co(1A)-C(14A)	105.2(8)

C(12A)-Co(1A)-C(8A)	99.4(7)

C(13A)-Co(1A)-C(8A)	140.7(7)

C(14A)-Co(1A)-C(8A)	105.4(7)

C(12A)-Co(1A)-C(7A)	101.1(7)

C(13A)-Co(1A)-C(7A)	103.4(7)

C(14A)-Co(1A)-C(7A)	142.1(7)

C(8A)-Co(1A)-C(7A)	39.2(5)

C(12A)-Co(1A)-Co(2A)	148.9(5)

C(13A)-Co(1A)-Co(2A)	99.3(5)

C(14A)-Co(1A)-Co(2A)	100.3(5)

C(8A)-Co(1A)-Co(2A)	51.3(4)

C(7A)-Co(1A)-Co(2A)	50.6(4)

C(17A)-Co(2A)-C(16A)	105.0(8)

C(17A)-Co(2A)-C(15A)	100.9(7)

C(16A)-Co(2A)-C(15A)	99.4(7)

C(17A)-Co(2A)-C(7A)	139.1(7)

C(16A)-Co(2A)-C(7A)	105.4(7)

C(15A)-Co(2A)-C(7A)	100.4(7)

C(17A)-Co(2A)-C(8A)	102.5(7)

C(16A)-Co(2A)-C(8A)	142.6(7)

C(15A)-Co(2A)-C(8A)	99.8(7)

C(7A)-Co(2A)-C(8A)	39.4(5)

C(17A)-Co(2A)-Co(1A)	96.2(5)

C(16A)-Co(2A)-Co(1A)	100.8(6)

C(15A)-Co(2A)-Co(1A)	149.1(5)

C(7A)-Co(2A)-Co(1A)	51.6(4)

C(8A)-Co(2A)-Co(1A)	51.1(4)

C(23A)-Co(3A)-C(25A)	100.8(7)

C(23A)-Co(3A)-C(24A)	99.5(8)

C(25A)-Co(3A)-C(24A)	104.4(8)

C(23A)-Co(3A)-C(18A)	99.4(7)

C(25A)-Co(3A)-C(18A)	101.1(7)

C(24A)-Co(3A)-C(18A)	144.6(7)

C(23A)-Co(3A)-C(19A)	99.5(6)

C(25A)-Co(3A)-C(19A)	137.9(7)

C(24A)-Co(3A)-C(19A)	108.1(7)

C(18A)-Co(3A)-C(19A)	39.0(5)

C(23A)-Co(3A)-Co(4A)	148.3(6)

C(25A)-Co(3A)-Co(4A)	97.3(5)

C(24A)-Co(3A)-Co(4A)	101.0(6)

C(18A)-Co(3A)-Co(4A)	51.3(4)

C(19A)-Co(3A)-Co(4A)	51.0(4)

C(27A)-Co(4A)-C(28A)	97.4(8)

C(27A)-Co(4A)-C(26A)	101.3(8)

C(28A)-Co(4A)-C(26A)	103.7(8)

C(27A)-Co(4A)-C(19A)	98.9(7)

C(28A)-Co(4A)-C(19A)	143.4(7)

C(26A)-Co(4A)-C(19A)	104.9(7)

C(27A)-Co(4A)-C(18A)	100.6(7)

C(28A)-Co(4A)-C(18A)	105.4(7)

C(26A)-Co(4A)-C(18A)	140.7(7)

C(19A)-Co(4A)-C(18A)	39.2(5)

C(27A)-Co(4A)-Co(3A)	149.0(6)

C(28A)-Co(4A)-Co(3A)	102.2(5)

C(26A)-Co(4A)-Co(3A)	97.1(5)

C(19A)-Co(4A)-Co(3A)	52.0(4)

C(18A)-Co(4A)-Co(3A)	51.2(4)

C(11A)-Si(1A)-C(10A)	110.5(7)

C(11A)-Si(1A)-C(8A)	109.2(7)

C(10A)-Si(1A)-C(8A)	107.9(7)

C(11A)-Si(1A)-C(9A)	111.8(7)

C(10A)-Si(1A)-C(9A)	109.2(8)

C(8A)-Si(1A)-C(9A)	108.2(7)

C(22A)-Si(2A)-C(21A)	109.4(8)

C(22A)-Si(2A)-C(20A)	111.3(9)

C(21A)-Si(2A)-C(20A)	111.9(8)

C(22A)-Si(2A)-C(19A)	108.0(8)

C(21A)-Si(2A)-C(19A)	107.6(7)

C(20A)-Si(2A)-C(19A)	108.5(7)

C(1A)-O(1A)-H(1A)	109.5

C(3B)-C(1A)-C(6A)	121(2)

C(3B)-C(1A)-C(2A)	51.6(18)

C(6A)-C(1A)-C(2A)	108.5(17)

C(3B)-C(1A)-C(7A)	123(2)

C(6A)-C(1A)-C(7A)	116.0(15)

C(2A)-C(1A)-C(7A)	110.4(16)

C(3B)-C(1A)-O(1A)	48.9(17)

C(6A)-C(1A)-O(1A)	115.0(16)

C(2A)-C(1A)-O(1A)	100.3(17)

C(7A)-C(1A)-O(1A)	105.5(15)

C(1A)-C(2A)-C(3A)	114(2)

C(1A)-C(2A)-H(2AB)	108.8

C(3A)-C(2A)-H(2AB)	108.8

C(1A)-C(2A)-H(2AA)	108.8

C(3A)-C(2A)-H(2AA)	108.8

H(2AB)-C(2A)-H(2AA)	107.6

C(4A)-C(2B)-C(3B)	113(3)

C(4A)-C(2B)-H(2BB)	109.0

C(3B)-C(2B)-H(2BB)	109.0

C(4A)-C(2B)-H(2BA)	109.0

C(3B)-C(2B)-H(2BA)	109.0

H(2BB)-C(2B)-H(2BA)	107.8

C(4A)-C(3A)-C(2A)	121(3)

C(4A)-C(3A)-H(3A)	119.4

C(2A)-C(3A)-H(3A)	119.4

C(1A)-C(3B)-C(2B)	120(3)

C(1A)-C(3B)-H(3B)	120.0

C(2B)-C(3B)-H(3B)	120.0

C(4A)-O(4A)-H(4A)	109.5

C(3A)-C(4A)-C(2B)	58(2)

C(3A)-C(4A)-C(5A)	121(2)

C(2B)-C(4A)-C(5A)	104(2)

C(3A)-C(4A)-C(18A)	126(2)

C(2B)-C(4A)-C(18A)	115(2)

C(5A)-C(4A)-C(18A)	112.7(15)

C(3A)-C(4A)-O(4A)	47.3(15)

C(2B)-C(4A)-O(4A)	105(2)

C(5A)-C(4A)-O(4A)	116.4(17)

C(18A)-C(4A)-O(4A)	103.5(15)

C(4A)-C(5A)-C(6A)	114.1(17)

C(4A)-C(5A)-H(5C)	108.7

C(6A)-C(5A)-H(5C)	108.7

C(4A)-C(5A)-H(5D)	108.7

C(6A)-C(5A)-H(5D)	108.7

H(5C)-C(5A)-H(5D)	107.6

C(1A)-C(6A)-C(5A)	114.6(16)

C(1A)-C(6A)-H(6D)	108.6

C(5A)-C(6A)-H(6D)	108.6

C(1A)-C(6A)-H(6C)	108.6

C(5A)-C(6A)-H(6C)	108.6

H(6D)-C(6A)-H(6C)	107.6

C(8A)-C(7A)-C(1A)	142.4(14)

C(8A)-C(7A)-Co(2A)	71.2(9)

C(1A)-C(7A)-Co(2A)	136.5(11)

C(8A)-C(7A)-Co(1A)	69.9(9)

C(1A)-C(7A)-Co(1A)	131.0(11)

Co(2A)-C(7A)-Co(1A)	77.8(5)

C(7A)-C(8A)-Si(1A)	146.6(13)

C(7A)-C(8A)-Co(1A)	70.9(9)

Si(1A)-C(8A)-Co(1A)	132.3(8)

C(7A)-C(8A)-Co(2A)	69.4(9)

Si(1A)-C(8A)-Co(2A)	131.8(8)

Co(1A)-C(8A)-Co(2A)	77.6(5)

Si(1A)-C(9A)-H(9F)	109.5

Si(1A)-C(9A)-H(9E)	109.5

H(9F)-C(9A)-H(9E)	109.5

Si(1A)-C(9A)-H(9D)	109.5

H(9F)-C(9A)-H(9D)	109.5

H(9E)-C(9A)-H(9D)	109.5

Si(1A)-C(10A)-H(10F)	109.5

Si(1A)-C(10A)-H(10E)	109.5

H(10F)-C(10A)-H(10E)	109.5

Si(1A)-C(10A)-H(10D)	109.5

H(10F)-C(10A)-H(10D)	109.5

H(10E)-C(10A)-H(10D)	109.5

Si(1A)-C(11A)-H(11F)	109.5

Si(1A)-C(11A)-H(11E)	109.5

H(11F)-C(11A)-H(11E)	109.5

Si(1A)-C(11A)-H(11D)	109.5

H(11F)-C(11A)-H(11D)	109.5

H(11E)-C(11A)-H(11D)	109.5

O(12A)-C(12A)-Co(1A)	175.6(16)

O(13A)-C(13A)-Co(1A)	178.2(17)

O(14A)-C(14A)-Co(1A)	176.4(16)

O(15A)-C(15A)-Co(2A)	176.6(16)

O(16A)-C(16A)-Co(2A)	178.1(17)

O(17A)-C(17A)-Co(2A)	177.2(16)

C(19A)-C(18A)-C(4A)	143.0(15)

C(19A)-C(18A)-Co(3A)	71.6(9)

C(4A)-C(18A)-Co(3A)	132.9(11)

C(19A)-C(18A)-Co(4A)	70.2(9)

C(4A)-C(18A)-Co(4A)	133.9(11)

Co(3A)-C(18A)-Co(4A)	77.6(6)

C(18A)-C(19A)-Si(2A)	148.8(12)

C(18A)-C(19A)-Co(4A)	70.5(9)

Si(2A)-C(19A)-Co(4A)	130.2(8)

C(18A)-C(19A)-Co(3A)	69.4(9)

Si(2A)-C(19A)-Co(3A)	132.0(8)

Co(4A)-C(19A)-Co(3A)	77.0(5)

Si(2A)-C(20A)-H(20F)	109.5

Si(2A)-C(20A)-H(20E)	109.5

H(20F)-C(20A)-H(20E)	109.5

Si(2A)-C(20A)-H(20D)	109.5

H(20F)-C(20A)-H(20D)	109.5

H(20E)-C(20A)-H(20D)	109.5

Si(2A)-C(21A)-H(21F)	109.5

Si(2A)-C(21A)-H(21E)	109.5

H(21F)-C(21A)-H(21E)	109.5

Si(2A)-C(21A)-H(21D)	109.5

H(21F)-C(21A)-H(21D)	109.5

H(21E)-C(21A)-H(21D)	109.5

Si(2A)-C(22A)-H(22F)	109.5

Si(2A)-C(22A)-H(22E)	109.5

H(22F)-C(22A)-H(22E)	109.5

Si(2A)-C(22A)-H(22D)	109.5

H(22F)-C(22A)-H(22D)	109.5

H(22E)-C(22A)-H(22D)	109.5

O(23A)-C(23A)-Co(3A)	178.9(17)

O(24A)-C(24A)-Co(3A)	180(2)

O(25A)-C(25A)-Co(3A)	175.1(16)

O(26A)-C(26A)-Co(4A)	176.1(17)

O(27A)-C(27A)-Co(4A)	177.7(16)

O(28A)-C(28A)-Co(4A)	178.8(18)

______________________________________________________________________________________

Table S4:  Anisotropic displacement parameters (Å2 x 103) for 151.  The anisotropic

displacement factor exponent takes the form:  -2(2[ h2 a*2U11 + ...  + 2 h k a* b* U12 ]

______________________________________________________________________________

U11	U22 	U33	U23	U13	U12

______________________________________________________________________________

Co(1)	13(2) 	22(1)	20(1) 	-8(1)	5(1) 	-2(1)

Co(2)	18(2) 	24(1)	17(1) 	-4(1)	-1(1) 	2(1)

Co(3)	18(2) 	21(1)	18(2) 	2(1)	4(1) 	4(1)

Co(4)	20(2) 	20(1)	17(1) 	-1(1)	4(1) 	1(1)

Si(1)	23(3) 	36(3)	18(3) 	-4(3)	-3(2) 	5(3)

Si(2)	20(3) 	23(3)	20(3) 	-2(2)	-3(2) 	-4(2)

O(12)	61(10) 	20(7)	51(9) 	9(6)	19(7) 	-19(7)

O(13)	51(9) 	49(9)	25(8) 	-14(7)	5(7) 	-6(7)

O(14)	24(9) 	40(8)	61(9) 	-12(7)	9(7) 	-12(7)

O(15)	76(11) 	26(8)	26(8) 	-4(6)	-14(7) 	1(7)

O(16)	47(9) 	44(8)	35(8) 	-16(7)	15(7) 	16(7)

O(17)	24(9) 	52(9)	63(10) 	-2(7)	6(7) 	-11(7)

O(23)	50(9) 	32(8)	34(8) 	6(6)	-11(7) 	20(7)

O(24)	79(12) 	23(8)	65(10) 	-18(7)	-12(8) 	31(8)

O(25)	15(8) 	60(9)	62(9) 	33(7)	2(7) 	-5(7)

O(26)	15(8) 	57(9)	52(9) 	9(7)	1(7) 	8(7)

O(27)	65(11) 	42(9)	52(9) 	17(8)	-2(8) 	-10(8)

O(28)	56(10) 	37(8)	18(7) 	-5(6)	-10(7) 	-7(7)

Co(1A)	19(2) 	26(1)	18(1) 	6(1)	3(1) 	1(1)

Co(2A)	19(2) 	25(2)	18(1) 	-3(1)	2(1) 	-2(1)

Co(3A)	15(2) 	32(2)	14(1) 	2(1)	2(1) 	-3(1)

Co(4A)	11(1) 	24(1)	21(1) 	-2(1)	-2(1) 	-2(1)

Si(1A)	19(3) 	30(3)	20(3) 	-2(2)	-4(2) 	-2(2)

Si(2A)	27(4) 	30(3)	34(3) 	6(3)	-4(3) 	2(3)

O(12A)	75(11) 	27(8)	46(9) 	5(7)	13(8) 	13(7)

O(13A)	21(8) 	90(11)	41(9) 	12(8)	7(7) 	7(8)

O(14A)	36(9) 	44(8)	50(9) 	11(7)	6(7) 	-7(7)

O(15A)	45(9) 	27(8)	62(9) 	14(7)	-2(7) 	-15(7)

O(16A)	46(9) 	65(10)	31(8) 	-7(7)	4(7) 	-19(8)

O(17A)	23(8) 	38(8)	40(8) 	-6(6)	-2(6) 	8(6)

O(23A)	94(13) 	43(9)	59(10) 	-30(8)	-6(9) 	-30(9)

O(24A)	22(9) 	109(13)	56(10) 	-18(8)	10(7) 	21(9)

O(25A)	33(9) 	54(9)	48(9) 	17(7)	-6(7) 	10(7)

O(26A)	15(8) 	49(9)	64(10) 	2(7)	15(7) 	-4(7)

O(27A)	94(13) 	78(11)	29(9) 	-9(8)	24(8) 	-6(9)

O(28A)	54(10) 	25(8)	92(11) 	26(8)	-13(8) 	9(7)

______________________________________________________________________________

Table S5:  Hydrogen coordinates ( x 104) and isotropic displacement parameters (Å2 x 10 3)

for 151.

________________________________________________________________________________

x 	y 	z 	U(eq)

________________________________________________________________________________

H(1)	359	1689	-213	313

H(2B)	261	2156	-1218	51

H(2A)	280	2832	-1276	51

H(3)	-1088	2478	-1122	91

H(5A)	-438	2494	928	59

H(5B)	-539	3149	725	59

H(6A)	749	2648	792	64

H(6B)	593	3217	335	64

H(9C)	2648	1313	708	47

H(9B)	1943	1617	1141	47

H(9A)	2784	1516	1549	47

H(10C)	2827	3253	1264	62

H(10B)	2894	2792	1915	62

H(10A)	2057	2903	1503	62

H(11C)	4053	2012	167	75

H(11B)	4251	2230	992	75

H(11A)	4106	2679	336	75

H(20C)	-2154	1831	-1585	47

H(20B)	-3006	1765	-1985	47

H(20A)	-2862	1521	-1164	47

H(21C)	-2211	3122	-1831	56

H(21B)	-2939	3485	-1525	56

H(21A)	-3069	3074	-2224	56

H(22C)	-4277	2216	-621	44

H(22B)	-4424	2480	-1431	44

H(22A)	-4294	2891	-730	44

H(1A)	3507	813	2617	86

H(2AB)	3394	-312	3381	11

H(2AA)	3240	-789	2763	11

H(2BB)	1985	101	3597	81

H(2BA)	1974	573	2958	81

H(3A)	2050	-543	3560	33

H(3B)	3359	142	3411	46

H(4A)	1760	-854	3280	73

H(5C)	1729	364	1761	95

H(5D)	1592	-274	1484	95

H(6D)	2891	-477	1498	60

H(6C)	2931	184	1304	60

H(9F)	5271	1095	3586	45

H(9E)	5373	809	4389	45

H(9D)	4534	779	3955	45

H(10F)	5283	-873	3823	55

H(10E)	4544	-511	4111	55

H(10D)	5383	-478	4542	55

H(11F)	6639	-294	3054	42

H(11E)	6793	108	3759	42

H(11D)	6645	382	2955	42

H(20F)	729	1372	2207	63

H(20E)	114	1425	2871	63

H(20D)	-90	1708	2082	63

H(21F)	-1643	347	2065	62

H(21E)	-1669	1024	1989	62

H(21D)	-1468	738	2777	62

H(22F)	-479	241	877	100

H(22E)	357	566	915	100

H(22D)	-444	914	748	100

________________________________________________________________________________